Supporting Information

Theoretical Research on Cage-like Oxadiazole-based Energetic Compounds and Its Derivatives

Yan Huang, Le-Wu Zhan, Qian Zhang, Jing Hou*, and Bin-Dong Li*

School of Chemical Engineering, Nanjing University of Science and Technology, Nanjing 210094, China

Figure S1. Designed Molecules Structures (B3PW91/6-311G++(2d,p))

Figure S2. Derivatives Molecular Structures (B3PW91/6-311G++(2d,p))

Table S1. HOMO and LUMO Energy and Energy Gaps of Designed Compounds

| Compounds | Formula | MW | HOMO |  | LUMO |  | ∆ELUMO-HOMO |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Orbital | a.u | Orbital | a.u | a.u |
| I | C6O3N8 | 232.12 | 58 | -0.328801 | 59 | -0.120653 | 0.208148 |
| II | C8H2O3N6 | 230.14 | 58 | -0.330917 | 59 | -0.10294 | 0.227977 |
| A | C8H4O3N8 | 260.17 | 66 | -0.305563 | 67 | -0.099324 | 0.206239 |
| B | C8H3O5N9 | 305.17 | 77 | -0.315438 | 78 | -0.113028 | 0.20241 |
| C | C8H2O7N10 | 350.17 | 88 | -0.344907 | 89 | -0.127938 | 0.216968 |
| D | C8H2O5N8 | 290.16 | 73 | -0.318699 | 74 | -0.121806 | 0.196893 |
| E | C8H2O6N8 | 306.15 | 77 | -0.314756 | 78 | -0.111098 | 0.203658 |
| F | C8H2O3N10 | 286.17 | 72 | -0.311115 | 73 | -0.107806 | 0.20331 |
| G | C9H3O7N9 | 349.18 | 88 | -0.317565 | 89 | -0.127408 | 0.190157 |
| H | C9H2O9N10 | 394.18 | 99 | -0.320204 | 100 | -0.145924 | 0.17428 |
| I | C8O7N8 | 320.14 | 80 | -0.359228 | 81 | -0.133461 | 0.225767 |
| J | C8O9N8 | 352.14 | 88 | -0.347981 | 89 | -0.120126 | 0.227855 |

Figure S3. Molecular HOMO and LUMO Energy and Energy Gaps

The orbital-weighted nucleophilic Fukui function as:

fw-r=i=1HOMOwiρi(r)  (1)

where wi are the weightings factor and can be obtained by:

wi=exp⁡[-μ-εi∆2]iHOMOexp⁡[-μ-εi∆2]  (2)

where μ, εi, and Δ represent the chemical potential, orbital energy in au, and the width of the Gaussian function.

fw+r=i=LUMOI=∞wiρi(r)  (3)

fw(2)r=fw+r-fw-r  (4)

Table S2. Physicochemical Properties of Designed Compounds

| Compounds | Volume | σ+2 | σ-2 | v | vσtot2 | ∆Hvap | ∆Hsub | Sm0 | Cp,m0 | HT0 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| I | 1366.15 | 116.74 | 13.88 | 0.09 | 12.40 | 15.44 | 19.30 | 392.50 | 172.30 | -891.73 |
| II | 1441.31 | 122.82 | 15.75 | 0.10 | 13.96 | 16.28 | 20.57 | 399.01 | 178.62 | -859.72 |
| A | 1667.14 | 147.27 | 21.69 | 0.11 | 18.91 | 18.50 | 24.26 | 463.59 | 229.54 | -970.38 |
| B | 1862.68 | 188.22 | 32.48 | 0.13 | 27.70 | 20.95 | 28.79 | 520.53 | 260.27 | -1174.84 |
| C | 2059.14 | 213.71 | 29.61 | 0.11 | 26.01 | 22.36 | 31.88 | 566.26 | 291.01 | -1379.29 |
| D | 1755.25 | 180.11 | 25.74 | 0.11 | 22.52 | 17.04 | 21.99 | 480.84 | 234.16 | -1119.51 |
| E | 1829.23 | 152.66 | 14.02 | 0.08 | 12.84 | 19.24 | 25.70 | 519.02 | 257.02 | -1194.69 |
| F | 1789.29 | 139.87 | 18.22 | 0.10 | 16.12 | 19.43 | 26.01 | 502.73 | 243.80 | -1078.60 |
| G | 2094.35 | 201.24 | 19.66 | 0.08 | 17.91 | 21.39 | 30.09 | 580.33 | 297.89 | -1363.26 |
| H | 2274.64 | 187.28 | 10.35 | 0.05 | 9.81 | 21.24 | 30.35 | 622.32 | 337.56 | -1567.71 |
| I | 1842.64 | 169.18 | 14.15 | 0.07 | 13.06 | 19.27 | 25.77 | 544.78 | 255.57 | -1268.63 |
| J | 1991.19 | 108.64 | 8.40 | 0.07 | 7.79 | 19.88 | 27.32 | 563.11 | 284.65 | -1418.99 |

* σ+2, σ-2, vσtot2: (kal/mol)^2; ∆Hvap, ∆Hsub: kal/mol; Sm0, Cp,m0: J/mol/K;

HT0: kJ/mol

Table S3. Condensed Fukui Functions Properties of Designed Molecules Calculated Using PBE0/def2-SVP Method

| Compounds | ∆=0.1 Hartree |
| --- | --- |
| I | Atom q(N) q(N+1) q(N-1) f- f+ f0 CDD 1(C ) 0.0659 0.0150 0.1031 0.0372 0.0510 0.0441 0.0138 2(C ) 0.0660 0.0150 0.1030 0.0371 0.0510 0.0440 0.0139 3(C ) 0.0660 0.0471 0.1030 0.0371 0.0188 0.0280 -0.0183 4(C ) 0.0660 0.0471 0.1030 0.0370 0.0188 0.0279 -0.0182 5(C ) 0.0660 0.0472 0.1032 0.0371 0.0188 0.0280 -0.0183 6(C ) 0.0660 0.0472 0.1031 0.0371 0.0188 0.0279 -0.0183 7(O ) 0.0332 -0.0964 0.0785 0.1117 0.0632 0.0874 -0.0484 8(O ) 0.0332 -0.0964 0.0785 0.1117 0.0632 0.0874 -0.0485 9(O ) 0.0333 -0.1203 0.0785 0.1118 0.0871 0.0994 -0.0247 10(N ) 0.0263 -0.1530 0.0382 0.0645 0.1266 0.0956 0.0621 11(N ) 0.0263 -0.1530 0.0382 0.0645 0.1267 0.0956 0.0622 12(N ) 0.0263 -0.1023 0.0382 0.0645 0.0760 0.0703 0.0115 13(N ) 0.0263 -0.1023 0.0382 0.0645 0.0760 0.0703 0.0115 14(N ) 0.0263 -0.1024 0.0382 0.0645 0.0761 0.0703 0.0116 15(N ) 0.0263 -0.1024 0.0382 0.0645 0.0761 0.0703 0.0116 16(N ) 0.0692 -0.0951 0.0415 0.0276 0.0259 0.0268 -0.0017 17(N ) 0.0692 -0.0951 0.0415 0.0276 0.0259 0.0268 -0.0017 |
| II | Atom q(N) q(N+1) q(N-1) f- f+ f0 CDD 1(C ) 0.0232 0.0058 0.0407 0.0176 0.0174 0.0175 -0.0002 2(C ) 0.0232 0.0058 0.0407 0.0176 0.0174 0.0175 -0.0002 3(H ) 0.0863 0.0621 0.1105 0.0242 0.0242 0.0242 -0.0000 4(H ) 0.0863 0.0621 0.1105 0.0242 0.0242 0.0242 -0.0000 5(O ) -0.0441 -0.1059 0.0648 0.1089 0.0617 0.0853 -0.0472 6(O ) -0.0442 -0.1297 0.0647 0.1088 0.0855 0.0972 -0.0233 7(O ) -0.0441 -0.1059 0.0647 0.1088 0.0618 0.0853 -0.0470 8(N ) -0.0492 -0.1223 0.0122 0.0614 0.0731 0.0673 0.0117 9(N ) -0.0492 -0.1223 0.0122 0.0614 0.0731 0.0673 0.0117 10(N ) -0.0492 -0.1222 0.0122 0.0614 0.0730 0.0672 0.0115 11(N ) -0.0492 -0.1222 0.0122 0.0614 0.0730 0.0672 0.0116 12(N ) -0.0492 -0.1706 0.0122 0.0614 0.1214 0.0914 0.0600 13(N ) -0.0492 -0.1706 0.0122 0.0614 0.1214 0.0914 0.0600 14(C ) 0.0347 0.0165 0.0717 0.0369 0.0182 0.0276 -0.0187 15(C ) 0.0348 0.0165 0.0716 0.0369 0.0182 0.0276 -0.0186 16(C ) 0.0348 -0.0153 0.0717 0.0369 0.0500 0.0435 0.0131 17(C ) 0.0348 -0.0153 0.0717 0.0369 0.0501 0.0435 0.0132 18(C ) 0.0348 0.0167 0.0717 0.0370 0.0181 0.0275 -0.0188 19(C ) 0.0348 0.0167 0.0717 0.0369 0.0181 0.0275 -0.0188 |

Table S4 Orbital Contribution(%) of Designed Molecules (∆=0.1 Hartree)

| Orbital | I | II |
| --- | --- | --- |
| HOMO energy | -0.312929 a.u. | -0.307703 a.u. |
| LUMO energy | -0.190834 a.u. | -0.157882 a.u. |
| Chemical potential | -0.251882 a.u. | -0.232793 a.u. |
| *HOMO | 17.49 % | 13.48 % |
| *HOMO-1 | 12.26 % | 9.19 % |
| *HOMO-2 | 8.14 % | 8.97 % |
| *HOMO-3 | 7.80 % | 8.97 % |
| *HOMO-4 | 7.10 % | 8.66 % |
| *HOMO-5 | 7.10 % | 8.66 % |
| *HOMO-6 | 6.94 % | 8.53 % |
| *HOMO-7 | 6.94 % | 7.93 % |
| *HOMO-8 | 6.39 % | 7.93 % |
| *HOMO-9 | 6.38 % | 5.53 % |
| **LUMO | 24.24 % | 28.82 % |
| **LUMO+1 | 24.24 % | 28.81 % |
| **LUMO+2 | 12.31 % | 13.71 % |
| **LUMO+3 | 11.46 % | 6.91 % |
| **LUMO+4 | 6.63 % | 6.91 % |
| **LUMO+5 | 6.62 % | 6.12 % |
| **LUMO+6 | 4.66 % | 2.96 % |
| **LUMO+7 | 4.66 % | 2.96 % |
| **LUMO+8 | 3.94 % | 1.88 % |

* 10 Highest weights in orbital-weighted f-;

** 10 Highest weights in orbital-weighted f+.

Figure S4. RDG Graft of Designed Molecules

(Left: Molecule I; Right: Molecule II)