Supplementary information

Revisit hydrophobically modified urethane-ethoxylate polymers: terminal sticker groups influences on thickening and dispersing

- GPC results

Table 1 Molecule weight of the ethoxylated urethane polymer series by GPC

| No. | TP series (TSP) | Mn | MP series (MPEG2000) | Mn |
| --- | --- | --- | --- | --- |
| 1 | TP-1 | 21965 | MP-1 | 20426 |
| 2 | TP-2 | 22863 | MP-2 | 19881 |
| 3 | TP-3 | 25521 | MP-3 | 25651 |
| 4 | TP-4 | 34835 | MP-4 | 33655 |
| 5 | TP-5 | 44223 | MP-5 | 46086 |
| 6 | TP-6 | 56105 | MP-6 | 57048 |
| 7 | TP-7 | 65644 | MP-7 | 67982 |
| 8 | TP-8 | 78287 | MP-8 | 68942 |
| 9 | TP-9 | 81428 | MP-9 | 76936 |

- Figure 1 GPC graph of Sample TP-3

- TEM of carbon black dispersion with different polymers

Figure 2 TEM images of carbon black preparations. (a)(c) TP-4, (b)(d) MP-4

Fig 3 TEM images of carbon black preparations. (a)(c) TP-6, (b)(d) MP-6

Fig 4 TEM images of carbon black preparations. (a)(c) TP-8, (b)(d) MP-8

3. The storage stability of pigment preparations

Figure 5 Storage stability of carbon black dispersions:(a) TP , (b) MP series

- 4.Estimation of CMC by fluorescence spectra in polymer solutions.

- Figure 6 CMC of polymer solution by fluorescence spectrometry.

- (a)TP-1, (b)MP-1 (c)TP-3, (d)MP-3, (e)TP-9, (f)MP-9