Supplementary data

Novel fabricated chitosan supported bimetallic nanocomposites for paracetamol removal from homogeneous solutions and heterogeneous mixtures with focused antibacterial studies

Gautam V. Priyadarshia, Nirav P. Ravalb, Damia Barceloc,d, and Mrugesh H. Trivedia,*

a Department of Earth and Environmental Science, KSKV Kachchh University, Bhuj-Kachchh, Gujarat – 370001, India

b Department of Environmental Science and Engineering, School of Engineering and Sciences, SRM University-AP, Amaravati, Andhra Pradesh – 522 240, India

c Department of Environmental Chemistry, Institute of Environmental Assessment and Water Research, IDAEA-CSIC, Jordi Girona, 18-26, 08034 Barcelona, Spain.

d Sustainability Cluster, School of Engineering, UPES, Dehradun, India.

*Corresponding Author:

Mrugesh H. Trivedi, Ph.D.

Assistant Professor | Dept. of Earth and Environmental Science | Block-A|

Krantiguru Shyamji Krishna Verma Kachchh University | Bhuj-Kachchh |

Gujarat - 370015 | India |

+91-9429613901  |

drmrugesh.trivedi@gmail.com | drmrugesh.trivedi@kskvku.ac.in|

List of Supplementary Figures and Tables

| Fig. S1. | TEM images of synthesized ZnO NPs (a), Fe3O4 NPs (b) and bimetal-oxide (Zn-Fe) NPs (c). |
| --- | --- |
| Fig. S2. | EDS spectra of synthesized nanocomposite beads before and after PCM adsorption. |
| Fig. S3. | XPS analysis of CTS-TPP/Zn, CTS-TPP/Fe & CTS-TPP/Zn-Fe beads high resolution spectrum for C 1s (a-c), N 1s (d-e) and O 1s (g-i). |
| Fig. S4. | Proposed adsorptive removal mechanism for PCM using CTS supported metal-oxide nanocomposite beads. |
| Table S1 | Physicochemical characteristics of PCM. |
| Table S2 | Isotherm and kinetic equations used to model the PCM adsorption onto nanocomposite beads. |

|  | (a) (b) |
| --- | --- |
| (c) |  |  |

Fig. S1.

| Fig. S2. |  |
| --- | --- |

Fig. S3.

Fig. S4.

Table S1. Physicochemical characteristics of PCM.

| Molecular Weight | 151.16 |
| --- | --- |
| Molecular Formula | C8H9NO2 |
| Molecular weight | 151.16 |
| CAS No. | 103-90-2 |
| Melting Point | 169 °C (336 °F) |
| Solubility in water at 28 °C | 19 g L-1 |
| pH speciation curve for PCM |  |
| pH | 5.5 – 6.5 at 20 °C |
| Decomposition temperature | > 180 °C |

Table S2: Isotherm and kinetic equations used to model the PCM adsorption onto nanocomposite beads.

| PCM removal efficiency (%) |  | Ci-CfCi X 100 % | Ci (mg L-1) = Initial concentrations of PCM Cf (mg L-1) = Equilibrium concentrations of PCM. |
| --- | --- | --- | --- |
| PCM adsorption capacity onto beads (mg g-1) |  | Ci - Cf ×(V)W | V (L) = PCM solution volume W (g) = Amount of adsorbent. |
| Isotherm | Model |  | Parameters |
| Langmuir | Qe=Qmax KL Cf1+ KL Cf |  | Cf (mg L-1) = equilibrium concentrations of PCM, Qmax (mg g–1) = Langmuir monolayer adsorption capacity, Qe (mg g–1) = Equilibrium adsorption concentration of PCM onto beads, KL (L mg–1) = Langmuir constant |
| Freundlich | Qe= KF Cf1/n |  | KF (L mg-1) and 1/n = the empirical Freundlich adsorption constant and exponent associated with the adsorption capacity and intensity, respectively. |
| Kinetics | Model |  | Parameters |
| Pseudo-first-order | Qt= Qe (1 - e-k1 t) |  | Qe and Qt (mg g-1) = PCM adsorption capacity at time equilibrium and at time t, respectively. k1 (min−1) = the pseudo-first order rate constant. |
| Pseudo-second-order | Qt=Qe2 k2 t1+ Qek2 t |  | k2 (g mg−1 min−1) = the pseudo-second order rate constant. |