Supplementary Information for “Spontaneous Donor Defects and Voltage–Assisted Hole Doping in Beta-Gallium Oxides under Multiple Epitaxy Conditions”

Chenxi Nie1, Kai Liu1, Chengxuan Ke1, Xisong Jiang2, Yifeng He2, Yonghong Deng1, Yanhua Yan2,*, and Guangfu Luo1,3,*

1Department of Materials Science and Engineering, Southern University of Science and Technology, Shenzhen 518055, China

2Shenzhen CAPCHEM Technology Co. Ltd., Shabo Tongfuyu Industry Zone, Pingshan District, Shenzhen 518118, China

3Guangdong Provincial Key Laboratory of Computational Science and Material Design, Southern University of Science and Technology, Shenzhen 518055, China

*E-mail: yanyh@capchem.com, luogf@sustech.edu.cn

I. Selection of Defects to Investigate

For intrinsic point defects, we consider 10 vacancies and antisite defects, namely, VO1, VO2, VO3, VGa1, VGa2, GaO1, GaO2, GaO3, OGa1, and OGa2. Also, we include 4 relatively stable Ga and O interstitials, namely, Gai1, Gai3, Oi1, and Oi3, based on the PBE results (Supplementary Fig. 1a). For complex defects made of two-point defects, we exclude those related to the unstable GaO and OGa (Supplementary Fig. 2), those made of point defects with the same charge, and those that transform automatically to single points. Eventually, we select 17 intrinsic defects for HSE06+U calculations: VO1, VO2, VO3, VGa1, VGa2, GaO1, GaO2, GaO3, OGa1, OGa2, Gai1, Gai3, Oi1, Oi3, Gai3+Oi1, VO2+Oi1, and VO2+VGa2.

For impurity point defects, we examine the substitutional defects at both Ga and O sites and interstitial defects for C, H, and Cl impurities, based on previous experimental observations (Table 1). Given that CGa1 is more stable than CGa21, HO1 is more stable than HO2 and HO3, and ClO1 is more stable than ClO2 and ClO32, we calculate 17 point impurity defects using PBE method: CGa1, CO1, Ci1, Ci2, Ci3, HGa1, HGa2, HO1, Hi1, Hi2, Hi3, ClGa1, ClGa2, ClO1, Cli1, Cli2, and Cli3. The PBE results in Supplementary Fig. 1(b-d) reveal 6 impurity defects, namely, CGa1, HGa1, Hi1, Hi2, ClGa1, and ClO1, with relatively low formation energies and thus are examined further with HSE06+U method.

For impurity-related complex defects, we apply the same principles as intrinsic complex defects and calculate 12 ones using PBE method: CGa1+VGa2, CGa1+Oi1, HGa1+CGa1, Hi2+VGa2, HGa1+Hi2, HGa1+VO2, Hi2+Oi1, HGa1+Gai3, ClO1+VGa2, ClGa1+VO2, ClO1+Oi1, and ClGa1+ClO1. Based on the PBE results in Supplementary Fig. 1(e-g), we choose 4 impurity-related defects: CGa1+VGa2, HGa1+CGa1, HGa1+Hi2, and ClO1+VGa2 for HSE06+U calculations.

Besides the above 27 ones, we also examine 7 additional defects proposed in literature, including VGa1+VGa2+Gai13,4, 2VGa1+Gai23,4, 2VGa1+Gai33,4, 2VGa1+Gai2+VO15,6, 2VGa1+Gai2+2VO15, 2VGa1+Gai3+VO35, 2HGa1+Gai27. In total, we calculate 34 defects using the HSE06+U method.

Supplementary Figure 1. Defect formation energies of (a) Ga and O interstitials, and point defects related to impurities (b) C, (c) H, (d) Cl at the PBE level; defect formation energies for the (e) C-related, (f) H-related, and (g) Cl-related complex defects at the PBE level. The chemical potentials µ of O and Ga are based on the growth conditions of MOCVD for (a, e, f) and HVPE for (g); µC is the total energy of graphite per atom, µCl is the total energy of Cl2 gas per atom, µH = 0.5*(µH2O - µO).

Supplementary Figure 2. Formation energy of intrinsic point defects for (a)MBE, (b)HVPE, and (c)HVPE. The data here is same as that in Fig. 2(a, d, g) but shown with a wider energy range.

II. Transition Energy Level of MgGa20/-

Supplementary Table 1 compares the charge transition levels of MgGa20/- among experimental reports and theoretical predictions. Our HSE06+U (Ueff = 2.7 eV) calculations predict an energy level of 0.58 eV, which agrees with an experimental value of EVBM(240‑260 K) + 0.65 eV based on electron paramagnetic resonance8. However, the prediction based on HSE( = 0.32) is ~1.05 eV according to both literature9,10 and our own calculation, and there are also experimental reports with values falling in the range of 1.05–1.20 eV11,12. See defect formation energies of MgGa2 based on HSE06+U (Ueff = 2.7 eV) in Supplementary Fig. 3. One cause of the above divergence is that the experimental identification of defects relies heavily on comparison with theoretical prediction. Although it may be too early to conclude on this issue here, it is worth noting that certain native defects, such as 2VGa1+Gai3+VO3, indeed exhibit both high concentration and an acceptor level ~1.1 eV above VBM according to our results in Fig. 6.

Supplementary Table 1 Summary of charge transition level of MgGa20/-

| Method | E(0/-) |
| --- | --- |
| HSE( = 0.32) | EVBM(0 K) + 1.06 eV10 EVBM(0 K) + 1.05 eV9 EVBM(0 K) + 1.03 eV [this work] |
| Photoinduced electron paramagnetic resonance | EVBM(130 K) + 1.2 eV11 |
| Photoinduced current transient spectroscopy | EVBM(370‑410 K) + 1.05 eV12 |
| HSE06+U, Ueff = 2.7 eV | EVBM(0 K) + 0.58 eV [this work] |
| Electron paramagnetic resonance | EVBM(240‑260 K) + 0.65 eV8 |

Supplementary Figure 3. Formation energy of MgGa2 based on HSE06+U (Ueff = 2.7 eV) calculated by this work. VBM energy at 0 K is used and µMg and µGa are set to zero for convenience.

III. Tests of Computational Parameters for the HSE+U Method

To identify the optimal parameters for the HSE+U method, we examine the dependence of band gap and formation enthalpy of β-Ga2O3 as a function of Ueff and the Hatree-Fock mixing parameter  in the HSE functional. As shown in Supplementary Figure 1, the parameters in the overlapping region between Egexpt ± 0.1 eV and ΔHexpt ± 0.1 eV exhibit the best overall performance. Given that the widely used HSE06 functional (α = 0.25) falls in this overlapping region, we choose α = 0.25 and Ueff = 2.7 eV for our calculations.

Supplementary Figure 4. Predicted band gap and formation enthalpy of β-Ga2O3 as a function of Ueff and the Hatree-Fock mixing parameter  in the HSE functional. Yellow star corresponds to HSE06 functional (  0.25) and Ueff  2.7 eV; gray dots indicate the examined parameters. The experimental band gap near 0 K is 4.86 eV13,14 and the experimental formation enthalpy is -11.29 eV obtained at 298.15 K and 1 bar15,16.

Supplementary Table 2. Comparison of lattice constant, band gap, and formation enthalpy of β-Ga2O3 among predictions by different computational methods and experimental values.

|  | HSE06 | HSE ( 0.32) | HSE06+U, Ueff = 2.7 eV | Experiment |
| --- | --- | --- | --- | --- |
| a (Å) | 12.273 | 12.193 | 12.053 | 12.228† |
| b (Å) | 3.043 | 3.034 | 2.985 | 3.038† |
| c (Å) | 5.798 | 5.790 | 5.710 | 5.803† |
| (o) | 103.678 | 103.915 | 103.796 | 103.843† |
| Eg (eV) | 4.19 | 4.86 | 4.81 | ~4.86§ |
| ΔH (eV) | -10.26 | -10.52 | -11.33 | -11.29‡ |

†The lattice constants are extrapolated to 0 K based on experimental results in the temperature range of 4–1200 K17-19.

§The band gap is an average of the GW prediction of 4.80 eV at 0 K14 and the experimental value of 4.92 eV at 20 K13.

‡The experimental formation enthalpy was obtained under 298.15 K and 1 bar15,16.

Supplementary Table 2 indicates that HSE06+U (Ueff = 2.7 eV) gives the best overall predictions on lattice constants, bandgap, and formation enthalpy of β-Ga2O3, with errors no greater than 1.8% of the experimental values. By contrast, the HSE method with α = 0.32, widely used in previous studies of β-Ga2O35,9,10, significantly underestimate the formation enthalpy by ~0.77 eV, despite its satisfactory prediction of the band gap.

IV. Temperature Dependence of Band Edges of β-Ga2O3

To obtain the temperature dependence of VBM energy of β-Ga2O3, we carry out molecular dynamics (MD) simulations at the PBE level under 400, 800, 1200, 1600, and 2000 K. Given the weak thermal expansion of β-Ga2O317-19, we adopt the NVT ensemble and a 12.05 × 8.95 × 11.42 Å3 supercell predicted by HSE06+U geometry optimization. After reaching thermal equilibrium, several MD structures are extracted to obtain the average VBM and CBM energies at the HSE06+U level (Supplementary Fig. 5a). The temperature dependence of band gap in Supplementary Fig. 5b are in the general trend with the available experiment values13,20-23, which currently exhibit deviations at the level of ~0.3 eV.

Supplementary Figure 5. Temperature dependence of (a) band edges and (b) band gap for β-Ga2O3 from 0 to 2000 K. Available experimental band gaps13,20-23are included for comparison.

References

1	Lyons, J. L., Steiauf, D., Janotti, A. & Van de Walle, C. G. Carbon as a shallow donor in transparent conducting oxides. Phys. Rev. Appl. 2, 064005 (2014).

2	Varley, J. B., Weber, J. R., Janotti, A. & Van de Walle, C. G. Oxygen vacancies and donor impurities in β-Ga2O3. Appl. Phys. Lett. 97, 142106 (2010).

3	Varley, J. B., Peelaers, H., Janotti, A. & Van de Walle, C. G. Hydrogenated cation vacancies in semiconducting oxides. J. Phys. Condens. Matter 23, 334212 (2011).

4	Johnson, J. M., Chen, Z., Varley, J. B., Jackson, C. M., Farzana, E. et al. Unusual formation of point-defect complexes in the ultrawide-band-gap semiconductor β-Ga2O3. Phys. Rev. X 9, 041027 (2019).

5	Ingebrigtsen, M. E., Kuznetsov, A. Y., Svensson, B. G., Alfieri, G., Mihaila, A. et al. Impact of proton irradiation on conductivity and deep level defects in β-Ga2O3. APL Mater. 7, 022510 (2019).

6	Frodason, Y. K., Zimmermann, C., Verhoeven, E. F., Weiser, P. M., Vines, L. et al. Multistability of isolated and hydrogenated Ga-O divacancies in β-Ga2O3. Phys. Rev. Mater. 5, 025402 (2021).

7	Weiser, P., Stavola, M., Fowler, W. B., Qin, Y. & Pearton, S. Structure and vibrational properties of the dominant O-H center in β-Ga2O3. Appl. Phys. Lett. 112, 232104 (2018).

8	Lenyk, C. A., Gustafson, T. D., Basun, S. A., Halliburton, L. E. & Giles, N. C. Experimental determination of the (0/-) level for Mg acceptors in β-Ga2O3 crystals. Appl. Phys. Lett. 116, 142101 (2020).

9	Kyrtsos, A., Matsubara, M. & Bellotti, E. On the feasibility of p-type Ga2O3. Appl. Phys. Lett. 112, 032108 (2018).

10	Ritter, J. R., Huso, J., Dickens, P. T., Varley, J. B., Lynn, K. G. et al. Compensation and hydrogen passivation of magnesium acceptors in β-Ga2O3. Appl. Phys. Lett. 113, 052101 (2018).

11	Bhandari, S., Lyons, J. L., Wickramaratne, D. & Zvanut, M. E. Optical transitions of neutral Mg in Mg-doped β-Ga2O3. APL Mater. 10, 021103 (2022).

12	Polyakov, A. Y., Smirnov, N. B., Shchemerov, I. V., Yakimov, E. B., Pearton, S. J. et al. Electrical Properties, Deep Trap and Luminescence Spectra in Semi-Insulating, Czochralski β-Ga2O3 (Mg). ECS J. Solid State Sci. Technol. 8, Q3019-Q3023 (2019).

13	Mohamed, M., Unger, I., Janowitz, C., Manzke, R., Galazka, Z. et al. The surface band structure of β-Ga2O3. J. Phys. Conf. Ser. 286, 012027 (2010).

14	Ratnaparkhe, A. & Lambrecht, W. R. L. Quasiparticle self-consistent GW band structure of β-Ga2O3 and the anisotropy of the absorption onset. Appl. Phys. Lett. 110, 132103 (2017).

15	Barin, I. & Platzki, G. Thermochemical data of pure substances.  (Wiley Online Library, 1989).

16	Wagman, D. D., Evans, W. H., Parker, V. B., Schumm, R. H. & Halow, I. The NBS tables of chemical thermodynamic properties. Selected values for inorganic and C1 and C2 organic substances in SI units. J. Phys. Chem. Ref. Data 11, 131 (1982).

17	Víllora, E. G., Shimamura, K., Ujiie, T. & Aoki, K. Electrical conductivity and lattice expansion of β-Ga2O3 below room temperature. Appl. Phys. Lett. 92, 202118 (2008).

18	Orlandi, F., Mezzadri, F., Calestani, G., Boschi, F. & Fornari, R. Thermal expansion coefficients of β-Ga2O3 single crystals. Appl. Phys. Express 8, 111101 (2015).

19	Cheng, Z. Z., Hanke, M., Galazka, Z. & Trampert, A. Thermal expansion of single-crystalline β-Ga2O3 from RT to 1200 K studied by synchrotron-based high resolution x-ray diffraction. Appl. Phys. Lett. 113, 182102 (2018).

20	Onuma, T., Saito, S., Sasaki, K., Masui, T., Yamaguchi, T. et al. Valence band ordering in β-Ga2O3 studied by polarized transmittance and reflectance spectroscopy. Jpn. J. Appl. Phys. 54, 112601 (2015).

21	Rafique, S., Han, L., Mou, S. & Zhao, H. P. Temperature and doping concentration dependence of the energy band gap in β-Ga2O3 thin films grown on sapphire. Opt. Mater. Express 7, 3561-3570 (2017).

22	Li, G. L., Zhang, F. B., Cui, Y. T., Oji, H., Son, J. Y. et al. Electronic structure of β-Ga2O3 single crystals investigated by hard X-ray photoelectron spectroscopy. Appl. Phys. Lett. 107, 022109 (2015).

23	Mock, A., VanDerslice, J., Korlacki, R., Woollam, J. A. & Schubert, M. Elevated temperature dependence of the anisotropic visible-to-ultraviolet dielectric function of monoclinic β-Ga2O3. Appl. Phys. Lett. 112, 041905 (2018).