Tab. 1 Overview of ANN parameters for simulation of optical parameters of thin film of MoO3

| The name of ANN | No. HLs | (No. of Ns) | Inputs | epochs | MSE (training) | MSE (test) | MSE (validation) | R (training) | R (test) | R (validation) | Outputs |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Net. 1 | 1 | 10 | λ, d of film on glass | 77 | 8.1445x10-7 | 1.9 x10-7 | 5.538x10-6 | 0.999979 | 0.99997 | 0.99993 | T |
| Net. 2 | 1 | 20 | λ, d of film on glass | 115 | 3.488x10-8 | 4.731x10-8 | 1.70x10-8 | 0.999981 | 0.999980 | 0.999985 | T |
| Net. 3 | 1 | 10 | λ, d of film on Quartz | 30 | 2.898x10-7 | 2.89x10-7 | 3.47x10-7 | 0.999972 | 0.99978 | 0.99963 | R |
| Net. 4 | 1 | 10 | λ, d of film on Quartz | 94 | 5.116x10-9 | 2.877x10-9 | 6.72 x10-9 | 0.999972 | 0.999986 | 0.999961 | R |
| Net. 5 | 1 | 10 | λ, d of film on glass | 92 | 1.586x10-3 | 1.51x10-3 | 2.47x10-3 | 0.9964 | 0.9937 | 0.9964 | n |
| Net. 6 | 1 | 10 | λ, d of film on Quartz | 5 | 1.709x10-3 | 3.054x10-4 | 2.206x10-4 | 0.9952 | 0.9929 | 0.9847 | n |
| Net. 7 | 1 | 10 | λ, d of film on glass | 62 | 4.807x10-7 | 8.573x10-7 | 7.300x10-7 | 0.9992 | 0.9993 | 0.9993 | k |
| Net. 8 | 1 | 10 | λ, d of film on Quartz | 21 | 2.970x10-7 | 6.862x10-7 | 2.189x10-7 | 0.9983 | 0.9965 | 0.9955 | k |
| Net. 9 | 1 | 10 | E2 , d of film on glass | 14 | 1.0949x10-5 | 6.126x10-6 | 6.501x10-6 | 0.99905 | 0.99755 | 0.99937 | (n2-1)-1 |
| Net.10 | 1 | 10 | E2 , d of film on Quartz | 1000 | 1.0981x10-12 | 2.32x10-12 | 2.009x10-7 | 0.99999 | 0.99999 | 0.99999 | (n2-1)-1 |
| Net.11 | 1 | 25 | λ2, d of film on glass | 17 | 1.209x10-0 | 8.812x10-1 | 9.944410-1 | 0.92266 | 0.9937 | 0.96670 | n2 |
| Net. 12 | 1 | 10 | λ2, d of film on Quartz | 42 | 1.295x10-4 | 8.907x10-4 | 2.521x10-4 | 0.9809 | 0.99816 | 0.99913 | n2 |
| Net.13 | 1 | 10 | E, d of film on glass | 2 | 0.001348 | 0.0043231 | 0.0034301 | 0.999988 | 0.999990 | 0.999995 | (αE)2 |
| Net. 14 | 1 | 10 | E, d of film on Quartz | 22 | 0.175x10-5 | 1.263x10-5 | 3.139x10-5 | 0.99931 | 0.99999 | 0.93751 | (αE)2 |
| Net. 15 | 1 | 15 | E, d of film on glass | 2 | 1.978x10-1 | 1.183x10-2 | 2.078x10-2 | 0.99445 | 0.9995 | 0.9958 | ε1 |
| Net. 16 | 1 | 15 | E, d of film on Quartz | 5 | 6.653x10-3 | 9.392x10-2 | 5.841x10-3 | 0.99921 | 0.99604 | 0.9956 | ε1 |
| Net. 17 | 1 | 15 | E, d of film on glass | 14 | 8.496x10-6 | 2.005x10-5 | 1.22x10-4 | 0.99997 | 0.99944 | 0.98121 | ε2 |
| Net. 18 | 1 | 5 | E, d of film on Quartz | 4 | 3.257x10-4 | 1.234x10-4 | 4.572x10-4 | 0.97749 | 0.93199 | 0.85273 | ε2 |
| Net. 19 | 1 | 10 | E, d of film on glass | 13 | 1.868x10-8 | 2.639x10-8 | 1.751x10-7 | 0.999 | 0.9952 | 0.9965 | VELF |
| Net. 20 | 1 | 15 | E, d of film on Quartz | 3 | 4.389x10-6 | 2.501x10-7 | 1.449x10-6 | 0.9989 | 0.9941 | 0.95537 | VELF |
| Net. 21 | 1 | 10 | E, d of film on glass | 12 | 1.178x10-8 | 1.652x10-8 | 2.743x10-8 | 0.9993 | 0.9971 | 0.9974 | SELF |
| Net. 22 | 1 | 10 | E, d of film on Quartz | 30 | 2.369x10-7 | 3.473x10-7 | 1.675x10-7 | 0.9963 | 0.9878 | 0.9970 | SELF |

Tab. 2: The energy gap of a thin film of MoO3 with those published in the literature.

| Samples MoO3 onto glass MoO3 onto quartz | Eg (eV) (3.75)(experimental) and (3.77) ANN model (3.6)(experimental) and (3.62) ANN model | References Present work Present work |
| --- | --- | --- |
| α-MoO3 | 3.35 | [25] |
| α-MoO3 MoO3 α-MoO3 α-MoO3 α-MoO3 α-MoO3 β-MoO3 h-MoO3 | 3.2 2.8-3.2 3.18 2.9-3.9 3.75 3.15 3.01 2.99 | [26] [27] [28] [29] [30] [31] [31] [32] |

Tab. 3 Estimation between the ANN model simulation results and the dispersion parameters and energy gap of MoO3 thin film onto glass and quartz substrate

| Dispersion parameters | The obtained Experimental data | The obtained simulation results by ANN model |
| --- | --- | --- |
| E0 (MoO3 film onto glass) | 3.65 eV | 3.6 eV |
| E0 (MoO3 film onto quartz) | 2.36 eV | 2.37 eV |
| Ed (MoO3 film onto glass) | 25.8 eV | 25 eV |
| Ed (MoO3 film onto quartz) | 8.45 eV | 8.45 eV |
| εL (MoO3 film onto glass) | 8.15 | 8.2 |
| εL (MoO3 film onto quartz) | 7 | 6.95 |
| Eg(MoO3 film onto glass) | 3.75 eV | 3.77 eV |
| Eg (MoO3 film onto quartz) | 3.6 eV | 3.62 eV |