Supplementary Info

Fabrication of Scalable Mesoporous Zincospiroffite (Zn2Te3O8) -RGO Hybrid Electrodes for Low-Cost High-Performance Supercapacitors

Aswini Ramakrishnana, Bhabina Ninnora Meethalb, Shaniba Thekkethila, Sindhu Swaminathana*

aDepartment of Nanoscience and Technology, University of Calicut, Kerala 673635, India

bR. S. M. SNDP Yogam College, Koyilandi, Kozhikode, Kerala 673305, India

*Corresponding author: sindhus@uoc.ac.in

FTIR spectrum

From Fig S1. the stretching modes of O-H bonds are responsible for the broad peak at 3437 cm-1. It is not practical to remove all of the water content from the surface of graphene oxide. This is a component of the graphene oxide structure and is derived from tertiary alcohols. The hydroxyl group is responsible for it. This is because graphene oxide is hydrophilic. It is also derived from the water molecule that is associated with the graphene oxide platform. The peaks at 2929 cm-1 and 2847 cm-1 correspond to symmetric and anti-symmetric CH2 vibrations, respectively. Graphene oxide is represented by the peaks at 1720 cm-1 and 1625 cm-1. They correspond to carboxylic and carbonyl moieties C=O stretching vibrations. There are no other bands nearby that are clearly visible. The correct position of the first peak ranges from 1719 cm-1 to 1734 cm-1, while the second ranges from 1615 cm-1 to 1626 cm-1. The bending vibrations of C-OH functional groups cause the peak at 1394 cm-1. The two-absorption peak at 1262 cm-1 corresponds to epoxy rings, while the C-O stretching vibrations peak at 1034 cm-1 corresponds to C-O stretching vibrations.

Figure S1. FTIR analysis of the graphene oxide

XRD analysis

A strong peak can be seen at 2q =10.89o with a stacking in the (0 0 2) direction seen in fig S2a. This is the graphene oxide diffraction peak. The interlayer spacing, or d spacing, is 0.816 nm. The presence of oxygen-containing functional groups causes the larger d spacing. This diffraction peak changes with changes in interlayer spacing depending on the concentration of KMnO4. The extent of oxidation and the number of water molecules intercalated into the interlayer spacing determine the d spacing of graphene oxide in the 0.6 nm to 1.0 nm range. The crystalline size, D, was calculated using Scherrer's equation and was found to be 5.1 nm. The graphene oxide XRD results show that the graphite powder has been successfully oxidised.  The variation of graphene oxide during synthesis made ZTR1 and ZTR4. The XRD pattern given in Fig S2b and is matching with JCPDS data.

Figure S2. XRD pattern of the (a) graphene oxide and (b) ZTR 1 and ZTR4

Raman analysis

The Raman spectrum reveals two distinct peaks: D-defects and G-graphite. The D band at 1347 cm-1 indicates that the size of the in-plane sp2 domains is reduced during oxidation. The intensity of the D peak indicates the degree of disorder, which is the defect in its structure. This band was created as a result of the breathing mode of a six-membered ring. The G band at 1599 cm-1 corresponds to graphene oxide in phase vibration. The obtained ID/IG ratio is 0.47 shown in fig S3a. The lower the ID/IG value, the higher the level of oxidation. The variation in ID/IG is seen at changing the volume of graphene oxide during the synthesis in fig S3b. The samples ZTR1 and ZTR4 behave similar to ZTR2.

Figure S3.  Raman spectra of (a) graphene oxide (ID/IG = 0.47) and (b) ZTR4 (ID/IG = 0.87 and 1.16)

SEM analysis

According to SEM micrographs, the structure of graphene oxide is look like two-dimensional sheet in fig S4a. (a) and (b). In addition, the SEM images shows that graphene oxide has a crumbled and rippled structure as a result of deformation during the stacking process. The addition different volume of graphene oxide like 1ml and 4 ml shown in fig S4c-d. The lower graphene concentration shows the flake like structure and the higher concentration shows the large sheet like formation.

Figure S4.  Different magnification of FE-SEM images of graphene oxide (a) 100 nm and (b) 200 nm, (c) ZTR1 and (d) ZTR4.

Surface Area Analysis

The specific surface area of ZTR1, ZTR and ZTR4 are 15.20 m2 g-1, 15.09 m2 g-1 and 3.64 m2 g-1 respectively.  As a result of the hybrid synthesis process, ZTR has twice the surface area of ZTO.

Figure S5. BET N2 adsorption –desorption of (a) ZTR1 and (b) ZTR4

The zincospiroffite was distributed across the graphene sheets with help of GO, enhancement in surface area and give rise to the doubled porosity. The ZTR's high specific surface area enhancing the electron transfer and mass flow in electrochemical process. This is featuring a good criterion for the material, which has a higher performance-specific capacitance. The BJH (Barrett-Joyner-Halenda) pore size distribution curve gives mean pore diameter of ZTR1- 3.56 nm, ZTR- 4.29 nm, ZTR4- 2.88 which corresponds to mesopore characteristics. The highlights of surface area analysis are given in table S1.

| Sample Name | SSABET(m2/gm) | TPV (cm3/g) | Pore diameter (nm) |
| --- | --- | --- | --- |
| ARGO | 242.57 | 0.228 | 3.76 |
| ZTO | 6.17 | 0.008 | 5.25 |
| ZTR1 | 15.20 | 0.013 | 3.56 |
| ZTR | 15.09 | 0.016 | 4.29 |
| ZTR4 | 3.64 | 0.002 | 2.88 |

Table S1. Specific surface area (SSA), total pore volume (TPV), and pore diameter of ZTO, ARGO, and ZTR hybrids.

Electrochemical Analysis

Comparing the CV (fig S6a) of ZTR1, ZTR and ZTR4, the ZTR with pore diameter of 4.29 nm displays better electrochemical activities than other two. The same trend observed in GCD profiles as seen in fig S6b. Evaluating the CV at 10 mV/s, ZTR1 gives 106.8 F/g, ZTR gives 513.51 F/g and ZTR4 gives 298.0 F/g.

Figure S6. Comparing electrochemical measurements of ZTR1, ZTR and ZTR4 (a) Cyclic voltammogram at 10 mV/s and (b) GCD profile comparison at 0.125 A/g.