Supplementary Information

Avalanche tuning in bionic MoS2/WS2 transistor for high-frequency visual behavior beyond human retina

Figure 1. Optical microscopy images of the device structure and electrical connections for the junction filed effect transistor (JFET) consisting of an ultrathin MoS2 transport channel and top WSe2 gate.

Figure 2. EDX analysis of cross sectional MoS2/WSe2 interface, corresponding to (a) MoS2 and (b) WSe2, respectively.

Figure 3. In situ surface potential difference (SPD) plot of the measured MoS2/WSe2 interface.

Figure 4. The linear part of the I-V curve. The ideal factor (n) is calculated using the formula: n=qkbTdVdlnI, where q, kb and T are elementary charge, Boltzmann constant and Kelvin temperature.

Figure 5. Transfer (a) and output (b) characteristics of the device acting JFET. The transfer curves at VDS at 4, 8 and 10 V are nearly overlapped, showing the device enters the saturation region from 4 to 10 V, which is consistent with output curve.

Figure 6. The definition of the VEB at different gate voltage (VGS). The VEB is the intersection of the extension of the linear region of the saturation current and the IDS.

Figure 7. Noise spectral density (Sn) of the device at different VDS by the Fourier transformation of dark current traces.

Figure 8. The ionization index at different VGS.

Figure 9. Avalanche external quantum efficiency (EQE) at VDS = 20 V as function of light power.

Figure 10. The definition of the VEB under different fixed laser power. The VEB is the intersection of the extension of the linear region of the saturation current and the IDS.

Figure 11. The VEB as function of laser power.

Figure 12. Photo-response of the device at different VDS under light power of 50.2 pW.

Figure 13. Photo-response at VDS = 6 V under different fixed light power.

Figure 14. Photo-response as function of light power at VDS = 6 V.

Figure 15. Photo-response at VDS = 20 V under different fixed light power.

Figure 16. Photo-response as function of light power at VDS = 20 V, showing the PPC and NPC effect at weak and strong laser illumination, respectively.

Figure 17. Photo-response with different frequency at VDS = 20 V and laser power of 2622.5 pW.

Figure 18. Photo-response with different frequency at VDS = 20 V and laser power of 50.2 pW..

Figure 19. Time-varying current by switching laser power between 50.2 and 2622.5 pW with different frequency at VDS = 20 V.