On the Performance of Sargassum derived Calcium Alginate Ion Exchange Resins for Pb2+ Adsorption: Batch and Packed Bed Applications

Akeem Mohammeda, Chantal Mohammeda Andreas Mautnerb,c, Matika Kistowa, Pooran Chaitrama, Alexander Bismarckc, Keeran Wardd*.

aDepartment of Chemical Engineering, The University of West Indies St. Augustine, Trinidad and Tobago

bInstitute of Environmental Biotechnology, IFA-Tulln, University of Natural Resources and Life Sciences Vienna, Konrad-Lorenz-Str. 20, 3430 Tulln, 1180 Vienna, Austria

cInstitute of Materials Chemistry and Research, Polymer and Composite Engineering (PaCE) Group, Faculty of Chemistry, University of Vienna, Währinger Straße 42, 1090 Vienna, Austria

dSchool of Chemical and Process Engineering (SCAPE), University of Leeds, Leeds, LS2 9JT, United Kingdom

*Corresponding author, Dr. Keeran Ward, School of Chemical and Process Engineering (SCAPE), University of Leeds, Leeds, LS2 9JT, United Kingdom

Email: k.r.ward@leeds.ac.uk;

Tel: +44 7456 142816

Supplementary Information

Methodology

S1: Rheology Study

Sodium alginate concentration (2-8wt%) as well as GO (5-20% v/v) and AA (1-5 w/v%) were mixed  and their viscosities measured at 25oC and a torque of less than 10% using a rheometer (Brookfield, AMTEK, USA. Beads were fabricated for each mixture following the procedure in the main article (Section 2.3). Each resin was imaged using a light microscope (Amscope). The maximum inscribed and circumscribed circles as well as the diameters were recorded. The sphericity was determined using  equation (1), as shown below

Sphericity, φ=Di/Dc                                                      (1)

Where Di is the largest inscribed circle, and Dc is the smallest circumscribed circle.

S2: Cycle time and scale-up

The following equations were adapted from literature to determine the mass of adsorbent required, M (g) and diameter (cm) of the bed required. This scale-up requires knowledge of the breakthrough curve from a test column, which was operated at a predefined flow rate of Qb (cm3 min-1) resulting in a breakthrough time of Tb (min). The bed volume was estimated using equation (2).

Bed volume (BV) = QQb                                      					            (2)

The mass of the adsorbent, M (g) with a bulk density, φ, (g cm-3) for the design column was determined from equation (3).

M = φ × BV                                                   					           (3)

The pilot scale breakthrough volume which occurs during a breakthrough time of τ (mins)

(Yoon and Nelson model) was calculated using equation (4).

VB = Qb x τ                                                						           (4)

The volume of liquid treated per unit mass of adsorbent, VB, was then determined using equation (5).

VB= VBM                                                         						           (5)

The mass of adsorbent exhausted per hour, Mt, (g), and the breakthrough time, T (mins), for the design column was estimated using equation (6) and (7) respectively:

Mt = QVB                                                    						           (6)

T=MMt                                                   						           (7)

The volume, area, and diameter of the bed, VB (cm3), for the design column was then estimated using equations (8)-(10):

VB = Qb x T                                              						          (8)

A = VBh                                                   						          (9)

d = √4×Aπ                                                						          (10)