Supplementary Information

Low-Frequency Conductivity of Low Wear High-Entropy Alloys

Cheng-Hsien Yeh 1,6, Wen-Dung Hsu 2,5,6*, Bernard Haochih Liu 2,6*, Chan-Shan Yang 3,6,7,*, Chen-Yun Kuan 2, Yuan-Chun Chang 2, Kai-Sheng Huang 2, Song-Syun Jhang 2,

Chia-Yen Lu 3, Peter K. Liaw 4, and Chuan-Feng Shih 1,6,*

1 Department of Electrical Engineering, National Cheng Kung University, Tainan, Taiwan

2 Department of Materials Science and Engineering, National Cheng Kung University, Tainan, Taiwan

3 Institute and Undergraduate Program of Electro-Optical Engineering, National Taiwan Normal University, Taipei, Taiwan

4 Department of Materials Science and Engineering, The University of Tennessee, Knoxville, TN, USA

5 Program on Semiconductor Packaging and Testing, Academy of Innovative Semiconductor and Sustainable Manufacture, National Cheng Kung University, Tainan, Taiwan

6 Applied High Entropy Technology (AHET) Center, National Cheng Kung University, Tainan, Taiwan

7 Heterogeneously-integrated Silicon Photonic Integration Center (HiSiPIC), Ministry of Education, Taipei, Taiwan

*E-mail: cfshih@mail.ncku.edu.tw (Chuan-Feng Shih), wendung@mail.ncku.edu.tw (Wen-Dung Hsu), hcliu@mail.ncku.edu.tw (Bernard Haochih Liu), csyang@ntnu.edu.tw (Chan-Shan Yang)

Supplementary Table 5 | The calculation results of the derailed lattice data of NbMoTaW thin films.

| Nb25Mo25Ta25W25 | a | b | c | α | β | γ |
| --- | --- | --- | --- | --- | --- | --- |
| model1 | 3.23 | 3.23 | 3.22 | 90.15 | 90.31 | 90.11 |
| model2 | 3.23 | 3.22 | 3.23 | 89.63 | 90.15 | 90.09 |
| model3 | 3.22 | 3.23 | 3.23 | 90.27 | 90.01 | 90.06 |
| average | 3.23 | 3.22 | 3.23 | 90.02 | 90.16 | 90.09 |
| Nb15Mo15Ta35W35 | a | b | c | α | β | γ |
| model1 | 3.23 | 3.23 | 3.23 | 90.04 | 89.94 | 89.68 |
| model2 | 3.22 | 3.23 | 3.24 | 90.06 | 90.00 | 90.05 |
| model3 | 3.23 | 3.22 | 3.24 | 90.20 | 89.92 | 90.10 |
| average | 3.23 | 3.23 | 3.24 | 90.10 | 89.95 | 89.94 |
| Nb15Mo35Ta15W35 | a | b | c | α | β | γ |
| model1 | 3.20 | 3.20 | 3.21 | 90.00 | 90.02 | 90.16 |
| model2 | 3.20 | 3.20 | 3.21 | 89.96 | 90.04 | 89.97 |
| model3 | 3.20 | 3.20 | 3.21 | 90.04 | 90.02 | 89.92 |
| average | 3.20 | 3.20 | 3.21 | 90.00 | 90.03 | 90.01 |