Supplementary Information

Low-Frequency Conductivity of Low Wear High-Entropy Alloys

Cheng-Hsien Yeh 1,6, Wen-Dung Hsu 2,5,6*, Bernard Haochih Liu 2,6*, Chan-Shan Yang 3,6,7,*, Chen-Yun Kuan 2, Yuan-Chun Chang 2, Kai-Sheng Huang 2, Song-Syun Jhang 2,

Chia-Yen Lu 3, Peter K. Liaw 4, and Chuan-Feng Shih 1,6,*

1 Department of Electrical Engineering, National Cheng Kung University, Tainan, Taiwan

2 Department of Materials Science and Engineering, National Cheng Kung University, Tainan, Taiwan

3 Institute and Undergraduate Program of Electro-Optical Engineering, National Taiwan Normal University, Taipei, Taiwan

4 Department of Materials Science and Engineering, The University of Tennessee, Knoxville, TN, USA

5 Program on Semiconductor Packaging and Testing, Academy of Innovative Semiconductor and Sustainable Manufacture, National Cheng Kung University, Tainan, Taiwan

6 Applied High Entropy Technology (AHET) Center, National Cheng Kung University, Tainan, Taiwan

7 Heterogeneously-integrated Silicon Photonic Integration Center (HiSiPIC), Ministry of Education, Taipei, Taiwan

*E-mail: cfshih@mail.ncku.edu.tw (Chuan-Feng Shih), wendung@mail.ncku.edu.tw (Wen-Dung Hsu), hcliu@mail.ncku.edu.tw (Bernard Haochih Liu), csyang@ntnu.edu.tw (Chan-Shan Yang)

Supplementary Table 1 | The experimental values of conductivity, plasma frequency, and relaxation time for Nb, Mo, Ta, and W, , showing that Mo and W have the highest conductivity, followed by Ta, while Nb has the lowest conductivity 1.

| Element | Conductivity(S/m)_Exp. at 20℃ | ωDp (eV) | Relaxation time (s) |
| --- | --- | --- | --- |
| Nb | 6.90 × 106 | 9.11 | 4.07 × 10-15 |
| Mo | 1.89 × 107 | 9.01 | 11.4 × 10-15 |
| Ta | 7.60 × 106 | 8.86 | 4.73 × 10-15 |
| W | 1.89 × 107 | 7.93 | 14.7 × 10-15 |