Supplementary Information

Low-Frequency Conductivity of Low Wear High-Entropy Alloys

Cheng-Hsien Yeh 1,6, Wen-Dung Hsu 2,5,6*, Bernard Haochih Liu 2,6*, Chan-Shan Yang 3,6,7,*, Chen-Yun Kuan 2, Yuan-Chun Chang 2, Kai-Sheng Huang 2, Song-Syun Jhang 2,

Chia-Yen Lu 3, Peter K. Liaw 4, and Chuan-Feng Shih 1,6,*

1 Department of Electrical Engineering, National Cheng Kung University, Tainan, Taiwan

2 Department of Materials Science and Engineering, National Cheng Kung University, Tainan, Taiwan

3 Institute and Undergraduate Program of Electro-Optical Engineering, National Taiwan Normal University, Taipei, Taiwan

4 Department of Materials Science and Engineering, The University of Tennessee, Knoxville, TN, USA

5 Program on Semiconductor Packaging and Testing, Academy of Innovative Semiconductor and Sustainable Manufacture, National Cheng Kung University, Tainan, Taiwan

6 Applied High Entropy Technology (AHET) Center, National Cheng Kung University, Tainan, Taiwan

7 Heterogeneously-integrated Silicon Photonic Integration Center (HiSiPIC), Ministry of Education, Taipei, Taiwan

*E-mail: cfshih@mail.ncku.edu.tw (Chuan-Feng Shih), wendung@mail.ncku.edu.tw (Wen-Dung Hsu), hcliu@mail.ncku.edu.tw (Bernard Haochih Liu), csyang@ntnu.edu.tw (Chan-Shan Yang)

Supplementary Table 6 | Experimental results of the crystalline properties of the NbMoTaW films obtained from XRD.

| Composition | Lattice constant (Å) | 2θ | d (Å) | FWHM | Grain size (nm) |
| --- | --- | --- | --- | --- | --- |
| Nb25Mo25Ta25W25 | 3.2332 | 39.39° | 2.2854 | 0.491° | 16.95 |
| Nb15Mo15Ta35W35 | 3.2380 | 39.28° | 2.2920 | 0.475° | 15.88 |
| Nb15Mo35Ta15W35 | 3.1967 | 39.87° | 2.2593 | 0.423° | 19.98 |