Supplementary Information

Low-Frequency Conductivity of Low Wear High-Entropy Alloys

Cheng-Hsien Yeh 1,6, Wen-Dung Hsu 2,5,6*, Bernard Haochih Liu 2,6*, Chan-Shan Yang 3,6,7,*, Chen-Yun Kuan 2, Yuan-Chun Chang 2, Kai-Sheng Huang 2, Song-Syun Jhang 2,

Chia-Yen Lu 3, Peter K. Liaw 4, and Chuan-Feng Shih 1,6,*

1 Department of Electrical Engineering, National Cheng Kung University, Tainan, Taiwan

2 Department of Materials Science and Engineering, National Cheng Kung University, Tainan, Taiwan

3 Institute and Undergraduate Program of Electro-Optical Engineering, National Taiwan Normal University, Taipei, Taiwan

4 Department of Materials Science and Engineering, The University of Tennessee, Knoxville, TN, USA

5 Program on Semiconductor Packaging and Testing, Academy of Innovative Semiconductor and Sustainable Manufacture, National Cheng Kung University, Tainan, Taiwan

6 Applied High Entropy Technology (AHET) Center, National Cheng Kung University, Tainan, Taiwan

7 Heterogeneously-integrated Silicon Photonic Integration Center (HiSiPIC), Ministry of Education, Taipei, Taiwan

*E-mail: cfshih@mail.ncku.edu.tw (Chuan-Feng Shih), wendung@mail.ncku.edu.tw (Wen-Dung Hsu), hcliu@mail.ncku.edu.tw (Bernard Haochih Liu), csyang@ntnu.edu.tw (Chan-Shan Yang)

Supplementary Table 8 | Mechanical properties 8, elastic constants C11, C12, C44 (GPa), bulk modulus B (GPa), shear modulus G (GPa), Young’s modulus E (GPa), and hardness Hv (GPa).

| (Gpa) | C11 | C12 | C44 | B | G | E | Hardness |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Nb25Mo25Ta25W25 | 345 | 192 | 83 | 243 | 80 | 217 | 6.68 |
| Nb15Mo15Ta35W35 | 383 | 169 | 63 | 240 | 81 | 218 | 6.88 |
| Nb15Mo35Ta15W35 | 392 | 192 | 91 | 258 | 94 | 253 | 8.30 |
| NbMoTaW(DFT) 8 | 414 | 186 | 69 | 262 | 84 | 229 | 6.66 |
| NbMoTaW(DFT) 8 | 371 | 160 | 69 | 230 | 82 | 223 | 7.44 |