Supplementary Information

Low-Frequency Conductivity of Low Wear High-Entropy Alloys

Cheng-Hsien Yeh 1,6, Wen-Dung Hsu 2,5,6*, Bernard Haochih Liu 2,6*, Chan-Shan Yang 3,6,7,*, Chen-Yun Kuan 2, Yuan-Chun Chang 2, Kai-Sheng Huang 2, Song-Syun Jhang 2,

Chia-Yen Lu 3, Peter K. Liaw 4, and Chuan-Feng Shih 1,6,*

1 Department of Electrical Engineering, National Cheng Kung University, Tainan, Taiwan

2 Department of Materials Science and Engineering, National Cheng Kung University, Tainan, Taiwan

3 Institute and Undergraduate Program of Electro-Optical Engineering, National Taiwan Normal University, Taipei, Taiwan

4 Department of Materials Science and Engineering, The University of Tennessee, Knoxville, TN, USA

5 Program on Semiconductor Packaging and Testing, Academy of Innovative Semiconductor and Sustainable Manufacture, National Cheng Kung University, Tainan, Taiwan

6 Applied High Entropy Technology (AHET) Center, National Cheng Kung University, Tainan, Taiwan

7 Heterogeneously-integrated Silicon Photonic Integration Center (HiSiPIC), Ministry of Education, Taipei, Taiwan

*E-mail: cfshih@mail.ncku.edu.tw (Chuan-Feng Shih), wendung@mail.ncku.edu.tw (Wen-Dung Hsu), hcliu@mail.ncku.edu.tw (Bernard Haochih Liu), csyang@ntnu.edu.tw (Chan-Shan Yang)

Supplementary Table 2 | The relaxation time and DC conductivity of three different compositions of NbMoTaW high entropy alloys.

| Alloy |  | ωDp (eV) | Relaxation Time (s) | DC conductivity (S/m) |
| --- | --- | --- | --- | --- |
| Nb25Mo25Ta25W25 | Exp. | - | - | 1.39 × 106 |
|  | Cal. Method 1 | - | - | 1.31 × 107 |
|  | Cal. Method 2 | 4.54 | 8.73 × 10-15 | 3.67 × 106 |
|  | Cal. Method 3 |  | 1.99 × 10-15 | 0.84 × 106 |
| Nb15Mo15Ta35W35 | Exp. | - | - | 0.98 × 106 |
|  | Cal. Method 1 | - | - | 1.31 × 107 |
|  | Cal. Method 2 | 3.77 | 9.12 × 10-15 | 2.66 × 106 |
|  | Cal. Method 3 |  | 2.04 × 10-15 | 0.59 × 106 |
| Nb15Mo35Ta15W35 | Exp. | - | - | 2.51 × 106 |
|  | Cal. Method 1 | - | - | 1.54 × 107 |
|  | Cal. Method 2 | 4.66 | 10.5 × 10-15 | 4.65 × 106 |
|  | Cal. Method 3 |  | 2.00 × 10-15 | 0.89 × 106 |