Supplementary Information

Low-Frequency Conductivity of Low Wear High-Entropy Alloys

Cheng-Hsien Yeh 1,6, Wen-Dung Hsu 2,5,6*, Bernard Haochih Liu 2,6*, Chan-Shan Yang 3,6,7,*, Chen-Yun Kuan 2, Yuan-Chun Chang 2, Kai-Sheng Huang 2, Song-Syun Jhang 2,

Chia-Yen Lu 3, Peter K. Liaw 4, and Chuan-Feng Shih 1,6,*

1 Department of Electrical Engineering, National Cheng Kung University, Tainan, Taiwan

2 Department of Materials Science and Engineering, National Cheng Kung University, Tainan, Taiwan

3 Institute and Undergraduate Program of Electro-Optical Engineering, National Taiwan Normal University, Taipei, Taiwan

4 Department of Materials Science and Engineering, The University of Tennessee, Knoxville, TN, USA

5 Program on Semiconductor Packaging and Testing, Academy of Innovative Semiconductor and Sustainable Manufacture, National Cheng Kung University, Tainan, Taiwan

6 Applied High Entropy Technology (AHET) Center, National Cheng Kung University, Tainan, Taiwan

7 Heterogeneously-integrated Silicon Photonic Integration Center (HiSiPIC), Ministry of Education, Taipei, Taiwan

*E-mail: cfshih@mail.ncku.edu.tw (Chuan-Feng Shih), wendung@mail.ncku.edu.tw (Wen-Dung Hsu), hcliu@mail.ncku.edu.tw (Bernard Haochih Liu), csyang@ntnu.edu.tw (Chan-Shan Yang)

Supplementary Table 3 | The plasma frequency, free electron density, and effective electron mass of the elements Nb, Mo, Ta, W, and the high entropy alloys Nb25Mo25Ta25W25, Nb15Mo15Ta35W35, Nb15Mo35Ta15W35.

| Materials | ωDp (eV) | Free electron density (electron/m3) | Effective mass (electron mass) |
| --- | --- | --- | --- |
| Nb | 9.11 | 3.28 × 1028 | 1.01 |
| Mo | 9.01 | 1.71 × 1028 | 2.86 |
| Ta | 8.86 | 1.39 × 1028 | 1.41 |
| W | 7.93 | 1.01 × 1028 | 0.85 |
| Nb25Mo25Ta25W25 | 4.54 | 2.56 × 1026 | 6.26 |
| Nb15Mo15Ta35W35 | 3.77 | 3.21 × 1026 | 4.61 |
| Nb15Mo35Ta15W35 | 4.66 | 2.47 × 1026 | 5.79 |