Supplemental Material for “Layer reconstruction, collapse and metallization of van der Waals bonded ZrS2 under high pressure”

Linfei Yang,1,2 Junwei Li,1 Dongzhou Zhang,3 Yuegao Liu,4 and Qingyang Hu1,*

1Center for High Pressure Science and Technology Advanced Research, Beijing 100094, China 2School of Material Science and Engineering, Jingdezhen Ceramic university, Jingdezhen 333001, Jiangxi, China

3Hawai’i Institute of Geophysics and Planetology, School of Ocean and Earth Science and Technology, University of Hawai’i at Manoa, Honolulu, HI 96822, USA

4CAS Key Laboratory for Experimental Study under Deep-sea Extreme Conditions, Institute of Deep-sea Science and Engineering, Chinese Academy of Sciences, Sanya 572000, China

* Corresponding author.

Email addresses: qingyang.hu@hpstar.ac.cn

Supplementary Figures

FIG. S1: The pressure dependence of the collected 2θ angles of diffraction peaks. Most diffraction peaks disappeared in the disordered phase III.

FIG. S2: Full spectra at collected at 1.6 GPa and 15.0 GPa. The Miller indices (hkl) are drawn in diagram for P3m1 and Pmm2 phases.

Supplementary Table S1

TABLE S1: The frequencies of phonon modes in different phases of ZrS2 and their corresponding pressure derivatives. The error bars are less than the length of symbols.

| Phase | ω0 (cm-1) | dω/dP (cm-1/GPa) |
| --- | --- | --- |
| Phase I trigonal: P3m1 | 140.5 | 3.49 |
|  | 191.0 | 2.75 |
|  | 248.8 | 3.16 |
|  | 312.7 | 7.14 |
|  | 332.7 | 6.20 |
| Phase II Orthorhombic: Pmm2 | 112.6 | -0.22 |
|  | 134.4 | 1.14 |
|  | 181.0 | 1.19 |
|  | 263.1 | 1.26 |
|  | 285.6 | 2.26 |
|  | 348.4 | 4.86 |
|  | 364.5 | 3.87 |
| Phase III | 141.1 | 0.02 |
|  | 157.8 | -0.16 |
|  | 164.3 | 0.90 |
|  | 192.2 | 1.06 |
|  | 248.6 | 0.61 |
|  | 318.3 | 1.82 |
|  | 378.1 | 1.89 |
|  | 408.3 | 3.41 |
|  | 456.2 | 2.59 |