Supporting Information

Functional cellulose paper with high transparency, high haze, and UV-blocking for perovskite solar cells

Yanhua Guana, Haodong Hea, Dexi Tanga, Xiaoqin Hanc, Haixia Zhangc, Jiayun Xud, Lin Dai*a,b,c, Zhanhua Huang*b, Chuanling Si*a

aState Key Laboratory of Biobased Fiber Manufacturing Technology, Tianjin Key Laboratory of Pulp and Paper, College of Light Industry and Engineering, Tianjin University of Science and Technology, Tianjin 300457, China

bKey Laboratory of Bio‑Based Material Science and Technology, Ministry of Education, College of Material Science and Engineering, Northeast Forestry University, Harbin, China

cWuzhou Special Paper Group Co., Ltd., Quzhou, China

dLaboratory of Natural Materials Technology, Åbo Akademi University, Turku FI-20500, Finland

*Corresponding author.

E-mail: dailin@tust.edu.cn (L. Dai), huangzh1975@163.com (Z. Huang), sichli@tust.edu.cn (C. Si).

Tel: 8622-60601313

Table of Contents

1. Supplementary Tables

Table S1. Dimension of cellulose fiber.

2. Supplementary Figures

Fig. S1. FTIR spectra of the cellulose paper, CMC film, TA, TH paper, and FTH paper.

Fig. S2. The transparency of the cellulose paper with different density.

Fig. S3. The haze of the cellulose paper with different density

Fig. S4. 40g/m2, 30g/m2, 25g/m2, and 20g/m2 of cellulose paper with 1wt% CMC solution.

Fig. S5. The transparency of the cellulose paper with different amount of CMC.

Fig. S6. The haze of the cellulose paper with with different amount of CMC.

Fig. S7. The transparency of TA solution with different concentration.

Fig. S8. The transparency of FTH paper with 16 wt% CMC and different amount of TA.

Table S1. Dimension of cellulose fiber.

| Fiber type | Average length | Average width |
| --- | --- | --- |
| Bleached kraft softwood pulp (BKP) | 1.666 mm | 30.9 μm |

Fig. S1. FTIR spectra of the cellulose paper, CMC film, TA, TH paper, and FTH paper.

Fig. S2. The transparency of the cellulose paper with different density.

Fig. S3. The haze of the cellulose paper with different density.

Fig. S4. 40g/m2, 30g/m2, 25g/m2, and 20g/m2 of cellulose paper with 1wt% CMC solution.

Fig. S5. The transparency of the cellulose paper with different amount of CMC.

Fig. S6. The haze of the cellulose paper with with different amount of CMC.

Fig. S7. The transparency of TA solution with different concentration.

Fig. S8. The transparency of FTH paper with 16 wt% CMC and different amount of TA.