Supplementary Information for “Active control of bulk photovoltaic effect in CuInP2S6 via flexoelectric engineering”

Junxi Yu,,,#, Boyuan Huang2,3,#,*, Songjie Yang1,2, Yuan Zhang2,3, Yinxin Bai, Wenjie Ming2,3, Wenyuan Liu, Junling Wang4, Changjian Li2,3, Qingyuan Wang1,,*, Jiangyu Li2,3,*

Fig. S1 The piezoresponse image, with a scan size larger than that of Fig. 2b, showing the substrate-supported region comprising both upward and downward polarizations. a Topography. b PFM phase. c Phase line profile along the red dashed line marked in (b).

Fig. S2 a AFM topography of Gr/CIPS/Gr as a function of different tip loading force. b line profile of topography along the red dashed line marked in (a). c, d Radius of curvature (c) and corresponding strain gradient (d) as a function of scanning force.

Fig. S3 a I-V curves under illumination measured at different tip loading force with dark and red lines representing smaller and larger forces, respectively. b, c Tuning curves measured at the same region with smaller (b) and larger (c) forces.

Institute for Advanced Study, Chengdu University, Chengdu 610100, China.

Department of Materials Science and Engineering, Southern University of Science and Technology, Shenzhen 518055, China.

﻿Guangdong Provincial Key Laboratory of Functional Oxide Materials and Devices, Southern University of Science and Technology, Shenzhen, Guangdong 518055, China.

﻿Department of Physics, Southern University of Science and Technology, Shenzhen, Guangdong 518055, China.

Institute of Flexible Electronics Technology of THU, Jiaxing, Zhejiang 314000, China.

﻿Failure Mechanics and Engineering Disaster Prevention and Mitigation Key Laboratory of Sichuan Province, Sichuan University, Chengdu 610065, China.

# These authors contributed equally to this work.

* Authors to whom the correspondence should be addressed to: lijy@sustech.edu.cn, wangqy@scu.edu.cn, and  huangby@sustech.edu.cn.