Supplementary information

Ultrafast carrier-lattice interactions and interlayer modulations of Bi2Se3 by X-ray free electron laser diffraction

Sungwon Kim1, Youngsam Kim2, Jaeseung Kim1, Sungwook Choi1, Kyuseok Yun1, Dongjin Kim1, Soo Yeon Lim1, Sunam Kim3, Sae Hwan Chun3, Jaeku Park3, Intae Eom3, Kyung Sook Kim3, Tae-Yeong Koo3, Yunbo Ou4, Ferhat Katmis4, Haidan Wen5, Anthony Dichiara5, Donald Walko5, Eric C. Landahl6, Hyeonsik Cheong1, Eunji Sim2, Jagadeesh Moodera4,7, and Hyunjung Kim1*

1Department of Physics, Sogang University, Seoul, 04107, Korea
2Department of Chemistry, Yonsei University, Seoul, 03722, Korea
3Pohang Accelerator Laboratory, Pohang, 37673, Korea
4Francis Bitter Magnet Laboratory, MIT, Cambridge, MA 02139, USA
5Advanced Photon Source, Argonne National Laboratory, Argonne, IL 60439, USA
6Department of Physics, DePaul University, Chicago, IL 60614, USA
7Department of Physics, MIT, Cambridge, MA 02139, USA

This file includes

Supplementary Notes 1-4
Supplementary Figures 1-10
	Supplementary Tables 1-3
Supplementary References

Supplementary Notes

Supplementary Note 1. Film thickness determination by X-ray reflectivity measurements

We measured X-ray reflectivity (XRR) and X-ray diffraction (XRD) to determine the thickness of the samples. Supplementary Fig. 1 shows (a) XRR results and fitting for the 16, 26, 43, and 78 QL samples and (b) (006) Bragg peak and fringes from 5, 7, and 16 QL samples. In XRR measurements, the wave vector transfer Qz in Supplementary Fig. 1a is 4π/λ sin θ, where θ is the incident angle, and λ is the X-ray wavelength. Kiessig fringes from the Bi2Se3 surface and the interface between the substrate in the reflectivity curves are from the thickness Bi2Se3. The recursive Parratt formalism with modified Fresnel coefficients was used to fit the XRR data1. The electron density profile of Bi2Se3 and Al2O3 was obtained with the surface and interface of tanh-profile for the roughness distribution function. The layer thicknesses are obtained as 157.0, 256.0, 430.3, and 780.3 Å from the Fourier transform of the XRR result.2

Sample thicknesses of 5, 7, and 16 QL are obtained from the XRD measurements. The thickness (d) is calculated from the fringe spacing (ΔQz) of (006) Bragg peak with the relation d= 2πΔQz. They are 47.0, 66.1, and 161.1Å.

Supplementary Note 2. Reduction of crystal truncation rods

Crystal truncation rods (CTRs) from multiple domains are detected at the (006) Bragg reflection. Supplementary Fig S2 shows the mean intensity profile along in-plane Qxy of Fig. 1a in the main text. The blue line is obtained from raw data. The sharp spikes from the CTR peak are clearly seen. Crystal truncation rods are excluded from the raw data to trace the Bragg peak position. The intensity profile shows only the central Bragg peak and fringes after excluding the column pixels of the detector image, which contains CTRs (red).

Supplementary Note 3. Raman measurement of Bi2Se3

Hexagonally close-packed Bi2Se3 with D3d point group has the irreducible representations of Γbulk=3Eu+3A2u+2Eg+2A1g, Γodd=5N-12A1g+Eg+5N+12(A2u+Eu) (N=1,3,5…), and Γeven=5N2A1g+A2u+Eg+Eu (N=2,4,6…), for bulk, odd-, and even-layer, respectively. To separate breathing modes (Ag modes) and shear modes (Eg modes), we used a λ/4 waveplate to convert the linearly polarized light to circularly polarized light, or vice versa. Incident and scattered light propagate along the z-axis of samples in back-scattering geometry. The Raman intensity is proportional to, where R represents the Raman tensor of each mode and  represents a vector of the circularly polarized incident and scattered light with  in back-scattering geometry. Raman tensors of A1g and Eg mode are given by , , and , respectively.

For the same circular polarization [(σ+σ+) or (σ-σ-)], the intensity of A1g mode is proportional to a2 whereas the intensity of Eg mode is zero.

On the other hand, the intensity of A1g mode is zero for the opposite circular polarization [(σ+σ-) or (σ-σ+)] whereas the intensity of Eg mode is proportional to c2. Since two Eg modes are degenerate, the polarization dependence has a superposed form of the two modes.

From these results, we observed the breathing (A1g) and shear modes (Eg) separately. For linearly polarized light, only the shear mode (Eg mode) is observed in cross-polarization ( ). In contrast, both the breathing (A1g) and the shear (Eg) modes are observed in parallel polarization () with the incident and scattered light represented by  in back-scattering geometry.

Since two Eg modes are degenerate, Raman intensity is proportional to the superposed form of .

We used the 632.8 nm of a He–Ne laser for Raman measurements. The laser beam was focused onto the sample by a 40× microscope objective lens (0.6 N.A.), and the scattered signal was collected and collimated by the same objective lens. The scattered signal was dispersed with a Jobin-Yvon Horiba iHR550 spectrometer (2400 grooves/mm) and detected with a liquid-nitrogen-cooled charge-coupled-device (CCD) detector. Reflective volume holographic filters (OptiGrate) were used to reject the Rayleigh-scattered light to access the low-frequency range below 100 cm−1. The samples were kept in a vacuum chamber during Raman measurements and the laser power was kept below 0.1 mW in order to avoid degradation. For linearly and circularly polarized Raman measurements, λ/2 and λ/4 waveplates were used to rotate or convert the polarization of the incident and scattered light. An analyzer selectively passed signals using parallel and cross-polarization configurations.

Supplementary Note 4. Exponential relaxations in the extended time delay range

In the time scale of hundreds of picosecond, the exponential relaxations are observed. Supplementary Fig. S7 shows the strain curve of (a) 26 QL and (b) 16 QL. Additional UTXRD experiment for (006) Bragg peak was carried out at 7-ID-C, Advanced Photon Source, USA. The rocking curve measurements are measured for each laser- x-ray delay position with ±0.8° centered at (006) Bragg peak position. The time resolution of the experimental setup was 50 ps, and the minimum time step chosen was 100 ps. A pump laser with an 800 nm wavelength was used. The relaxation of expansive strain up to the 8 ns time delay fits with a double-exponential relaxation function. The time constants are classified; one the relaxation time constant τrlx1 also observed in UTXRD in XFEL to Δt~1000ps and the additional relaxation time constant τrlx2 dominant in the nanosecond time scale. We found τrlx2 dominant after ~1.5 ns.

Supplementary Figures

Supplementary Figure 1. X-ray reflectivity and (006) Bragg X-ray diffraction measurements of the Bi2Se3 thin films used in the UTXRD. (a) The film thicknesses of 16, 26, 43, and 77 QL are confirmed by the fitting of X-ray reflectivity intensity data. (b) The thickness of the 5, 7, and 16 QL sample is determined by the fringe gap (ΔQz).

Supplementary Figure 2. In-plane mean valued intensity data of Figure 1 c in the main text. Mean valued raw data (red) and CTR excluded data (blue) are displayed. The intensity and the movement of the center of mass (COM) of the (006) Bragg peak are determined free from CTR contribution.

Supplementary Figure 3. An image of (006) and (015) Bragg peaks under simultaneous diffraction conditions. (a) (006) and (015) Bragg peaks diffracted on the detector at once. In this geometry, the vertical (horizontal) direction corresponds to Qz (Qxy) and out-of-plane (in-plane) direction.

Supplementary Figure 4. In-plane and out-of-plane change of the center of mass of the (006) and (015) Bragg peaks. (a-b) Out-of-plane components of center of mass (COM) of (006) Bragg peak with (red) and without laser (black) are shown. (c-d) In-plane components of COM of (006) Bragg peak with (red) and without laser (black) are shown.

Supplementary Figure 5. Damping constants. The damping constants obtained from the fit are plotted as a function of (a) the fluence for 16 QL and (b) the samples' thickness with 1.1 mJcm-2 of laser fluence. The damping constant is almost insensitive to the fluence, whereas it shows a linear dependence with the sample thickness.

Supplementary Figure 6. Circularly polarized Raman spectroscopy result. (a) Circularly polarized Raman spectra measured from 5 and 7 QL samples. Simple linear chain model fit the Raman shifts of (b) breathing mode with Kz=5.48×1019Nm-3 and (c) shear mode with Kx = 2.45×1019 Nm-3.

Supplementary Figure 7. The result of UTXRD over an extended time delay range. (a) Laser-induced strain extracted from (006) Bragg peak of (a) 26QL and (b) 16 QL Bi2Se3 up to 6 nanoseconds are shown. Ultrafast time-resolved X-ray diffraction experiment for the (006) Bragg peak was carried out at 7-ID-C, Advanced Photon Source, USA. The single data point for each laser- x-ray delay position is obtained from the rocking curve measurement with ±0.8° centered at (006) Bragg peak position. The time resolution of the experimental setup was 50 ps, and the minimum time step was 100 ps.

Supplementary Figure 8. Results from the 800 nm laser reflectance and transmittance measurement on the 16 QL sample. We measured the transmission and the reflectance of an 800 nm laser pulse for the same sample used in the UTXRD experiment to get the number of absorbed photons to the sample. The excited carrier density per unit volume (cm-3) is obtained by dividing the number of photons per unit area (cm-2) by the thickness of the sample. Note that the total thickness was considered for calculating the carrier concentration (n) since the penetration depth of the laser is estimated ~81 nm at the incident angle of 15.6° 3.

Supplementary Figure 9. The unit cell structure of Bi2Se3 used in Density Functional Theory calculations.

Supplementary Figure 10. DFT calculated band structure with interlayer distance expansion. (a) Equilibrium band structure. (b) Band structure with 0.26 Å expansion which is observed maximum expansion on 16 QL. (c) Band structure with 0.34 Å expansion where the band touching is observed. (d) Band structure with 0.6 Å expansion where the topological phase transition to the normal insulator is observed.

Supplementary Tables

Supplementary Table 1. The carrier density was obtained from the fluences used in UTXRD.

| Fluence (mJcm-2) | Reflectance (%) | Transmittance (%) | Absorbance (%) | electron/cm3 (×1019) |
| --- | --- | --- | --- | --- |
| 0.02 | 79.00 | 0.00 | 21.00 | 1.06 |
| 0.04 | 79.00 | 0.00 | 21.00 | 2.11 |
| 0.06 | 76.00 | 0.00 | 24.00 | 3.62 |
| 0.1 | 76.00 | 0.00 | 24.00 | 6.04 |
| 0.14 | 74.10 | 0.00 | 25.90 | 9.13 |
| 0.2 | 71.72 | 0.00 | 28.28 | 14.24 |
| 0.4 | 63.00 | 1.60 | 35.40 | 35.64 |
| 1.1 | 39.79 | 6.86 | 53.35 | 147.72 |
| 2.2 | 19.37 | 7.92 | 72.71 | 402.64 |
| 3.3 | 9.426 | 8.00 | 82.58 | 685.98 |

Supplementary Table 2. Lattice constants of Bi2Se3 unit cell used in DFT.

|  | x (Å) | y (Å) | z (Å) |
| --- | --- | --- | --- |
| a1 | 4.17000 | 0.00000 | 0.00000 |
| a2 | -2.08500 | 3.61133 | 0.00000 |
| a3 | 0.00000 | 0.00000 | 28.64000 |

Supplementary Table 3. Optimized atomic position of Bi2Se3 unit cell.

|  | x | y | z |
| --- | --- | --- | --- |
| Bi | 0.00000 | 2.40755 | 1.90340 |
| Bi | 0.00000 | 2.40755 | 7.64327 |
| Bi | 2.08500 | 3.61133 | 11.45006 |
| Bi | 0.00000 | 0.00000 | 17.18994 |
| Bi | 2.08500 | 1.20378 | 20.99673 |
| Bi | 2.08500 | 1.20378 | 26.73660 |
| Se | 0.00000 | 0.00000 | 0.00000 |
| Se | 2.08500 | 1.20377 | 3.48112 |
| Se | 4.17000 | 0.00000 | 6.06554 |
| Se | 2.08500 | 1.20378 | 9.54667 |
| Se | 0.00000 | 2.40755 | 13.02779 |
| Se | 2.08500 | 1.20378 | 15.61221 |
| Se | 0.00000 | 2.40755 | 19.09333 |
| Se | -2.08500 | 3.61133 | 22.57446 |
| Se | 0.00000 | 2.40755 | 25.15888 |

Supplementary References

1. Tolan, M. X-ray Scattering from Soft-Matter Thin Films; Springer, (1999).

2. Parratt, L. G. Surface studies of solids by total reflection of x-rays. Phys. Rev. 95, 359–369 (1954).

3. Kannan, A. G. & Manjulavalli, T. E. Structural, optical and electrical properties of Bi2Se3 thin films prepared by spray pyrolysis technique. Int. J. ChemTech Res. 8, 599–606 (2015).