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Fig.S1. Standard curve for UPLC quantitative analysis of dihydrotanshinone I.
Tab.S1 Factors and levels
	Levels
	Factors

	                
	     A                      B                         C

	
	Organic phase concentration (g/mL)
	Ratio of drug to polymer (g/g)
	Volume ratio of the organic phase to the aqueous phase (v/v)

	1
	1%
	1∶2
	1∶10

	2
	1.5%
	1.25∶1
	1∶1.8

	3
	2%
	2∶1
	1∶1




Tab.S2 Results of orthogonal experimental investigation
	Test number 
	Organic phase concentration (A)
	Mass ratio of drugs to polymer materials (B)
	Volume ratio of the organic phase to the aqueous phase (C)
	Encapsulation efficiency (EE) （%）

	1
	2
	1
	3
	14.51

	2
	2
	1
	2
	54.49

	3
	1
	3
	3
	44.41

	4
	3
	3
	1
	30.55

	5
	1
	1
	1
	15.20

	6
	2
	2
	1
	34.48

	7
	3
	1
	2
	15.69

	8
	3
	2
	3
	29.39

	9
	1
	2
	2
	36.09



Tab.S3 Error analysis results
	Source of variance
	Quadratic sum 
	f
	Mean square 
	F
	Sig

	Correcting the model
	1468.416
	6
	244.736
	8.438
	0.110

	Nodal increment
	8391.171
	1
	8391.171
	289.295
	0.003

	A
	137.662
	2
	68.831
	2.373
	0.296

	B
	1212.317
	2
	606.159
	20.898
	0.046

	C
	118.437
	2
	59.218
	2.042
	0.329

	Error
	58.011
	2
	29.006
	
	

	Grand total
	9917.598
	9
	
	
	

	Total of corrected
	1526.427
	8
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[bookmark: _GoBack]Fig.S2. PD-L1 expression on the GES-1 and HGC-27 cells determined by western blot.
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