Supporting Information

PD-L1 Antibody Conjugated Dihydrotanshinone I-loaded Polymeric Nanoparticle for Targeted Cancer Immunotherapy Combining PD-L1 Blockade with Immunogenic Cell Death

Fig.S1. Standard curve for UPLC quantitative analysis of dihydrotanshinone I.

Tab.S1 Factors and levels

| Levels | Factors |  |  |
| --- | --- | --- | --- |
|  | A B C |  |  |
|  | Organic phase concentration (g/mL) | Ratio of drug to polymer (g/g) | Volume ratio of the organic phase to the aqueous phase (v/v) |
| 1 | 1% | 1∶2 | 1∶10 |
| 2 | 1.5% | 1.25∶1 | 1∶1.8 |
| 3 | 2% | 2∶1 | 1∶1 |

Tab.S2 Results of orthogonal experimental investigation

| Test number | Organic phase concentration (A) | Mass ratio of drugs to polymer materials (B) | Volume ratio of the organic phase to the aqueous phase (C) | Encapsulation efficiency (EE) （%） |
| --- | --- | --- | --- | --- |
| 1 | 2 | 1 | 3 | 14.51 |
| 2 | 2 | 1 | 2 | 54.49 |
| 3 | 1 | 3 | 3 | 44.41 |
| 4 | 3 | 3 | 1 | 30.55 |
| 5 | 1 | 1 | 1 | 15.20 |
| 6 | 2 | 2 | 1 | 34.48 |
| 7 | 3 | 1 | 2 | 15.69 |
| 8 | 3 | 2 | 3 | 29.39 |
| 9 | 1 | 2 | 2 | 36.09 |

Tab.S3 Error analysis results

| Source of variance | Quadratic sum | f | Mean square | F | Sig |
| --- | --- | --- | --- | --- | --- |
| Correcting the model | 1468.416 | 6 | 244.736 | 8.438 | 0.110 |
| Nodal increment | 8391.171 | 1 | 8391.171 | 289.295 | 0.003 |
| A | 137.662 | 2 | 68.831 | 2.373 | 0.296 |
| B | 1212.317 | 2 | 606.159 | 20.898 | 0.046 |
| C | 118.437 | 2 | 59.218 | 2.042 | 0.329 |
| Error | 58.011 | 2 | 29.006 |  |  |
| Grand total | 9917.598 | 9 |  |  |  |
| Total of corrected | 1526.427 | 8 |  |  |  |

Fig.S2. PD-L1 expression on the GES-1 and HGC-27 cells determined by western blot.