Supplementary Information

Thermodynamically spontaneously intercalated crystal H3O+ enables long-lasting LiMn2O4 cathodes with enhanced proton tolerance in aqueous battery chemistry

Jiangfeng Huang1,+, Liang Xue1,+,*, Yin Huang1, Yanchen Jiang1, Ping Wu2, Xiulin Fan3, Junwu Zhu1,*

1Key Laboratory for Soft Chemistry and Functional Materials, Ministry of Education, School of Chemistry and Chemical Engineering, Nanjing University of Science and Technology, Nanjing 210094, China.

2Jiangsu Key Laboratory of New Power Batteries, School of Chemistry and Materials Science, Nanjing Normal University, Nanjing 210023, China.

3State Key Laboratory of Silicon and Advanced Semiconductor Materials, School of Materials Science and Engineering, Zhejiang University, Hangzhou 310027, China.

+These authors contributed equally: Jiangfeng Huang, Liang Xue.

*Corresponding Authors: Junwu Zhu (email: zhujw@njust.edu.cn), Liang Xue (email: xueliang@njust.edu.cn).

Supplementary Figures

Supplementary Fig. 1 The XRD spectrum of the synthesized LMO.

Supplementary Fig. 2 The SEM images of the synthesized LMO.

Supplementary Fig. 3 The charge/discharge curves of the LMO in aqueous electrolyte (orange) and organic electrolyte (violet).

Supplementary Fig. 4 The cycle performance of the LMO cycled in aqueous electrolyte (orange) and organic electrolyte (violet).

Supplementary Fig. 5 The mass changes of the LMO electrode during 200 cycles.

Supplementary Fig. 6 The partial EQCM curve and the analysis of the Δm/e−1.

Supplementary Fig. 7 Atomic configuration of LMO with (a) Li+ vacancies (b) H2O in tetrahedral sites (c) H2O in octahedral sites (d) H3O+ in tetrahedral sites and (e) H3O+ in octahedral sites.

Supplementary Fig. 8 The XRD spectra of the LMO charged in (a) aqueous electrolyte and (b) organic electrolyte before and after immersion in water for 12h.

Supplementary Fig. 9 (a) Li+ occupied the tetrahedral sites. (b) H3O+ occupied the octahedral sites.

Supplementary Fig. 10 The in situ XRD pattern of the LMO during charge/discharge progress in organic electrolyte.

Supplementary Fig. 11 The in situ XRD pattern of the LMO during charge/discharge progress in aqueous electrolyte.

Supplementary Fig. 12 The in situ XRD pattern of the LMO cycled after 200 cycles during charge/discharge progress in aqueous electrolyte.

Supplementary Fig. 13 The (a) HRTEM and (b) FFT analysis of the pristine LMO.

Supplementary Fig. 14 The (a) HRTEM and (b) FFT analysis of the LMO cycled in aqueous electrolyte after 200 cycles.

Supplementary Fig. 15 The XRD spectra of the LMO after 50 cycles in (a) organic electrolyte, (b) aqueous electrolyte, and (c) after 200 cycles in aqueous electrolyte.

Supplementary Fig. 16 The partial in situ XRD pattern of the LMO cycled after 200 cycles during charge/discharge progress in aqueous electrolyte.

Supplementary Fig. 17 The a-axis lattice parameter changes of LMO lattice in aqueous electrolyte (obtained from Rietveld refinements).

Supplementary Fig. 18 dQ/dV analyses of LMO in organic electrolyte at 1st, 100th, 200th, and 300th cycles.

Supplementary Fig. 19 dQ/dV analyses of LMO in aqueous electrolyte at 1st, 100th, 200th, and 300th cycles.

Supplementary Fig. 20 The LSV curves of the LMO in 1 M Li2SO4 with different content of ACN.

Supplementary Fig. 21 The C1s XPS spectra of the LMO after 100 cycles in 1 M Li2SO4 with 50% ACN

Supplementary Fig. 22 The N1s XPS spectra of the LMO after 100 cycles in 1 M Li2SO4 with 50% ACN

Supplementary Fig. 23 O 1s XPS spectra of LMO cycled in 1 M Li2SO4 with (a) 0% (b) 10% (c) 50% vol% of ACN.

Supplementary Fig. 24 dQ/dV analyses of LMO in 1 M Li2SO4 with different content of ACN.