Table S1 Ceramicizable resin mixing mass ratio

|  | ZrB2 particle | SiC particle | Silica resin |
| --- | --- | --- | --- |
| S0QRP | 0 | 0 | 4 |
| S1QRP | 3 | 0 | 1 |
| S2QRP | 1.5 | 1.5 | 1 |
| S3QRP | 2.25 | 0.75 | 1 |