Supplementary Material

Isolation of KH2PO4 from crude glycerol purified using Acromonia aculleata charcoal as adsorbent.

Milton de Souza Freitas1, João Victor Godinho1, David Lee Nelson1, Alexandre P. Wentz1, Claudio Roberto Neri2, Lucas D. Zanatta2, Fernando L. P. Pessoa3, Sandro L. Barbosa1*

1Department of Pharmacy, Universidade Federal dos Vales do Jequitinhonha e Mucuri-UFVJM, Campus JK, Rodovia MGT 367 - Km 583, nº 5.000, Alto da Jacuba, CEP 39100-000, Diamantina/MG, Brazil. e-mail: milton.freitas@ufvjm.edu.br (M.S.F.); sousa.joao@ufvjm.edu.br (J.V.S.); dleenelson@gmail.com (D.L.N.); wentzap@hotmail.com (A.P.W.); sandro.barbosa@ufvjm.edu (S.L.B.).

2Departamento de Química da Faculdade de Filosofia, Ciências e Letras de Ribeirão Preto da Universidade de São Paulo, Av. Bandeirantes 3900, Monte Alegre, CEP 14040-901, Ribeirão Preto/SP, Brazil. e-mail: crneri@usp.br (C.R.N.); lucaszanatta@alumni.usp.br (L.D.Z.).

3Centro Universitário SENAI-CIMATEC, Av. Orlando Gomes, 1845, Piatã, Salvador 41650-010, Brazil; fernando.pessoa@fieb.org.br (F.L.P.P.)

*Corresponding author. Tel.: +55-38-35321234; fax: +55-38-35321234; e-mail: sandro.barbosa@ufvjm.edu.br

_____________________________________________________________________________________

Abstract: Activated charcoal was prepared from Acrocomia aculeata (macaúba) endocarp by ZnCl2 activation. The charcoal was used for the adsorptive purification of pretreated crude glycerol (CG) and potassium dihydrogen phosphate (KH2PO4 or KDP) was formed by the addition of H3PO4 to the crude glycerol containing KOH, which was used as catalyst in the production of biodiesel and glycerol. The KH2PO4 was isolated and purified by recrystallization from aqueous solution. The KH2PO4 was characterized by X-Ray diffraction (XRD), thermal analysis (TGA/DTA) and spectrophotometry in the infrared region – FTIR. From 216.0 m of crude glycerol, 20.1038 g of purified KH2PO4 was obtained.

Keywords: Environmentally friendly processes; potassium dihydrogen phosphate; waste management; crystallization process, glycerol, fatty acid methyl ester.

_____________________________________________________________________________________

Copies of EDXRF of the KH2PO4.

- Commercial standard KH2PO4

Figure S1. XRD patterns of commercial standard KH2PO4.

- Sample 1 KH2PO4

Figure S2. XRD patterns of KH2PO4 (prepared dry solid samples).

- Sample 2 KH2PO4

Figure S3. XRD patterns of KH2PO4 (prepared dry solid samples).

- Sample 3 KH2PO4

Figure S4. XRD patterns of KH2PO4 (prepared dry solid samples).

- Sample 4 of KH2PO4

Figure S5. XRD patterns of KH2PO4 (prepared dry solid samples).

Copies of IV spectra for KH2PO4.

- Commercial standard KH2PO4.

Figure S6. FTIR on KBr pellet of the commercial standard of KH2PO4.

- Sample 1 KH2PO4.

Figure S7. FTIR on KBr pellet of the samples 1 of KH2PO4.

- Sample 2 KH2PO4.

Figure S8. FTIR on KBr pellet of the samples 2 of KH2PO4.

- Sample 3 KH2PO4.

Figure S9. FTIR on KBr pellet of the sample 3 of KH2PO4.

- Sample 4 KH2PO4.

Figure S10. FTIR on KBr pellet of the sample 4 of KH2PO4.