Appendix A: data on measurement of photocatalytic activity of metal oxide doped PP yarns

A.1 Measurement of fluorescence of residual sodium salicylate

Scan speed 600nm/min, excitation wave length 285 nm, emission wave length 400 nm.

Table A1: Luminescence measurement for control sample, datapoint used for halftime interpolation in bold

| t | Fluorescence measurement |  |  |  | C/C0 | Conversion |
| --- | --- | --- | --- | --- | --- | --- |
| hours | no.1 | no.2 | no.3 | Average |  | % |
| 0 | 7943 | 7476 | 7609 | 7676,000 | 1 | 0 |
| 24 | 5515 | 5159 | 5270 | 5314,667 | 0,6924 | 30,7625 |
| 48 | 4821 | 4826 | 4876 | 4841,000 | 0,6307 | 36,9333 |
| 72 | 4413 | 4512 | 4494 | 4473,000 | 0,5827 | 41,7275 |
| 96 | 4014 | 4060 | 4000 | 4024,667 | 0,5243 | 47,5682 |
| 120 | 3826 | 3830 | 3845 | 3833,667 | 0,4994 | 50,0565 |
| 168 | 3753 | 3729 | 3569 | 3683,667 | 0,4799 | 52,0106 |

Table A2: Luminescence measurement for control sample containing 1% Fe2O3, datapoint used for halftime interpolation in bold

| t | Fluorescence measurement |  |  |  | C/C0 | Conversion |
| --- | --- | --- | --- | --- | --- | --- |
| hours | no.1 | no.2 | no.3 | Average |  | % |
| 0 | 2239 | 2148 | 2329 | 2238,667 | 1 | 0 |
| 24 | 1720 | 1750 | 1738 | 1736,000 | 0,7753 | 22,4654 |
| 48 | 1395 | 1407 | 1379 | 1393,667 | 0,6225 | 37,7550 |
| 72 | 1320 | 1298 | 1278 | 1298,667 | 0,5800 | 41,9979 |
| 120 | 1162 | 1117 | 1120 | 1133,000 | 0,5060 | 49,3971 |
| 144 | 1105 | 1107 | 1095 | 1102,333 | 0,4923 | 50,7667 |

Table A3: Luminescence measurement for sample containing 1% TiO2, datapoint used for halftime interpolation in bold

| t | Fluorescence measurement |  |  |  | C/C0 | Conversion |
| --- | --- | --- | --- | --- | --- | --- |
| hours | no.1 | no.2 | no.3 | Average |  | % |
| 0 | 12090 | 11480 | 12704 | 12091,333 | 1 | 0 |
| 24 | 11170 | 10873 | 10856 | 10966,333 | 0,9070 | 9,3017 |
| 48 | 7950 | 8652 | 8487 | 8363,000 | 0,6917 | 30,8329 |
| 72 | 6734 | 6995 | 6913 | 6880,667 | 0,5691 | 43,0927 |
| 96 | 5665 | 6064 | 5980 | 5903,000 | 0,4882 | 51,1786 |
| 120 | 4973 | 4869 | 4987 | 4943,000 | 0,4088 | 59,1184 |
| 168 | 4138 | 5311 | 4737 | 4728,667 | 0,3911 | 60,8910 |

Table A4: Luminescence measurement for sample containing 1% ZnO, datapoint used for halftime interpolation in bold

| t | Fluorescence measurement |  |  |  | C/C0 | Conversion |
| --- | --- | --- | --- | --- | --- | --- |
| hours | no.1 | no.2 | no.3 | Average |  | % |
| 0 | 7473 | 7385 | 7452 | 7436,667 | 1 | 0 |
| 24 | 5711 | 5465 | 5609 | 5595,000 | 0,7523 | 24,7681 |
| 48 | 4606 | 4286 | 4740 | 4544,000 | 0,6110 | 38,9001 |
| 72 | 4303 | 4072 | 4050 | 4141,667 | 0,5569 | 44,3100 |
| 96 | 3439 | 3720 | 3666 | 3608,333 | 0,4852 | 51,4813 |
| 120 | 2825 | 3267 | 3019 | 3037,000 | 0,4084 | 59,1636 |
| 168 | 2732 | 2820 | 2805 | 2785,667 | 0,3746 | 62,5431 |

A.2 Measurement of absorbance of Ornage II solution at 485 nm

Table A5. Absorbance at 485 nm for solution irradiated with control sample – pure PP textile.

| time | Absorbance | c/c0 |
| --- | --- | --- |
| (hours) | (-) | (-) |
| 0,0 | 0,9995 | 1,00 |
| 0,5 | 0,9870 | 0,99 |
| 1,0 | 0,9810 | 0,98 |
| 2,5 | 0,9903 | 0,99 |
| 3,5 | 0,9945 | 0,99 |
| 4,5 | 0,9925 | 0,99 |
| 5,5 | 0,9852 | 0,99 |
| 8,5 | 0,9670 | 0,97 |
| 9,5 | 0,9544 | 0,95 |
| 11,0 | 0,9685 | 0,97 |
| 13,5 | 0,9787 | 0,98 |
| 15,5 | 0,9936 | 0,99 |
| 18,5 | 0,9843 | 0,98 |
| 21,5 | 0,9950 | 1,00 |
| 24,0 | 0,9947 | 1,00 |

Table A6. Absorbance at 485 nm for solution irradiated with PP textile containing 1% TiO2, datapoint used for halftime interpolation in bold

| time | Absorbance | c/c0 |
| --- | --- | --- |
| (hours) | (-) | (-) |
| 0,0 | 1,0004 | 1,00 |
| 0,5 | 0,9794 | 0,98 |
| 1,0 | 0,9663 | 0,97 |
| 2,5 | 0,9294 | 0,93 |
| 3,5 | 0,8793 | 0,88 |
| 4,5 | 0,8462 | 0,85 |
| 5,5 | 0,8006 | 0,80 |
| 8,5 | 0,6460 | 0,65 |
| 9,5 | 0,6361 | 0,64 |
| 11,0 | 0,5830 | 0,58 |
| 13,5 | 0,5228 | 0,52 |
| 15,5 | 0,4762 | 0,48 |
| 18,5 | 0,3382 | 0,34 |
| 21,5 | 0,2367 | 0,24 |
| 24,0 | 0,2107 | 0,21 |

Table A7. Absorbance at 485 nm for solution irradiated with PP textile containing 1% ZnO, datapoint used for halftime interpolation in bold

| time | Absorbance | c/c0 |
| --- | --- | --- |
| (hours) | (-) | (-) |
| 0,0 | 0,9957 | 1,00 |
| 0,5 | 0,9804 | 0,98 |
| 1,0 | 0,9790 | 0,98 |
| 2,5 | 0,9751 | 0,98 |
| 3,5 | 0,9620 | 0,97 |
| 4,5 | 0,9527 | 0,96 |
| 5,5 | 0,9312 | 0,94 |
| 8,5 | 0,8504 | 0,85 |
| 9,5 | 0,8339 | 0,84 |
| 11,0 | 0,8123 | 0,82 |
| 13,5 | 0,7545 | 0,76 |
| 15,5 | 0,7286 | 0,73 |
| 18,5 | 0,6502 | 0,65 |
| 21,5 | 0,5479 | 0,55 |
| 24,0 | 0,4390 | 0,44 |