Supporting Information

Lateral Heterostructures of WS2 and MoS2 Monolayers for Photo-Synaptic Transistor

Jaeseo Park1,†, Jun Oh Kim1,†, and Sang-Woo Kang1,2,*

1Advanced Instrumentation Institute, Korea Research Institute of Standards and Science, Daejeon 34113, Republic of Korea

2Precision Measurement, University of Science and Technology, Daejeon 34113, Republic of Korea

†Jaeseo Park and Jun Oh Kim contributed equally to this work

*Corresponding author. E-mail: swkang@kriss.re.kr

Figure S1. Output and transfer characteristics of the laterally-heterostructured WS2/MoS2-FET. (a) Output curves of IDS-VDS for various VG values from 0 V to +20 V in step of 5 V. (b) Transfer curve of IDS-VG at VDS of +1 V with a sweeping range from −30 V to +30 V.

Figure S2. Device structure and transfer characteristics of the MoS2-based back-gated FET. (a) Schematic illustration of the back-gated MoS2-based photo-transistor. Transfer characteristics with a wavelength of (b) 635 nm and (c) 532 nm are shown. Based on the IDS-VG transfer characteristic of the MoS2-FET, the on/off ratio of ~104, threshold voltage (VTH) of −16.98 V, and sub-threshold voltage (SS) of 3.93 V/dec are calculated (Experimental Section).

Figure S3. Time-resolved IDS under dark and 532 nm light illumination conditions at VDS of +1 V for 120 seconds. At VG of +30 V, the time-resolved IDS under (a) dark and (b) 532 nm light illumination conditions are shown. At VG of −30 V, the time-resolved IDS under (c) dark and (d) 532 nm light illumination conditions are shown.

Figure S4. Photo-response behavior of the MoS2-based photo-transistor under the illumination with different wavelengths of 532 nm (green) and 635 nm (red). The IDS of the photo-transistor was measured to time when illuminated by a single light pulse of 2 seconds at VG = −30 V and VDS = +1 V. After a single light pulse of 532 nm and 635 nm, the current immediately returned to its initial state.

Figure S5. Characteristics of (a-b) WS2/MoS2- and (c-d) MoS2-based photo-synaptic transistor under VG = −30 V, VDS = +1 V, and a 2-second light pulse with a wavelength of 532 nm. (a,c) EPSC triggered by a single light pulse. (b,d) EPSC triggered by 32 light pulses with an applied pulse width and time interval 2 seconds.