Preparation of durable superhydrophobic cotton fabric for self-cleaning and oil–water separation

Qingbo Xu*1 • Xiating Ke2 • Zongqian Wang1 • Peng Wang*1 • Changlong Li1

1Key Laboratory of Textile Fabric, College of Textiles and Clothing, Anhui Polytechnic University, Wuhu, Anhui 241000, China;

2State Key Laboratory of Photocatalysis on Energy and Environment, College of Chemistry, Fuzhou University, Fuzhou, Fujian 350002, P. R. China.

*Corresponding authors:

Email: xuqingbo@ahpu.edu.cn (Qingbo Xu); wangpeng@ahpu.edu.cn (Peng Wang)

- Materials

The reagents including N-hexane, cyclohexane, toluene, chloroform, dichloromethane (DCM), MMA, TFMA and 2, 2-azobis (2-methylpropionitrile) (AIBN) were obtained from Shanghai Aladdin Co., Ltd. (China). The cotton fabric (60 ends/cm, 30 picks/cm, 0.42 mm thickness, 120 g/m weight, 35.2 m2/g specific surface area) was obtained from Shaoxing Qidong Textile Co., Ltd. Before chemical modification, the cotton samples (3.0 cm × 3.0 cm) were cleaned by ultrasonic washing in 1 % sodium laurylsulfonate solution for 30 min, then washing in ethanol (2 h) and deionized water (30 min × 3 times).

- Characterizations

The water contact angle (WCA) was measured using deionized water droplets (4 μL) with a Kruss contact angle instrument (DSA 100, Kruss, Germany) at 25 °C. Average contact angle values were obtained by measuring three different positions on the same sample. Nuclear magnetic resonance (1H NMR) spectra were obtained on a 400 MHz ASCEND spectrometer (Bruker, Germany) in acetone-D6 as the solvent. Surface morphology of the cotton fabrics was investigated using an FE-SEM set (Ultra-55, Zeiss, Germany) with an energy dispersive X-ray spectrometer (EDS). Surface roughness was tested by using an atomic force microscope (AFM, Bruker Dimension Icon, Germany). Fourier transform infrared (FTIR) measurements were performed on a Nicolet Avatar 370 spectrometer (Nicolet Company, Madison, USA) in a normal transmission mode. Attenuated total reflectance infrared (ATR-IR) spectra were collected utilizing a Nicolet Avatar 370 spectrometer (Nicolet Company, Madison, USA) equipped with an ATR accessory. The X-ray diffraction (XRD) analyses for the modified fabrics were obtained using an X-ray diffractometer (D8 DISVOVER, Bruker, Germany). The X-ray photoelectron spectroscopy (XPS) analysis was performed using an AXIS multifunctional X-ray photoelectron spectrometer (ULTRA DLD, Shimadzu Ltd., Japan) at a power of 450 W.

Laundering durability was evaluated by monitoring WCA on the fabric surface periodically after every stringent washing process. The fabric samples (15 mm × 15 mm) were washed by 50 mL of an aqueous solution of sodium dodecanesulphonate (0.15 mol/L) in a beaker (diameter, 50 mm) with stirring (300 rpm, magnetic stirrer, 9 mm × 25 mm) at 25 °C for 10 min, rinsed with deionized water (35 °C, 10 mL × 4 times), and dried at 100 °C for 1 h.

The wearing durability tests were carried out on a Martindale type fabric abrader (HZ-8029A, China). The abrasive material was pure cotton fabric and the loading pressure was 12 KPa. The abrasion rotation rate of the top pure cotton fabric (D=120 mm) against the modified fabric surface (D = 20 mm) was 50 rpm.

Water absorptivity was examined by weighting the weight increment of the fabric sample after soaking in plenty of deionized water for 10 min and hanging out for another 10 min. It is expressed as the weight ratio of adsorbed water to the fabric sample.

Water vapour permeability was evaluated using ASTM E-96 (open cup test) method. The test fabric sample was placed tightly over a shallow dish containing distilled water. The weight loss of the test assembly over 24 h was measured and the vapor transmission rate (g m−2 d−1) was calculated as water vapour permeability.

Flexibility was determined by the flat loop method (IS 7016 Part 11). Fabric samples were cut from warp and weft directions (40 mm × 160 mm). A loop was made and was placed on a horizontal plane. The height of the loop was measured as an idea of the flexibility of the fabric. The lower the height of the loop, the greater is the flexibility.

Fig. S1. The FTIR spectra of the PMT.

Fig. S2. The 1HNMR spectra of the PMT.

Table S1. The element content of the fabric surface analysis by XPS technique

| Sample | C1s (%) | O1s (%) | F1s (%) |
| --- | --- | --- | --- |
| Pristine fabric | 64.38 | 35.62 | -- |
| SC-1 | 58.38 | 40.11 | 1.51 |
| SC-2 | 59.59 | 35.97 | 4.44 |
| SC-3 | 62.49 | 31.39 | 6.13 |