Supplementary Information for

A polymer-like ultrahigh-strength metal alloy

Zhizhi Xu1, Yuanchao Ji1*, Tianyu Ma1, Chang Liu3, Liqiang He1, Ye Yuan4, Yu Qian1, Wenjia Wang1, Yang Yang1, Xiaobing Ren1,2*

1 Frontier Institute of Science and Technology, and State Key Laboratory for Mechanical Behaviour of Materials, Xi’an Jiaotong University, Xi’an 710049, China

2 Center for Functional Materials, National Institute for Materials Science, Tsukuba 305-0047, Ibaraki, Japan

3 School of Materials Science and Engineering, Sichuan University, Chengdu 610065, China

4 Beijing National Laboratory for Condensed Matter Physics, Institute of Physics, Chinese Academy of Sciences, 100190 Beijing, China.

*Correspondence to: jyc.xjtu@xjtu.edu.cn (YJ) and REN.Xiaobing@nims.go.jp (XR)

This file includes:

- Supplementary Movie 1

- Supplementary Table 1

Supplementary Movie 1. A metal alloy showing simultaneously polymer-like ultrahigh flexibility and steel-like ultrahigh strength.

All the samples here were in the same "dog bone" shape and size as those used for tensile testing (described in Method section). A light load of 0.02 kg (~0.03 GPa) was used to examine the flexibility and a heavy load of 1.02 kg (1.3 GPa, for spring steel and DS-STG alloy) or 0.52 kg (~0.65 GPa, for FRP) was used to examine the yield strength.

Supplementary Table 1.  Data source for mechanical properties of typical metal alloys and organic materials used in Fig. 1a. Metal alloys include steel, Ti-alloy, Al-alloy, Cu-alloy, Mg-alloy and Ti-Ni-based shape memory alloys. Organic materials include bamboo, wood, bone, polyether ether ketone (PEEK), polyphenylene sulfide (PPS) and fiber reinforced polymers (FRP).

| Materials system | Yield stress (GPa) |  | Young’s modulus (GPa) |  | Elastic compliance (1/GPa) |  | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Min | Max | Min | Max | Min | Max |  |
| DS-STG alloy | 1.1 | 1.8 | 9.2 | 12.1 | 0.0826 | 0.1087 | Our work |
| Steel | 0.2 | 1.2 | 190 | 220 | 0.0045 | 0.0053 | Materials Selection in Mechanical Design 4th edn (Elsevier, 2011) |
|  | 0.6 | 2.25 | 190 | 190 | 0.0053 | 0.0053 | Science 357, 1029–1032 (2017) |
|  | 0.15 | 1.7 | 200 | 200 | 0.005 | 0.005 | Prog. Mater. Sci. 94, 174–242 (2018) |
| Ti-alloy | 0.25 | 1.2 | 88 | 120 | 0.008 | 0.11 | Materials Selection in Mechanical Design 4th edn (Elsevier, 2011) |
|  | 0.2 | 1.18 | 40 | 110 | 0.009 | 0.03 | Adv. Eng. Mater. 21, 1801215 (2019) |
| Al-alloy | 0.04 | 0.5 | 68 | 82 | 0.012 | 0.015 | Materials Selection in Mechanical Design 4th edn (Elsevier, 2011) |
|  | 0.17 | 0.47 | 63 | 75 | 0.013 | 0.016 | Nature 549, 365–369 (2017) |
|  | 0.2 | 0.5 | 70 | 70 | 0.014 | 0.014 | Science 363, 972–975 (2019) |
|  | 0.07 | 0.55 | 60 | 70 | 0.014 | 0.0167 | Nature 602, 437–441 (2022) |
| Cu-alloy | 0.06 | 0.5 | 110 | 150 | 0.007 | 0.009 | Materials Selection in Mechanical Design 4th edn (Elsevier, 2011) |
|  | 0.06 | 0.4 | 110 | 110 | 0.009 | 0.009 | Acta Mater. 110, 61–72 (2016) |
| Mg-alloy | 0.07 | 0.4 | 42 | 47 | 0.021 | 0.024 | Materials Selection in Mechanical Design 4th edn (Elsevier, 2011) |
|  | 0.05 | 0.4 | 15 | 47 | 0.021 | 0.067 | Nat. Mater. 21, 1003–1007 (2022) |
| Ti-Ni SMA | 0.35 | 0. 5 | 28.6 | 75.5 | 0.013 | 0.034 | Adv. Eng. Mater. 24, 2200239 (2022) |
|  | 1.42 | 1.42 | 33 | 33 | 0.030 | 0.030 | J. Mater. Sci. Technol. 57, 197–203 (2020) |
|  | 0.28 | 0.68 | 28 | 68 | 0.015 | 0.036 | Scr. Mater. 209, 114374 (2022) |
|  | 0.5 | 2 | 35 | 57 | 0.018 | 0.029 | Acta Mater. 231, 117890 (2022) |
|  | 0.42 | 0.42 | 70 | 70 | 0.014 | 0.014 | Science 353, 559–562 (2016) |
| NICSMA | 1.65 | 1.65 | 28 | 28 | 0.036 | 0.036 | Science 339, 1191–1194 (2013) |
| Bamboo | 0.15 | 0.35 | 11 | 30 | 0.033 | 0.091 | Mater. Des. 63, 820–828 (2014) |
| Wood | 0.03 | 0.07 | 6 | 20 | 0.050 | 0.167 | Materials Selection in Mechanical Design 4th edn (Elsevier, 2011) |
|  | 0.04 | 0.12 | 5 | 12 | 0.083 | 0.200 | Wood handbook: Wood as an Engineering Material (USDA, 2021) |
| Bone | 0.06 | 0.15 | 15 | 24 | 0.042 | 0.067 | Adv. Eng. Mater. 21, 1801215 (2019) |
| PEEK | 0.09 | 0.11 | 3.5 | 3.9 | 0.256 | 0.286 | Polymer Properties & Chemical Resistance of Plastics. (specialchem.com) |
| PPS | 0.05 | 0.08 | 3.3 | 4 | 0.250 | 0.303 | Polymer Properties & Chemical Resistance of Plastics (specialchem.com) |
| FRP | 0.06 | 0.23 | 3 | 37 | 0.027 | 0.333 | Polymer Properties & Chemical Resistance of Plastics (specialchem.com) |