Highlights

- 3D printed Ti6Al4V alloys with customized microstructures and microhardness were made by DLMD method.

- Effects of various laser powers on the growth mechanism of the alloys were determined.

- Changing laser power significantly impacted the alloys structures, morphology, microhardness, and stability.

- Produced alloys showed the nucleation of porous spherical grains of mean size around 50-81 𝜇𝑚.

- Alloy deposited at 300 W and 0.495 mm/s gained the highest hardness of 859.2 HV0.5 without cracks and porosity.

- Growth of α+β martensitic phase in alloys was responsible for mechanical properties enhancement.

- Proposed 3D printed Ti6Al4V alloy can be useful for high-performance applications.