Supplementary Information for

Synergic Light-Induced Electron Transfer and [4 + 4] Cycloaddition toward Switchable Photoluminescence and Single-Molecule Magnet Behavior in a Dy4 Cubane

Zhen-Ni Gao1†, Yu-Han Wang1†, Jie-Li1†, Wu-Ji Wei1, Song-De Han1, Yi-Quan Zhang2*, Ji-Xiang Hu1*, and Guo-Ming Wang1*

1College of Chemistry and Chemical Engineering, Qingdao University, Shandong, 266071, P. R. China.

2Jiangsu Key Laboratory for NSLSCS, School of Physical Science and Technology, Nanjing Normal University, Nanjing 210023, China.

*Corresponding Authors: Guo-Ming Wang: gmwang_pub@163.com; Ji-Xiang Hu: hujixiang@qdu.edu.cn; Yi-Quan Zhang: zhangyiquan@njnu.edu.cn.

Supplementary Figures

Supplementary Figure 1. The TG plot of compound 1 under N2 atmosphere.

Supplementary Figure 2. The TG plot of compound 2 under N2 atmosphere.

Supplementary Figure 3. The TG plot of compound 3 under N2 atmosphere.

Supplementary Figure 4. Crystal structures of 2 (top) and 2a (bottom) exhibiting the stacking of the anthracene in 2 before and after photodimerization to 2a. Atomic scheme: Gd, green; C, gray 40%; O, red; and N, light blue.

Supplementary Figure 5. Crystal structures of 3 (top) and 3a (bottom) exhibiting the stacking of the anthracene in 3 before and after photodimerization to 3a. Atomic scheme: Y, green; C, gray 40%; O, red; and N, light blue.

Supplementary Figure 6. Color change images of compound 1 powder samples under different irradiation times.

Supplementary Figure 7. Color change images of compound 2 powder samples under different irradiation times.

Supplementary Figure 8. Color change images of compound 3 powder samples under different irradiation times.

Supplementary Figure 9. Time-dependent UV-vis spectra of 2 in the solid state upon irradiation under ambient conditions. Insert: the photocoloration of the crystalline powder samples at different irradiation time.

Supplementary Figure 10. Time-dependent UV-vis spectra of 3 in the solid state upon irradiation under ambient conditions. Insert: the photocoloration of the crystalline powder samples at different irradiation time.

Supplementary Figure 11. Time-dependent fluorescent spectra of 2 at solid state upon light irradiation when excited at 360 nm.

Supplementary Figure 12. Time-dependent fluorescent spectra of 3 at solid state upon light irradiation when excited at 360 nm.

Supplementary Figure 13. The ESR spectra of 3, 3a, 3b and 3b after irradiation at solid state.

Supplementary Figure 14. The ESR spectra of 2, 2a, 2b and 2b after irradiation at solid state.

Supplementary Figure 15. IR plots for compounds 1, 1a and 1b. Insert: enlarged IR spectrum between 1000 and 400 cm-1.

Supplementary Figure 16. IR plots for compounds 2, 2a and 2b. Insert: enlarged IR spectrum between 1000 and 400 cm-1.

Supplementary Figure 17. IR plots for compounds 3, 3a and 3b. Insert: enlarged IR spectrum between 1000 and 400 cm-1.

Supplementary Figure 18. PXRD patterns of 1, 1a and 1a after grinding.

Supplementary Figure 19. PXRD patterns of 2, 2a and 2a after grinding.

Supplementary Figure 20. PXRD patterns of 3, 3a and 3a after grinding.

Supplementary Figure 21. The schematic diagram of the proposed mechanism for the photo-induced production of compound 1. The structural change parts are represented as black color.

Supplementary Figure 22. (a) Color of 1 before irradiation (first), after irradiation (second), regrinding (third), and reillumination (fourth); (b) Solid-state luminescence color under UV light (365 nm) of powder sample of 1 before (first), after (second), regrinding (third), and reillumination (fourth).

Supplementary Figure 23. (a) Color of 2 before irradiation (first), after irradiation (second), regrinding (third), and reillumination (fourth); (b) Solid-state luminescence color under UV light (365 nm) of powder sample of 2 before (first), after (second), regrinding (third), and reillumination (fourth).

Supplementary Figure 24. (a) Color of 3 before irradiation (first), after irradiation (second), regrinding (third), and reillumination (fourth); (b) Solid-state luminescence color under UV light (365 nm) of powder sample of 3 before (first), after (second), regrinding (third), and reillumination (fourth).

Supplementary Figure 25. UV-vis spectra of 2, 2a, 2b and 2b after irradiation.

Supplementary Figure 26. UV-vis spectra of 3, 3a, 3b and 3b after irradiation.

Supplementary Figure 27. Fluorescence spectra of 2, 2a, 2b and 2b after irradiation.

Supplementary Figure 28. Fluorescence spectra of 3, 3a, 3b and 3b after irradiation.

Supplementary Figure 29. The intermolecular H-bonding and C-H···π interactions among the cubane structures for 1. Parts anthracene rings in which the carboxyl carbon atoms are labeled as black are omitted for clarity.

Supplementary Figure 30. Temperature-dependent susceptibilities for 3a under a dc field of 1000 Oe.

Supplementary Figure 31. Temperature-dependent susceptibilities for 2 and 2a under a dc magnetic field of 1000 Oe.

Supplementary Figure 32. Field dependence of magnetization for 1 and 1a at 2 K.

Supplementary Figure 33. Field dependence of magnetization of 2 and 2a at 2 K.

Supplementary Figure 34. Temperature dependence of the in-phase and out-of-phase components of ac magnetic susceptibility for 1 in a zero-dc and 5 ac field at various ac frequencies.

Supplementary Figure 35. Temperature dependence of the in-phase and out-of-phase components of ac magnetic susceptibility for 1a in a zero-dc and 5 ac field at various ac frequencies.

Supplementary Figure 36. Field dependence of the c" component of ac susceptibility components for 1a with ω = 1000 Hz at 2 K.

Supplementary Figure 37. Frequency dependence of the in-phase components of 1a in a 1200 Oe dc field between 2–10 K.

Supplementary Figure 38. Frequency dependence of the out-of-phase components of 1a in a 1200 Oe dc field between 2–10 K.

1_Dy1                                            1_Dy2

1_Dy3                                              1_Dy4

1a_Dy1                                                1a_Dy2

1a_Dy3                                               1a_Dy4

Supplementary Figure 39. Calculated eight individual DyⅢ fragments of 1_Dy1, 1_Dy2, 1_Dy3, 1_Dy4, 1a_Dy1, 1a_Dy2, 1a_Dy3 and 1a_Dy4; H atoms are omitted for clarify.

1                                       1a

Supplementary Figure 40. Scheme of the DyⅢ-DyⅢ and DyⅢ-radical interactions in 1 and 1a.

- 1a

Supplementary Figure 41. Calculated orientations of the local main magnetic axes on DyIII ions of 1 and 1a in their ground KDs.

Supplementary Tables

Supplementary Table 1. Crystallographic data for compounds 1 and 1a.

|  | 1 | 1a |
| --- | --- | --- |
| Formula | C135H95Dy4NO29 | C270 H176Dy8N2O55 |
| Mr (g·mol-1) | 2845.08 | 5628.12 |
| Temperature | 180(2) K | 120(2) K |
| Space group | P21/n | P21/n |
| Crystal system | Monoclinic | Monoclinic |
| a (Å) | 19.0929(14) | 19.0742(4) |
| b (Å) | 26.7829(17) | 26.6163(6) |
| c (Å) | 24.9829(18) | 24.9581(6) |
| α (°) | 90 | 90 |
| β (°) | 91.547(3) | 91.5030(10) |
| γ (°) | 90 | 90 |
| V (Å3) | 12770.7(15) | 12666.5(5) |
| Z | 4 | 2 |
| F (000) | 5616 | 5556 |
| Dc (gcm-3) | 1.478 | 1.476 |
| μ (mm-1) | 2.386 | 2.404 |
| Rint | 0.0617 | 0.0344 |
| limiting indices | -22<=h<=24 -34<=k<=34 -32<=l<=28 | -24<=h<=21 -29<=k<=34 -32<=l<=32 |
| Collected reflections | 103790 | 111389 |
| Unique reflections | 29233 | 29102 |
| GOF on F2 | 1.044 | 1.041 |
| R1, wR2 [I>2σ(I)] | 0.0587 0.1487 | 0.0419 0.1237 |
| R1, wR2 [all data] | 0.0954 0.1664 | 0.0560 0.1339 |
| aR1 =∑ ¦¦F0¦ − ¦Fc¦¦/∑¦Fo¦. bwR2 = {∑ [w(F02 − Fc2)2]/∑w(F02)2}1/2. |  |  |

Supplementary Table 2. Crystallographic data for compounds 2, 2a, 3, 3m and 3a.

|  | 2 | 2a | 3 | 3m | 3a |
| --- | --- | --- | --- | --- | --- |
| Formula | C135H95Gd4NO29 | C270H176Gd8N2O55 | C135H95Y4NO29 | C135H95Y4NO29 | C270H176Y8N2O55 |
| Mr (g·mol-1) | 2824.08 | 5586.12 | 2550.72 | 2550.75 | 5047.40 |
| Temperature | 293(2) K | 293(2) K | 293(2) K | 293(2) K | 293(2) K |
| Space group | P21/n | P21/n | P21/n | P21/n | P21/n |
| Crystal system | Monoclinic | Monoclinic | Monoclinic | Monoclinic | Monoclinic |
| a (Å) | 19.1149(3) | 19.1968(4) | 19.09040(10) | 19.1796(7) | 19.17010(10) |
| b (Å) | 26.8237(5) | 27.0713(5) | 26.7042(2) | 26.7579(11) | 26.56360(10) |
| c (Å) | 24.8999(4) | 25.2042(4) | 24.9905(2) | 24.9832(8) | 24.88060(10) |
| α (°) | 90 | 90 | 90 | 90 | 90 |
| β (°) | 91.480(2) | 92.012(2) | 92.4440(10) | 92.183(3) | 92.3000(10) |
| γ (°) | 90 | 90 | 90 | 90 | 90 |
| V (Å3) | 12762.7(4) | 13090.1(4) | 12728.42(15) | 12812.2(8) | 12659.66(10) |
| Z | 4 | 2 | 4 | 4 | 2 |
| F (000) | 5584 | 5524 | 5184 | 5200 | 5124 |
| Dc (gcm-3) | 1.468 | 1.417 | 1.329 | 1.322 | 1.322 |
| μ (mm-1) | 2.124 | 2.069 | 2.966 | 1.866 | 3.030 |
| Rint | 0.0518 | 0.0496 | 0.0442 | 0.0728 | 0.0401 |
| limiting indices | -22<=h<=22 -31<=k<=31 -29<=l<=29 | -22<=h<=22 -32<=k<=29 -29<=l<=29 | -23<=h<=24 -32<=k<=30 -30<=l<=30 | -22<=h<=22 -31<=k<=31 -29<=l<=29 | -23<=h<=24 -33<=k<=32 -31<=l<=28 |
| Collected reflections | 110973 | 104695 | 96075 | 84119 | 95694 |
| Unique reflections | 22504 | 23027 | 25643 | 22595 | 25869 |
| GOF on F2 | 1.001 | 1.024 | 1.091 | 1.014 | 1.063 |
| R1, wR2 [I>2σ(I)] | 0.0583 0.1497 | 0.0460 0.1195 | 0.0581 0.1755 | 0.0747 0.2231 | 0.0485, 0.1382 |
| R1, wR2 [all data] | 0.0893 0.1657 | 0.0642 0.1376 | 0.0619 0.1788 | 0.1300, 0.1464 | 0.0529, 0.1417 |
| aR1 =∑ ¦¦F0¦ − ¦Fc¦¦/∑¦Fo¦. bwR2 = {∑ [w(F02 − Fc2)2]/∑w(F02)2}1/2. |  |  |  |  |  |

Supplementary Table 3. Continuous Shape Measure (CShM) analyses of geometries for compound 1 by SHAPE 2.0 Software.

| Geometry | Dy1 | Dy2 | Dy3 | Dy4 |
| --- | --- | --- | --- | --- |
| Octagon (D8h) | 30.590 | 29.231 | 29.355 | 28.770 |
| Heptagonal pyramid (C7v) | 23.578 | 22.130 | 22.398 | 21.497 |
| Hexagonal bipyramid (D6h) | 16.421 | 14.527 | 15.102 | 14.755 |
| Cube (Oh) | 11.540 | 13.636 | 13.630 | 13.522 |
| Square antiprism (D4d) | 3.398 | 3.420 | 3.808 | 3.123 |
| Triangular dodecahedron (D2d) | 0.693 | 1.399 | 1.218 | 1.223 |
| Johnson gyrobifastigium J26 (D2d) | 12.317 | 12.304 | 12.469 | 12.266 |
| Johnson elongated triangular bipyramid J14 (D3h) | 27.981 | 27.058 | 27.250 | 28.064 |
| Biaugmented trigonal prism J50 (C2v) | 2.909 | 3.044 | 3.290 | 2.574 |
| Biaugmented trigonal prism (C2v) | 2.020 | 2.399 | 2.723 | 1.763 |
| Snub diphenoid J84 (D2d) | 2.426 | 2.748 | 2.457 | 2.586 |
| Triakis tetrahedron (Td) | 12.297 | 14.336 | 14.354 | 14.210 |
| Elongated trigonal bipyramid (D3h) | 23.861 | 23.910 | 24.276 | 24.279 |

Supplementary Table 4. Continuous Shape Measure (CShM) analyses of geometries for compound 1a by SHAPE 2.0 Software.

| Geometry | Dy1 | Dy2 | Dy3 | Dy4 |
| --- | --- | --- | --- | --- |
| Octagon (D8h) | 31.521 | 28.814 | 29.672 | 30.300 |
| Heptagonal pyramid (C7v) | 23.590 | 21.856 | 22.298 | 21.787 |
| Hexagonal bipyramid (D6h) | 16.083 | 14.471 | 15.259 | 14.728 |
| Cube (Oh) | 11.398 | 13.547 | 13.354 | 13.837 |
| Square antiprism (D4d) | 2.503 | 3.263 | 3.884 | 3.873 |
| Triangular dodecahedron (D2d) | 0.668 | 1.400 | 1.177 | 1.192 |
| Johnson gyrobifastigium J26 (D2d) | 12.631 | 12.227 | 12.674 | 12.113 |
| Johnson elongated triangular bipyramid J14 (D3h) | 27.593 | 26.920 | 27.305 | 28.517 |
| Biaugmented trigonal prism J50 (C2v) | 2.526 | 2.936 | 3.230 | 3.226 |
| Biaugmented trigonal prism (C2v) | 2.116 | 2.351 | 2.681 | 2.503 |
| Snub diphenoid J84 (D2d) | 2.290 | 2.703 | 2.607 | 2.576 |
| Triakis tetrahedron (Td) | 12.046 | 14.269 | 14.011 | 14.496 |
| Elongated trigonal bipyramid (D3h) | 23.630 | 23.808 | 24.343 | 24.879 |

Supplementary Table 5. Continuous Shape Measure (CShM) analyses of geometries for compound 2 by SHAPE 2.0 Software.

| Geometry | Gd1 | Gd2 | Gd3 | Gd4 |
| --- | --- | --- | --- | --- |
| Octagon (D8h) | 30.809 | 28.364 | 28.895 | 29.321 |
| Heptagonal pyramid (C7v) | 23.567 | 21.283 | 21.971 | 22.288 |
| Hexagonal bipyramid (D6h) | 16.462 | 14.833 | 14.609 | 14.993 |
| Cube (Oh) | 11.435 | 13.588 | 13.621 | 13.777 |
| Square antiprism (D4d) | 3.392 | 3.157 | 3.340 | 3.794 |
| Triangular dodecahedron (D2d) | 0.772 | 1.307 | 1.461 | 1.279 |
| Johnson gyrobifastigium J26 (D2d) | 12.300 | 12.378 | 12.377 | 12.388 |
| Johnson elongated triangular bipyramid J14 (D3h) | 27.502 | 27.881 | 26.733 | 27.403 |
| Biaugmented trigonal prism J50 (C2v) | 2.779 | 2.590 | 3.040 | 3.242 |
| Biaugmented trigonal prism (C2v) | 1.894 | 1.743 | 2.443 | 2.690 |
| Snub diphenoid J84 (D2d) | 2.553 | 2.659 | 2.752 | 2.544 |
| Triakis tetrahedron (Td) | 12.171 | 14.258 | 14.317 | 14.481 |
| Elongated trigonal bipyramid (D3h) | 23.501 | 24.035 | 23.592 | 24.410 |

Supplementary Table 6. Continuous Shape Measure (CShM) analyses of geometries for compound 2a by SHAPE 2.0 Software.

| Geometry | Gd1 | Gd2 | Gd3 | Gd4 |
| --- | --- | --- | --- | --- |
| Octagon (D8h) | 29.902 | 31.402 | 29.594 | 28.805 |
| Heptagonal pyramid (C7v) | 21.686 | 23.718 | 22.089 | 21.557 |
| Hexagonal bipyramid (D6h) | 14.722 | 15.852 | 15.058 | 14.275 |
| Cube (Oh) | 14.089 | 11.540 | 13.656 | 13.502 |
| Square antiprism (D4d) | 3.943 | 2.487 | 3.956 | 3.312 |
| Triangular dodecahedron (D2d) | 1.313 | 0.703 | 1.298 | 1.395 |
| Johnson gyrobifastigium J26 (D2d) | 12.064 | 12.489 | 12.583 | 12.115 |
| Johnson elongated triangular bipyramid J14 (D3h) | 28.027 | 27.909 | 27.360 | 27.354 |
| Biaugmented trigonal prism J50 (C2v) | 3.143 | 2.415 | 3.327 | 3.107 |
| Biaugmented trigonal prism (C2v) | 2.396 | 1.984 | 2.738 | 2.521 |
| Snub diphenoid J84 (D2d) | 2.619 | 2.401 | 2.674 | 2.691 |
| Triakis tetrahedron (Td) | 14.749 | 12.237 | 14.302 | 14.190 |
| Elongated trigonal bipyramid (D3h) | 24.419 | 23.879 | 24.484 | 24.294 |

Supplementary Table 7. Continuous Shape Measure (CShM) analyses of geometries for compound 3 by SHAPE 2.0 Software.

| Geometry | Y1 | Y2 | Y3 | Y4 |
| --- | --- | --- | --- | --- |
| Octagon (D8h) | 29.286 | 30.877 | 29.243 | 28.975 |
| Heptagonal pyramid (C7v) | 21.712 | 23.830 | 22.529 | 21.890 |
| Hexagonal bipyramid (D6h) | 14.721 | 16.568 | 15.384 | 14.529 |
| Cube (Oh) | 13.547 | 11.298 | 13.277 | 13.750 |
| Square antiprism (D4d) | 3.254 | 3.303 | 3.525 | 3.378 |
| Triangular dodecahedron (D2d) | 1.152 | 0.628 | 1.108 | 1.272 |
| Johnson gyrobifastigium J26 (D2d) | 12.321 | 12.346 | 12.627 | 12.091 |
| Johnson elongated triangular bipyramid J14 (D3h) | 28.156 | 28.009 | 27.531 | 27.779 |
| Biaugmented trigonal prism J50 (C2v) | 2.735 | 2.759 | 3.148 | 3.188 |
| Biaugmented trigonal prism (C2v) | 2.019 | 2.128 | 2.613 | 2.651 |
| Snub diphenoid J84 (D2d) | 2.536 | 2.335 | 2.535 | 2.513 |
| Triakis tetrahedron (Td) | 14.220 | 12.010 | 13.952 | 14.416 |
| Elongated trigonal bipyramid (D3h) | 24.524 | 24.010 | 24.435 | 24.777 |

Supplementary Table 8. Continuous Shape Measure (CShM) analyses of geometries for compound 3m by SHAPE 2.0 Software.

| Geometry | Y1 | Y2 | Y3 | Y4 |
| --- | --- | --- | --- | --- |
| Octagon (D8h) | 28.777 | 31.441 | 29.656 | 29.478 |
| Heptagonal pyramid (C7v) | 21.990 | 24.098 | 21.651 | 22.277 |
| Hexagonal bipyramid (D6h) | 14.610 | 16.068 | 14.452 | 15.091 |
| Cube (Oh) | 13.573 | 11.426 | 13.738 | 13.508 |
| Square antiprism (D4d) | 3.231 | 2.719 | 3.527 | 3.772 |
| Triangular dodecahedron (D2d) | 1.271 | 0.676 | 1.257 | 1.173 |
| Johnson gyrobifastigium J26 (D2d) | 12.214 | 12.258 | 12.135 | 12.525 |
| Johnson elongated triangular bipyramid J14 (D3h) | 27.637 | 27.640 | 28.193 | 27.618 |
| Biaugmented trigonal prism J50 (C2v) | 2.997 | 2.368 | 3.000 | 3.233 |
| Biaugmented trigonal prism (C2v) | 2.444 | 1.901 | 2.280 | 2.645 |
| Snub diphenoid J84 (D2d) | 2.556 | 2.350 | 2.608 | 2.581 |
| Triakis tetrahedron (Td) | 14.278 | 12.112 | 14.282 | 14.180 |
| Elongated trigonal bipyramid (D3h) | 24.593 | 23.977 | 25.144 | 24.668 |

Supplementary Table 9. Continuous Shape Measure (CShM) analyses of geometries for compound 3a by SHAPE 2.0 Software.

| Geometry | Y1 | Y2 | Y3 | Y4 |
| --- | --- | --- | --- | --- |
| Octagon (D8h) | 30.275 | 31.288 | 29.227 | 28.587 |
| Heptagonal pyramid (C7v) | 21.912 | 23.637 | 22.470 | 21.619 |
| Hexagonal bipyramid (D6h) | 14.715 | 16.124 | 15.470 | 14.461 |
| Cube (Oh) | 13.814 | 11.408 | 13.222 | 13.413 |
| Square antiprism (D4d) | 3.763 | 2.511 | 3.534 | 3.085 |
| Triangular dodecahedron (D2d) | 1.161 | 0.634 | 1.120 | 1.274 |
| Johnson gyrobifastigium J26 (D2d) | 12.179 | 12.512 | 12.683 | 12.197 |
| Johnson elongated triangular bipyramid J14 (D3h) | 28.314 | 27.841 | 27.478 | 27.788 |
| Biaugmented trigonal prism J50 (C2v) | 3.155 | 2.331 | 3.008 | 3.007 |
| Biaugmented trigonal prism (C2v) | 2.501 | 1.912 | 2.426 | 2.464 |
| Snub diphenoid J84 (D2d) | 2.541 | 2.247 | 2.592 | 2.562 |
| Triakis tetrahedron (Td) | 14.491 | 12.077 | 13.878 | 14.099 |
| Elongated trigonal bipyramid (D3h) | 24.973 | 23.880 | 24.452 | 24.710 |

Supplementary Table 10. Selected bond lengths (Å) and angles (o) for compound 1 at 180(2) K.

| Compound 1 |  |  |  |
| --- | --- | --- | --- |
| Dy(1)-O(2) | 2.294(5) | Dy(3)-O(25) | 2.291(5) |
| Dy(1)-O(4) | 2.350(5) | Dy(3)-O(12) | 2.312(5) |
| Dy(1)-O(6) | 2.356(5) | Dy(3)-O(15) | 2.335(5) |
| Dy(1)-O(19) | 2.357(6) | Dy(3)-O(20) | 2.338(5) |
| Dy(1)-O(24) | 2.358(4) | Dy(3)-O(26) | 2.362(5) |
| Dy(1)-O(23) | 2.372(4) | Dy(3)-O(23) | 2.378(4) |
| Dy(1)-O(25) | 2.428(4) | Dy(3)-O(14) | 2.410(5) |
| Dy(1)-O(3) | 2.451(5) | Dy(3)-O(13) | 2.473(5) |
| Dy(2)-O(24) | 2.319(4) | Dy(4)-O(24) | 2.317(4) |
| Dy(2)-O(26) | 2.321(5) | Dy(4)-O(16) | 2.363(6) |
| Dy(2)-O(11) | 2.325(5) | Dy(4)-O(22) | 2.366(5) |
| Dy(2)-O(23) | 2.349(5) | Dy(4)-O(1) | 2.365(6) |
| Dy(2)-O(21) | 2.354(5) | Dy(4)-O(25) | 2.382(5) |
| Dy(2)-O(7) | 2.380(5) | Dy(4)-O(26) | 2.389(5) |
| Dy(2)-O(8) | 2.452(6) | Dy(4)-O(17) | 2.422(5) |
| Dy(2)-O(10) | 2.473(5) | Dy(4)-O(18) | 2.456(5) |
| O(2)-Dy(1)-O(4) | 74.53(19) | O(25)-Dy(3)-O(26) | 71.44(16) |
| O(2)-Dy(1)-O(6) | 146.62(19) | O(12)-Dy(3)-O(26) | 83.39(18) |
| O(4)-Dy(1)-O(6) | 74.94(19) | O(15)-Dy(3)-O(26) | 72.60(17) |
| O(2)-Dy(1)-O(19) | 102.3(2) | O(20)-Dy(3)-O(26) | 142.38(17) |
| O(4)-Dy(1)-O(19) | 137.12(19) | O(25)-Dy(3)-O(23) | 70.67(16) |
| O(6)-Dy(1)-O(19) | 91.0(2) | O(12)-Dy(3)-O(23) | 78.68(16) |
| O(2)-Dy(1)-O(24) | 96.22(18) | O(15)-Dy(3)-O(23) | 140.65(18) |
| O(4)-Dy(1)-O(24) | 77.80(17) | O(20)-Dy(3)-O(23) | 74.40(18) |
| O(6)-Dy(1)-O(24) | 90.24(18) | O(26)-Dy(3)-O(23) | 68.13(16) |
| O(19)-Dy(1)-O(24) | 143.74(17) | O(25)-Dy(3)-O(14) | 128.8(2) |
| O(2)-Dy(1)-O(23) | 139.18(17) | O(12)-Dy(3)-O(14) | 85.2(2) |
| O(4)-Dy(1)-O(23) | 135.19(16) | O(15)-Dy(3)-O(14) | 74.14(19) |
| O(6)-Dy(1)-O(23) | 73.75(17) | O(20)-Dy(3)-O(14) | 73.77(18) |
| O(19)-Dy(1)-O(23) | 74.49(17) | O(26)-Dy(3)-O(14) | 142.38(17) |
| O(24)-Dy(1)-O(23) | 71.13(16) | O(23)-Dy(3)-O(14) | 143.39(18) |
| O(2)-Dy(1)-O(25) | 70.70(17) | O(25)-Dy(3)-O(13) | 75.22(18) |
| O(4)-Dy(1)-O(25) | 129.87(17) | O(12)-Dy(3)-O(13) | 138.79(19) |
| O(6)-Dy(1)-O(25) | 141.58(17) | O(15)-Dy(3)-O(13) | 73.08(19) |
| O(19)-Dy(1)-O(25) | 85.63(18) | O(20)-Dy(3)-O(13) | 75.84(18) |
| O(24)-Dy(1)-O(25) | 71.42(16) | O(26)-Dy(3)-O(13) | 129.04(17) |
| O(23)-Dy(1)-O(25) | 68.48(16) | O(23)-Dy(3)-O(13) | 132.56(17) |
| O(2)-Dy(1)-O(3) | 77.65(19) | O(14)-Dy(3)-O(13) | 53.6(2) |
| O(4)-Dy(1)-O(3) | 67.2(2) | O(24)-Dy(4)-O(16) | 146.23(19) |
| O(6)-Dy(1)-O(3) | 78.36(19) | O(24)-Dy(4)-O(22) | 91.64(18) |
| O(19)-Dy(1)-O(3) | 70.4(2) | O(16)-Dy(4)-O(22) | 91.2(2) |
| O(24)-Dy(1)-O(3) | 144.88(19) | O(24)-Dy(4)-O(1) | 91.21(19) |
| O(23)-Dy(1)-O(3) | 134.16(19) | O(16)-Dy(4)-O(1) | 106.1(2) |
| O(25)-Dy(1)-O(3) | 134.83(18) | O(22)-Dy(4)-O(1) | 143.2(2) |
| O(24)-Dy(2)-O(26) | 72.39(16) | O(24)-Dy(4)-O(25) | 72.94(16) |
| O(24)-Dy(2)-O(11) | 147.64(17) | O(16)-Dy(4)-O(25) | 84.51(18) |
| O(26)-Dy(2)-O(11) | 82.83(17) | O(22)-Dy(4)-O(25) | 142.12(18) |
| O(24)-Dy(2)-O(23) | 72.23(16) | O(1)-Dy(4)-O(25) | 73.06(18) |
| O(26)-Dy(2)-O(23) | 69.29(16) | O(24)-Dy(4)-O(26) | 71.19(16) |
| O(11)-Dy(2)-O(23) | 79.81(17) | O(16)-Dy(4)-O(26) | 77.56(19) |
| O(24)-Dy(2)-O(21) | 96.36(19) | O(22)-Dy(4)-O(26) | 72.89(18) |
| O(26)-Dy(2)-O(21) | 73.44(17) | O(1)-Dy(4)-O(26) | 141.77(18) |
| O(11)-Dy(2)-O(21) | 96.1(2) | O(25)-Dy(4)-O(26) | 69.42(16) |
| O(23)-Dy(2)-O(21) | 142.73(17) | O(24)-Dy(4)-O(17) | 80.08(16) |
| O(24)-Dy(2)-O(7) | 99.31(17) | O(16)-Dy(4)-O(17) | 132.52(19) |
| O(26)-Dy(2)-O(7) | 141.44(17) | O(22)-Dy(4)-O(17) | 72.62(19) |
| O(11)-Dy(2)-O(7) | 87.11(18) | O(1)-Dy(4)-O(17) | 71.8(2) |
| O(23)-Dy(2)-O(7) | 72.31(16) | O(25)-Dy(4)-O(17) | 134.67(17) |
| O(21)-Dy(2)-O(7) | 144.87(18) | O(26)-Dy(4)-O(17) | 133.82(17) |
| O(24)-Dy(2)-O(8) | 77.36(16) | O(24)-Dy(4)-O(18) | 133.88(16) |
| O(26)-Dy(2)-O(8) | 134.61(17) | O(16)-Dy(4)-O(18) | 79.36(19) |
| O(11)-Dy(2)-O(8) | 134.64(17) | O(22)-Dy(4)-O(18) | 76.8(2) |
| O(23)-Dy(2)-O(8) | 130.96(17) | O(1)-Dy(4)-O(18) | 74.96(19) |
| O(21)-Dy(2)-O(8) | 77.24(19) | O(25)-Dy(4)-O(18) | 138.28(17) |
| O(7)-Dy(2)-O(8) | 75.84(19) | O(26)-Dy(4)-O(18) | 141.17(17) |
| O(24)-Dy(2)-O(10) | 129.66(17) | O(17)-Dy(4)-O(18) | 53.81(16) |
| O(26)-Dy(2)-O(10) | 141.66(17) | Dy(2)-O(23)-Dy(1) | 104.10(18) |
| O(11)-Dy(2)-O(10) | 82.59(17) | Dy(2)-O(23)-Dy(3) | 108.35(18) |
| O(23)-Dy(2)-O(10) | 141.31(17) | Dy(1)-O(23)-Dy(3) | 107.10(17) |
| O(21)-Dy(2)-O(10) | 73.14(19) | Dy(2)-O(24)-Dy(4) | 106.34(17) |
| O(7)-Dy(2)-O(10) | 72.63(18) | Dy(2)-O(24)-Dy(1) | 105.52(17) |
| O(8)-Dy(2)-O(10) | 52.34(16) | Dy(4)-O(24)-Dy(1) | 106.77(18) |
| O(25)-Dy(3)-O(12) | 145.75(17) | Dy(3)-O(25)-Dy(4) | 107.78(19) |
| O(25)-Dy(3)-O(15) | 94.85(19) | Dy(3)-O(25)-Dy(1) | 108.11(18) |
| O(12)-Dy(3)-O(15) | 99.4(2) | Dy(4)-O(25)-Dy(1) | 102.57(17) |
| O(25)-Dy(3)-O(20) | 93.47(18) | Dy(2)-O(26)-Dy(3) | 109.84(18) |
| O(12)-Dy(3)-O(20) | 92.7(2) | Dy(2)-O(26)-Dy(4) | 103.97(18) |
| O(15)-Dy(3)-O(20) | 144.48(19) | Dy(3)-O(26)-Dy(4) | 105.25(17) |

Supplementary Table 11. Selected bond lengths (Å) and angles (o) for compound 1a at 120(2) K.

| Compound 1a |  |  |  |
| --- | --- | --- | --- |
| Dy(1)-O(2) | 2.278(3) | Dy(3)-O(25) | 2.273(3) |
| Dy(1)-O(19) | 2.328(3) | Dy(3)-O(12) | 2.306(3) |
| Dy(1)-O(6) | 2.339(3) | Dy(3)-O(20) | 2.340(4) |
| Dy(1)-O(24) | 2.354(3) | Dy(3)-O(26) | 2.340(3) |
| Dy(1)-O(4) | 2.382(3) | Dy(3)-O(15) | 2.378(4) |
| Dy(1)-O(23) | 2.390(3) | Dy(3)-O(23) | 2.386(3) |
| Dy(1)-O(3) | 2.432(4) | Dy(3)-O(14) | 2.391(3) |
| Dy(1)-O(25) | 2.430(3) | Dy(3)-O(13) | 2.444(3) |
| Dy(2)-O(24) | 2.309(3) | Dy(4)-O(24) | 2.313(3) |
| Dy(2)-O(26) | 2.327(3) | Dy(4)-O(16) | 2.327(4) |
| Dy(2)-O(11) | 2.336(3) | Dy(4)-O(25) | 2.370(3) |
| Dy(2)-O(23) | 2.337(3) | Dy(4)-O(22) | 2.382(3) |
| Dy(2)-O(21) | 2.341(4) | Dy(4)-O(26) | 2.398(3) |
| Dy(2)-O(7) | 2.384(4) | Dy(4)-O(1) | 2.419(3) |
| Dy(2)-O(8) | 2.457(3) | Dy(4)-O(17) | 2.418(3) |
| Dy(2)-O(10) | 2.495(3) | Dy(4)-O(18) | 2.454(3) |
| O(2)-Dy(1)-O(19) | 97.50(12) | O(25)-Dy(3)-O(15) | 95.31(12) |
| O(2)-Dy(1)-O(6) | 148.47(13) | O(12)-Dy(3)-O(15) | 100.60(14) |
| O(19)-Dy(1)-O(6) | 95.41(14) | O(20)-Dy(3)-O(15) | 143.52(13) |
| O(2)-Dy(1)-O(24) | 98.58(11) | O(26)-Dy(3)-O(15) | 72.55(12) |
| O(19)-Dy(1)-O(24) | 142.85(13) | O(25)-Dy(3)-O(23) | 70.27(12) |
| O(6)-Dy(1)-O(24) | 87.99(13) | O(12)-Dy(3)-O(23) | 78.28(12) |
| O(2)-Dy(1)-O(4) | 75.06(12) | O(20)-Dy(3)-O(23) | 74.58(12) |
| O(19)-Dy(1)-O(4) | 139.32(13) | O(26)-Dy(3)-O(23) | 68.64(11) |
| O(6)-Dy(1)-O(4) | 76.40(13) | O(15)-Dy(3)-O(23) | 141.10(11) |
| O(24)-Dy(1)-O(4) | 77.42(12) | O(25)-Dy(3)-O(14) | 128.70(11) |
| O(2)-Dy(1)-O(23) | 137.31(11) | O(12)-Dy(3)-O(14) | 85.32(12) |
| O(19)-Dy(1)-O(23) | 74.65(12) | O(20)-Dy(3)-O(14) | 74.29(12) |
| O(6)-Dy(1)-O(23) | 73.98(12) | O(26)-Dy(3)-O(14) | 141.93(12) |
| O(24)-Dy(1)-O(23) | 70.82(11) | O(15)-Dy(3)-O(14) | 73.58(12) |
| O(4)-Dy(1)-O(23) | 136.77(11) | O(23)-Dy(3)-O(14) | 143.62(11) |
| O(2)-Dy(1)-O(3) | 79.85(13) | O(25)-Dy(3)-O(13) | 74.66(11) |
| O(19)-Dy(1)-O(3) | 69.73(14) | O(12)-Dy(3)-O(13) | 139.41(12) |
| O(6)-Dy(1)-O(3) | 77.88(14) | O(20)-Dy(3)-O(13) | 75.30(13) |
| O(24)-Dy(1)-O(3) | 146.28(13) | O(26)-Dy(3)-O(13) | 127.66(11) |
| O(4)-Dy(1)-O(3) | 69.60(14) | O(15)-Dy(3)-O(13) | 72.10(13) |
| O(23)-Dy(1)-O(3) | 131.61(13) | O(23)-Dy(3)-O(13) | 132.47(11) |
| O(2)-Dy(1)-O(25) | 69.78(11) | O(14)-Dy(3)-O(13) | 54.14(11) |
| O(19)-Dy(1)-O(25) | 83.28(12) | O(24)-Dy(4)-O(16) | 146.39(12) |
| O(6)-Dy(1)-O(25) | 140.55(12) | O(24)-Dy(4)-O(25) | 73.17(11) |
| O(24)-Dy(1)-O(25) | 71.38(11) | O(16)-Dy(4)-O(25) | 83.60(12) |
| O(4)-Dy(1)-O(25) | 127.91(12) | O(24)-Dy(4)-O(22) | 90.11(12) |
| O(23)-Dy(1)-O(25) | 67.64(11) | O(16)-Dy(4)-O(22) | 93.35(14) |
| O(3)-Dy(1)-O(25) | 136.05(12) | O(25)-Dy(4)-O(22) | 141.25(12) |
| O(24)-Dy(2)-O(26) | 72.15(12) | O(24)-Dy(4)-O(26) | 70.81(12) |
| O(24)-Dy(2)-O(11) | 148.15(12) | O(16)-Dy(4)-O(26) | 78.39(12) |
| O(26)-Dy(2)-O(11) | 83.62(12) | O(25)-Dy(4)-O(26) | 68.92(11) |
| O(24)-Dy(2)-O(23) | 72.52(11) | O(22)-Dy(4)-O(26) | 72.62(12) |
| O(26)-Dy(2)-O(23) | 69.66(11) | O(24)-Dy(4)-O(1) | 95.60(12) |
| O(11)-Dy(2)-O(23) | 79.94(12) | O(16)-Dy(4)-O(1) | 99.66(13) |
| O(24)-Dy(2)-O(21) | 95.61(13) | O(25)-Dy(4)-O(1) | 71.38(11) |
| O(26)-Dy(2)-O(21) | 73.27(12) | O(22)-Dy(4)-O(1) | 146.45(12) |
| O(11)-Dy(2)-O(21) | 96.87(14) | O(26)-Dy(4)-O(1) | 140.22(11) |
| O(23)-Dy(2)-O(21) | 142.93(12) | O(24)-Dy(4)-O(17) | 79.06(12) |
| O(24)-Dy(2)-O(7) | 100.27(12) | O(16)-Dy(4)-O(17) | 133.87(13) |
| O(26)-Dy(2)-O(7) | 142.80(11) | O(25)-Dy(4)-O(17) | 133.19(12) |
| O(11)-Dy(2)-O(7) | 86.53(13) | O(22)-Dy(4)-O(17) | 73.93(13) |
| O(23)-Dy(2)-O(7) | 73.33(11) | O(26)-Dy(4)-O(17) | 134.30(11) |
| O(21)-Dy(2)-O(7) | 143.69(12) | O(1)-Dy(4)-O(17) | 74.78(12) |
| O(24)-Dy(2)-O(8) | 78.33(11) | O(24)-Dy(4)-O(18) | 132.64(11) |
| O(26)-Dy(2)-O(8) | 134.76(12) | O(16)-Dy(4)-O(18) | 80.36(12) |
| O(11)-Dy(2)-O(8) | 133.16(12) | O(25)-Dy(4)-O(18) | 140.43(11) |
| O(23)-Dy(2)-O(8) | 131.76(12) | O(22)-Dy(4)-O(18) | 75.92(13) |
| O(21)-Dy(2)-O(8) | 76.43(13) | O(26)-Dy(4)-O(18) | 140.57(12) |
| O(7)-Dy(2)-O(8) | 75.15(12) | O(1)-Dy(4)-O(18) | 76.00(12) |
| O(24)-Dy(2)-O(10) | 130.14(12) | O(17)-Dy(4)-O(18) | 53.65(12) |
| O(26)-Dy(2)-O(10) | 140.47(12) | Dy(2)-O(23)-Dy(3) | 107.59(13) |
| O(11)-Dy(2)-O(10) | 81.64(12) | Dy(2)-O(23)-Dy(1) | 103.77(12) |
| O(23)-Dy(2)-O(10) | 141.80(12) | Dy(3)-O(23)-Dy(1) | 107.36(12) |
| O(21)-Dy(2)-O(10) | 72.37(12) | Dy(2)-O(24)-Dy(4) | 107.48(14) |
| O(7)-Dy(2)-O(10) | 72.41(12) | Dy(2)-O(24)-Dy(1) | 105.80(12) |
| O(8)-Dy(2)-O(10) | 51.89(12) | Dy(4)-O(24)-Dy(1) | 106.00(12) |
| O(25)-Dy(3)-O(12) | 145.54(12) | Dy(3)-O(25)-Dy(4) | 108.16(13) |
| O(25)-Dy(3)-O(20) | 91.45(12) | Dy(3)-O(25)-Dy(1) | 109.75(13) |
| O(12)-Dy(3)-O(20) | 93.53(14) | Dy(4)-O(25)-Dy(1) | 101.86(11) |
| O(25)-Dy(3)-O(26) | 71.58(11) | Dy(2)-O(26)-Dy(3) | 109.50(13) |
| O(12)-Dy(3)-O(26) | 84.30(13) | Dy(2)-O(26)-Dy(4) | 104.11(13) |
| O(20)-Dy(3)-O(26) | 142.83(12) | Dy(3)-O(26)-Dy(4) | 105.07(12) |
| Symmetry codes: #1 -x,-y+1,-z+1 |  |  |  |

Supplementary Table 12. Selected bond lengths (Å) and angles (o) for compound 2 at 293(2) K.

| Compound 2 |  |  |  |
| --- | --- | --- | --- |
| O(20)-Gd(2) | 2.470(6) | Gd(3)-O(3) | 2.340(5) |
| Gd(1)-O(18) | 2.323(7) | Gd(3)-O(10) | 2.351(5) |
| Gd(1)-O(12) | 2.366(6) | Gd(3)-O(2) | 2.360(5) |
| Gd(1)-O(16) | 2.386(6) | Gd(3)-O(23) | 2.364(6) |
| Gd(1)-O(3) | 2.386(5) | Gd(3)-O(4) | 2.384(5) |
| Gd(1)-O(4) | 2.393(5) | Gd(3)-O(11) | 2.407(6) |
| Gd(1)-O(8) | 2.390(6) | Gd(3)-O(14) | 2.483(6) |
| Gd(1)-O(1) | 2.444(5) | Gd(3)-O(13) | 2.500(6) |
| Gd(1)-O(26) | 2.465(7) | Gd(4)-O(1) | 2.320(5) |
| Gd(2)-O(3) | 2.346(5) | Gd(4)-O(9) | 2.342(6) |
| Gd(2)-O(25) | 2.373(6) | Gd(4)-O(24) | 2.358(7) |
| Gd(2)-O(22) | 2.394(6) | Gd(4)-O(7) | 2.357(6) |
| Gd(2)-O(19) | 2.389(8) | Gd(4)-O(4) | 2.396(5) |
| Gd(2)-O(2) | 2.410(6) | Gd(4)-O(2) | 2.394(5) |
| Gd(2)-O(1) | 2.418(5) | Gd(4)-O(5) | 2.424(5) |
| Gd(2)-O(21) | 2.450(5) | Gd(4)-O(6) | 2.482(5) |
| O(24)-C(1)-O(25) | 124.0(9) | O(10)-Gd(3)-O(14) | 135.76(19) |
| O(18)-Gd(1)-O(12) | 146.8(2) | O(2)-Gd(3)-O(14) | 134.17(19) |
| O(18)-Gd(1)-O(16) | 74.9(2) | O(23)-Gd(3)-O(14) | 77.3(2) |
| O(12)-Gd(1)-O(16) | 74.1(2) | O(4)-Gd(3)-O(14) | 130.15(19) |
| O(18)-Gd(1)-O(3) | 96.1(2) | O(11)-Gd(3)-O(14) | 76.2(2) |
| O(12)-Gd(1)-O(3) | 88.9(2) | O(3)-Gd(3)-O(13) | 129.46(18) |
| O(16)-Gd(1)-O(3) | 77.77(19) | O(10)-Gd(3)-O(13) | 83.97(18) |
| O(18)-Gd(1)-O(4) | 139.2(2) | O(2)-Gd(3)-O(13) | 142.06(19) |
| O(12)-Gd(1)-O(4) | 73.24(19) | O(23)-Gd(3)-O(13) | 73.4(2) |
| O(16)-Gd(1)-O(4) | 134.25(19) | O(4)-Gd(3)-O(13) | 141.83(19) |
| O(3)-Gd(1)-O(4) | 70.45(17) | O(11)-Gd(3)-O(13) | 73.0(2) |
| O(18)-Gd(1)-O(8) | 104.1(2) | O(14)-Gd(3)-O(13) | 52.20(18) |
| O(12)-Gd(1)-O(8) | 90.6(2) | O(1)-Gd(4)-O(9) | 145.57(18) |
| O(16)-Gd(1)-O(8) | 137.0(2) | O(1)-Gd(4)-O(24) | 94.3(2) |
| O(3)-Gd(1)-O(8) | 143.17(19) | O(9)-Gd(4)-O(24) | 100.8(3) |
| O(4)-Gd(1)-O(8) | 74.18(19) | O(1)-Gd(4)-O(7) | 92.4(2) |
| O(18)-Gd(1)-O(1) | 70.7(2) | O(9)-Gd(4)-O(7) | 92.5(2) |
| O(12)-Gd(1)-O(1) | 140.84(19) | O(24)-Gd(4)-O(7) | 145.2(2) |
| O(16)-Gd(1)-O(1) | 130.1(2) | O(1)-Gd(4)-O(4) | 70.45(18) |
| O(3)-Gd(1)-O(1) | 71.17(17) | O(9)-Gd(4)-O(4) | 78.28(19) |
| O(4)-Gd(1)-O(1) | 68.46(18) | O(24)-Gd(4)-O(4) | 140.11(19) |
| O(8)-Gd(1)-O(1) | 86.7(2) | O(7)-Gd(4)-O(4) | 73.93(19) |
| O(18)-Gd(1)-O(26) | 78.2(3) | O(1)-Gd(4)-O(2) | 71.56(18) |
| O(12)-Gd(1)-O(26) | 79.7(2) | O(9)-Gd(4)-O(2) | 84.0(2) |
| O(16)-Gd(1)-O(26) | 68.8(3) | O(24)-Gd(4)-O(2) | 71.7(2) |
| O(3)-Gd(1)-O(26) | 146.5(2) | O(7)-Gd(4)-O(2) | 142.2(2) |
| O(4)-Gd(1)-O(26) | 133.5(2) | O(4)-Gd(4)-O(2) | 68.52(17) |
| O(8)-Gd(1)-O(26) | 69.0(3) | O(1)-Gd(4)-O(5) | 128.61(18) |
| O(1)-Gd(1)-O(26) | 134.2(2) | O(9)-Gd(4)-O(5) | 85.44(19) |
| O(3)-Gd(2)-O(25) | 145.3(2) | O(24)-Gd(4)-O(5) | 74.7(2) |
| O(3)-Gd(2)-O(22) | 91.4(2) | O(7)-Gd(4)-O(5) | 74.5(2) |
| O(25)-Gd(2)-O(22) | 90.8(3) | O(4)-Gd(4)-O(5) | 143.62(18) |
| O(3)-Gd(2)-O(19) | 90.8(2) | O(2)-Gd(4)-O(5) | 142.03(18) |
| O(25)-Gd(2)-O(19) | 107.6(3) | O(1)-Gd(4)-O(6) | 75.57(17) |
| O(22)-Gd(2)-O(19) | 143.0(2) | O(9)-Gd(4)-O(6) | 138.45(19) |
| O(3)-Gd(2)-O(2) | 70.76(18) | O(24)-Gd(4)-O(6) | 73.1(2) |
| O(25)-Gd(2)-O(2) | 76.9(2) | O(7)-Gd(4)-O(6) | 75.6(2) |
| O(22)-Gd(2)-O(2) | 72.7(2) | O(4)-Gd(4)-O(6) | 132.64(17) |
| O(19)-Gd(2)-O(2) | 141.8(2) | O(2)-Gd(4)-O(6) | 129.03(19) |
| O(3)-Gd(2)-O(1) | 72.30(17) | O(5)-Gd(4)-O(6) | 53.09(18) |
| O(25)-Gd(2)-O(1) | 85.0(2) | O(15)-N(1)-O(14) | 121.2(8) |
| O(22)-Gd(2)-O(1) | 142.1(2) | O(15)-N(1)-O(13) | 120.9(8) |
| O(19)-Gd(2)-O(1) | 73.0(2) | O(14)-N(1)-O(13) | 117.9(7) |
| O(2)-Gd(2)-O(1) | 69.64(18) | Gd(3)-O(2)-Gd(4) | 109.2(2) |
| O(3)-Gd(2)-O(21) | 80.79(18) | Gd(3)-O(2)-Gd(2) | 104.27(19) |
| O(25)-Gd(2)-O(21) | 132.5(2) | Gd(4)-O(2)-Gd(2) | 105.3(2) |
| O(22)-Gd(2)-O(21) | 72.1(2) | Gd(3)-O(4)-Gd(1) | 104.67(19) |
| O(19)-Gd(2)-O(21) | 71.8(2) | Gd(3)-O(4)-Gd(4) | 108.31(19) |
| O(2)-Gd(2)-O(21) | 133.52(19) | Gd(1)-O(4)-Gd(4) | 107.31(19) |
| O(1)-Gd(2)-O(21) | 134.84(19) | Gd(3)-O(3)-Gd(2) | 107.0(2) |
| O(3)-Gd(2)-O(20) | 133.63(17) | Gd(3)-O(3)-Gd(1) | 106.30(19) |
| O(25)-Gd(2)-O(20) | 80.4(2) | Gd(2)-O(3)-Gd(1) | 107.0(2) |
| O(22)-Gd(2)-O(20) | 76.1(2) | Gd(4)-O(1)-Gd(2) | 107.4(2) |
| O(19)-Gd(2)-O(20) | 75.8(2) | Gd(4)-O(1)-Gd(1) | 108.1(2) |
| O(2)-Gd(2)-O(20) | 140.7(2) | Gd(2)-O(1)-Gd(1) | 102.94(18) |
| O(1)-Gd(2)-O(20) | 139.4(2) | C(1)-O(25)-Gd(2) | 137.8(8) |
| O(21)-Gd(2)-O(20) | 52.84(18) | C(1)-O(24)-Gd(4) | 134.2(6) |
| O(3)-Gd(3)-O(10) | 146.40(18) | C(16)-O(6)-Gd(4) | 91.6(5) |
| O(3)-Gd(3)-O(2) | 71.75(18) | C(16)-O(5)-Gd(4) | 93.6(4) |
| O(10)-Gd(3)-O(2) | 82.94(19) | C(91)-O(19)-Gd(2) | 136.8(7) |
| O(3)-Gd(3)-O(23) | 95.9(2) | C(91)-O(18)-Gd(1) | 134.6(7) |
| O(10)-Gd(3)-O(23) | 97.6(2) | C(106)-O(21)-Gd(2) | 92.7(5) |
| O(2)-Gd(3)-O(23) | 73.3(2) | C(76)-O(16)-Gd(1) | 138.9(6) |
| O(3)-Gd(3)-O(4) | 71.38(17) | C(61)-O(12)-Gd(1) | 141.7(6) |
| O(10)-Gd(3)-O(4) | 79.28(18) | C(61)-O(11)-Gd(3) | 129.5(6) |
| O(2)-Gd(3)-O(4) | 69.27(18) | C(31)-O(8)-Gd(1) | 138.2(5) |
| O(23)-Gd(3)-O(4) | 142.55(19) | C(31)-O(7)-Gd(4) | 135.6(6) |
| O(3)-Gd(3)-O(11) | 99.4(2) | C(46)-O(10)-Gd(3) | 136.6(5) |
| O(10)-Gd(3)-O(11) | 86.4(2) | C(46)-O(9)-Gd(4) | 137.3(5) |
| O(2)-Gd(3)-O(11) | 141.07(18) | N(1)-O(14)-Gd(3) | 95.7(5) |
| O(23)-Gd(3)-O(11) | 145.4(2) | N(1)-O(13)-Gd(3) | 94.2(5) |
| O(4)-Gd(3)-O(11) | 71.98(18) | C(121)-O(23)-Gd(3) | 133.1(6) |
| O(3)-Gd(3)-O(14) | 77.31(18) | C(121)-O(22)-Gd(2) | 137.5(6) |

Supplementary Table 13. Selected bond lengths (Å) and angles (o) for compound 2a at 293(2) K.

| Compound 2a |  |  |  |
| --- | --- | --- | --- |
| Gd(1)-O(25) | 2.351(5) | Gd(3)-O(4) | 2.305(4) |
| Gd(1)-O(2) | 2.350(4) | Gd(3)-O(14) | 2.338(4) |
| Gd(1)-O(4) | 2.403(4) | Gd(3)-O(18) | 2.372(5) |
| Gd(1)-O(9) | 2.407(4) | Gd(3)-O(3) | 2.380(4) |
| Gd(1)-O(3) | 2.435(4) | Gd(3)-O(1) | 2.405(4) |
| Gd(1)-O(5) | 2.452(4) | Gd(3)-O(24) | 2.406(5) |
| Gd(1)-O(8) | 2.455(5) | Gd(3)-O(17) | 2.436(4) |
| Gd(1)-O(7) | 2.493(4) | Gd(3)-O(16) | 2.479(4) |
| Gd(2)-O(6) | 2.340(4) | Gd(4)-O(2) | 2.345(4) |
| Gd(2)-O(19) | 2.359(5) | Gd(4)-O(3) | 2.358(4) |
| Gd(2)-O(23) | 2.378(4) | Gd(4)-O(15) | 2.360(4) |
| Gd(2)-O(2) | 2.390(4) | Gd(4)-O(1) | 2.373(4) |
| Gd(2)-O(20) | 2.389(5) | Gd(4)-O(10) | 2.381(4) |
| Gd(2)-O(1) | 2.427(4) | Gd(4)-O(27) | 2.405(4) |
| Gd(2)-O(26) | 2.464(5) | Gd(4)-O(11) | 2.482(5) |
| Gd(2)-O(4) | 2.461(4) | Gd(4)-O(13) | 2.510(4) |
| O(25)-Gd(1)-O(2) | 145.33(16) | O(14)-Gd(3)-O(17) | 86.45(16) |
| O(25)-Gd(1)-O(4) | 83.87(16) | O(18)-Gd(3)-O(17) | 75.06(17) |
| O(2)-Gd(1)-O(4) | 72.94(13) | O(3)-Gd(3)-O(17) | 142.04(15) |
| O(25)-Gd(1)-O(9) | 92.91(19) | O(1)-Gd(3)-O(17) | 144.36(14) |
| O(2)-Gd(1)-O(9) | 89.44(16) | O(24)-Gd(3)-O(17) | 74.04(16) |
| O(4)-Gd(1)-O(9) | 140.87(15) | O(4)-Gd(3)-O(16) | 74.96(14) |
| O(25)-Gd(1)-O(3) | 77.26(16) | O(14)-Gd(3)-O(16) | 139.69(16) |
| O(2)-Gd(1)-O(3) | 70.49(14) | O(18)-Gd(3)-O(16) | 75.76(17) |
| O(4)-Gd(1)-O(3) | 68.56(13) | O(3)-Gd(3)-O(16) | 127.09(14) |
| O(9)-Gd(1)-O(3) | 72.68(15) | O(1)-Gd(3)-O(16) | 133.03(14) |
| O(25)-Gd(1)-O(5) | 101.38(19) | O(24)-Gd(3)-O(16) | 71.95(17) |
| O(2)-Gd(1)-O(5) | 94.98(15) | O(17)-Gd(3)-O(16) | 53.27(14) |
| O(4)-Gd(1)-O(5) | 70.73(14) | O(2)-Gd(4)-O(3) | 71.92(14) |
| O(9)-Gd(1)-O(5) | 147.14(16) | O(2)-Gd(4)-O(15) | 147.47(15) |
| O(3)-Gd(1)-O(5) | 139.18(14) | O(3)-Gd(4)-O(15) | 83.48(15) |
| O(25)-Gd(1)-O(8) | 133.78(16) | O(2)-Gd(4)-O(1) | 72.19(13) |
| O(2)-Gd(1)-O(8) | 79.96(14) | O(3)-Gd(4)-O(1) | 69.34(14) |
| O(4)-Gd(1)-O(8) | 133.23(14) | O(15)-Gd(4)-O(1) | 79.48(15) |
| O(9)-Gd(1)-O(8) | 74.19(17) | O(2)-Gd(4)-O(10) | 94.87(17) |
| O(3)-Gd(1)-O(8) | 135.22(14) | O(3)-Gd(4)-O(10) | 72.74(15) |
| O(5)-Gd(1)-O(8) | 74.58(16) | O(15)-Gd(4)-O(10) | 97.85(18) |
| O(25)-Gd(1)-O(7) | 81.07(16) | O(1)-Gd(4)-O(10) | 142.05(15) |
| O(2)-Gd(1)-O(7) | 132.77(14) | O(2)-Gd(4)-O(27) | 98.81(15) |
| O(4)-Gd(1)-O(7) | 140.60(14) | O(3)-Gd(4)-O(27) | 142.07(15) |
| O(9)-Gd(1)-O(7) | 76.32(16) | O(15)-Gd(4)-O(27) | 87.52(17) |
| O(3)-Gd(1)-O(7) | 140.84(15) | O(1)-Gd(4)-O(27) | 72.81(15) |
| O(5)-Gd(1)-O(7) | 76.90(16) | O(10)-Gd(4)-O(27) | 145.15(16) |
| O(8)-Gd(1)-O(7) | 52.90(15) | O(2)-Gd(4)-O(11) | 79.73(14) |
| O(6)-Gd(2)-O(19) | 96.70(17) | O(3)-Gd(4)-O(11) | 135.39(15) |
| O(6)-Gd(2)-O(23) | 149.83(17) | O(15)-Gd(4)-O(11) | 132.42(15) |
| O(19)-Gd(2)-O(23) | 94.76(19) | O(1)-Gd(4)-O(11) | 132.69(15) |
| O(6)-Gd(2)-O(2) | 99.67(14) | O(10)-Gd(4)-O(11) | 76.25(17) |
| O(19)-Gd(2)-O(2) | 142.42(16) | O(27)-Gd(4)-O(11) | 74.91(17) |
| O(23)-Gd(2)-O(2) | 87.75(16) | O(2)-Gd(4)-O(13) | 131.02(16) |
| O(6)-Gd(2)-O(20) | 76.51(16) | O(3)-Gd(4)-O(13) | 140.50(15) |
| O(19)-Gd(2)-O(20) | 140.13(17) | O(15)-Gd(4)-O(13) | 81.42(17) |
| O(23)-Gd(2)-O(20) | 76.82(17) | O(1)-Gd(4)-O(13) | 141.57(15) |
| O(2)-Gd(2)-O(20) | 76.92(15) | O(10)-Gd(4)-O(13) | 73.48(16) |
| O(6)-Gd(2)-O(1) | 136.21(15) | O(27)-Gd(4)-O(13) | 73.34(16) |
| O(19)-Gd(2)-O(1) | 74.28(15) | O(11)-Gd(4)-O(13) | 51.36(16) |
| O(23)-Gd(2)-O(1) | 73.86(15) | Gd(4)-O(1)-Gd(3) | 108.01(15) |
| O(2)-Gd(2)-O(1) | 70.47(13) | Gd(4)-O(1)-Gd(2) | 104.08(15) |
| O(20)-Gd(2)-O(1) | 136.42(14) | Gd(3)-O(1)-Gd(2) | 107.62(14) |
| O(6)-Gd(2)-O(26) | 79.41(17) | Gd(4)-O(2)-Gd(1) | 107.60(16) |
| O(19)-Gd(2)-O(26) | 70.31(19) | Gd(4)-O(2)-Gd(2) | 106.13(15) |
| O(23)-Gd(2)-O(26) | 78.37(18) | Gd(1)-O(2)-Gd(2) | 105.85(15) |
| O(2)-Gd(2)-O(26) | 146.03(17) | Gd(4)-O(3)-Gd(3) | 109.33(16) |
| O(20)-Gd(2)-O(26) | 69.82(19) | Gd(4)-O(3)-Gd(1) | 104.44(15) |
| O(1)-Gd(2)-O(26) | 132.37(16) | Gd(3)-O(3)-Gd(1) | 105.31(14) |
| O(6)-Gd(2)-O(4) | 69.22(14) | Gd(3)-O(4)-Gd(1) | 108.78(15) |
| O(19)-Gd(2)-O(4) | 83.58(16) | Gd(3)-O(4)-Gd(2) | 109.76(15) |
| O(23)-Gd(2)-O(4) | 140.01(15) | Gd(1)-O(4)-Gd(2) | 102.03(14) |
| O(2)-Gd(2)-O(4) | 71.22(13) | C(15)-O(5)-Gd(1) | 134.6(4) |
| O(20)-Gd(2)-O(4) | 127.45(15) | C(15)-O(6)-Gd(2) | 136.2(4) |
| O(1)-Gd(2)-O(4) | 67.22(13) | C(16)-O(7)-Gd(1) | 91.0(4) |
| O(26)-Gd(2)-O(4) | 136.25(15) | C(16)-O(8)-Gd(1) | 92.6(4) |
| O(4)-Gd(3)-O(14) | 145.00(16) | C(91)-O(9)-Gd(1) | 138.8(5) |
| O(4)-Gd(3)-O(18) | 90.78(17) | C(91)-O(10)-Gd(4) | 133.8(5) |
| O(14)-Gd(3)-O(18) | 94.04(19) | N(1)-O(11)-Gd(4) | 96.8(4) |
| O(4)-Gd(3)-O(3) | 71.11(14) | N(1)-O(13)-Gd(4) | 95.1(4) |
| O(14)-Gd(3)-O(3) | 84.40(16) | C(76)-O(27)-Gd(4) | 129.2(4) |
| O(18)-Gd(3)-O(3) | 142.26(16) | C(121)-O(14)-Gd(3) | 137.6(5) |
| O(4)-Gd(3)-O(1) | 70.11(14) | C(121)-O(15)-Gd(4) | 135.9(4) |
| O(14)-Gd(3)-O(1) | 77.91(16) | C(46)-O(16)-Gd(3) | 91.1(4) |
| O(18)-Gd(3)-O(1) | 74.36(15) | C(46)-O(17)-Gd(3) | 92.8(4) |
| O(3)-Gd(3)-O(1) | 68.44(13) | C(61)-O(18)-Gd(3) | 135.0(5) |
| O(4)-Gd(3)-O(24) | 94.72(16) | C(61)-O(19)-Gd(2) | 140.5(5) |
| O(14)-Gd(3)-O(24) | 101.03(19) | C(106)-O(20)-Gd(2) | 136.9(4) |
| O(18)-Gd(3)-O(24) | 144.50(18) | C(76)-O(23)-Gd(2) | 140.6(5) |
| O(3)-Gd(3)-O(24) | 71.75(15) | C(31)-O(24)-Gd(3) | 129.6(5) |
| O(1)-Gd(3)-O(24) | 140.10(15) | C(31)-O(25)-Gd(1) | 138.5(5) |
| O(4)-Gd(3)-O(17) | 128.13(14) |  |  |
| Symmetry codes: ##1 -x+1,-y+1,-z+2 |  |  |  |

Supplementary Table 14. Selected bond lengths (Å) and angles (o) for compound 3 at 293(2) K.

| Compound 3 |  |  |  |
| --- | --- | --- | --- |
| O(1)-Y(1) | 2.420(3) | O(19)-Y(3) | 2.440(3) |
| O(2)-Y(1) | 2.423(3) | O(20)-Y(3) | 2.339(3) |
| O(3)-Y(1) | 2.335(3) | O(21)-Y(1) | 2.362(3) |
| O(4)-Y(4) | 2.336(3) | O(22)-Y(4) | 2.297(2) |
| O(5)-Y(2) | 2.357(3) | O(22)-Y(1) | 2.304(2) |
| O(7)-Y(2) | 2.293(3) | O(22)-Y(2) | 2.352(2) |
| O(8)-Y(1) | 2.358(3) | O(23)-Y(3) | 2.266(2) |
| O(9)-Y(4) | 2.447(3) | O(23)-Y(1) | 2.368(2) |
| O(10)-Y(4) | 2.465(3) | O(23)-Y(2) | 2.413(2) |
| O(12)-Y(4) | 2.357(2) | O(24)-Y(4) | 2.340(2) |
| O(13)-Y(2) | 2.320(2) | O(24)-Y(3) | 2.352(2) |
| O(14)-Y(4) | 2.302(3) | O(24)-Y(2) | 2.372(2) |
| O(15)-Y(3) | 2.313(3) | O(25)-Y(4) | 2.314(2) |
| O(16)-Y(2) | 2.343(2) | O(25)-Y(3) | 2.336(2) |
| O(17)-Y(3) | 2.326(3) | O(25)-Y(1) | 2.371(3) |
| O(18)-Y(3) | 2.378(2) | O(26)-Y(2) | 2.450(3) |
| C(16)-O(1)-Y(1) | 93.0(2) | O(22)-Y(2)-O(24) | 70.98(8) |
| C(16)-O(2)-Y(1) | 92.7(2) | O(5)-Y(2)-O(24) | 134.79(8) |
| C(46)-O(3)-Y(1) | 136.9(3) | O(7)-Y(2)-O(23) | 71.08(9) |
| C(46)-O(4)-Y(4) | 134.3(3) | O(13)-Y(2)-O(23) | 142.55(9) |
| C(61)-O(5)-Y(2) | 138.4(3) | O(16)-Y(2)-O(23) | 85.62(9) |
| C(15)-O(7)-Y(2) | 134.8(3) | O(22)-Y(2)-O(23) | 71.76(8) |
| C(15)-O(8)-Y(1) | 137.1(3) | O(5)-Y(2)-O(23) | 129.18(9) |
| N(1)-O(9)-Y(4) | 96.4(2) | O(24)-Y(2)-O(23) | 68.44(8) |
| N(1)-O(10)-Y(4) | 95.5(2) | O(7)-Y(2)-O(26) | 76.23(11) |
| C(76)-O(12)-Y(4) | 132.3(2) | O(13)-Y(2)-O(26) | 77.95(10) |
| C(76)-O(13)-Y(2) | 138.2(2) | O(16)-Y(2)-O(26) | 69.92(11) |
| C(91)-O(14)-Y(4) | 135.2(2) | O(22)-Y(2)-O(26) | 144.91(10) |
| C(91)-O(15)-Y(3) | 137.1(2) | O(5)-Y(2)-O(26) | 68.15(11) |
| C(106)-O(16)-Y(2) | 138.0(2) | O(24)-Y(2)-O(26) | 134.65(10) |
| C(106)-O(17)-Y(3) | 133.5(2) | O(23)-Y(2)-O(26) | 134.17(9) |
| C(121)-O(18)-Y(3) | 93.4(2) | O(23)-Y(3)-O(15) | 145.93(9) |
| C(121)-O(19)-Y(3) | 90.9(2) | O(23)-Y(3)-O(17) | 93.89(9) |
| C(31)-O(20)-Y(3) | 132.8(3) | O(15)-Y(3)-O(17) | 92.76(11) |
| C(31)-O(21)-Y(1) | 134.4(3) | O(23)-Y(3)-O(25) | 71.63(9) |
| Y(4)-O(22)-Y(1) | 106.25(10) | O(15)-Y(3)-O(25) | 83.24(9) |
| Y(4)-O(22)-Y(2) | 106.00(9) | O(17)-Y(3)-O(25) | 143.15(9) |
| Y(1)-O(22)-Y(2) | 106.00(9) | O(23)-Y(3)-O(20) | 93.51(10) |
| Y(3)-O(23)-Y(1) | 107.97(10) | O(15)-Y(3)-O(20) | 100.55(11) |
| Y(3)-O(23)-Y(2) | 108.13(9) | O(17)-Y(3)-O(20) | 143.80(10) |
| Y(1)-O(23)-Y(2) | 102.14(9) | O(25)-Y(3)-O(20) | 72.37(9) |
| Y(4)-O(24)-Y(3) | 107.96(9) | O(23)-Y(3)-O(24) | 71.27(9) |
| Y(4)-O(24)-Y(2) | 103.99(9) | O(15)-Y(3)-O(24) | 78.49(9) |
| Y(3)-O(24)-Y(2) | 106.67(9) | O(17)-Y(3)-O(24) | 74.41(9) |
| Y(4)-O(25)-Y(3) | 109.35(10) | O(25)-Y(3)-O(24) | 68.89(8) |
| Y(4)-O(25)-Y(1) | 103.57(10) | O(20)-Y(3)-O(24) | 141.10(9) |
| Y(3)-O(25)-Y(1) | 105.57(10) | O(23)-Y(3)-O(18) | 129.14(9) |
| O(22)-Y(1)-O(3) | 92.31(10) | O(15)-Y(3)-O(18) | 84.77(9) |
| O(22)-Y(1)-O(21) | 148.06(10) | O(17)-Y(3)-O(18) | 74.07(9) |
| O(3)-Y(1)-O(21) | 92.42(12) | O(25)-Y(3)-O(18) | 141.23(9) |
| O(22)-Y(1)-O(8) | 92.06(10) | O(20)-Y(3)-O(18) | 73.84(9) |
| O(3)-Y(1)-O(8) | 142.66(11) | O(24)-Y(3)-O(18) | 143.32(8) |
| O(21)-Y(1)-O(8) | 102.95(13) | O(23)-Y(3)-O(19) | 74.76(8) |
| O(22)-Y(1)-O(23) | 73.40(8) | O(15)-Y(3)-O(19) | 139.08(9) |
| O(3)-Y(1)-O(23) | 143.13(10) | O(17)-Y(3)-O(19) | 75.30(10) |
| O(21)-Y(1)-O(23) | 84.11(9) | O(25)-Y(3)-O(19) | 128.99(9) |
| O(8)-Y(1)-O(23) | 73.08(9) | O(20)-Y(3)-O(19) | 72.62(10) |
| O(22)-Y(1)-O(25) | 71.48(9) | O(24)-Y(3)-O(19) | 132.11(9) |
| O(3)-Y(1)-O(25) | 73.98(10) | O(18)-Y(3)-O(19) | 54.38(9) |
| O(21)-Y(1)-O(25) | 79.56(11) | O(22)-Y(4)-O(14) | 148.70(9) |
| O(8)-Y(1)-O(25) | 141.83(9) | O(22)-Y(4)-O(25) | 72.63(9) |
| O(23)-Y(1)-O(25) | 69.28(8) | O(14)-Y(4)-O(25) | 84.02(9) |
| O(22)-Y(1)-O(1) | 80.01(9) | O(22)-Y(4)-O(4) | 95.00(10) |
| O(3)-Y(1)-O(1) | 72.46(11) | O(14)-Y(4)-O(4) | 98.32(11) |
| O(21)-Y(1)-O(1) | 131.33(10) | O(25)-Y(4)-O(4) | 73.96(9) |
| O(8)-Y(1)-O(1) | 71.85(10) | O(22)-Y(4)-O(24) | 72.51(8) |
| O(23)-Y(1)-O(1) | 134.63(9) | O(14)-Y(4)-O(24) | 80.01(9) |
| O(25)-Y(1)-O(1) | 134.45(9) | O(25)-Y(4)-O(24) | 69.45(8) |
| O(22)-Y(1)-O(2) | 133.76(9) | O(4)-Y(4)-O(24) | 143.36(9) |
| O(3)-Y(1)-O(2) | 75.88(11) | O(22)-Y(4)-O(12) | 96.95(9) |
| O(21)-Y(1)-O(2) | 77.90(10) | O(14)-Y(4)-O(12) | 88.64(10) |
| O(8)-Y(1)-O(2) | 74.47(11) | O(25)-Y(4)-O(12) | 141.94(9) |
| O(23)-Y(1)-O(2) | 137.98(9) | O(4)-Y(4)-O(12) | 144.10(9) |
| O(25)-Y(1)-O(2) | 141.21(10) | O(24)-Y(4)-O(12) | 72.50(8) |
| O(1)-Y(1)-O(2) | 53.76(9) | O(22)-Y(4)-O(9) | 79.17(9) |
| O(7)-Y(2)-O(13) | 145.63(10) | O(14)-Y(4)-O(9) | 131.71(9) |
| O(7)-Y(2)-O(16) | 100.98(10) | O(25)-Y(4)-O(9) | 135.27(9) |
| O(13)-Y(2)-O(16) | 90.97(10) | O(4)-Y(4)-O(9) | 74.73(10) |
| O(7)-Y(2)-O(22) | 97.45(9) | O(24)-Y(4)-O(9) | 132.85(9) |
| O(13)-Y(2)-O(22) | 90.80(9) | O(12)-Y(4)-O(9) | 74.49(9) |
| O(16)-Y(2)-O(22) | 144.24(9) | O(22)-Y(4)-O(10) | 131.10(9) |
| O(7)-Y(2)-O(5) | 74.64(10) | O(14)-Y(4)-O(10) | 80.01(9) |
| O(13)-Y(2)-O(5) | 74.91(10) | O(25)-Y(4)-O(10) | 141.07(9) |
| O(16)-Y(2)-O(5) | 137.65(10) | O(4)-Y(4)-O(10) | 73.57(10) |
| O(22)-Y(2)-O(5) | 76.87(9) | O(24)-Y(4)-O(10) | 140.29(9) |
| O(7)-Y(2)-O(24) | 139.51(9) | O(12)-Y(4)-O(10) | 73.07(9) |
| O(13)-Y(2)-O(24) | 74.64(9) | O(9)-Y(4)-O(10) | 51.94(9) |
| O(16)-Y(2)-O(24) | 75.11(9) |  |  |

Supplementary Table 15. Selected bond lengths (Å) and angles (o) for compound 3m at 293(2) K.

| Compound 3m |  |  |  |
| --- | --- | --- | --- |
| Y(1)-O(19) | 2.304(4) | Y(3)-O(19) | 2.305(4) |
| Y(1)-O(20) | 2.313(4) | Y(3)-O(7) | 2.321(5) |
| Y(1)-O(14) | 2.300(4) | Y(3)-O(22) | 2.361(4) |
| Y(1)-O(6) | 2.331(4) | Y(3)-O(5) | 2.357(5) |
| Y(1)-O(21) | 2.330(4) | Y(3)-O(20) | 2.394(4) |
| Y(1)-O(16) | 2.359(4) | Y(3)-O(2) | 2.414(5) |
| Y(1)-O(23) | 2.435(5) | Y(3)-O(3) | 2.401(4) |
| Y(1)-O(24) | 2.466(4) | Y(3)-O(4) | 2.436(5) |
| Y(2)-O(1) | 2.293(5) | Y(4)-O(22) | 2.266(4) |
| Y(2)-O(15) | 2.318(4) | Y(4)-O(13) | 2.307(5) |
| Y(2)-O(12) | 2.335(5) | Y(4)-O(20) | 2.339(4) |
| Y(2)-O(19) | 2.353(4) | Y(4)-O(11) | 2.348(5) |
| Y(2)-O(17) | 2.357(5) | Y(4)-O(8) | 2.351(5) |
| Y(2)-O(21) | 2.381(4) | Y(4)-O(21) | 2.363(4) |
| Y(2)-O(22) | 2.419(4) | Y(4)-O(10) | 2.391(4) |
| Y(2)-O(26) | 2.438(5) | Y(4)-O(9) | 2.429(5) |
| O(19)-Y(1)-O(20) | 72.32(14) | O(7)-Y(3)-O(3) | 132.32(17) |
| O(19)-Y(1)-O(14) | 148.32(15) | O(22)-Y(3)-O(3) | 134.50(15) |
| O(20)-Y(1)-O(14) | 83.51(15) | O(5)-Y(3)-O(3) | 74.48(18) |
| O(19)-Y(1)-O(6) | 94.36(17) | O(20)-Y(3)-O(3) | 134.48(16) |
| O(20)-Y(1)-O(6) | 73.02(15) | O(2)-Y(3)-O(3) | 74.63(18) |
| O(14)-Y(1)-O(6) | 97.90(18) | O(19)-Y(3)-O(4) | 133.43(15) |
| O(19)-Y(1)-O(21) | 72.51(14) | O(7)-Y(3)-O(4) | 79.14(17) |
| O(20)-Y(1)-O(21) | 69.34(14) | O(22)-Y(3)-O(4) | 139.26(15) |
| O(14)-Y(1)-O(21) | 80.06(14) | O(5)-Y(3)-O(4) | 76.18(17) |
| O(6)-Y(1)-O(21) | 142.31(15) | O(20)-Y(3)-O(4) | 140.82(16) |
| O(19)-Y(1)-O(16) | 98.71(15) | O(2)-Y(3)-O(4) | 76.29(17) |
| O(20)-Y(1)-O(16) | 142.19(14) | O(3)-Y(3)-O(4) | 53.46(16) |
| O(14)-Y(1)-O(16) | 87.85(17) | O(22)-Y(4)-O(13) | 145.68(16) |
| O(6)-Y(1)-O(16) | 144.76(16) | O(22)-Y(4)-O(20) | 71.47(14) |
| O(21)-Y(1)-O(16) | 72.92(14) | O(13)-Y(4)-O(20) | 84.17(16) |
| O(19)-Y(1)-O(23) | 79.08(15) | O(22)-Y(4)-O(11) | 92.26(16) |
| O(20)-Y(1)-O(23) | 135.13(16) | O(13)-Y(4)-O(11) | 92.85(19) |
| O(14)-Y(1)-O(23) | 132.29(16) | O(20)-Y(4)-O(11) | 142.48(16) |
| O(6)-Y(1)-O(23) | 75.54(17) | O(22)-Y(4)-O(8) | 94.35(17) |
| O(21)-Y(1)-O(23) | 132.72(15) | O(13)-Y(4)-O(8) | 100.56(19) |
| O(16)-Y(1)-O(23) | 75.05(16) | O(20)-Y(4)-O(8) | 71.52(15) |
| O(19)-Y(1)-O(24) | 131.60(16) | O(11)-Y(4)-O(8) | 145.06(17) |
| O(20)-Y(1)-O(24) | 140.64(15) | O(22)-Y(4)-O(21) | 70.55(14) |
| O(14)-Y(1)-O(24) | 79.97(17) | O(13)-Y(4)-O(21) | 78.26(15) |
| O(6)-Y(1)-O(24) | 74.21(17) | O(20)-Y(4)-O(21) | 68.36(13) |
| O(21)-Y(1)-O(24) | 140.53(16) | O(11)-Y(4)-O(21) | 74.40(15) |
| O(16)-Y(1)-O(24) | 72.63(16) | O(8)-Y(4)-O(21) | 139.79(15) |
| O(23)-Y(1)-O(24) | 52.54(16) | O(22)-Y(4)-O(10) | 129.71(15) |
| O(1)-Y(2)-O(15) | 147.63(18) | O(13)-Y(4)-O(10) | 84.26(17) |
| O(1)-Y(2)-O(12) | 96.82(17) | O(20)-Y(4)-O(10) | 141.48(15) |
| O(15)-Y(2)-O(12) | 92.53(18) | O(11)-Y(4)-O(10) | 74.72(17) |
| O(1)-Y(2)-O(19) | 100.81(15) | O(8)-Y(4)-O(10) | 74.73(17) |
| O(15)-Y(2)-O(19) | 89.40(16) | O(21)-Y(4)-O(10) | 143.46(15) |
| O(12)-Y(2)-O(19) | 143.51(16) | O(22)-Y(4)-O(9) | 75.17(14) |
| O(1)-Y(2)-O(17) | 76.71(17) | O(13)-Y(4)-O(9) | 138.82(16) |
| O(15)-Y(2)-O(17) | 75.75(17) | O(20)-Y(4)-O(9) | 128.14(14) |
| O(12)-Y(2)-O(17) | 138.27(17) | O(11)-Y(4)-O(9) | 75.95(17) |
| O(19)-Y(2)-O(17) | 77.29(15) | O(8)-Y(4)-O(9) | 72.73(17) |
| O(1)-Y(2)-O(21) | 137.66(16) | O(21)-Y(4)-O(9) | 133.05(14) |
| O(15)-Y(2)-O(21) | 74.70(15) | O(10)-Y(4)-O(9) | 54.61(15) |
| O(12)-Y(2)-O(21) | 74.66(15) | C(15)-O(1)-Y(2) | 135.1(5) |
| O(19)-Y(2)-O(21) | 70.77(13) | C(15)-O(2)-Y(3) | 134.7(5) |
| O(17)-Y(2)-O(21) | 136.15(14) | C(16)-O(3)-Y(3) | 92.9(4) |
| O(1)-Y(2)-O(22) | 70.27(15) | C(16)-O(4)-Y(3) | 91.9(4) |
| O(15)-Y(2)-O(22) | 141.66(15) | C(46)-O(5)-Y(3) | 136.7(5) |
| O(12)-Y(2)-O(22) | 84.89(16) | C(46)-O(6)-Y(1) | 134.7(5) |
| O(19)-Y(2)-O(22) | 71.64(13) | C(121)-O(7)-Y(3) | 136.4(5) |
| O(17)-Y(2)-O(22) | 128.53(15) | C(121)-O(8)-Y(4) | 131.3(5) |
| O(21)-Y(2)-O(22) | 67.72(14) | C(106)-O(9)-Y(4) | 90.3(4) |
| O(1)-Y(2)-O(26) | 76.72(17) | C(106)-O(10)-Y(4) | 93.3(4) |
| O(15)-Y(2)-O(26) | 77.84(17) | C(91)-O(11)-Y(4) | 134.3(4) |
| O(12)-Y(2)-O(26) | 69.22(19) | C(91)-O(12)-Y(2) | 139.8(4) |
| O(19)-Y(2)-O(26) | 146.08(17) | C(76)-O(13)-Y(4) | 137.3(4) |
| O(17)-Y(2)-O(26) | 69.17(18) | C(76)-O(14)-Y(1) | 135.8(4) |
| O(21)-Y(2)-O(26) | 133.00(17) | C(61)-O(15)-Y(2) | 138.4(4) |
| O(22)-Y(2)-O(26) | 134.90(15) | C(61)-O(16)-Y(1) | 129.7(4) |
| O(19)-Y(3)-O(7) | 146.86(16) | C(31)-O(17)-Y(2) | 138.4(4) |
| O(19)-Y(3)-O(22) | 73.53(14) | Y(1)-O(19)-Y(3) | 107.27(16) |
| O(7)-Y(3)-O(22) | 83.82(15) | Y(1)-O(19)-Y(2) | 105.75(15) |
| O(19)-Y(3)-O(5) | 91.80(16) | Y(3)-O(19)-Y(2) | 105.55(15) |
| O(7)-Y(3)-O(5) | 91.05(19) | Y(1)-O(20)-Y(4) | 109.53(16) |
| O(22)-Y(3)-O(5) | 141.21(16) | Y(1)-O(20)-Y(3) | 104.07(15) |
| O(19)-Y(3)-O(20) | 70.85(14) | Y(4)-O(20)-Y(3) | 105.07(15) |
| O(7)-Y(3)-O(20) | 78.64(16) | Y(1)-O(21)-Y(4) | 108.14(14) |
| O(22)-Y(3)-O(20) | 68.89(14) | Y(1)-O(21)-Y(2) | 104.06(14) |
| O(5)-Y(3)-O(20) | 72.39(15) | Y(4)-O(21)-Y(2) | 107.24(15) |
| O(19)-Y(3)-O(2) | 94.04(16) | Y(4)-O(22)-Y(3) | 108.57(15) |
| O(7)-Y(3)-O(2) | 101.3(2) | Y(4)-O(22)-Y(2) | 109.18(16) |
| O(22)-Y(3)-O(2) | 71.16(15) | Y(3)-O(22)-Y(2) | 101.79(14) |
| O(5)-Y(3)-O(2) | 146.99(18) | N(1)-O(23)-Y(1) | 96.5(4) |
| O(20)-Y(3)-O(2) | 139.83(15) | N(1)-O(24)-Y(1) | 95.0(4) |
| O(19)-Y(3)-O(3) | 79.98(16) |  |  |

Supplementary Table 16. Selected bond lengths (Å) and angles (o) for compound 3a at 293(2) K.

| Compound 3a |  |  |  |
| --- | --- | --- | --- |
| O(1)-Y(4) | 2.310(2) | O(9)-Y(3) | 2.433(2) |
| O(1)-Y(3) | 2.330(2) | O(10)-Y(3) | 2.380(2) |
| O(1)-Y(1) | 2.391(2) | O(11)-Y(3) | 2.336(2) |
| O(2)-Y(4) | 2.2980(19) | O(12)-Y(2) | 2.323(2) |
| O(2)-Y(1) | 2.300(2) | O(13)-Y(3) | 2.306(2) |
| O(2)-Y(2) | 2.342(2) | O(14)-Y(4) | 2.316(2) |
| O(3)-Y(3) | 2.263(2) | O(15)-Y(4) | 2.367(2) |
| O(3)-Y(1) | 2.356(2) | O(16)-Y(2) | 2.324(2) |
| O(3)-Y(2) | 2.419(2) | O(18)-Y(2) | 2.373(2) |
| O(4)-Y(4) | 2.328(2) | O(19)-Y(4) | 2.471(2) |
| O(4)-Y(3) | 2.364(2) | O(20)-Y(4) | 2.451(2) |
| O(4)-Y(2) | 2.388(2) | O(22)-Y(2) | 2.434(3) |
| O(5)-Y(1) | 2.410(2) | O(23)-Y(4) | 2.327(2) |
| O(6)-Y(2) | 2.293(2) | O(24)-Y(1) | 2.351(2) |
| O(7)-Y(1) | 2.330(2) | O(25)-Y(1) | 2.414(2) |
| O(8)-Y(3) | 2.363(2) | O(26)-Y(1) | 2.433(2) |
| Y(4)-O(1)-Y(3) | 109.23(8) | O(2)-Y(2)-O(4) | 70.73(7) |
| Y(4)-O(1)-Y(1) | 103.78(8) | O(18)-Y(2)-O(4) | 136.18(7) |
| Y(3)-O(1)-Y(1) | 104.99(8) | O(6)-Y(2)-O(3) | 70.37(7) |
| Y(4)-O(2)-Y(1) | 107.11(8) | O(12)-Y(2)-O(3) | 83.73(8) |
| Y(4)-O(2)-Y(2) | 106.23(8) | O(16)-Y(2)-O(3) | 141.27(7) |
| Y(1)-O(2)-Y(2) | 105.68(8) | O(2)-Y(2)-O(3) | 71.59(7) |
| Y(3)-O(3)-Y(1) | 108.35(8) | O(18)-Y(2)-O(3) | 128.01(8) |
| Y(3)-O(3)-Y(2) | 109.37(8) | O(4)-Y(2)-O(3) | 67.78(7) |
| Y(1)-O(3)-Y(2) | 101.57(7) | O(6)-Y(2)-O(22) | 78.24(9) |
| Y(4)-O(4)-Y(3) | 107.45(8) | O(12)-Y(2)-O(22) | 70.61(9) |
| Y(4)-O(4)-Y(2) | 103.79(8) | O(16)-Y(2)-O(22) | 76.91(9) |
| Y(3)-O(4)-Y(2) | 107.05(8) | O(2)-Y(2)-O(22) | 145.04(9) |
| C(15)-O(5)-Y(1) | 133.6(2) | O(18)-Y(2)-O(22) | 68.65(9) |
| C(15)-O(6)-Y(2) | 134.83(19) | O(4)-Y(2)-O(22) | 132.60(9) |
| C(91)-O(7)-Y(1) | 136.1(2) | O(3)-Y(2)-O(22) | 136.49(8) |
| C(91)-O(8)-Y(3) | 131.0(2) | O(3)-Y(3)-O(13) | 145.68(8) |
| C(76)-O(9)-Y(3) | 90.81(19) | O(3)-Y(3)-O(1) | 71.76(7) |
| C(76)-O(10)-Y(3) | 93.24(18) | O(13)-Y(3)-O(1) | 84.02(8) |
| C(61)-O(11)-Y(3) | 133.0(2) | O(3)-Y(3)-O(11) | 92.35(8) |
| C(61)-O(12)-Y(2) | 139.8(2) | O(13)-Y(3)-O(11) | 92.83(9) |
| C(46)-O(13)-Y(3) | 137.6(2) | O(1)-Y(3)-O(11) | 142.95(8) |
| C(46)-O(14)-Y(4) | 134.2(2) | O(3)-Y(3)-O(8) | 93.39(8) |
| C(31)-O(15)-Y(4) | 129.0(2) | O(13)-Y(3)-O(8) | 102.28(9) |
| C(31)-O(16)-Y(2) | 139.5(2) | O(1)-Y(3)-O(8) | 72.52(8) |
| C(16)-O(18)-Y(2) | 136.5(2) | O(11)-Y(3)-O(8) | 143.37(8) |
| N(1)-O(19)-Y(4) | 95.57(16) | O(3)-Y(3)-O(4) | 70.78(7) |
| N(1)-O(20)-Y(4) | 96.33(17) | O(13)-Y(3)-O(4) | 78.09(8) |
| C(121)-O(23)-Y(4) | 134.6(2) | O(1)-Y(3)-O(4) | 68.94(7) |
| C(121)-O(24)-Y(1) | 137.2(2) | O(11)-Y(3)-O(4) | 74.28(8) |
| C(106)-O(25)-Y(1) | 92.7(2) | O(8)-Y(3)-O(4) | 141.21(8) |
| C(106)-O(26)-Y(1) | 91.87(19) | O(3)-Y(3)-O(10) | 129.11(7) |
| O(2)-Y(1)-O(7) | 147.99(8) | O(13)-Y(3)-O(10) | 84.88(8) |
| O(2)-Y(1)-O(24) | 91.22(8) | O(1)-Y(3)-O(10) | 141.07(8) |
| O(7)-Y(1)-O(24) | 93.15(9) | O(11)-Y(3)-O(10) | 74.75(8) |
| O(2)-Y(1)-O(3) | 73.48(7) | O(8)-Y(3)-O(10) | 73.65(8) |
| O(7)-Y(1)-O(3) | 83.94(8) | O(4)-Y(3)-O(10) | 143.64(8) |
| O(24)-Y(1)-O(3) | 142.20(8) | O(3)-Y(3)-O(9) | 74.61(7) |
| O(2)-Y(1)-O(1) | 71.06(7) | O(13)-Y(3)-O(9) | 139.28(8) |
| O(7)-Y(1)-O(1) | 79.92(8) | O(1)-Y(3)-O(9) | 128.44(7) |
| O(24)-Y(1)-O(1) | 73.28(8) | O(11)-Y(3)-O(9) | 75.08(9) |
| O(3)-Y(1)-O(1) | 69.10(7) | O(8)-Y(3)-O(9) | 71.71(8) |
| O(2)-Y(1)-O(5) | 94.99(8) | O(4)-Y(3)-O(9) | 132.06(7) |
| O(7)-Y(1)-O(5) | 98.99(9) | O(10)-Y(3)-O(9) | 54.52(7) |
| O(24)-Y(1)-O(5) | 145.73(8) | O(2)-Y(4)-O(1) | 72.57(7) |
| O(3)-Y(1)-O(5) | 71.35(7) | O(2)-Y(4)-O(14) | 149.09(8) |
| O(1)-Y(1)-O(5) | 140.32(7) | O(1)-Y(4)-O(14) | 84.29(8) |
| O(2)-Y(1)-O(25) | 79.06(8) | O(2)-Y(4)-O(4) | 72.57(7) |
| O(7)-Y(1)-O(25) | 132.50(8) | O(1)-Y(4)-O(4) | 69.88(7) |
| O(24)-Y(1)-O(25) | 74.15(9) | O(14)-Y(4)-O(4) | 80.48(7) |
| O(3)-Y(1)-O(25) | 133.06(7) | O(2)-Y(4)-O(23) | 94.12(8) |
| O(1)-Y(1)-O(25) | 134.69(8) | O(1)-Y(4)-O(23) | 74.04(8) |
| O(5)-Y(1)-O(25) | 74.03(8) | O(14)-Y(4)-O(23) | 98.99(9) |
| O(2)-Y(1)-O(26) | 132.99(8) | O(4)-Y(4)-O(23) | 143.80(8) |
| O(7)-Y(1)-O(26) | 78.63(9) | O(2)-Y(4)-O(15) | 98.74(8) |
| O(24)-Y(1)-O(26) | 75.70(8) | O(1)-Y(4)-O(15) | 142.77(8) |
| O(3)-Y(1)-O(26) | 139.35(7) | O(14)-Y(4)-O(15) | 87.30(8) |
| O(1)-Y(1)-O(26) | 140.90(8) | O(4)-Y(4)-O(15) | 72.97(7) |
| O(5)-Y(1)-O(26) | 75.50(8) | O(23)-Y(4)-O(15) | 143.18(8) |
| O(25)-Y(1)-O(26) | 53.97(8) | O(2)-Y(4)-O(20) | 80.27(7) |
| O(6)-Y(2)-O(12) | 96.70(8) | O(1)-Y(4)-O(20) | 136.24(8) |
| O(6)-Y(2)-O(16) | 147.68(8) | O(14)-Y(4)-O(20) | 130.21(8) |
| O(12)-Y(2)-O(16) | 94.21(9) | O(4)-Y(4)-O(20) | 132.81(7) |
| O(6)-Y(2)-O(2) | 100.07(7) | O(23)-Y(4)-O(20) | 74.44(8) |
| O(12)-Y(2)-O(2) | 143.15(8) | O(15)-Y(4)-O(20) | 73.99(8) |
| O(16)-Y(2)-O(2) | 88.85(8) | O(2)-Y(4)-O(19) | 132.19(7) |
| O(6)-Y(2)-O(18) | 75.75(8) | O(1)-Y(4)-O(19) | 139.69(7) |
| O(12)-Y(2)-O(18) | 139.25(8) | O(14)-Y(4)-O(19) | 78.60(8) |
| O(16)-Y(2)-O(18) | 76.15(8) | O(4)-Y(4)-O(19) | 140.40(7) |
| O(2)-Y(2)-O(18) | 77.04(8) | O(23)-Y(4)-O(19) | 73.01(8) |
| O(6)-Y(2)-O(4) | 137.93(7) | O(15)-Y(4)-O(19) | 72.81(8) |
| O(12)-Y(2)-O(4) | 74.81(8) | O(20)-Y(4)-O(19) | 51.98(7) |
| O(16)-Y(2)-O(4) | 74.35(7) |  |  |
| Symmetry codes: #1 -x+1,-y+1,-z+2 |  |  |  |

Supplementary Table 17. Calculated energy levels (cm−1), g (gx, gy, gz) tensors and predominant mJ values of the lowest eight Kramers doublets (KDs) of individual DyⅢ fragments for 1 and 1a using CASSCF/RASSI-SO with the OpenMolcas.

| KDs | 1_Dy1 |  |  | 1_Dy2 |  |  | 1_Dy3 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | E | g | mJ | E | g | mJ |  |  |  |
| 1 | 0.0 | 0.392 1.049 18.956 | ±15/2 | 0.0 | 0.614 2.282 17.738 | ±15/2 | 0.0 | 0.312 0.993 18.843 | ±15/2 |
| 2 | 31.0 | 0.098 1.052 16.253 | ±13/2 | 48.1 | 2.772 4.060 11.359 | ±13/2 | 52.0 | 1.711 2.684 15.238 | ±9/2 |
| 3 | 114.4 | 1.914 2.779 12.282 |  | 103.3 | 7.480 5.777 0.453 |  | 96.0 | 8.734 7.244 3.096 |  |
| 4 | 165.5 | 3.299 4.247 12.414 |  | 164.7 | 2.032 3.540 13.114 |  | 129.1 | 0.109 2.697 15.031 |  |
| 5 | 213.5 | 1.434 2.099 11.774 |  | 189.1 | 0.712 2.257 13.912 |  | 135.3 | 1.070 2.982 11.247 |  |
| 6 | 298.7 | 0.284 0.323 14.617 |  | 250.6 | 0.548 1.018 15.625 |  | 203.0 | 1.057 1.634 14.076 |  |
| 7 | 377.1 | 0.032 0.061 17.928 |  | 334.3 | 0.186 0.314 18.860 |  | 307.3 | 0.181 0.343 18.700 |  |
| 8 | 510.2 | 0.000 0.007 19.706 |  | 445.5 | 0.038 0.070 19.609 |  | 396.1 | 0.065 0.144 19.440 |  |
| KDs | 1_Dy4 |  |  | 1a_Dy1 |  |  | 1a_Dy2 |  |  |
|  | E | g | mJ | E | g | mJ | E | g | mJ |
| 1 | 0.0 | 0.115 0.778 19.073 | ±15/2 | 0.0 | 0.320 0.806 18.624 | ±15/2 | 0.0 | 0.935 4.193 16.215 | ±15/2 |
| 2 | 27.2 | 0.324 0.867 18.467 | ±9/2 | 47.6 | 1.004 1.588 16.984 | ±9/2 | 38.0 | 2.408 3.657 9.102 | ±13/2 |
| 3 | 96.8 | 3.658 5.000 11.568 |  | 101.1 | 0.699 2.854 12.132 |  | 94.4 | 8.000 5.085 0.263 |  |
| 4 | 139.5 | 8.431 5.585 0.925 |  | 126.9 | 3.114 3.902 11.062 |  | 150.1 | 0.891 2.295 14.668 |  |
| 5 | 182.4 | 1.061 2.667 13.050 |  | 177.2 | 2.448 3.115 11.289 |  | 178.0 | 1.532 3.101 12.749 |  |
| 6 | 224.1 | 0.929 1.618 15.239 |  | 247.4 | 0.312 0.429 17.005 |  | 237.6 | 0.012 0.923 14.985 |  |
| 7 | 344.1 | 0.003 0.156 18.387 |  | 356.6 | 0.110 0.507 14.995 |  | 284.5 | 0.357 0.513 18.550 |  |
| 8 | 410.8 | 0.044 0.124 19.337 |  | 373.8 | 0.070 0.565 16.203 |  | 450.2 | 0.013 0.018 19.692 |  |
| KDs | 1a_Dy3 |  |  | 1a_Dy4 |  |  |  |  |  |
|  | E | g | mJ | E | g | mJ |  |  |  |
| 1 | 0.0 | 0.183 0.442 19.077 | ±15/2 | 0.0 | 0.495 1.908 18.115 | ±15/2 |  |  |  |
| 2 | 59.3 | 1.293 1.508 16.449 | ±13/2 | 17.5 | 0.826 1.126 16.797 | ±9/2 |  |  |  |
| 3 | 91.3 | 0.222 1.015 16.922 |  | 110.7 | 3.445 5.140 11.385 |  |  |  |  |
| 4 | 114.5 | 2.576 3.907 11.424 |  | 156.9 | 1.567 4.996 8.633 |  |  |  |  |
| 5 | 142.4 | 8.715 6.997 2.925 |  | 202.1 | 1.331 2.312 12.352 |  |  |  |  |
| 6 | 189.0 | 1.061 1.290 13.698 |  | 249.3 | 0.570 0.977 15.827 |  |  |  |  |
| 7 | 327.4 | 0.400 0.698 17.942 |  | 379.6 | 0.157 0.243 15.920 |  |  |  |  |
| 8 | 362.1 | 0.236 1.032 18.539 |  | 414.0 | 0.087 0.380 17.412 |  |  |  |  |

Supplementary Table 18. Wave functions with definite projection of the total moment | mJ > for the lowest eight KDs of individual DyⅢ fragments for 1 and 1a using CASSCF/RASSI-SO with the OpenMolcas.

|  | E/cm−1 | wave functions |
| --- | --- | --- |
| 1_Dy1 | 0.0 | 90.7%¦±15/2> |
|  | 31.0 | 59.0%¦±13/2>+11.0%¦±11/2>+9.4%¦±9/2>+6.2%¦±5/2> |
| 1_Dy2 | 0.0 | 78.1%¦±15/2>+12.6%¦±11/2> |
|  | 48.1 | 23.8%¦±13/2>+22.6%¦±9/2>+16.7%¦±5/2>+11.0%¦±1/2> |
| 1_Dy3 | 0.0 | 89.3%¦±15/2> |
|  | 52.0 | 14.2%¦±13/2>+24.3%¦±9/2>+12.7%¦±7/2>+14.2%¦±5/2>+10.3%¦±3/2>+12.4%¦±1/2> |
| 1_Dy4 | 0.0 | 93.8%¦±15/2> |
|  | 27.2 | 11.1%¦±13/2>+18.5%¦±11/2>+18.8%¦±9/2>+13.0%¦±7/2>+12.7%¦±5/2>+11.2%¦±3/2> |
| 1a_Dy1 | 0.0 | 82.8%¦±15/2>+13.1%¦±11/2> |
|  | 47.6 | 14.2%¦±13/2>+31.5%¦±9/2>+15.7%¦±7/2>+16.5%¦±5/2>+8.3%¦±11/2> |
| 1a_Dy2 | 0.0 | 65.3%¦±15/2>+19.3%¦±11/2>+6.1%¦±7/2> |
|  | 38.0 | 10.4%¦±15/2>+36.9%¦±13/2>+20.2%¦±9/2>+13.6%¦±5/2>+9.5%¦±1/2> |
| 1a_Dy3 | 0.0 | 90.1%¦±15/2>+5.5%¦±11/2> |
|  | 59.3 | 35.1%¦±13/2>+17.4%¦±11/2>+22.9%¦±9/2>+7.1%¦±5/2>+5.7%¦±3/2> |
| 1a_Dy4 | 0.0 | 81.5%¦±15/2>+10.9%¦±11/2> |
|  | 17.5 | 22.8%¦±13/2>+13.3%¦±11/2>+30.1%¦±9/2>+11.3%¦±7/2>+9.2%¦±5/2>+8.1%¦±15/2> |

Supplementary Table 19. Exchange energies E (cm−1), the energy differences between each exchange doublet Δt (cm−1) and the main values of the gz for the lowest 8 and 24 exchange doublets arising from the exchange interactions on magnetic centers 1 and 1a, respectively.

|  | 1 |  |  |
| --- | --- | --- | --- |
| Exchange doublets | E | Δt | gz |
| 0 | 0.000000000000 | 5.804×10−5 | 11.352 |
|  | 0.000058040242 |  |  |
| 1 | 0.064846180120 | 1.561×10−5 | 17.016 |
|  | 0.064861792418 |  |  |
| 2 | 0.260623200251 | 2.285×10−5 | 28.100 |
|  | 0.260646045784 |  |  |
| 3 | 0.420659441243 | 9.976×10−4 | 26.947 |
|  | 0.421657051588 |  |  |
| 4 | 0.425802215259 | 5.417×10−4 | 26.066 |
|  | 0.426343873568 |  |  |
| 5 | 0.437666535482 | 1.378×10−3 | 34.471 |
|  | 0.439044767528 |  |  |
| 6 | 0.640913056419 | 8.973×10−5 | 42.536 |
|  | 0.641002786104 |  |  |
| 7 | 1.589310199493 | 9.302×10−6 | 65.627 |
|  | 1.589319501063 |  |  |
|  | 1a |  |  |
| Exchange doublets | E | Δt | gz |
| 0 | 0.000000000000 | 3.277×10−6 | 11.712 |
|  | 0.000003276751 |  |  |
| 1 | 0.027868199111 | 1.821×10−6 | 13.551 |
|  | 0.027870020199 |  |  |
| 2 | 0.104006823686 | 8.675×10−6 | 16.301 |
|  | 0.104007691234 |  |  |
| 3 | 0.379884934887 | 4.500×10−5 | 26.569 |
|  | 0.379929934965 |  |  |
| 4 | 0.431200347324 | 3.600×10−4 | 11.853 |
|  | 0.431560395086 |  |  |
| 5 | 0.452857782795 | 3.387×10−4 | 14.020 |
|  | 0.453196490021 |  |  |
| 6 | 0.544761314967 | 1.235×10−4 | 24.692 |
|  | 0.544884808440 |  |  |
| 7 | 0.553642492272 | 2.338×10−4 | 26.011 |
|  | 0.553876295764 |  |  |
| 8 | 0.560923826581 | 3.154×10−4 | 15.935 |
|  | 0.561239213967 |  |  |
| 9 | 0.693102329412 | 4.318×10−6 | 42.631 |
|  | 0.693106647216 |  |  |
| 10 | 0.838492857810 | 2.600×10−4 | 29.857 |
|  | 0.838752859259 |  |  |
| 11 | 0.891227891178 | 3.785×10−5 | 11.885 |
|  | 0.891265744021 |  |  |
| 12 | 0.915645225560 | 4.771×10−5 | 13.522 |
|  | 0.915692935923 |  |  |
| 13 | 0.980974091295 | 9.521×10−4 | 29.439 |
|  | 0.981926216136 |  |  |
| 14 | 0.991931351610 | 8.509×10−4 | 32.147 |
|  | 0.992782201925 |  |  |
| 15 | 1.006676713324 | 6.712×10−5 | 20.032 |
|  | 1.006743836528 |  |  |
| 16 | 1.139376293414 | 2.291×10−4 | 40.470 |
|  | 1.139605344121 |  |  |
| 17 | 1.287337990864 | 8.285×10−7 | 34.675 |
|  | 1.287338819317 |  |  |
| 18 | 1.416658910093 | 1.656×10−6 | 38.725 |
|  | 1.416660565726 |  |  |
| 19 | 1.431330751871 | 9.169×10−7 | 39.358 |
|  | 1.431331668784 |  |  |
| 20 | 1.586636957075 | 9.106×10−7 | 38.550 |
|  | 1.586637867628 |  |  |
| 21 | 1.982512644841 | 6.093×10−8 | 63.000 |
|  | 1.982512705770 |  |  |
| 22 | 2.424701662233 | 1.314×10−5 | 66.550 |
|  | 2.424714802982 |  |  |
| 23 | 2.868837973922 | 3.745×10−8 | 69.980 |
|  | 2.868838011369 |  |  |

Supplementary References

- Galván, I. F.; Vacher, M.; Alavi, A.; Angeli, C.; Aquilante, F.; Autschbach, J.; Bao, J. J.; Bokarev, S. I.; Bogdanov, N. A.; Carlson, R. K.; Chibotaru, L. F.; Creutzberg, J.; Dattani, N.; Delcey, M. G.; Dong, S. S.; Dreuw, A.; Freitag, L.; Frutos, L. M.; Gagliardi, L.; Gendron, F.; Giussani, A.; González, L.; Grell, G.; Guo, M. Y.; Hoyer, C. E.; Johansson, M.; Keller, S.; Knecht, S.; Kovacevic, G.; Källman, E.; Manni, G. L.; Lundberg, M.; Ma, Y. J.; Mai, S.; Malhado, J. P.; Malmqvist, P. Å.; Marquetand, P.; Mewes, S. A.; Norell, J.; Olivucci, M.; Oppel, M.; Phung, Q. M.; Pierloot, K.; Plasser, F.; Reiher, M.; Sand, A. M.; Schapiro, I.; Sharma, P.; Stein, C. J.; Sørensen, L. K.; Truhlar, D. G.; Ugandi, M.; Ungur, L.; Valentini, A.; Vancoillie, S.; Veryazov, V.; Weser, O.; Wesołowski, T. A.; Widmark, Per-Olof.; Wouters, S.; Zech, A.; Zobel, J. P.; Lindh. R. J. Chem. Theory Comput. 15, 5925–5964 (2019).

- Chibotaru, L. F.; Ungur, L.; Soncini, A. Angew. Chem., Int. Ed. 47, 4126–4129 (2008).

- Ungur, L.; Van den Heuvel, W.; Chibotaru, L. F. New J. Chem. 33, 1224–1230 (2009).

- Chibotaru, L. F.; Ungur, L.; Aronica, C.; Elmoll, H.; Pilet, G.; Luneau, D. J. Am. Chem. Soc. 130, 12445–12455 (2008).

- Lines, M. E. J. Chem. Phys. 55, 2977−2984 (1971).

- Mondal, K. C.; Sundt, A.; Lan, Y. H.; Kostakis, G. E.; Waldmann, O.; Ungur, L.; Chibotaru, L. F.; Anson, C. E.; Powell, A. K. Angew. Chem., Int. Ed. 51, 7550−7554 (2012).

- Langley, S. K.; Wielechowski, D. P.; Vieru, V.; Chilton, N. F.; Moubaraki, B.; Abrahams, B. F.; Chibotaru, L. F.; Murray, K. S. Angew. Chem., Int. Ed. 52, 12014–12019 (2013).