Supplementary materials

Figure S1 Thermogravimetric curves of DA-HA and HA

Figure S2 DA-HA and HA photoelectron spectra

Table S1 The heat loss rate of HA and DA-HA

| Sample |  | Initial temperature /℃ | Weight loss /% |
| --- | --- | --- | --- |
| HA | First heat loss | 56.74 | 15.52 |
|  | Second heat loss | 241.74 | 59.36 |
| DA-HA | First heat loss | 67.93 | 7.629 |
|  | Second heat loss | 212.18 | 62.52 |

Table S2 Oil-water interfacial tension at different concentrations of DA-HA

| C（mg/mL） | γDA-HA-white oil（mN/m） | γwater-white oil（mN/m） |
| --- | --- | --- |
| 10 | 36.59±1.63 | 45.70±1.09 |
| 5 | 39.09±1.55 |  |
| 2.5 | 39.81±2.31 |  |
| 1 | 42.05±1.41 |  |