Carboxymethyl-imidazolium O-vanillin Schiff base grafted into NH2-tagged MIL-101 (Cr) for effective removal of cupric ions from aqueous effluents

Moustafa A. Rizk a, Rana Yahya b, Raiedhah A. Alsaiari a,*, Mabkhoot A. Alsaiari a, Ahmed Shahat c, Reda F. M. Elshaarawy,c,d,*

a Department of Chemistry, Faculty of Science and Arts at Sharurah, Najran University, Sharurah 68342, Saudi Arabia.

b University of Jeddah, College of Science, Department of Chemistry, Jeddah, Saudi Arabia. E-mail: Ryahiya@uj.edu.sa

c   Department of Chemistry, Faculty of Science, Suez University, 43533 Suez, Egypt.

d  Institut für Anorganische Chemie und Strukturchemie, Heinrich-Heine Universität Düsseldorf, Düsseldorf, Germany.

* Corresponding authors

Email: reda.elshaarawy@suezuniv.edu.eg; raalsayari@nu.edu.sa

- Chemicals

Chemicals were utilized just as they were provided, include 2-aminophthalic acid (NH2-H2BDC), O-vanillin (Sigma-aldrich Co., Germany), ZnCl2, , Cr(NO3)3·9H2O and CuCl2.2H2O  (Merk KGaA Co., Germany).

- Characterization

Melting points were measured using a BÜCHI melting point B-540 apparatus; all melting points were measured in open glass capillaries and are uncorrected. FT-IR spectra were recorded on a BRUKER Tensor-37 FTIR spectrophotometer in the range of 400–4000 cm–1 as KBr disc with 2 cm–1 resolution. For signal intensities the following abbreviations were used: br (broad), sh (sharp), w (weak), m (medium), s (strong), vs (very strong).NMR-spectra were obtained with a BrukerAvance DRX200 (200 MHz for 1H) or BrukerAvanceDRX500 (125MHz for 13C) spectrometer with calibration to the residual proton solvent signal in DMSO-d6 (1H NMR: 2.52 ppm, 13C NMR: 39.5 ppm), CDCl3 (1H NMR: 7.26 ppm, 13C NMR: 77.16 ppm) against TMS (δ = 0.00 ppm) for 1H and 13C. Multiplicities of the signals were specified ass (singlet), d (doublet), t (triplet), q (quartet) or m (multiplet). The mass spectra of the synthesized compounds were acquired in the linear mode for positive ions on UHR-QTOF maXis 4G (BrukerDaltonics) and Bruker Ultraflex MALDI-TOF instrument equipped with a 337 nm nitrogen laser pulsing at a repetition rate of 10 Hz. The 2+ charge assignment of ions in ESI-MS was confirmed by the m/z = 0.5 difference between the isotope peaks (x, x+1, x+2). Peaks with chlorine showed the isotope ratio 35/37Cl = 75.8:24.2. For the mass spectral assignment: Peaks are based on 12C with 12.0000 Da and 35Cl with 34.968 Da. The XRD powder forms have been plotted on an Fe-filtered PAN analytical X'PERT PRO instrument CuK radiation (λ=1.5406 Å) 2θ from 5 to 50° and a temporal scanning of 0.3 second. UV-Visible spectra have been noted by using (HACH LANGE DR5000) UV-Vis spectrophotometry instrument. N2 adsorption and desorption behaviors have been measured at liquid nitrogen's boiling point (-196°C) on ASAP 2020 (Micrometrics, USA). The sample was prepared by subject to vacuum (5×10−3 torr) at 200oC in order to ensure a clean surface. The Brunauer-Emmett-Teller (BET) was measured using Brunauer-Emmett-Teller (BET) surface area and Barrett-Joyner-Halenda (BJH) pore volumes were measured. Scanning electron microscope (SEM) was carried on JEOL-JSM-6510 LV.

  - Synthesis of H2N-MIL-101(Cr)

A mild solvothermal process was used to prepare NH2-MIL-101(Cr) [1]. Slowly add 3.2 g of Cr(NO3)3·9H2O and 1.44 g of 2-aminoterephthalic acid to a 60 mL H2O solution with 0.8 g NaOH. After stirring at room temperature for 30 minutes, the mixture was transferred into a 100 mL Teflon-lined stainless-steel autoclave and kept at 150 ◦C for 12 hours. The mixture, following natural cooling, was collected by centrifugation at 7000 rpm for 2 min. The green powder was rinsed multiple times with water, DMF, and methanol, then dried overnight at 100 ◦C. Next, we obtained the activated NH2-MIL-101(Cr).

Table S1: Linear and non-linear mathematical formula for the adsorption isotherms and kinetic models used in this work (Experimental conditions: MILSB dose = 1.0 mg/mL, pH = 6, contact time = 45 min, T = 303 K)

| Model | Linear formula | Non-linear formula |
| --- | --- | --- |
| Langmuir isotherm a | 1qe =1qmax+1qmaxbCe Eq. 3 | qe =qmaxbCe(1+ bCe) Eq. 4 |
| Freundlich isotherm b | logqe=logKf+1nlogCe Eq. 5 | qe = KfCe1n Eq. 6 |
| Sips isotherm c | ln(qeqmax-qe)=lnKS+1nslnCe Eq. 7 | qe =qmax(KsCe)1nS(1+ (KsCe)1nS) Eq. 8 |
| Pseudo-1st-order kinetic d | log (qe- qt)=logqe+k1 t2.303 Eq. 9 | qt=qe(1-e-k1t) Eq. 10 |
| Pseudo-2nd-order kinetic d | tqt=1k2qe2 +tqe Eq. 11 | qt=qe2k2t1+k2qe2t Eq. 12 |
| Intraparticle diffusion kineticd | qt=kidt1/2+C Eq. 13 |  |

[1] X. Li, Y. Pi, Q. Xia, Z. Li, J. Xiao, TiO2 encapsulated in Salicylaldehyde-NH2-MIL-101 (Cr) for enhanced visible light-driven photodegradation of MB, Applied Catalysis B: Environmental 191 (2016) 192-201.