Supplementary Information

One-pot synthesis of high-capacity silicon-lithium anodes via on-copper growth of a semi-conducting, porous polymer

Jieyang Huang1, Andréa Martin1, Anna Urbanski2, Ranjit Kulkarni1, Patrick Amsalem3, Moritz Exner1, Johannes Müller3, David Burmeister1, Norbert Koch3,4, Nicola Pinna1, Petra Uhlmann2, Michael J. Bojdys*,1,5

1 Institut für Chemie and IRIS Adlershof, Humboldt-Universität zu Berlin, Brook-Taylor-Str. 2, 12489 Berlin, Germany.
2 Leibniz-Institut für Polymerforschung Dresden (IPF) e. V., Institut für Physikalische Chemie and Physik der Polymere, 01069 Dresden, Germany.
3 Institut für Physik and IRIS Adlershof, Humboldt-Universität zu Berlin, Brook-Taylor-Str. 2, 12489 Berlin, Germany.

4 Helmholtz-Zentrum Berlin GmbH, Albert-Einstein-Str. 15, 12489 Berlin, Germany
5 Department of Chemistry, King's College London, Britannia House Guy's Campus, 7 Trinity Street, London, SE1 1DB, UK.

Corresponding Author

e-mail: m.j.bojdys.02@cantab.net

Contents

S1 EXPERIMENTAL SECTION	4

S1.1 Materials	4

S1.2 Synthesis of 2, 4, 6-tris(4-bromophenyl)-1, 3, 5-triazine (1)	5

S1.3 Synthesis of 2,4,6-tris(4-[(trimethylsilyl)ethynyl]phenyl)-1,3,5-triazine (2)	5

S1.4 Synthesis of 2,4,6-tris(4-ethynylphenyl)-1,3,5-triazine (3)	6

S1.5 Method 1 for the preparation of triazine-based graphdiyene/silicon nano-particles electrodes, TzG/Si@Cu (TzG/Si = 25/75 wt%)	6

S1.6 Method 1 for the preparation of triazine-based graphdiyene/silicon nano-particles/carbon black electrodes, TzG/Si/CB@Cu (TzG/Si/CB = 20/60/20 wt%)	9

S1.7 Method 2 for the preparation the triazine-based graphdiyene/silicon nano-particles electrodes, TzG/Si@Cu (TzG/Si = 25/75 wt%)	9

S1.8 Method 3 for the preparation of triazine-based graphdiyene/silicon nano-particles electrodes, TzG/Si@Cu (TzG/Si = 25/75 wt%)	11

S1.9 Electrochemical testing methods	12

S1.10 Characterization methods	14

S2 RESULTS AND DISCUSSION	17

S2.1 Characterization of TzG/Si@Cu and of its components (TzG and Si NPs)	17

S2.2 Conductivity measurements and cyclic voltammetry of the electrode systems	21

S2.3 Study of the SEI formation on TzG/Si@Cu by XPS, SEM and TEM	23

S2.4 Electrochemical performance of TzG/Si-type electrodes, and evaluation of their density and the mass loading	33

S2.5 Optimization of the preparation of the TzG/Si@Cu electrodes (method 2 and method 3) and their performances	39

REFERENCES	49

# S1 EXPERIMENTAL SECTION

## S1.1 Materials

All chemicals and solvents were used as received without any further purification. Conversion of organic reagents was monitored by TLC using silica gel-covered aluminum plates (Merck 60, F-254) and visualized by UV detection (λ = 254 nm). Purification by column chromatography was performed using silica gel (0.063–0.2 mm, 100 mesh ASTM) from PENTA s.r.o. (Prague, CZ).

Trifluoromethanesulfonic acid (TFMSA), 4-bromobenzonitrile, and trimethylsilylacetylene were purchased from ABCR (Karlsruhe, Germany). Chloroform, copper (I) iodide, triethylamine (Et3N), tetrakis(triphenylphosphine)palladium(0) and K2CO3 were purchased from Sigma-Aldrich (Germany). Tetrahydrofuran (THF), NaOH, MgSO4 and dichloromethane (DCM) were purchased from Carl Roth GmbH (Karlsruhe, Germany).

Silicon nanoparticles (Si-NPs: purity 98+%, mean diameter 30-50 nm, laser synthesized) were purchased from US Research Nanomaterials (USA). Conductive carbon black (CB) powder (TIMCAL Super C65) was purchased from MTI Corporation (USA). Copper foil with a size of 2000 mm × 300 mm × 0.1 mm was purchased from MARKÉTA LUKÁČOVÁ (Prague, CZ). Copper foil with a size of 2000 mm × 150 mm × 0.025 mm was purchased from Goodfellow Cambridge Ltd.

The electrolyte mixture composed of 1.0 M lithium hexafluorophosphate (LiPF6) dissolved in ethylene carbonate (EC) and dimethyl carbonate (DMC), EC/DMC = 1:1 (v/v), battery grade, was purchased from Sigma Aldrich (Germany). Fluoroethylene carbonate (FEC) was purchased from Acros Organics (Germany).

## S1.2 Synthesis of 2, 4, 6-tris(4-bromophenyl)-1, 3, 5-triazine (1)

2, 4, 6-tris(4-bromophenyl)-1, 3, 5-triazine was synthesized with a modified method reported by Meyer et al.1 TFMSA (10 mL, 113 mmol) and 25 mL anhydrous chloroform were added into a 500 mL three-neck flask after argon purging. Under continuous stirring under and argon atmosphere, the solution was cooled down to 0 ℃, and subsequently, 4-bromobenzonitrile (10 g, 54.9 mmol) in 150 mL anhydrous chloroform was added dropwise. The mixture was stirred at 0 ℃ for 2 h and further stirred at ambient temperature for 24 h. The acidic mixture was neutralized with a NaOH aqueous solution and was filtered to obtain filter cake. The filter cake was further washed three times with water and 5 mL chloroform. After drying at 60 ℃ under vacuum overnight, 6.90 g (12.6 mmol for C21H12Br3N3, 69.0% yield) of 2, 4, 6-tris(4-bromophenyl)-1, 3, 5-triazine (1) was obtained as a white solid. 1H NMR (500 MHz, CDCl3): 8.54 (6H, d, J = 8.6 Hz), 7.65 (6H, d, J = 8.6 Hz).

## S1.3 Synthesis of 2,4,6-tris(4-[(trimethylsilyl)ethynyl]phenyl)-1,3,5-triazine (2)

2,4,6-tris(4-[(trimethylsilyl)ethynyl]phenyl)-1,3,5-triazine was synthesized with a modified Sonogashira protocol based on a report by Yam et al.2 Tetrakis(triphenylphosphine)palladium(0) (1.267 g, 1.10 mmol), copper(I) iodide (0.418 g, 2.20 mmol) and 1 (4 g, 7.33 mmol) were added into a 2 L three-neck flask after purged under argon. In a separate 1 L flask, triethylamine/THF (4:1 v/v, 640 mL) was degassed for 1 h and then added into the 2 L flask to dissolve the solid starting materials. Subsequently, trimethylsilylacetylene (6.68 mL, 48.3 mmol) was added into the mixture under argon, and the mixture was further degassed for 1 h. The mixture was stirred and refluxed for 24 h under argon. After volatile compounds were removed under vacuum, the crude product was purified by column chromatography on silica gel using hexane/toluene (12:1 v/v) as an eluent to give 3.86 g (6.56 mmol for C36H39N3Si3, 89.5% yield) of 2,4,6-tris(4-[(trimethylsilyl)ethynyl]phenyl)-1,3,5-triazine (2) as a white solid. 1H NMR (400 MHz, CDCl3): 8.68 (6H, d, J = 8.6 Hz), 7.66 (6H, d, J = 8.6 Hz), 0.33 (27H, s).

## S1.4 Synthesis of 2,4,6-tris(4-ethynylphenyl)-1,3,5-triazine (3)

In a 500 mL single-neck flask, K2CO3 (0.362 g, 2.62 mmol) and 2 (2.5 g, 4.18 mmol) were added into a solution of 15 mL methanol and 111 mL THF. After stirring at R.T. for 24 h, the mixture was washed with water and extracted with DCM. The organic phase was washed with a NaCl aqueous solution and then dried with MgSO4. After removing DCM, 1.51 g (3.96 mmol for C27H15N3, 94.7% yield) of 2,4,6-tris(4-ethynylphenyl)-1,3,5-triazine (3) was obtained as a pale-yellow solid. 1H NMR (400 MHz, CDCl3): 8.74 (6H, d, J = 8.6 Hz), 7.72 (6H, d, J = 8.5 Hz), 3.31 (3H, s). The synthetic route for monomer 3 was presented in Scheme S1.

Scheme S1. Synthetic route for monomer 2,4,6-tris(4-ethynylphenyl)-1,3,5-triazine (3)

## S1.5 Method 1 for the preparation of triazine-based graphdiyene/silicon nano-particles electrodes, TzG/Si@Cu (TzG/Si = 25/75 wt%)

The preparation procedure of the triazine-based graphdiyene/silicon nano-particles electrodes, TzG/Si@Cu (TzG/Si = 25/75 wt%) following method 1 is shown in Scheme S2. The Cu foil was cut into a square with dimensions of 160 mm × 160 mm and then folded into a cuboid boat with dimensions of 60 mm length, 60 mm width, and 50 mm height. The Cu boat was washed under ultrasonication in an aqueous solution of 1 M HCl for 10 min followed by a second wash using methanol for 10 min. After having wash, it three time with acetone, the Cu boat was placed into a desiccator and dried on the Schlenk line under vacuum. The desiccator was purged under argon twice and was kept under an argon atmosphere.

27.6 mg of Si-nanoparticles (NPs) was added into 160 mL of pyridine in a 250 mL single-neck flask. After stirring for 30 min and ultrasonic dispersion, the low viscosity dispersion of Si-NPs in pyridine was filled into the Cu boat. The desiccator was heated by an oil bath at 70 ℃ for 1 h. When the Si-NPs/pyridine dispersion reached 60 ℃ in the Cu boat, a solution of 9.2 mg monomer 3 dissolved in 10 mL of pyridine was added into the Cu boat for polymerization. A detailed synthetic route of monomer 3, (2,4,6-tris(4-ethynylphenyl)-1,3,5-triazine, is shown in Scheme S1). The temperature of the mixture was kept at 60 ℃ for 3 days. The desiccator as reaction vessel was protected under an argon atmosphere and was covered by a glass fiber cloth to maintain the temperature over the course of the reaction. During the reaction, pyridine was slowly evaporated and refluxed from the condenser. Evaporated pyridine was gradually removed from the Cu boat and connected at the bottom of the desiccator.

After a 3-day reaction, the product inside the Cu boat was completely dry. The brown material (TzG/Si) grows predominantly at the bottom of the Cu boat and partially on the walls of the Cu boat. The Cu boat was immersed in water, DMF, and acetone for 5 min each to remove the unreacted residuals. After drying under vacuum at 120 ℃ overnight, the TzG/Si@Cu preparation was punched out from the bottom of the Cu boat into circular electrodes with a diameter of 10 mm. The resulting mass composition of TzG/Si was 25/75 wt%.

NOTE: The control electrode TzG@Cu was prepared using a variation of method 1 described here that leaves out Si NPs from the reaction mixture.

Scheme S2. Preparation the TzG/Si@Cu (TzG/Si = 25/75 wt%) electrodes following method 1.

## S1.6 Method 1 for the preparation of triazine-based graphdiyene/silicon nano-particles/carbon black electrodes, TzG/Si/CB@Cu (TzG/Si/CB = 20/60/20 wt%)

Carbon black (CB) is a common conductive additive in conventional electrode formulations to improve the electrical wiring between the active material and the current collector. TzG/Si/CB@Cu was prepared following a modified method 1 with the addition of 9.2 mg of CB into the Si NPs/pyridine reaction mixture prior to the ultrasonic bath treatment. The resulting mass composition of TzG/Si/CB is 20/60/20 wt%.

## S1.7 Method 2 for the preparation the triazine-based graphdiyene/silicon nano-particles electrodes, TzG/Si@Cu (TzG/Si = 25/75 wt%)

The preparation procedure of the triazine-based graphdiyene/silicon nano-particles electrodes, TzG/Si@Cu (TzG/Si = 25/75 wt%), following method 2 is shown in Scheme S3. A 25 μm thick Cu foil was cut into a square with dimensions of 150 mm × 150 mm and then spread out on a 210 mm × 210 mm × 0.4 cm stainless steel plate, which was placed on an IKA® heater. 27 mg of Si NPs and 9 mg of the monomer 3 were dispersed/dissolved in 1 mL of pyridine. The reaction mixture was transferred into a 3 mL vial. After stirring the mixture for 1 min and ultrasonic dispersion for 1 h. The resulting slurry was cast onto the prepared Cu foil, and the entire set-up was covered with a desiccator lid to maintain the pyridine vapor atmosphere during the polymerization reaction. The experiment set-up was heated to 60 °C and kept for 1 h at this temperature. Subsequently, the lid was removed, and the heater was set at 120 °C in order to remove the solvent from the preparation. As a result, a stable brown film (TzG/Si) was obtained on top of the Cu foil. After drying under vacuum at 120 ℃ overnight, TzG/Si@Cu preparation was punched out as disks of 18 mm diameter. The resulting mass composition of TzG/Si was 25/75 wt%.

Scheme S3. Preparation of theTzG/Si@Cu (TzG/Si = 25/75 wt%) electrodes following method 2.

## S1.8 Method 3 for the preparation of triazine-based graphdiyene/silicon nano-particles electrodes, TzG/Si@Cu (TzG/Si = 25/75 wt%)

The preparation procedure for the triazine-based graphdiyene/silicon nano-particles electrodes, TzG/Si@Cu (TzG/Si = 25/75 wt%) following method 3 is shown in Scheme S4. A 25 μm thick Cu foil was indented using a cylinder mold with a 20 mm diameter (and a 3 mm height). The cylindrical perforations in the Cu foil have a volume of 0.94 mL. 14 of these indented Cu foils were placed on a 210 mm × 210 mm × 0.4 cm stainless steel plate set on an IKA® heater. Two different concentrations of Si NPs/monomer 3 were used for control experiments, a) 36 mg/12 mg in 3 mL of pyridine and b) 72 mg/24 mg in 3 mL of pyridine. The reaction mixture was stirred for 1 min and dispersed for 1 h. 0.2 mL of the resulting slurries were introduced into each indentation on the Cu foil. The entire reaction set-up was covered with a desiccator lid to maintain the pyridine vapor atmosphere during the polymerization reaction. The metallic plate was heated up to 60 °C and kept for 1 h at this temperature. Subsequently, the lid was removed, and the heater was set to 120 °C in order to evaporate off the excess solvent from the preparation. A stable brown film (TzG/Si) was obtained on the inner surface of the indented Cu foils. After drying under vacuum at 120 ℃ overnight, the TzG/Si@Cu preparation following method 3 was punched into electrodes of 18 mm diameter. The resulting mass composition of TzG/Si was 25/75 wt%.

Scheme S4. Preparation the TzG/Si@Cu (TzG/Si = 25/75 wt%) electrodes following method 3.

## S1.9 Electrochemical testing methods

Half-cell testing of TzG/Si@Cu, TzG/Si/CB@Cu and TzG@Cu prepared following method 1

The electrochemical properties of the TzG/Si@Cu, TzG/Si/CB@Cu, and TzG@Cu electrodes prepared following method 1 were carried out using Swagelok cells (Swagelok, Germany), which were assembled in a glove box under an argon atmosphere (H2O ≤ 1 ppm, O2 ≤ 1 ppm). Prior to the cell assembly, the TzG/Si@Cu electrodes were dried again under vacuum at 100 ℃ and then transferred into a glove box. A lithium metal circular disk was used as the counter and reference electrode for the half-cell setup. Two circular disks of Whatman membranes (Fiberglass, Grade GF/D, Whatman, USA) with a diameter of 10.5 mm were used as separators. The electrolyte composition for battery testing was 1 M LiPF6 in EC/DMC = 1:1 (v/v) with 10 wt% of FEC and 250 μL of this electrolyte was used each Swagelok setup.

Cyclic voltammetry (CV) measurements were measured on an IVIUM-n-Stat, IVIUM potentiostat within a 0.01 V and 1.5 V (vs. Li/ Li+) potential window, with a scan rate of 0.1 mV s-1. The cyclic voltammetry (CV) was measured with a constant potential sweep rate (IVIUM-n-Stat, IVIUM). The starting voltage of the CV measurements was 1.5 V, and the potential range was between 0.01 V and 1.5 V (vs. Li/ Li+). The sweeping rate was 0.1 mV s-1.

Galvanostatic charge-discharge cycling with potential limitation (GCPL) was evaluated by a BST8-MA Multichannel Battery Analyzer (MTI Corporation, USA) using the constant current mode within a voltage range of 0.01-1.2 V (vs. Li/ Li+). All the current densities were calculated on the weighted mass of silicon. The actual weight of the electrode materials on Cu was evaluated by an analytical balance with an accuracy of +/-0.01 mg.

TzG/Si@Cu electrodes prepared following method 2 and method 3 for half-cell testing

The electrochemical properties of the samples were carried out using coin cells made of stainless steel 304. The electrodes were dried in a glass chamber (BÜCHI) under vacuum at 120 ℃ overnight to remove any possible traces of humidity and oxygen and then transferred into a glove box under an argon atmosphere (H2O ≤ 1 ppm, O2 ≤ 1 ppm). Circular disks of Whatman membranes (Fiberglass, Grade GF/D, Whatman, USA) were used as separators. Metallic lithium disks were used as counter- and reference-electrodes. The same electrolyte composition was used for the electrochemical test throughout, namely 1 M LiPF6 in EC/DMC = 1:1 (v/v) with 10 wt% of FEC. The coin cells were sealed by the mean of a mechanical press at 80 kg cm-2. GCPL experiments were evaluated on a CT2001A Battery Analyzer (Wuhan LAND Electronics Co.,Ltd., China) using the constant current mode within a voltage range of 0.01-1.2 V (vs. Li/ Li+). All the current densities are calculated on the weighted mass of silicon. The actual weight of electrode materials on Cu was evaluated by an analytical balance with an accuracy of +/-0.01 mg.

## S1.10 Characterization methods

Nuclear magnetic resonance (NMR) spectra of small molecules were recorded on a Bruker Advance 400 MHz / 500 MHz spectrometer. Chemical shifts (δ) were reported in ppm.

Solid-state NMR spectra were recorded on a Agilent DD2 600 Solid NMR System with 3.2 mm zirconia rotors, and samples were collected by scratching the materials out from the Cu surface. 13C cross‐polarization–magic‐angle‐spinning (CP–MAS) solid-state NMR experiments were carried out with a MAS rate of 18 kHz, a contact time of 10 ms, and a relaxation delay of 0.5 s. 29Si single–pulse–magic‐angle‐spinning (SP–MAS) solid-state NMR experiments were carried out with a MAS rate of 18 kHz, a contact time of 10 ms and a relaxation delay of 2 s. Chemical shifts (δ) were reported in ppm.

Fourier transform infrared (FT-IR) spectra were recorded from solid diluted in KBr pellets on a Thermo Scientific Nicolet iS5 spectrometer (Thermo Fisher Scientific, Waltham, MA, USA) in the wavenumber range of 4000-400 cm-1 with resolution of 4 cm-1.

Solid-state Raman spectra were recorded on a DXR Raman spectrometer (Thermo Scientific) equipped with a 532 nm laser for illumination. A 20× objective lens of an Olympus microscope was used to focus the laser beam on the sample. The raw spectrum was reported with a fluorescence background.

Scanning electron microscopy (SEM). The morphology, structure and elemental analysis of the electrodes were investigated using a scanning electron microscope (SEM, GeminiSEM 500, Carl Zeiss GmbH, Germany) operating at 15 kV acceleration voltage. The electrodes were examined in plain view and in cross section geometries. To reduce charging effects from the electron beam, the cross-section samples were sputtered with approximately 10 nm of carbon (Sputter Coater MED 010, Balzers Union Limited, Liechtenstein).

Transmission electron microscopy (TEM) images were recorded using a TEM Libra120 (Carl Zeiss Microscopy GmbH, Oberkochen, Germany) equipped with an omega-type energy filter and operated at 120 kV. The elemental distribution was determined from energy-filtered images by a 3-window method. High-resolution (HR) TEM images were recorded on a Philips CM 200 microscope equipped with a LaB6 cathode and operated at 200 kV.

X-ray photoelectron spectroscopy (XPS) measurements were performed in an ultra-high vacuum setup (base pressure 5×10-5 mbar) equipped with a Jeol JPS-9030 hemispherical energy analyzer and a monochromated Al Kα (1486.6 eV) source. The energy resolution as determined from the full-width half-maximum of the Ag3d5/2 of a clean polycrystalline silver substrate was 0.9 eV. For ex-situ experiments of the electrodes, the samples were transferred into the XPS setup in a N2 filled container and evacuated in the load-lock chamber of the vacuum system. Therefore, the samples were not exposed to air prior to XPS measurements. The core level signals were fitted using Voigt peaks (Gaussian/Lorentzian) and a non-linear Shirley-type background. Energy scale and binding energy of the spectrometer were calibrated with Cu(0) at the binding energies of Cu 2p 3/2 (933 eV), with C (sp2) at binding energies of C 1s spectrum at 284.3 eV or with C-O at the binding energies of C 1s spectrum at 286.5 eV, based on specific spectra conditions.

XPS spectra fitting method: (i) For neat compound or specific chemical environment, an identical full width at half maximum (FWHM) was adopted for peak-fitting in each spectrum. Si 2p signals were fit into two spaced spin-orbit components (Si 2p1/2 and Si 2p3/2 with ΔBE = 0.63eV, area ratio = 1:2). (ii) for mixtures containing uncertain quantity of neat compounds or specific chemical environments, e.g. SiOx, LixPFyOz, SiOxFy, LixSi, LixSiOy, no constrain were applied on the full width at FWHM in order to deliver correct information without over-interpreting the spectra.

Conductivity measurements. To evaluate the conductivity of the electrode materials, a gold top electrode was deposited by physical vapor deposition (PVD). The deposited electrodes (90 µm × 90 µm, 100 nm thickness) were contacted with an Imina mibot micromanipulator, equipped with a 500 nm tungsten needle. The IV characterization was conducted at 20 °C in a two-wire measurement using a Keithley 4200A SCS Parameter Analyzer equipped with a 4200-SMU module. To access the resistance, a linear fit of the IV curve was calculated. The inverse of the slope of the fit function corresponds to the resistance.

# S2 RESULTS AND DISCUSSION

## S2.1 Characterization of TzG/Si@Cu and of its components (TzG and Si NPs)

Figure S1. 29Si SP-MAS solid-state NMR spectrum of TzG/Si@Cu. NOTE: some Si surface structures such as SiOx, -Si(-OH)x and -Si-(OSi)x also influence the main broad signal of bulk Si, which is difficult to resolve clearly.3

Figure S2. FT-IR spectra of Si NPs and TzG/Si@Cu prepared following method 1.

Figure S3. XPS spectra with molar ratio: a, C 1s spectrum and b, Si 2p spectrum of TzG/Si@Cu prepared following method 1; c, C 1s spectrum and d, Si 2p spectrum of pristine Si NPs. Note: the inhomogeneous thickness of semi-conductive Si NPs on sample holder of carbon tape contribute to corresponding inhomogeneous binding energy shifts, resulting average and broad signals in c and d; the C-O and C-C signals in carbon tape inevitably overlap with C 1s signals of Si-surfactant in c.

Figure S3, respective C 1s and S 2p spectra obtained from the TzG/Si@Cu. The C 1s spectrum was fitted with four components at binding energies of 287.9 eV, 286.0 eV, 284.3°eV, and 283.8 eV. The environment at 283.8 eV is carbon in termina Si-CH3 of Si NPs surfactant.4 The environment at 287.9 eV has been assigned to sp2 carbons in the triazine (C3N3) ring, while that at 286.0 eV has been assigned to terminal sp carbons in C≡C bridges.5,6 The environment at 284.3 eV is typical of graphitic sp2 carbons that are part of TzG, or of adventitious carbon contamination commonly seen on surfaces by XPS.7 Integration of peak intensities from the C 1s region suggest a molar ratio of sp2 carbons in the triazine (C3N3) ring of 0.61 (calculated 1), sp carbons of 2.0 (calculated 2), and sp2 carbons in the polymer backbone of 6.4 (calculated 6) (Figure S3a). XPS peak positions and relative composition is consistent with the other analyses presented here and in previous reports for neat TzG polymer.8

The Si 2p spectrum of TzG/Si@Cu was fitted with three components at binding energies of 98.3 eV, 99.0 eV and 102.1 eV (Figure S3b). The peak at 98.3 eV stems from Si 2p3/2 and the one at 99.0 eV from Si 2p1/2 of elemental Si.9,10 The peak at 102.1 eV corresponds to silicon oxide SiOx environments.11-13 The molar ratio from peak integration is 34% SiOx and 66% elemental Si in TzG/Si@Cu, compared to as-received Si NPs that contain 21% of SiOx and 79% of Si(0) environments. Apparent differences in relative composition between embedded and as-received Si NPs can be attributed to the surface sensitivity of XPS.

Figure S4. Cross-section SEM image of the pristine TzG/Si@Cu (TzG/Si = 25/75 wt%) electrodes prepared following method 1 embedded into a resin (to achieve clear SEM image, the sample was sputtered by carbon in order to increase the conductivity due to the insulating character of the resin).

Figure S5. TEM images of a, the TzG@Cu electrodes prepared following method 1; b, pristine Si NPs.

## S2.2 Conductivity measurements and cyclic voltammetry of the electrode systems

Electrodes prepared following method 1, with and without conductive additive, were subject to the following conductivity measurements. A plot of current vs. voltage shows that the pristine TzG/Si@Cu electrodes have a low electric conductivity of 0.0664 μS cm-1 (Figure S6). This value is more than three magnitudes lower than that of TzG/Si/CB@Cu, and also lower than values reported for commercial, conductive binders.14 Comparing TzG/Si@Cu with TzG/Si/CB@Cu during cyclic voltammetry (CV) tests, we find no significant difference in current densities over the cathodic and anodic sweeps (Figure S7). The excellent performances of TzG/Si@Cu are surprising since a good initial conductivity of electrodes before electrochemical testing is thought to be a primordial factor for good electrochemical performances. In the first cathodic scan, we observe (i) a narrow wave centred at 0.1 V (vs. Li/Li+) attributed to the alloying reaction between lithium and silicon, and (ii) an intense reduction wave across the entire range of the scan attributed to SEI formation. The broad feature disappears in the second cathodic scan, indicating that the formation of a stable SEI is completed. In the first anodic scan, the typical anodic peaks at 0.33 and 0.51 V (vs. Li/Li+) are attributed to delithiation of different, amorphous LixSi phases. In the second cathodic scan, the cathodic peak at 0.14 V (vs. Li/Li+) is ascribed to the lithiation of amorphous Si, which results from the conversion of crystalline Si during the first cycle.15,16 Si is active within 0.01-1.2 V (vs. Li/Li+), and this voltage range is proper for half-cell cycling tests. CV measurements demonstrate that lithium ions can easily diffuse through the TzG polymer and then react with the Si NPs. The similarity of the voltammograms of TzG/Si@Cu and TzG/Si/CB@Cu (i.e. with and without conductive additive) suggests that the TzG polymer is chiefly responsible for the electron transport and lithium diffusion. The TzG polymer was also grown on copper without active material or conductive additive (TzG@Cu) to understand whether the material would participate in the overall capacity of the electrode or the SEI formation. In Figure S7c, the two initial CV curves of the sample TzG@Cu are compared. No obvious cathodic peak or anodic peak can be observed in the first cycle starting at 1.5 V, translating no faradic contribution of the TzG polymer to the capacity.

Figure S6. I-V curves of copper electrodes with a, TzG/Si@Cu and b, TzG/Si/CB@Cu prepared following method 1. Linear fits are shown as dashed lines, indicating resistances values for TzG/Si of 269.6 x 106 Ω and for TzG/Si/CB of 81.27 x 103 Ω. Material thicknesses measured by SEM of c, 14.5 μm for TzG/Si@Cu and of d, of 25 μm for TzG/Si/CB@Cu. Based on I-V curves and SEM thickness measurements, the calculated conductivity of TzG/Si is 0.0664 μS cm-1 and of TzG/Si/CB is 380 μS cm-1. NOTE: (i) calculations of the conductivity are subject to large uncertainty that stems from thickness estimations of the films by local SEM. However, they are accurate within one order of magnitude. (ii) The estimated thickness is subject to errors arising from the angle and distance at which SEM images were collected.

Figure S7. CV curves of the initial two cycles obtained at 0.1 mV s-1 in the range of 0.01-1.5 V (vs. Li/Li+) for the samples: a, TzG/Si@Cu; b, TzG/Si/CB@Cu; c, TzG@Cu prepared following method 1.

Moreover, when carbon black is added to the formulation of our electrodes, the resulting electrochemical performances are lower (Figure S13 and Figure S14). This could be explained by the growth of the TzG polymer onto the carbon black nanoparticles, effectively depleting the available volume of the TzG polymer for the embedding of the Si NPs, and thus diminishing the ability of the covalent organic framework to buffer the volume expansion of the silicon active material.

## S2.3 Study of the SEI formation on TzG/Si@Cu by XPS, SEM and TEM

We investigated the de-/lithiation and SEI formation processes in the TzG/Si@Cu and TzG@Cu systems during cycling by comparison of the pristine TzG/Si@Cu and TzG@Cu electrodes, and further samples recovered after the first lithiation, the first delithiation, and 100th delithiation in the case of the TzG/Si@Cu and TzG@Cu electrodes. During the galvanostatic charge/discharge experiments, we applied a constant current of 0.32 mA cm-2, corresponding to a current density of C/8 regarding the silicon specific capacity, within a 0.01-1.2 V (vs. Li/Li+) potential window.

The chemical composition of the electrode surface was probed to a depth of approx. 10 nm with X-ray photoelectron spectroscopy (XPS), and the relative molar concentrations of elements were calculated using peak fitting of XPS data recorded for the electrodes TzG@Cu, TzG/Si@Cu and TzG/Si/CB@Cu at different cycling stages (Figure S8, Figure S9, Figure S10 and Table S1).

To understand the electrochemical properties of the neat TzG, XPS C 1s and F 1s spectra of the TzG@Cu electrodes cycled at a constant current of 0.32 mA cm-2 within 0.01-1.2 V (vs. Li/Li+) were recorded (Figure S8a, b, c and Figure S9). Starting with the first lithiation cycle using the TzG@Cu electrode, we see overall low concentrations of lithium and of other elements originating from the electrolyte (F and P) that get deposited within the film with a sum total of up to 10.4 mol% (Table S1). No high binding energy (BE) peaks of C-F (C 1s >290 eV, F 1s >688 eV) or of Li2CO3 (C 1s >290 eV) can be observed from any of the components that are the decomposition products of the electrolyte during SEI formation.9-11,17-19 The absence of these signals means that there is no apparent SEI formation on TzG during lithiation. Carbon and nitrogen environments indicative of the neat TzG polymer backbone remain generally unaltered during de-/lithiation (C 1s spectra in Figure S8a, b and c). In the N 1s region, we observe a systematic shift of the peak attributed to nitrogen atoms in the triazine (C3N3) ring towards higher binding energies (Figure S8d). This shift indicates n-doping of the TzG polymer during the first lithiation cycle,20-22 and it is accompanied by an increase in conductivity of the TzG matrix as evidenced by the cycling performance of additive-free TzG/Si@Cu electrodes (Figure S7).

Comparing the XPS data sets from the C 1s region for TzG/Si@Cu in the pristine state, after the first lithiation, after the first delithiation, and after the 100th delithiation (Figure S10), we notice that carbon environments attributed to the TzG polymer are overlayed and attenuated by C 1s peaks corresponding to LiCO3, O=C-O and C-O (Figure S10a, ii-iv). These carbon environments correspond to the newly formed SEI that includes elements from the electrolyte mixture (LiPF6, EC, FEC and DMC).

Similar compositions of elements that constitute the SEI layer are present in the XPS data for the TzG/Si/CB@Cu electrode after the 100th delithiation (Figure S13). Here, we detect no peaks corresponding to TzG or CB in the C 1s region. There are numerous examples of the SEI occluding XPS signals that originate from the binder or from the Si active material in literature.9,10,12,23,24

XPS data from the Si 2p region of TzG/Si@Cu indicate that the SEI layer becomes stable at an early stage of cycling (Figure 2a). Comparing the XPS regions C 1s and F 1s of TzG@Cu (Figure S8 and Figure S9) with those of TzG/Si@Cu, we conclude that the SEI is formed only in the presence of Si NPs. In cycled TzG/Si@Cu electrodes, the SEI layer completely obfuscates signals originating from the TzG polymer, and it partially covers signals corresponding to Si NPs (Figure S10). Overall, the covalent backbone of the TzG polymer that encases Si NPs seems to limit the growth and the mechanical abrasion/reformation of the SEI layer that occurs during the volumetric expansion that accompanies the lithiation of Si NPs.

Cross-sectional SEM images of TzG/Si@Cu reveal a reversible change of the thickness of films during the first de-/lithiation cycle (Figure S11). TEM and SEM images show that even after 100 cycles the TzG polymer effectively accommodates the mechanical stress and strain caused by the volumetric expansion of Si. Raman spectroscopy provides further evidence that the TzG/Si composite retains its chemical integrity, as we continue to observe the stretching band of the phenyl subunits of the TzG polymer throughout the cycling processes (Figure S12).

Table S1. Relative molar concentrations of elements as determined by peak integration using X-ray photoelectron spectroscopy (XPS) data recorded at 1486.6 eV for TzG@Cu, TzG/Si@Cu and TzG/Si/CB@Cu electrodes. Electrodes were prepared following method 1, cycled at a constant current of 0.32 mA cm-2 (corresponding to a current density of C/8 regarding the silicon specific capacity, within a 0.01-1.2 V (vs. Li/Li+) potential window. ), and essayed at the indicated stages of de-/lithiation.

| Sample | Stage during cycling | C (%) | Si (%) | N (%) | O (%) | Li (%) | F (%) | P (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TzG@Cu | pristine | 78.2 | 0.00 | 8.87 | 12.9 | 0.00 | 0.00 | 0.00 |
| TzG@Cu | 1st lithiation | 69.8 | 0.00 | 7.60 | 11.3 | 2.81 | 7.38 | 1.15 |
| TzG@Cu | 1st delithiation | 69.0 | 0.00 | 6.67 | 14.8 | 2.65 | 5.95 | 0.92 |
| TzG/Si@Cu | pristine | 17.8 | 40.8 | 2.17 | 39.3 | 0.00 | 0.00 | 0.00 |
| TzG/Si@Cu | 1st lithiation | 23.0 | 1.90 | 0.65 | 28.2 | 28.1 | 15.8 | 2.36 |
| TzG/Si@Cu | 1st delithiation | 29.4 | 1.71 | 0.16 | 27.3 | 22.4 | 17.8 | 1.24 |
| TzG/Si@Cu | 100th delithiation | 44.5 | 0.84 | 0.00 | 32.0 | 15.9 | 6.31 | 0.44 |
| TzG/Si/CB@Cu | pristine | 51.1 | 20.9 | 3.79 | 24.2 | 0.00 | 0.00 | 0.00 |
| TzG/Si/CB@Cu | 100th delithiation | 46.7 | 0.69 | 0.00 | 26.9 | 18.3 | 6.97 | 0.45 |

Figure S8. XPS spectra of the TzG@Cu electrodes prepared following method 1 cycled at a constant current of 0.32 mA cm-2 within 0.01-1.2 V vs. Li/Li+: a, C 1s spectrum of the pristine electrode; b, C 1s spectrum of the electrode after the first lithiation; c, C 1s spectrum of the electrode after the first delithiation; d, overlay of the N 1s spectra of the pristine electrode, of the electrode after the first lithiation and of the electrode after the first delithiation.

Figure S9. XPS spectra showing the F 1s region a, after the first lithiation and b, after the first delithiation for the TzG@Cu electrode prepared following method 1. The electrodes were cycled at a constant current of 0.32 mA cm-2 within 0.01-1.2 V vs. Li/Li+.

Figure S10. XPS spectra showing a, the C 1s region, b, the F 1s region, and c, the Li 1s region of the TzG/Si@Cu electrode prepared following method 1 (i) in the pristine state, (ii) after the first lithiation, (iii) after the first delithiation, and (iv) after the 100th delithiation cycled at 0.32 mA cm-2,  corresponding to a current density of C/8 regarding the silicon specific capacity, within a 0.01-1.2 V (vs. Li/Li+) potential window.

Figure S11. SEM images of TzG/Si@Cu electrodes prepared following method 1 showing cross-sections of the TzG/Si films a, after the first lithiation (~26 μm), b, after first delithiation (~16 μm), and c, after the 100th delithiation (~40 μm) cycled at 0.32 mA cm-2, corresponding to a current density of C/8 regarding the silicon specific capacity, within a 0.01-1.2 V (vs. Li/Li+) potential window. The estimated thickness is subject to errors arising from (i) exposure of the electrode to air during the transfer to the SEM set-up, (ii) deformation of the film during the transfer from the electrochemical half-cell setup, and (iii) the angle and distance at which SEM images were collected.

Figure S12. Raman spectra collected for TzG/Si@Cu electrodes prepared following method 1 with fluorescence background illuminated by a 532 nm laser. Samples were cycled at a constant current of 0.32 mA cm-2, corresponding to a current density of C/8 regarding the silicon specific capacity, within a 0.01-1.2 V (vs. Li/Li+) potential window and Raman spectra were recorded a, after the first lithiation, b, after the first delithiation, and c, after the 100th delithiation.

Figure S13. XPS spectra showing the C 1s region of TzG/Si/CB@Cu electrodes prepared following method 1 in a, the pristine state, and b, after the 100th delithiation. Electrodes were cycled at a constant current of 0.32 mA cm-2, corresponding to a current density of C/8 regarding the silicon specific capacity, within a 0.01-1.2 V (vs. Li/Li+) potential window.

## S2.4 Electrochemical performance of TzG/Si-type electrodes, and evaluation of their density and the mass loading

Figure S14. Half-cell performance of TzG/Si/CB@Cu electrodes prepared following method 1 showing a, specific capacities normalized to Si mass / CE vs. cycle number, b, de-/lithiation curves, and c, areal capacities / CE vs. cycle number. Electrodes were cycled at a constant current of 0.32 mA cm-2, corresponding to a current density of C/8 regarding the silicon specific capacity, within a 0.01-1.2 V (vs. Li/Li+) potential window.

Figure S15. Half-cell performance of TzG/Si@Cu electrodes prepared following method 1 showing a, specific capacities normalized to Si mass / CE vs. cycle number, b, de-/lithiation curves, c, areal capacities / CE vs. cycle number, and d, volumetric capacities / CE vs. cycle number. Electrodes were cycled at a constant current of 0.32 mA cm-2, corresponding to a current density of C/8 regarding the silicon specific capacity, within a 0.01-1.2 V (vs. Li/Li+) potential window.

Figure S16. Half-cell performance data of the electrodes TzG/Si@Cu (in red), and TzG/Si/CB@Cu (in black) prepared following method 1 compared to electrodes using conventional components PAA/Si/CB@Cu (in blue) and PVdF/Si/CB@Cu (in green): Specific capacities normalized to Si mass / CE vs. cycle number. All electrodes were cycled at C/2.5, including the initial two pre-cycles at C/20 within a voltage range of 0.01-1.2 V vs. Li/Li+. PAA/Si/CB@Cu electrodes were prepared from a slurry with a composition of PAA 20 wt%/Si 60 wt%/CB 20 wt%. PVdF/Si/CB@Cu electrodes were prepared from a slurry with a composition of PVdF 20 wt%/Si 60 wt%/CB 20 wt%.

To investigate the gravimetric capacity normalized to the TzG/Si mass and the specific capacity normalized to the Si mass, the TzG/Si materials were carefully scratched from the Cu current collectors and weighed. The average weights of the films are summarized in Table S2. Similarly, the weights of the materials from TzG/Si/CB@Cu prepared following method 1 were summarized in Table S3.

Since cross-section SEM imaging offers only a local estimation of sample dimensions, we employed an Eddy current method to measure the thickness of TzG/Si films in a more reliable and statistically significant way. These thickness values were then used to calculate the volumetric energy densities of the electrodes. For the Eddy current set-up, we selected three electrodes with a diameter of 18 mm. The gauge probe tip was gently put into contact with the top of the electrodes in a circular region with a diameter of 5.6 mm, and the largest value for film thickness was recorded. Any selected position was essayed ten times for better accuracy. For each electrode, we measured three positions: (i) one site close to the edge, (ii) one site at the center, and (iii) another site close to the electrode edge. After thickness measurements, the mass-loading of the materials was evaluated by comparison of the weights of the electrode before and after removal of the TzG/Si film from the current collector. The obtained density value for TzG/Si was 0.261 g cm-3 with a standard deviation of 0.0153 g cm-3. The original data source used for density calculations can be found in Appendix 1. NOTE: Eddy current measurements give a value of the electrode film thickness at its highest point over a circular region of 5.6 mm in diameter , hence, the calculated density of the film is biased towards smaller values. Density values obtained with this protocol were then used to calculate the volumetric capacity and to plot the corresponding values for the TzG/Si electrode systems.

Table S2. Recorded weights of TzG/Si composites after delamination from the Cu current collector collected from several electrodes of TzG/Si@Cu (TzG/Si=25/75 wt%) prepared following method 1. (The actual weight of the TzG/Si film materials on Cu was evaluated by an analytical balance with an error of 0.001 mg. The weight of the film material is m1-m2, where m1 is the weight of the electrode TzG/Si@Cu, and m2 is the weight of the Cu current collector after removal of the TzG/Si composite.)

| Sample | TzG/Si weight (mg) | Si weight calculated by 75% feed ratio (mg) | Si areal mass loading (mg cm-2) |
| --- | --- | --- | --- |
| Electrode-a | 0.708 | 0.531 | 0.676 |
| Electrode-b | 0.541 | 0.406 | 0.517 |
| Electrode-c | 0.797 | 0.598 | 0.761 |
| Electrode-d | 0.660 | 0.495 | 0.630 |
| Electrode-e | 0.985 | 0.739 | 0.941 |
| Average | 0.7382 | 0.5537 | 0.7050 |
| Standard deviation | 0.1485 | 0.1114 | 0.1418 |
| Theoretical max. weight (assuming full conversion of the reaction mixture) | 0.8029 | 0.6022 | 0.7667 |

Table S3. Recorded weights of TzG/Si/CB composites after delamination from the Cu current collector collected from several electrodes of TzG/Si/CB@Cu (TzG/Si/CB=20/60/20 wt%) prepared following method 1. (The actual weight of the TzG/Si/CB film materials on Cu was evaluated by an analytical balance with an error of 0.001 mg. The weight of the film material is m1-m2, where m1 is the weight of the electrode TzG/Si/CB@Cu, and m2 is the weight of the Cu current collector after removal of the TzG/Si/CB composite.)

| Sample | TzG/Si/CB weight (mg) | Si weight calculated by 60% feed ratio (mg) |  | Si areal weight loading (mg cm-2) |
| --- | --- | --- | --- | --- |
| Electrode-a | 1.178 | 0.707 | 0.900 |  |
| Electrode-b | 1.231 | 0.739 | 0.901 |  |
| Electrode-c | 0.930 | 0.558 | 0.710 |  |
| Electrode-d | 0.770 | 0.462 | 0.588 |  |
| Electrode-e | 0.857 | 0.514 | 0.654 |  |
| Average | 0.9932 | 0.5960 | 0.7589 |  |
| Standard deviation | 0.1806 | 0.1084 | 0.1380 |  |
| Theoretical max. weight (assuming full conversion of the reaction mixture) | 1.004 | 0.6022 | 0.7667 |  |

Table S4. Properties of various state-of-the-art Si-based electrodes for lithium ion storage (incl. references).

| Binder | Electrode composition | loading (mg cm-2) | Diameter of Si (nm) | Current density (mA g-1) | Capacity[a] (mA h g-1) | Retention @cycle[b] | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PR-PAA | Si/binder/CB = 80/10/10 | 1.07 | 1000-5000 | 600 | 2503 | 91%@100th | 25 |
| SHP | Si/binder/CB = 50/6.5/43.5 | 0.5-0.7 | 3000-8000 | 400-210 | 2617 | 80%@90th | 26 |
| SHP | Si/binder/CB = 67.7/3.5/29.8 | 0.5-0.6 | 800 | 420 | 2620 | 80%@500th | 27 |
| PAA-UPy | Si/binder/CB = 60/20/20 | 0.4-0.6 | 70 | 840 | 3565 | 74%@110th | 28 |
| Native-XG | Si/binder/CB = 60/20/20 | 0.3 | 60 | 3500 | 2977 | 72%@200th | 29 |
| PAA-PVA | Si/binder/CB = 60/20/20 | N/A | <100 | 4000 | 2668 | 69%@300th | 30 |
| PANI | Si/binder = 75/25 | 0.2-0.3 | 60 | 6000 | ~600 | 91%@5000th | 15 |
| PFFOMB | Si/binder = 66.7/33.3 | N/A | <100 | 420 | ~2500 | 84%@650th | 31 |
| PEDOT:PSS | Si/binder = 80/20 | 1.0 | 50-70 | 1000 | 2681 | 78%@100th | 32 |
| PEDOT:PSS/ PEI | Si/binder = 80/20 | 1.0 | 180 | 1000 | 2440 | 83@500th | 33 |

[a] Most references provide their baseline capacity from the first de-/lithiation cycle; or after several cycles when SEI growth has stabilized.

[b] Retention is calculated using the baseline capacity.

## S2.5 Optimization of the preparation of the TzG/Si@Cu electrodes (method 2 and method 3) and their performances

Even though TzG/Si@Cu electrodes show an outstanding performance and are relatively easy to produce in a one-pot process, we identified the following desirable changes to the synthetic protocol prior to industrial-scale rollout: (i) decrease of solvent volume (the here-presented method operates with a reaction mixture concentrated to only 0.216 mg mL-1), (ii) shortening of the preparation time, (iii) a synthetic protocol that eliminates inert gas during the synthesis, and (iv) departure from lab-scale, manual loading techniques of the reaction mixture onto Cu foil that may result in film inhomogeneities (Table S2). We have successfully deployed alternative synthetic procedures that (i) employ smaller volumes of pyridine, yielding a reaction mixture that is concentrated up to 36 mg mL-1, that (ii) operate with substantially shorter times for the polymerization of the TzG polymer (1 h compared to 3 days), and that (iii) work under ambient atmosphere (part of commercial IP and not reported here) (Scheme S3 and S4).34 Raman spectra collected for TzG/Si@Cu electrodes that were obtained using the improved synthetic protocol confirm the complete conversion of the starting monomer to the TzG polymer (Figure S17). The half-cell performance data of all electrodes achieved by the here-reported methods are comparable and can be found in the Supplementary Information (Figure S18-23, Table S5). TzG is a thermally stable polymer with a decomposition onset above 400 °C under air.8 Hence, we tested the performance of the TzG/Si@Cu half-cell after a heat treatment of 80 °C for 6 h, above temperatures experienced by Li-ion batteries in some industrial and military settings. The overall performance of the TzG/Si@Cu half-cell after the thermal-stress test remains at ~3000 mA h g-1 in the second cycle comparable to the performance of untreated electrodes. The difference in overall capacity and in capacity retention can be attributed to the partial decomposition of LiPF6 during the extended heat treatment (Figure S24).

Figure S17. Raman spectra with fluorescence background illuminated by a 532 nm laser, Raman shift calibrated based on stretching bands of crystalline Si-Si at 518 cm-1 (from Figure 1c). a, TzG/Si@Cu electrodes prepared following method 2 and b, TzG/Si@Cu electrodes prepared following method 3.

Figure S18. Half-cell performance data for TzG/Si@Cu electrodes prepared following method 2 showing a, specific capacities normalized to Si mass / CE vs. cycle number, b, de-/lithiation curves, c, areal capacities / CE vs. cycle number, and d, volumetric capacities / CE vs. cycle number. Electrodes were cycled at a constant current density of C/8 regarding the silicon specific capacity, within a 0.01-1.2 V (vs. Li/Li+) potential window.

Figure S19. Half-cell performance data for TzG/Si@Cu electrodes prepared following method 3 showing a, specific capacities normalized to Si mass / CE vs. cycle number, b, de-/lithiation curves, c, areal capacities / CE vs. cycle number, and d, volumetric capacities / CE vs. cycle number. Electrodes were cycled at a constant current density of C/8 regarding the silicon specific capacity, within a 0.01-1.2 V (vs. Li/Li+) potential window.

Figure S20. Half-cell performance data for TzG/Si@Cu electrodes prepared following method 2 and cycled at different C rates from C/8 to 2C (initial two cycles at C/20) showing a, specific capacities normalized to Si mass / CE vs. cycle number, b, de-/lithiation curves, c, areal capacities / CE vs. cycle number, and d, volumetric capacities / CE vs. cycle number. Electrodes were cycled within 0.01-1.2 V vs. Li/Li+ potential window.

Figure S21. Half-cell performance data for TzG/Si@Cu electrodes prepared following method 3 and cycled at different C rates from C/8 to 2C (initial two cycles at C/20) showing a, specific capacities normalized to Si mass / CE vs. cycle number, b, de-/lithiation curves, c, areal capacities / CE vs. cycle number, and d, volumetric capacities / CE vs. cycle number. Electrodes were cycled within 0.01-1.2 V vs. Li/Li+ potential window.

Figure S22. Half-cell performance data for TzG/Si@Cu electrodes prepared following method 2 with a high mass loading (>0.35 mg cm-2) showing a, specific capacities normalized to Si mass / CE vs. cycle number, b, de-/lithiation curves, c, areal capacities / CE vs. cycle number, and d, volumetric capacities / CE vs. cycle number. Electrodes were cycled at a constant current density of C/8 regarding the silicon specific capacity, within a 0.01-1.2 V (vs. Li/Li+) potential window. This data contributes towards Table S5.

Figure S23. Half-cell performance data for TzG/Si@Cu electrodes prepared following method 3 with high mass loading (>0.7 mg cm-2) showing a, specific capacities normalized to Si mass / CE vs. cycle number, b, de-/lithiation curves, c, areal capacities / CE vs. cycle number, and d, volumetric capacities / CE vs. cycle number. Electrodes were cycled at a constant current density of C/8 regarding the silicon specific capacity, within a 0.01-1.2 V (vs. Li/Li+) potential window. This data contributes towards Table S5.

Table S5. Physical and electrochemical performance parameters of TzG/Si@Cu electrodes (TzG/Si=25/75 wt%). Electrodes were cycled at a constant current density of C/8 regarding the silicon specific capacity, within a 0.01-1.2 V (vs. Li/Li+) potential window.

| Sample | Si areal mass-loading[a] |  | 2nd cycle lithiation capacity |  |  |  |  | Retention (100th cycle vs. 2nd cycle) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Average (mg cm-2) | Deviation ±(mg cm-2) & PCT | Areal capacity (mA h g-1) | Specific capacity (mA h g-1) | Deviation in specific capacity ±(mA h g-1) & PCT[e] | Volumetric capacity (mA h cm-3) | Deviation in volumetric capacity ±(mA h cm-3) & PCT[f] | (%) |
| TzG/Si@Cu method 1 | 0.705 | 0.142 & 20.1% | 2.49 | 3535 | 712 & 20.1% | 692 | 145 & 21.0% | 69.1% |
| TzG/Si@Cu method 2 | 0.155 | 0.0233 & 15.0% | 0.575 | 3710 | 558 & 15.0% | 726 | 117 & 16.1% | 70.4% |
| TzG/Si@Cu[b] method 2 | 0.390 | 0.0564 & 14.5% | 1.045 | 3128 | 528 & 16.9% | 612 | 102 & 16.5% | 67.4% [b] |
| TzG/Si@Cu method 3 | 0.370 | 0.0196 & 5.3% | 0.908 | 2455 | 130 & 5.3% | 481 | 38.0 & 7.9% | 79.2% |
| TzG/Si@Cu[c] method 3 | 0.714 | 0.0183 & 2.6% | 1.303 | 1825 | 46.8 & 2.6% | 357 | 22.8 &6.4% | 68.2%[c] |

[a] Average mass-loading on TzG/Si@Cu electrodes was obtained from an average of six sample. The average mass-loading on all other electrodes was obtained from an average of ten samples.

[b] TzG/Si@Cu electrodes prepared following method 2 with a high mass loading (>0.35 mg cm-2) were prepared to demonstrate method 2 can improve the overall mass-loading. However, deviations in mass loading are significant using this method. Cycling performance is shown in Figure S22, with Si mass loading of 0.334 mg cm-2.

[c] TzG/Si@Cu electrodes prepared following method 3 with high mass loading (>0.7 mg cm-2) were prepared to demonstrate method 3 can improve the overall mass-loading. Cycling performance is shown in Figure S23.

[e] Calculation based on the deviation in Si mass-loading.

[f] Calculation based on the deviation in the TzG/Si mass loading and the deviation in the TzG/Si density evaluation.

Figure S24. Half-cell performance data for TzG/Si@Cu electrodes prepared following method 2 after thermal stress-testing (at 80 °C for 6 h) showing a, specific capacities normalized to Si mass / CE vs. cycle number and b, de-/lithiation curves. Electrodes were cycled at a constant current density of C/8 regarding the silicon specific capacity, within a 0.01-1.2 V (vs. Li/Li+) potential window.

# REFERENCES

1	Ranganathan, A., Heisen, B. C., Dix, I. & Meyer, F. A triazine-based three-directional rigid-rod tecton forms a novel 1D channel structure. Chemical Communications, 3637-3639 (2007).

2	Hong, E. Y. H., Wong, H. L. & Yam, V. W. W. From Spherical to Leaf‐Like Morphologies: Tunable Supramolecular Assembly of Alkynylgold (I) Complexes through Variations of the Alkyl Chain Length. Chemistry–A European Journal 21, 5732-5735 (2015).

3	Faulkner, R., DiVerdi, J., Yang, Y., Kobayashi, T. & Maciel, G. The surface of nanoparticle silicon as studied by solid-state NMR. Materials 6, 18-46 (2013).

4	Bashouti, M. Y. et al. Silicon nanowires terminated with methyl functionalities exhibit stronger Si–C bonds than equivalent 2D surfaces. Physical Chemistry Chemical Physics 11, 3845-3848 (2009).

5	Li, C., Cao, C.-B. & Zhu, H.-S. Graphitic carbon nitride thin films deposited by electrodeposition. Materials Letters 58, 1903-1906 (2004).

6	Li, C., Yang, X., Yang, B., Yan, Y. & Qian, Y. Synthesis and characterization of nitrogen-rich graphitic carbon nitride. Materials chemistry and physics 103, 427-432 (2007).

7	Algara‐Siller, G. et al. Triazine‐based graphitic carbon nitride: a two‐dimensional semiconductor. Angewandte Chemie International Edition 53, 7450-7455 (2014).

8	Schwarz, D. et al. Twinned Growth of Metal‐Free, Triazine‐Based Photocatalyst Films as Mixed‐Dimensional (2D/3D) van der Waals Heterostructures. Advanced Materials 29, 1703399 (2017).

9	Radvanyi, E., De Vito, E., Porcher, W. & Larbi, S. J. S. An XPS/AES comparative study of the surface behaviour of nano-silicon anodes for Li-ion batteries. Journal of Analytical Atomic Spectrometry 29, 1120-1131 (2014).

10	Philippe, B. et al. Role of the LiPF6 salt for the long-term stability of silicon electrodes in Li-ion batteries–A photoelectron spectroscopy study. Chemistry of Materials 25, 394-404 (2013).

11	Nguyen, C. C., Yoon, T., Seo, D. M., Guduru, P. & Lucht, B. L. Systematic investigation of binders for silicon anodes: interactions of binder with silicon particles and electrolytes and effects of binders on solid electrolyte interphase formation. ACS applied materials & interfaces 8, 12211-12220 (2016).

12	Young, B. T. et al. Role of binders in solid electrolyte interphase formation in lithium ion batteries studied with hard X-ray photoelectron spectroscopy. Journal of Materials Research 34, 97-106 (2019).

13	Koo, B. et al. A highly cross‐linked polymeric binder for high‐performance silicon negative electrodes in lithium ion batteries. Angewandte Chemie International Edition 51, 8762-8767 (2012).

14	Lopez, J., Mackanic, D. G., Cui, Y. & Bao, Z. Designing polymers for advanced battery chemistries. Nature Reviews Materials, 1 (2019).

15	Wu, H. et al. Stable Li-ion battery anodes by in-situ polymerization of conducting hydrogel to conformally coat silicon nanoparticles. Nature communications 4, 1943 (2013).

16	Liu, B., Soares, P., Checkles, C., Zhao, Y. & Yu, G. J. N. l. Three-dimensional hierarchical ternary nanostructures for high-performance Li-ion battery anodes. Nano letters 13, 3414-3419 (2013).

17	Nie, M., Abraham, D. P., Chen, Y., Bose, A. & Lucht, B. L. Silicon solid electrolyte interphase (SEI) of lithium ion battery characterized by microscopy and spectroscopy. The Journal of Physical Chemistry C 117, 13403-13412 (2013).

18	Eshetu, G. G. & Figgemeier, E. Confronting the Challenges of Next‐Generation Silicon Anode‐Based Lithium‐Ion Batteries: Role of Designer Electrolyte Additives and Polymeric Binders. ChemSusChem 12, 2515-2539 (2019).

19	Ferraresi, G., Czornomaz, L., Villevieille, C., Novák, P. & El Kazzi, M. Elucidating the surface reactions of an amorphous Si thin film as a model electrode for Li-ion batteries. ACS applied materials & interfaces 8, 29791-29798 (2016).

20	Sezen, H. & Suzer, S. Communication: Enhancement of dopant dependent x-ray photoelectron spectroscopy peak shifts of Si by surface photovoltage. The Journal of Chemical Physics 14, 141102 (2011).

21	Putri, L. K. et al. Engineering nanoscale p–n junction via the synergetic dual-doping of p-type boron-doped graphene hybridized with n-type oxygen-doped carbon nitride for enhanced photocatalytic hydrogen evolution. Journal of Materials Chemistry A 6, 3181-3194 (2018).

22	Sakaushi, K. et al. An energy storage principle using bipolar porous polymeric frameworks. Angewandte Chemie International Edition 51, 7850-7854 (2012).

23	Kovalenko, I. et al. A major constituent of brown algae for use in high-capacity Li-ion batteries. Science 334, 75-79 (2011).

24	Xu, J. lnvestigation of the Critical Role of Polymeric Binders for Silicon Negative Electrodes in Lithium-lon Batteries.  (2016).

25	Choi, S., Kwon, T.-w., Coskun, A. & Choi, J. W. Highly elastic binders integrating polyrotaxanes for silicon microparticle anodes in lithium ion batteries. Science 357, 279-283 (2017).

26	Wang, C. et al. Self-healing chemistry enables the stable operation of silicon microparticle anodes for high-energy lithium-ion batteries. Nature chemistry 5, 1042 (2013).

27	Chen, Z. et al. High‐areal‐capacity silicon electrodes with low‐cost silicon particles based on spatial control of self‐healing binder. Advanced Energy Materials 5, 1401826 (2015).

28	Zhang, G. et al. A Quadruple‐Hydrogen‐Bonded Supramolecular Binder for High‐Performance Silicon Anodes in Lithium‐Ion Batteries. Small 14, 1801189 (2018).

29	Jeong, Y. K. et al. Millipede-inspired structural design principle for high performance polysaccharide binders in silicon anodes. Energy & Environmental Science 8, 1224-1230 (2015).

30	Song, J. et al. Interpenetrated gel polymer binder for high‐performance silicon anodes in lithium‐ion batteries. Advanced functional materials 24, 5904-5910 (2014).

31	Liu, G. et al. Polymers with tailored electronic structure for high capacity lithium battery electrodes. Advanced Materials 23, 4679-4683 (2011).

32	Higgins, T. M. et al. A commercial conducting polymer as both binder and conductive additive for silicon nanoparticle-based lithium-ion battery negative Electrodes. Acs Nano 10, 3702-3713 (2016).

33	Zeng, W. et al. Enhanced Ion Conductivity in Conducting Polymer Binder for High‐Performance Silicon Anodes in Advanced Lithium‐Ion Batteries. Advanced Energy Materials 8, 1702314 (2018).

34	Urbanski, A., Ulhmann, P., Huang, J. & Bojdys, M. J. Anode und Verfahren zu ihrer Herstellung. Germany patent DE102019110450 (2020).