Supramolecular Polynuclear Clusters Mediated Assembly of Cubic Hydrogen-Bonded Organic Frameworks with Octahedral Cages for Reversible Photochromism

Xiaojun Ding, Jing Chen, and Gang Ye*

Table S1. Crystallographic data and structure refinement data of TCA_NH4,.

| Single crystal | TCA_NH4 |
| --- | --- |
| Empirical formula | C84H81N10O27 |
| Formula weight | 1722.67 |
| Temperature/K | 170.00 |
| Crystal system | cubic |
| Space group | I23 |
| a/Å | 20.9737(2) |
| b/Å | 20.9737(2) |
| c/Å | 20.9737(2) |
| α/° | 90 |
| β/° | 90 |
| γ/° | 90 |
| Volume/Å3 | 9226.2(3) |
| Z | 4 |
| ρcalc g/cm3 | 1.241 |
| μ/mm-1 | 0.787 |
| F(000) | 3616.0 |
| Crystal size/mm3 | 0.2 × 0.16 × 0.15 |
| Radiation | CuKα (λ = 1.54178) |
| 2Θ range for data collection/° | 10.33 to 132.888 |
| Index ranges | -23 ≤ h ≤ 16, -22 ≤ k ≤ 24, -20 ≤ l ≤ 24 |
| Reflections collected | 21578 |
| Independent reflections | 2724 [Rint = 0.1528, Rsigma = 0.0642] |
| Data/restraints/parameters | 2724/0/184 |
| Goodness-of-fit on F2 | 1.020 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0745, wR2 = 0.2109 |
| Final R indexes [all data] | R1 = 0.0932, wR2 = 0.2271 |
| Largest diff. peak/hole / e Å-3 | 0.24/-0.31 |
| Flack parameter | 0.2(2) |
| CCDC number | 2309944 |

Figure S1. Images of prepared TCA_NH4, TCA_NH4@CHCl3, TCA_NH4@CHBr3, and TCA_NH4@CHI3.

Figure S2. A microscope picture of synthesized cubic TCA_NH4.

Table S2. Hydrogen bonds parameters in TCA_NH4.

| Donor | H | Acceptor | d(D-H)/ Å |  | d(H-A)/ Å | d(D-A)/ Å | D-H-A/° |
| --- | --- | --- | --- | --- | --- | --- | --- |
| N0061 | H00C | O003 | 0.909 | 1.830 |  | 2.739 | 179.6 |
| N006 | H00F | O0042 | 0.911 | 2.509 |  | 3.323 | 148.9 |
| N006 | H00A | O00M3 | 0.910 | 2.477 |  | 3.235 | 140.8 |
| O00M | H00M | O0044 | 0.718 | 2.069 |  | 2.756 | 160.9 |

1-z,1+x, -y; 21/2-x, 1/2-y, -1/2+z; 3-1/2+x, 1/2-y, -1/2-z; 41/2-x, -1/2+y, -1/2-z

Figure S3. Enclosed octahedral cages with size of about 12 Å in 2×2×2 lattice, depicted by mercury software with probe radius of 1.2 Å. All atoms were omitted for clarity.

Figure S4. Topological 2×2×2 networks of body-centered cubic TCA_NH4 crystal lattices with simplified SSBUs connecting adjacent cells along six directions of the plane. Nonhydrogen bonding hydrogen atoms are omitted for clarity.

Figure S5. (a) SSBU with concentrated polynuclear clusters and simplified two oxygen four nitrogen model. (b) Orthogonally connected SSBUs through intermolecular carboxylic O-H…O hydrogen bonds as in Figure 1b and Figure S4.

Figure S6. Simplified SSBUs interlaced orthogonally and O-H…O hydrogen bonds were omitted. All hydrogen atoms are also omitted for clarity.

Table S3. C-H…N hydrogen bond parameters of TCA_NH4@CHCl3, TCA_NH4@CHBr3, and TCA_NH4@CHI3.

|  | d/C-H…N | θ/C-H…N | Unit Cell Volume |
| --- | --- | --- | --- |
| TCA_NH4 | -- | -- | 9226.2 Å3 |
| TCA_NH4@CHCl3 | 2.805 Å | 180° | 9221.2 Å3 |
| TCA_NH4@CHBr3 | 3.007 Å | 180° | 9207.7 Å3 |
| TCA_NH4@CHI3 | 2.244 Å | 180° | 9204.7 Å3 |

Figure S7. (a) Truncated octahedral configuration and (b) encapsulated truncated octahedron within the cavity four CHX3 (X=Cl, Br, I)in different colors.

Table S4. C-H…I hydrogen bond parameters of TCA_NH4@CHI3.

| Donor | H | Acceptor | d(D-H)/ Å |  | d(H-A)/ Å | d(D-A)/ Å | D-H-A/° |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C00K1 | H00K | I1 | 0.930 | 2.817 |  | 3.600 | 142.4 |

11+y, -z, 1-x;

Table S5. Crystal parameters of TCA_NH4, TCA_NH4@CHCl3, TCA_NH4@CHBr3, and TCA_NH4@CHI3.

|  | TCA_NH4 | TCA_NH4@CHCl3 | TCA_NH4@CHBr3 | TCA_NH4@CHI3 |
| --- | --- | --- | --- | --- |
| Crystal system | cubic | cubic | cubic | cubic |
| Space group | I23 | I23 | I23 | I23 |
| a/Å | 20.9737(2) | 20.9699 (4) | 20.9596 (12) | 20.9574 (1) |
| b/Å | 20.9737(2) | 20.9699 (4) | 20.9596 (12) | 20.9574 (1) |
| c/Å | 20.9737(2) | 20.9699 (4) | 20.9596 (12) | 20.9574 (1) |
| α/° | 90 | 90 | 90 | 90 |
| β/° | 90 | 90 | 90 | 90 |
| γ/° | 90 | 90 | 90 | 90 |
| Volume/Å3 | 9226.2(3) | 9221.2 | 9207.7 | 9204.7 |

Figure S8. Powder X-ray diffraction of simulated TCA_NH4, measured TCA_NH4, TCA_NH4@CHCl3, TCA_NH4@CHBr3, and TCA_NH4@CHI3.

Figure S9. Thermogravimetric analysis of TCA_NH4, TCA_NH4@CHCl3, TCA_NH4@CHBr3, and TCA_NH4@CHI3 under N2 gas atmosphere with flow of 10ml/min.

Figure S10. XRD of TCA_NH4 after immersing in different solvent.

Figure S11. The distances of adjacent halogen atoms with highlighted X1 (X= Cl, Br, I) as center.

Figure S12. Solid state fluorescence reflection spectra of TCA_NH4, TCA_NH4@CHCl3, TCA_NH4@CHBr3, and TCA_NH4@CHI3.

Figure S13. Excitation spectra of TCA_NH4, TCA_NH4@CHCl3, TCA_NH4@CHBr3, and TCA_NH4@CHI3 emission at 470 nm.

Figure S14. Solid-state absorption spectra of TCA_NH4, TCA_NH4@CHCl3, TCA_NH4@CHBr3, and TCA_NH4@CHI3.

Table S6. Lifetime fitting of different crystals with time constants (τ), pre-exponential factor (B), and correlation coefficient (χ2).

|  | τ/ns | B | A | χ2 |
| --- | --- | --- | --- | --- |
| TCA_NH4 | 2.092 | 2046 | 1.575 | 1.093 |
| TCA_NH4@CHCl3 | 2.051 | 915.3 | 0.837 | 1.136 |
| TCA_NH4@CHBr3 | 1.694 | 806.6 | 0.742 | 1.065 |
| TCA_NH4@CHI3 | 2.433 | 998.9 | 0.845 | 1.069 |
| TCA_NH4@I2 | 2.369 | 962.5 | 0.977 | 0.978 |

Figure S15. EPR spectrum of TCA_NH4@CHI3 before and after irradiation with UV-vis lamp with power density of 200 mW/cm2.

Figure S16. EPR spectrum with magnetic field (a) and value g signals of TCA_NH4@CHCl3 before and after irradiation with UV-vis lamp power density of 200 mW/cm2.

Figure S17. 5 times photochromic images of TCA_NH4@CHI3 before irradiation and after irradiation under Xe lamp.

Table S7. Photosensitive efficiency of TCA_NH4@CHI3 with different light sources.

| Source | λ/nm | light power density/mW cm2 | Photochromic time |
| --- | --- | --- | --- |
| X ray | 1.54 (CuKα) |  | 30 mins |
| ultraviolet light | 365 | 5 | 5 mins |
| sun light | 290-2500 | 100 | 2 mins |
| LED | 450-460 | 8 | 3 mins |
| Xe lamp | 400 | 200 | 60 seconds |

Figure S18. Solid state absorption spectroscopy of photochromic process of TCA_NH4@CHI3 after 5 times irradiation and recovery.

Figure S19. Solid-state absorption spectrum of powder CHI3 with UV-vis Xe lamp irradiation for 10 minutes.

Figure S20. The normalized emission spectrum of TCA_NH4@CHI3 before and after Xe lamp irradiation.

Figure S21. The excitation spectrum of TCA_NH4@CHI3 before and after Xe lamp irradiation.