Supporting information

Journal of Applied Electrochemistry

Shape influence of β-MnO2 on catalytic activity in the oxygen reduction reaction in alkaline media

I. Cruz-Reyes1, B. Trujillo-Navarrete1*, R.M. Félix Navarro1, F. Paraguay-Delgado2

1 Tecnológico Nacional de México/ IT Tijuana. Blvd. Alberto Limón Padilla s/n Col. Otay Tecnológico, Tijuana, B.C. México.

2 Centro de Investigación en Materiales Avanzados, S.C. (CIMAV), Av. Miguel de Cervantes #120, Complejo Industrial Chihuahua, Chihuahua, Chih. México. C.P. 31136.

*e-mail: balter.trujillo@tectijuana.edu.mx

Figure SI-1 Rietveld refinement plots of β-MnO2 powders: (a) Commercial β-MnO2, rods, and (b) dandelions; Vertical bars (|) indicate the positions of the Bragg reflections of β-MnO2.

Table SI-1. R-factors of Rietveld refinement for shapes of β-MnO2.

| MnO2 | Dandelions | Nanorods | Commercial MnO2 |
| --- | --- | --- | --- |
| Rp(%) | 4.61 | 4.43 | 4.74 |
| Rwp(%) | 5.94 | 5.76 | 3.74 |
| 2 | 1.46 | 1.42 | 1.24 |

Figure SI-2 XPS survey of β-MnO2: Mn 2p peaks were identified, showing a distance between peaks    11.9 eV.

Figure SI-3 (a) ORR/OER micro-polarization region. (b) Tafel plots of β-MnO2 shapes recorded in O2-saturated 0.1 M NaOH.

Figure SI-4. (a) Percentage of H2O2 and (b) the number of electrons transferred (n) during ORR for β-MnO2 shapes and commercial MnO2 and MWCNT.