Supplementary

Environmentally Friendly nanomembrane from PEF–PHBv composites: Preparation and investigation of morphologies, thermal, and mechanical properties

Somprasong Thongkham1*, Tanatorn Thiamsing1, Chothika Onsuwan1, Orawan Termkunanon1, and Woraporn Kiwjaroun1

1 National Nanotechnology Center, 114 Thailand Science Park, Paholyothin Rd., Klong 1, Klong Luang, Pathumthani 12120, Thailand
E-mail: somprasong.tho@nanotec.or.th

Scheme S1. Synthesis of (Polyethylene 2,5-furandicarboxylate, PEF)

Figure S1. 1H NMR spectrum (500 MHz, CDCl3, 25 °C) of poly(ethylene furanoate)

Figure S2. PEF after SSP: white solid from reactor (left) and Power after grinding (right).

Table S1.  Tg, TCC, Tm, and HCC /Hm of PEF และ SSP-PEF

| Sample | Tg (oC) | Tcc (oC) | Tm (oC) | Hcc (J/g) | Hm (J/g) | Xc (%) |
| --- | --- | --- | --- | --- | --- | --- |
| PEF(2h) | 58.00 | 125.50 | 203.60 | 46.41 | 60.04 | 9.74 |
| PEF(3h) | 72.90 | 150.70 | 204.90 | 49.23 | 25.21 | 17.16 |
| PEF(4h) | 63.80 | 151.70 | 206.90 | 45.65 | 45.75 | 0.07 |
| SSP(1)_PEF(3h) | 68.70 | - | 205.90 | - | 63.11 | 45.08 |
| SSP(2)_PEF(3h) | 69.80 | - | 213.40 | - | 64.06 | 45.76 |
| SSP(3)_PEF(3h) | 67.50 | - | 221.50 | - | 63.21 | 45.15 |

|  | % Crystallinity (Xc) | = | ∆Hm-∆HCC∆Hm0× 100 |  |
| --- | --- | --- | --- | --- |

โดย	∆Hm  	=	heat of melting (J/g)

∆Hm0	=        heat of melting for 100% crystalline PEF sample (∆Hm0  = 137 J/g)

∆HCC   =         heat of cold crystallization (J/g)

Figure S3. Optimization parameters of electrospining using 30%wt of  PEF.

Figure S4. Nanofibers of  PHBv 5%(a) and 10% (b). The membranes are too brittle

Figure S5. Fibers of different ratio of PEF:PHBv observed by optical microscope.

Figure S6. Nanofibers of different ratio of PEF:PHBv observed by SEM.

Table S2.  Tg, Tm, Td, and Xc of PEF และ SSP-PEF

| Sample | Tg (oC) | Tm (oC) | Td onset (oC) | Td peak (oC) | Xc (%) |
| --- | --- | --- | --- | --- | --- |
| PEF | 85.5 | 210.9 | 249.17 | 405.42 | 13.53% |
| P95 | - | 195.8 | 319.33 | 400.10 | 27.17% |
| P85 | - | 194.2 | 325.27 | 405.21 | 20.20% |
| P60 | - | 183.5 | 325.30 | 399.21 | 12.33% |

Figure S7. Elongation at break of PEF nanofibers and PEF-PHBv composite nanofibers.

Table S3.  Avage contact angle of PEF (30%) nanofibers and PEF/PHBv composite nanofibers.

| Sample | Contact angle (°) At 180 s |
| --- | --- |
| PEF30 | 129.51±1.62 |
| P95:PHBv5 | 111.66±1.48 |
| P85:PHBV15 | 117.78±2.44 |
| P60:PHBv40 | 117.55±1.82 |