Supplementary Material: De novo inverse materials design by combining optimization algorithm, universal potential and universal property model

Guanjian Cheng1,2, Xin-Gao Gong3,2, Wan-Jian Yin1,2,4,*

1College of Energy, Soochow Institute for Energy and Materials InnovationS (SIEMIS), and Jiangsu Provincial Key Laboratory for Advanced Carbon Materials and Wearable Energy Technologies, Soochow University, Suzhou 215006, China

2Shanghai Qi Zhi Institute, Shanghai, 200232, China

3Key Laboratory for Computational Physical Sciences (MOE), Institute of Computational Physical Sciences, Fudan University, Shanghai, 200438, China

4Light Industry Institute of Electrochemical Power Sources, Soochow University, Suzhou 215006, China

*wjyin@suda.edu.cn

Supplementary Fig. 1. UPot-predicted and DFT-calculated (a) total energies, (b) atomic forces, and (c) stress for 2,944 testing materials.

(a)

(b)

(c)

(d)

(a)

(b)

(c)

(d)

Supplementary Fig. 2. a, b, The curve of the total energy of A follows lattice (a) and atomic coordinate (b) disturbances. c, d, The parity plots for the UBmod by EOS (c) and E-S (d), the dash lines (y=x) are guides for the eye.

Supplementary Fig. 3. Transfer learning flow chart.

Supplementary Fig. 4. 2D UMAP formed by extensive random sampling in full space. The heat map represents the relative cohesive energy.

Supplementary Table 1. Selection 50 typical compounds with the high atomic cohesion identified by the UPot-BO.

| # | a | c | s | Ebpred | ∆Hpred | EbDFT | ∆HDFT | Matched in MP |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Zr-C | 1-1 | Zr5C5 | -7.961 | -0.766 | -8.034 | -0.840 | mp-2795, mp-1009894 |
| 2 |  |  | Zr4C4 | -7.462 | -0.268 | -7.939 | -0.745 |  |
| 3 |  |  | Zr5C5 | -7.693 | -0.499 | -7.319 | -0.124 |  |
| 4 |  | 4-5 | Zr4C5 | -7.615 | -0.342 | -7.785 | -0.511 |  |
| 5 |  |  | Zr4C5 | -7.619 | -0.346 | -7.716 | -0.443 |  |
| 6 |  |  | Zr4C5 | -7.642 | -0.368 | -7.595 | -0.322 |  |
| 7 |  |  | Zr4C5 | -7.573 | -0.299 | -7.546 | -0.273 |  |
| 8 |  |  | Zr4C5 | -7.545 | -0.272 | -7.528 | -0.255 |  |
| 9 |  |  | Zr4C5 | -7.564 | -0.291 | -7.405 | -0.132 |  |
| 10 |  |  | Zr4C5 | -7.461 | -0.188 | -7.307 | -0.034 |  |
| 11 |  |  | Zr4C5 | -7.443 | -0.170 | -7.254 | 0.019 |  |
| 12 |  |  | Zr4C5 | -7.383 | -0.110 | -7.209 | 0.064 |  |
| 13 |  | 5-4 | Zr5C4 | -7.618 | -0.503 | -7.639 | -0.524 |  |
| 14 |  |  | Zr5C4 | -7.555 | -0.440 | -7.566 | -0.451 |  |
| 15 |  |  | Zr5C4 | -7.586 | -0.471 | -7.548 | -0.433 |  |
| 16 |  |  | Zr5C4 | -7.462 | -0.347 | -7.433 | -0.318 |  |
| 17 |  |  | Zr5C4 | -7.199 | -0.084 | -7.057 | 0.058 |  |
| 18 |  | 3-4 | Zr3C4 | -7.438 | -0.142 | -7.627 | -0.331 |  |
| 19 |  | 3-5 | Zr3C5 | -7.534 | -0.162 | -7.612 | -0.239 |  |
| 20 |  |  | Zr3C5 | -7.233 | 0.139 | -7.450 | -0.077 |  |
| 21 |  | 2-5 | Zr2C5 | -7.545 | -0.045 | -7.371 | 0.129 |  |
| 22 |  | 1-5 | Zr1C5 | -7.498 | 0.171 | -7.153 | 0.517 |  |
| 23 | Zr-N | 1-1 | Zr5N5 | -7.431 | -1.580 | -7.597 | -1.746 | mp-1352, mp-1009885 |
| 24 |  | 5-4 | Zr5N4 | -7.197 | -1.277 | -7.500 | -1.580 |  |
| 25 |  |  | Zr5N4 | -7.250 | -1.330 | -7.183 | -1.262 |  |
| 26 |  |  | Zr5N4 | -7.206 | -1.285 | -7.080 | -1.159 |  |
| 27 |  | 2-1 | Zr4N2 | -7.292 | -1.232 | -7.233 | -1.172 |  |
| 28 |  |  | Zr4N2 | -7.292 | -1.232 | -7.230 | -1.170 |  |
| 29 |  | 4-5 | Zr4N5 | -7.212 | -1.432 | -7.216 | -1.435 |  |
| 30 |  | 5-3 | Zr5N3 | -7.168 | -1.160 | -7.159 | -1.151 |  |
| 31 | Zr-O | 5-4 | Zr5O4 | -7.190 | -2.101 | -7.326 | -2.237 |  |
| 32 |  | 4-5 | Zr4O5 | -7.291 | -2.550 | -7.322 | -2.581 |  |
| 33 |  | 1-1 | Zr5O5 | -7.148 | -2.233 | -7.208 | -2.293 | mp-33088, mp-10197 |
| 34 |  | 5-3 | Zr5O3 | -7.082 | -1.776 | -7.183 | -1.876 |  |
| 35 |  | 2-1 | Zr4O2 | -7.111 | -1.674 | -7.031 | -1.593 |  |
| 36 | Zr-B | 4-5 | Zr4B5 | -7.169 | -0.771 | -7.147 | -0.750 |  |
| 37 |  | 5-4 | Zr5B4 | -7.082 | -0.668 | -7.050 | -0.636 |  |
| 38 |  | 2-5 | Zr2B5 | -7.083 | -0.709 | -6.841 | -0.467 |  |
| 39 |  | 1-1 | Zr5B5 | -6.778 | -0.372 | -6.796 | -0.390 | mp-451 |
| 40 | Ti-N | 5-3 | Ti5N3 | -6.712 | -1.216 | -7.103 | -1.207 |  |
| 41 | Y-O | 4-5 | Y4O5 | -7.011 | -3.196 | -7.033 | -3.217 |  |
| 42 |  | 3-5 | Y3O5 | -6.843 | -3.100 | -6.944 | -3.201 |  |
| 43 |  | 1-1 | Y5O5 | -6.764 | -2.890 | -6.675 | -2.800 |  |
| 44 | Ti-O | 1-1 | Ti5O5 | -6.912 | -2.406 | -7.012 | -2.186 |  |
| 45 |  | 2-1 | Ti4O2 | -6.712 | -1.822 | -7.004 | -1.686 |  |
| 46 | Sc-C | 1-2 | Sc2C4 | -6.735 | -0.008 | -6.699 | 0.031 |  |
| 47 | Sc-N | 1-1 | Sc5N5 | -6.713 | -1.914 | -6.667 | -1.869 | mp-2857, mp-1009750 |
| 48 |  | 5-4 | Sc5N4 | -6.246 | -1.496 | -6.431 | -1.679 |  |
| 49 | B-C | 5-4 | B5C4 | -6.852 | 0.180 | -6.594 | 0.438 |  |
| 50 |  | 1-1 | B5C5 | -7.049 | 0.070 | -6.538 | 0.582 |  |

Supplementary Table 2. Selection 50 typical compounds with the high atomic cohesion identified by the UPot-CHEERS.

| # | a | c | s | Ebpred | ∆Hpred | EbDFT | ∆HDFT | Matched in MP |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Zr-C | 1-1 | Zr4C4 | -7.961 | -0.767 | -8.039 | -0.844 | mp-2795, mp-1009894 |
| 2 |  |  | Zr4C4 | -7.871 | -0.677 | -7.871 | -0.677 | mp-1014307 |
| 3 |  |  | Zr4C4 | -7.666 | -0.472 | -7.650 | -0.455 |  |
| 4 |  |  | Zr4C4 | -7.839 | -0.645 | -7.643 | -0.448 | mp-1009894 |
| 5 |  |  | Zr4C4 | -7.620 | -0.425 | -7.616 | -0.422 |  |
| 6 |  |  | Zr4C4 | -7.535 | -0.340 | -7.523 | -0.328 |  |
| 7 |  |  | Zr4C4 | -7.618 | -0.424 | -7.501 | -0.307 |  |
| 8 |  | 5-4 | Zr5C4 | -7.541 | -0.426 | -7.885 | -0.771 |  |
| 9 |  |  | Zr5C4 | -7.560 | -0.445 | -7.535 | -0.420 |  |
| 10 |  | 4-3 | Zr4C3 | -7.900 | -0.808 | -7.882 | -0.790 |  |
| 11 |  |  | Zr4C3 | -7.539 | -0.447 | -7.509 | -0.416 |  |
| 12 |  | 4-5 | Zr4C5 | -7.749 | -0.479 | -7.818 | -0.544 |  |
| 13 |  |  | Zr4C5 | -7.631 | -0.358 | -7.636 | -0.363 |  |
| 14 |  | 3-2 | Zr3C2 | -7.738 | -0.687 | -7.771 | -0.720 |  |
| 15 |  |  | Zr3C2 | -7.641 | -0.589 | -7.397 | -0.345 |  |
| 16 |  | 5-3 | Zr5C3 | -7.573 | -0.557 | -7.691 | -0.676 |  |
| 17 |  | 2-3 | Zr2C3 | -7.614 | -0.277 | -7.676 | -0.340 |  |
| 18 |  |  | Zr2C3 | -7.639 | -0.302 | -7.619 | -0.282 |  |
| 19 |  |  | Zr2C3 | -7.566 | -0.229 | -7.555 | -0.218 |  |
| 20 |  |  | Zr2C3 | -7.562 | -0.225 | -7.377 | -0.041 |  |
| 21 |  | 3-4 | Zr3C4 | -7.636 | -0.340 | -7.667 | -0.371 |  |
| 22 |  |  | Zr3C4 | -7.585 | -0.289 | -7.580 | -0.284 |  |
| 23 |  |  | Zr3C4 | -7.547 | -0.251 | -7.483 | -0.187 |  |
| 24 |  | 2-1 | Zr4C2 | -7.668 | -0.712 | -7.578 | -0.622 |  |
| 25 |  | 1-2 | Zr2C4 | -7.538 | -0.106 | -7.457 | -0.025 |  |
| 26 |  | 3-5 | Zr3C5 | -7.533 | -0.160 | -7.414 | -0.042 |  |
| 27 | C | 1 | C4 | -7.895 | 0.013 | -7.915 | -0.007 | mp-48, mp-569304, mp-632329, mp-937760, mp-568363, mp-568286 |
| 28 |  |  | C4 | -7.895 | 0.012 | -7.914 | -0.006 | mp-169 |
| 29 |  |  | C4 | -7.894 | 0.013 | -7.907 | 0.001 | mp-48, mp-632329, mp-568363, mp-568806 |
| 30 |  |  | C4 | -7.843 | 0.064 | -7.894 | 0.014 | mp-48, mp-937760, mp-568363, mp-568286 |
| 31 | Ti-C | 1-1 | Ti1C1 | -7.599 | -0.815 | -7.869 | -0.764 | mp-631 |
| 32 |  | 3-2 | Ti3C2 | -7.289 | -0.730 | -7.621 | -0.676 |  |
| 33 |  | 2-3 | Ti2C3 | -7.326 | -0.317 | -7.440 | -0.175 |  |
| 34 | Zr-O | 1-2 | Zr1O2 | -7.681 | -3.288 | -7.777 | -3.383 | mp-775909, mp-754741, mp-556605, mp-1190186, mp-755759, mp-755089, mp-1565, mp-2574 |
| 35 |  |  | Zr1O2 | -7.601 | -3.208 | -7.641 | -3.247 |  |
| 36 |  |  | Zr1O2 | -7.600 | -3.207 | -7.625 | -3.231 |  |
| 37 |  | 2-3 | Zr2O3 | -7.478 | -2.876 | -7.548 | -2.946 |  |
| 38 |  | 3-4 | Zr3O4 | -7.233 | -2.546 | -7.330 | -2.638 |  |
| 39 |  | 1-1 | Zr1O1 | -7.137 | -2.221 | -7.205 | -2.289 |  |
| 40 | Zr-N | 1-1 | Zr2N2 | -7.431 | -1.580 | -7.593 | -1.742 | mp-1352, mp-1009885 |
| 41 | Ti-O | 2-3 | Ti2O3 | -7.140 | -2.866 | -7.395 | -2.864 |  |
| 42 |  | 3-5 | Ti3O5 | -7.043 | -2.827 | -7.330 | -2.872 |  |
| 43 | Ti-B | 1-2 | Ti2B4 | -7.169 | -1.061 | -7.364 | -1.042 | mp-1145 |
| 44 |  | 2-5 | Ti2B5 | -6.923 | -0.796 | -7.014 | -0.691 |  |
| 45 |  | 2-3 | Ti2B3 | -6.848 | -0.786 | -6.864 | -0.545 |  |
| 46 | C-O | 5-1 | C5O1 | -7.140 | 0.007 | -7.171 | -0.023 |  |
| 47 |  | 5-2 | C5O2 | -6.767 | -0.160 | -6.675 | -0.069 |  |
| 48 | B-C | 1-3 | B1C3 | -7.434 | 0.079 | -7.124 | 0.389 |  |
| 49 | Si-C | 1-5 | Si1C5 | -6.923 | 0.424 | -6.938 | 0.408 |  |
| 50 |  | 1-3 | Si1C3 | -6.595 | 0.471 | -6.596 | 0.470 |  |

Supplementary Table 3. Selection 50 typical compounds with the high bulk modulus identified by the UPot- UBmod-BO.

| # | a | c | s | Kpred | ∆Hpred | KDFT | ∆HDFT | Matched in MP |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | C | 1 | C6 | 433.157 | 0.140 | 434.443 | 0.133 | mp-569567, mp-66, mp-1080826, mp-24, mp-998866 |
| 2 |  |  | C6 | 392.998 | 0.871 | 390.724 | 1.067 |  |
| 3 |  |  | C6 | 326.852 | 0.653 | 341.414 | 0.878 | mp-1181996 |
| 4 |  |  | C7 | 285.489 | 0.844 | 339.092 | 0.855 |  |
| 5 |  |  | C7 | 358.389 | 0.761 | 337.543 | 0.765 |  |
| 6 |  |  | C4 | 361.873 | 0.766 | 333.434 | 0.932 | mp-632329, mp-568806 |
| 7 |  |  | C7 | 368.803 | 0.758 | 327.530 | 0.838 |  |
| 8 |  |  | C5 | 347.155 | 0.546 | 324.859 | 0.794 |  |
| 9 |  |  | C7 | 365.891 | 0.846 | 321.441 | 0.705 |  |
| 10 |  |  | C7 | 251.594 | 0.708 | 246.772 | 0.801 |  |
| 11 |  |  | C7 | 307.261 | 0.974 | 233.142 | 1.058 | mp-1182029 |
| 12 | B-C | 1-2 | B2C4 | 360.895 | 0.677 | 421.612 | 0.636 |  |
| 13 |  |  | B2C4 | 332.057 | 0.449 | 308.765 | 0.794 |  |
| 14 |  | 1-4 | B1C4 | 316.833 | 0.733 | 283.379 | 0.490 |  |
| 15 |  |  | B1C4 | 258.827 | 0.400 | 268.474 | 0.535 |  |
| 16 |  |  | B1C4 | 252.085 | 0.435 | 228.262 | 0.684 |  |
| 17 |  | 3-1 | B3C1 | 324.637 | 0.442 | 298.955 | 0.776 |  |
| 18 |  |  | B3C1 | 281.330 | 0.248 | 217.226 | 0.418 |  |
| 19 |  | 2-1 | B2C1 | 294.686 | 0.249 | 279.020 | 0.593 |  |
| 20 |  | 2-5 | B2C5 | 283.709 | 0.368 | 256.795 | 0.427 |  |
| 21 |  |  | B2C5 | 248.306 | 0.527 | 251.717 | 0.843 |  |
| 22 |  |  | B2C5 | 253.750 | 0.575 | 248.380 | 0.760 |  |
| 23 |  | 2-3 | B2C3 | 271.909 | 0.401 | 252.967 | 0.482 |  |
| 24 |  | 1-1 | B4C4 | 268.278 | 0.100 | 238.476 | 0.305 |  |
| 25 |  | 3-2 | B3C2 | 262.500 | 0.471 | 225.700 | 0.498 |  |
| 26 |  | 4-1 | B4C1 | 252.990 | 0.211 | 221.607 | 0.444 |  |
| 27 |  | 5-2 | B5C2 | 250.794 | 0.362 | 215.962 | 0.610 |  |
| 28 | C-N | 1-2 | C2N4 | 307.230 | 0.942 | 406.570 | 0.969 | mp-1009818 |
| 29 |  | 2-1 | C4N2 | 303.924 | 0.592 | 392.586 | 0.723 |  |
| 30 |  | 5-2 | C5N2 | 267.781 | 0.895 | 271.667 | 0.816 |  |
| 31 | B-N | 1-2 | B2N4 | 289.073 | 0.599 | 353.525 | 0.862 |  |
| 32 |  |  | B2N4 | 307.221 | 0.433 | 321.055 | 0.628 |  |
| 33 |  |  | B2N4 | 274.691 | -0.196 | 294.223 | -0.101 |  |
| 34 |  |  | B1N2 | 307.189 | 0.433 | 284.439 | 0.635 |  |
| 35 |  | 3-1 | B3N1 | 299.604 | -0.291 | 276.051 | -0.342 |  |
| 36 |  |  | B3N1 | 299.584 | -0.291 | 270.741 | -0.339 |  |
| 37 |  | 2-1 | B2N1 | 268.144 | -0.353 | 257.465 | 0.036 |  |
| 38 | Cu-C | 1-2 | Cu1C2 | 301.999 | 0.504 | 274.079 | 0.612 |  |
| 39 |  |  | Cu1C2 | 294.691 | 0.424 | 259.509 | 0.555 |  |
| 40 | Be-C | 1-3 | Be1C3 | 310.340 | 0.184 | 265.439 | 0.593 |  |
| 41 |  | 1-2 | Be2C4 | 319.757 | 0.407 | 255.115 | 0.430 |  |
| 42 |  |  | Be2C4 | 279.881 | 0.345 | 214.517 | 0.512 |  |
| 43 | Si-C | 1-2 | Si2C4 | 275.529 | 0.583 | 241.525 | 0.554 |  |
| 44 |  | 1-3 | Si1C3 | 277.035 | 0.918 | 238.698 | 0.925 |  |
| 45 | B | 1 | B7 | 248.541 | 0.271 | 224.757 | 0.432 |  |
| 46 | Be-N | 1-2 | Be2N4 | 277.249 | 0.317 | 231.711 | 0.484 |  |
| 47 |  | 3-2 | Be3N2 | 207.541 | -0.853 | 204.680 | -0.770 |  |
| 48 | Ti-C | 1-2 | Ti1C2 | 266.017 | 0.143 | 212.506 | 0.155 |  |
| 49 | Al-C | 1-2 | Al1C2 | 257.448 | 0.607 | 207.995 | 0.522 |  |
| 50 | Zr-N | 1-2 | Zr2N4 | 260.348 | -0.816 | 200.471 | -0.722 | mp-1178600 |

Supplementary Table 4. Selection 50 typical compounds with the high bulk modulus identified by the UPot- UBmod-CHEERS.

| # | a | c | s | Kpred | ∆Hpred | KDFT | ∆HDFT | Matched in MP |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | C | 1 | C8 | 433.166 | 0.140 | 434.480 | 0.134 | mp-569567, mp-66, mp-1080826, mp-24, mp-998866 |
| 2 |  |  | C8 | 425.168 | 0.164 | 430.949 | 0.154 | mp-47 |
| 3 |  |  | C7 | 412.372 | 0.465 | 408.277 | 0.552 |  |
| 4 |  |  | C8 | 405.881 | 0.319 | 400.033 | 0.326 | mp-1008395 |
| 5 |  |  | C8 | 405.347 | 0.359 | 398.909 | 0.335 |  |
| 6 |  |  | C3 | 393.001 | 0.871 | 390.982 | 1.067 |  |
| 7 |  |  | C6 | 390.886 | 0.349 | 388.651 | 0.239 |  |
| 8 |  |  | C8 | 395.041 | 0.474 | 370.068 | 0.454 | mp-1182029, mp-624889 |
| 9 |  |  | C7 | 344.445 | 0.522 | 351.796 | 0.629 |  |
| 10 |  |  | C8 | 352.804 | 0.412 | 350.546 | 0.432 | mp-1008374, mp-1182029, mp-1078845 |
| 11 |  |  | C7 | 359.095 | 0.845 | 345.622 | 0.912 |  |
| 12 |  |  | C6 | 341.759 | 0.656 | 344.558 | 0.606 | mp-1182029, mp-1056957, mp-1181996 |
| 13 |  |  | C3 | 322.751 | 0.695 | 344.146 | 0.877 | mp-1181996 |
| 14 |  |  | C9 | 373.631 | 0.749 | 343.846 | 0.937 |  |
| 15 |  |  | C6 | 333.230 | 0.576 | 334.618 | 0.586 | mp-1182029 |
| 16 |  |  | C8 | 342.450 | 0.554 | 334.092 | 0.539 |  |
| 17 |  |  | C8 | 361.015 | 0.765 | 333.258 | 0.932 | mp-632329, mp-568806 |
| 18 |  |  | C9 | 358.502 | 0.728 | 331.316 | 0.769 |  |
| 19 |  |  | C9 | 331.022 | 0.595 | 323.496 | 0.846 |  |
| 20 |  |  | C9 | 337.985 | 0.858 | 321.497 | 0.849 |  |
| 21 |  |  | C9 | 326.819 | 0.629 | 318.270 | 0.666 |  |
| 22 |  |  | C8 | 324.727 | 0.677 | 316.674 | 0.691 |  |
| 23 |  |  | C5 | 321.025 | 0.957 | 308.879 | 0.777 |  |
| 24 |  |  | C8 | 332.931 | 0.775 | 297.784 | 0.800 | mp-632329, mp-1056957, mp-568806 |
| 25 |  |  | C7 | 322.482 | 0.829 | 287.418 | 0.952 |  |
| 26 |  |  | C4 | 335.806 | 0.909 | 280.508 | 1.126 | mp-66, mp-1080826 |
| 27 | B-C | 1-5 | B1C5 | 342.559 | 0.408 | 425.180 | 0.244 | mp-1018649 |
| 28 |  |  | B1C5 | 339.289 | 0.802 | 376.300 | 0.270 | mp-1077125 |
| 29 |  |  | B1C5 | 385.036 | 0.430 | 351.317 | 0.544 |  |
| 30 |  |  | B1C5 | 362.147 | 0.564 | 335.811 | 0.531 |  |
| 31 |  |  | B1C5 | 317.506 | 0.776 | 306.776 | 0.711 |  |
| 32 |  |  | B1C5 | 315.617 | 0.574 | 302.909 | 0.772 |  |
| 33 |  | 1-4 | B1C4 | 393.781 | 0.893 | 359.365 | 0.460 |  |
| 34 |  |  | B1C4 | 341.717 | 0.590 | 323.580 | 0.475 |  |
| 35 |  | 1-3 | B1C3 | 379.358 | 0.297 | 347.889 | 0.309 |  |
| 36 |  | 1-2 | B1C2 | 332.762 | 0.449 | 308.271 | 0.796 |  |
| 37 | B-N | 1-1 | B4N4 | 341.498 | -1.198 | 371.513 | -1.218 | mp-1639 |
| 38 |  |  | B4N4 | 321.996 | -0.468 | 355.332 | -0.015 |  |
| 39 |  | 5-3 | B5N3 | 322.271 | 0.862 | 308.986 | 0.928 |  |
| 40 |  | 2-1 | B2N1 | 310.070 | -0.063 | 277.425 | -0.184 |  |
| 41 |  | 3-1 | B3N1 | 299.750 | -0.290 | 275.998 | -0.342 |  |
| 42 |  | 3-4 | B3N4 | 301.518 | -0.081 | 257.332 | 0.152 |  |
| 43 | Ti-N | 1-1 | Ti2N2 | 245.768 | -0.831 | 259.156 | -0.781 | mp-998903 |
| 44 |  | 1-3 | Ti1N3 | 264.739 | 0.782 | 233.593 | 0.903 |  |
| 45 | B-O | 4-3 | B4O3 | 245.851 | -0.460 | 250.276 | 0.234 |  |
| 46 |  | 5-1 | B5O1 | 217.202 | -0.528 | 227.137 | -0.128 |  |
| 47 |  | 2-1 | B4O2 | 212.428 | 0.400 | 200.270 | 0.551 |  |
| 48 | B | 1 | B4 | 308.398 | 0.675 | 233.155 | 1.070 |  |
| 49 | Ti-O | 1-1 | Ti2O2 | 251.185 | -2.187 | 223.011 | -1.925 |  |
| 50 | P-C | 1-1 | P4C4 | 249.851 | 0.666 | 216.954 | 0.856 |  |

(a)

(b)

(c)

(d)

(a)

(b)

(c)

(d)

Supplementary Fig. 5. The parity plots for the results of DNID. a, b, The 50 typical compounds with the high atomic cohesion identified by the UPot-BO (a) and UPot-CHEERS (b) approaches. c, d, The 50 typical compounds with the high atomic cohesion identified by the UPot-BO (c) and UPot-CHEERS (d) approaches.

(a)

(c)

(d)

(e)

(b)

(a)

(c)

(d)

(e)

(b)

Supplementary Fig. 6. The optimization process of atomic cohesion energy Eb for ternary compound AlBmCn (a), with the corresponding atomic compositions shown in (c)-(e). (b) The ZrC structure of the best material in (a).

Supplementary Fig. 7. The phonon spectra for selection 30 compounds in Table S1.

Supplementary Fig. 8. The phonon spectra for selection 30 compounds in Table S2.

Supplementary Fig. 9. The phonon spectra for selection 30 compounds in Table S3.

Supplementary Fig. 10. The phonon spectra for selection 30 compounds in Table S4.

Supplementary Fig. 11. The elapsed time of searching for large cohesive energy materials by DFT-BO, UPot-BO and UPot-CHEERS. The dashed curve extrapolates the estimated time.

(a)

(b)

(c)

(d)

(c)

(d)

Zr1O2

O8

Supplementary Fig. 12. a,b, The process of CDVAE to search the materials with large cohesive energy (a) and high bulk modulus (b). The dashed lines are the target values searched by DNID. c,d, The best candidate materials searched by CDVAE.