Adsorption characteristics of Cr6+ on microalgae immobilized by different carriers

Ran Chena1, Junjun Wangb1, Ling Fana, Linlin Cuia, Yejuan Zhanga, Xueling Wua, Jiaokun Lia, Weimin Zenga, Li Shena

Figure. S1 FTIR spectra of the microalgae before and after adsorption of Cr6+

Table S1 The orthogonal experiment of three factors and three levels on the ratio of chitosan to acetic acid, microalgae concentration, and immobilization time

| No. | A Chitosan : acetic acid (W/V) | B Microalgae concentration (cells/mL) | C Immobilization time (h) | Diameter (mm) | Form ball | Adsorption efficiency |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 1.5:40 | 106 | 6 | 2.9 | difficult to form ball and easy to adhere | 67.5% |
| 2 | 1.5:40 | 107 | 12 | 2.8 | difficult to form ball and easy to adhere | 72.1% |
| 3 | 1.5:40 | 108 | 18 | 3.0 | difficult to form ball and easy to adhere | 80.3% |
| 4 | 2.0:40 | 106 | 12 | 2.9 | easy to form a ball without tailing | 94.7% |
| 5 | 2.0:40 | 107 | 18 | 2.8 | easy to form a ball without tailing | 97.6% |
| 6 | 2.0:40 | 108 | 6 | 2.9 | easy to form a ball without tailing | 95.4% |
| 7 | 2.5:40 | 106 | 18 | 3.3 | difficult to form ball and easy to drag | 84.1% |
| 8 | 2.5:40 | 107 | 6 | 3.1 | difficult to form ball and easy to drag | 75.1% |
| 9 | 2.5:40 | 108 | 12 | 3.1 | difficult to form ball and easy to drag | 82.1% |
| K1 | 2.199 | 2.436 | 2.38 |  |  |  |
| K2 | 2.877 | 2.448 | 2.489 |  |  |  |
| K3 | 2.413 | 2.583 | 2.62 |  |  |  |
| k1 | 0.733 | 0.812 | 0.793 |  |  |  |
| k2 | 0.959 | 0.816 | 0.829 |  |  |  |
| k3 | 0.804 | 0.861 | 0.873 |  |  |  |
| Range | 0.226 | 0.049 | 0.08 |  |  |  |
| Primary and secondary order | A>C>B |  |  |  |  |  |
| Excellent level | A2 | B3 | C3 |  |  |  |
| Optimal combination | A2B3C3 |  |  |  |  |  |

a School of Minerals Processing and Bioengineering, Central South University, Changsha, Hunan 410083, China. E-mail: lishen@csu.edu.cn; Fax: +86-731-88879815; Tel: +86-731-88877472

b School of Metallurgy and Environment, Central South University, Changsha, Hunan 410083, China

1 These authors contributed equally to this work and should be considered co-first authors.