Exposing Baked Plastic Pinhole Plates to Air – Experiment Plan

Outline:

- In preparation:

  - Weigh plates

  - Measure plates’ dimensions

- Bake all plates simultaneously for ~48hours at 120C. Taking care to heat and cool slowly to avoid cracking. Increment temperature by 20C every 20 mins whilst heating. Unwrap foil and turn off heating tape, allow natural cooling.

- Once bake is complete, immediately place first plate (P0, plate-days naming scheme. Re-label plates once inserted with more precise time in hours, e.g P1 à P26) into b-shem. Place other plates in loosely wrapped foil and label them with time in days which they are sitting for.

- Times which plates will be exposed for are 0, 1, 2, 4, 7, 14 days. Majority of measurements <7days as most plates will not sit for longer than this before being used in the microscope.

- Perform a quick inspection of the aperture membranes for rupture and the plastic itself for cracks or deformation. Note potential colour change – previously plates appeared to become slightly green, take pictures under the bright ring light setup by a-shem.

- Monitor vacuum pressure during evacuation and start taking MIDI scans at 18amu with Hiden once a pressure which is “safe” for the detector is reached. Run scans continuously whilst logging the total chamber pressure so that the partial pressure of water can be found. Note: scans need to be timestamped so that they can be matched to the correct total pressure.

- Stop data collection 24 hours after evacuation process was started.

- If the next plate isn’t ready to go in yet, leave the current one under vacuum in the chamber.

- Replace with next plate. Note: sticking to exact multiples of 24 is not important, record time in hours.

- Repeat steps 3,4,5 until all plates done.

Prep to do:

- Enable pressure logging on b-shem

- Determine what a “safe” pressure is for the Hiden to start taking scans

- Need 6 plates total, potentially order more if any of the Glasgow ones need to be used for imaging immediately upon return.

- Plug oven pressure gauge into tic controller so it logs.