Nitro-oxidized Carboxycellulose Nanofibers from Moringa Plant: Effective Bioadsorbent for Mercury Removal

(Supporting Information)

Hui Chen1†, Sunil K. Sharma1†, Priyanka R. Sharma1*, Kai Chi1, Eric Fung1

Katherine Aubrecht1, Ngonye Keroletswe2, Samuel Chigome2, Benjamin S. Hsiao1*

1 Department of Chemistry

Stony Brook University

Stony Brook, New York 11794-3400, United States

2 Botswana Institute for Technology Research and Innovation

Private Bag 0082

Gaborone, Botswana

† Authors HC and SKS have equal contribution.

* Corresponding authors:

PRS: Tel: +16315423506, E-mail: priyanka.r.sharma@stonybrook.edu;

BSH: Tel: +16316327793, E-mail: benjamin.hsiao@stonybrook.edu

Fourier Transform Infra-Red Spectrometry (FTIR)

A PerkinElmer Spectrum One instrument was used to record the FTIR curves in the transmission mode, between 450 and 4000 cm−1. A total of 6 scans were taken per sample using the resolution of 4 cm−1. The solid samples were recorded in the attenuated total reﬂectance (ATR) mode.

Thermogravimetric Analysis (TGA)

The thermal stability of the final NOCNF and raw moringa samples was studied by a PerkinElmer STA-6000 (Simultaneous Thermal Analyzer) instrument. Both TGA and diﬀerential thermogravimetry (DTG) curves were measured. The samples were investigated at a heating rate of 10 °C/min in the range of 0−850 °C under a continuous nitrogen ﬂow (50 mL/min).

Wide-Angle X-ray Diﬀraction (WAXD)

Wide-angle X-ray diﬀraction measurements were carried out using a Benchtop Rigaku MiniFlex 600 instrument. The samples were prepared by coating (i.e., drop casting of NOCNF suspension and powder NOCNF deposition) on sample holders made of glass. The Cu Kα radiation was generated at 40 kV and 40 mA (λ = 0.154 nm) using a Ni ﬁlter. Data collection was carried out using a ﬂat holder in Bragg−Brentano geometry (5−50°; 10°min−1). Crystalinity of index (CI) was estimated using the following equation.

CI=I(200)-I(am)I(200)   ………………...Eq. S1

where I(200) is the intensity of the dominant (200) diﬀraction peak, and I(am) is the intensity of the amorphous peak, estimated as the broad background with a maxium peak located between the (200) and (110) diffraction peaks.(Segal, Creely et al. 1959)

Transmission Electron Microscopy (TEM)

TEM studies were carried out by a FEI Tecnai G2 Spirit BioTWIN instrument, operated at an accelerating voltage of 120 kV and equipped with a digital camera. The instrument also possessed photographic ﬁlm capability with goniometer and tilt stage accessories, as well as electron diﬀraction capability. In typical sample preparation, a 10 μL aliquot sample of 1 mg of NOCNF in 10 mL distilled water was deposited on freshly glow discharged carbon coated Cu grids (300 mesh, Ted Pella Inc.).

Atomic Force Microscopy (AFM)

AFM measurement was performed using a Bruker Dimension ICON scanning probe microscope (Bruker Corporation, U.S.A.) equipped with a Bruker OTESPA tip (tip radius (max.) = 10 nm). A 10 μL of 0.005 wt % NOCNF suspension was deposited on the surface of a silica plate, where the air-dried sample was measured in the tapping mode.

Scanning Electron Microscopy (SEM)

The morphological study was recorded by a Zeiss LEO 1550 SFEG-SEM instrument. This instrument consisted of the standard E-T detector, as well as an In-Lens Secondary Electron Detector and a Rutherford Backscatter Electron Detector. The instrument was also equipped with an EDS (energy dispersive X-ray spectroscopy) unit having an EDAX detector, which provided elemental composition information and X-ray maps of the various phases of the materials examined.

Contact Angle Meter (CAM)

An optical contact angle meter (CAM200, KSV instruments, LID) was used to analyze the hydrophobicity of the floc sample. In this measurement, the sample was fixated on a glass slide, where a 5 μL water droplet was dropped on the sample surface. Digital images were collected using the CAM software, where the water contact angle was estimated by a curve fitting method.

Conductometric Titration Method

The carboxyl content in NOCNF (the ionic form) having carboxylate (COONa) groups was determined by using the conductivity titration method.(Saito and Isogai 2004) In this method, 0.3 g of dried NOCNF sample was dispersed in 55 mL of distilled water. The suspension was then set to a pH value in the range of 2.5−3 by adding 0.1 M HCl. The 0.1 M NaOH solution was continuously added to the suspension until the pH value reached 11 (monitored by a pH meter), where the corresponding conductivity of the solution was recorded simultaneously. The carboxylate content of nanoﬁbers (degree of oxidation) was calculated by the following equation.

Content of carboxylatemmolg=V2-V1*C(NaOH)mass of fibers   ………………...Eq.S2

Inductively Coupled Plasma Mass Spectroscopy (ICP-MS)

Elemental concentration analyses were carried out on an Agilent 7500cx quadrupole ICP-MS instrument. Samples were diluted to generate signals that could match the mixed calibration standards, where unknown concentrations were calculated based on the standard calibration curves. The standard was run frequently between the unknown samples in order to monitor the drift in signal intensity of the instrument.

Reference

Saito, T. and A. Isogai (2004). "TEMPO-Mediated Oxidation of Native Cellulose. The Effect of Oxidation Conditions on Chemical and Crystal Structures of the Water-Insoluble Fractions." Biomacromolecules 5(5): 1983-1989.

Segal, L., J. J. Creely, A. E. Martin and C. M. Conrad (1959). "An Empirical Method for Estimating the Degree of Crystallinity of Native Cellulose Using the X-Ray Diffractometer." Textile Research Journal 29(10): 786-794.

Table S1: The pH change of the Hg solution before and after remediation experiments.

| ppm | pH (floc) | pH (before mixing) |
| --- | --- | --- |
| 2.5 | 6.67 | 5.02 |
| 10 | 6.4 | 4.92 |
| 25 | 6 | 4.45 |
| 50 | 5.83 | 4.24 |
| 100 | 5.58 | 4.07 |
| 125 | 5.46 | 3.9 |
| 250 | 5.2 | 3.73 |
| 500 | 5.09 | 3.58 |
| 1000 | 4.66 | 3.44 |

Table S2. Variables from the Hg remediation study.

| Original Hg2+ conc (ppm) Ce | Mass of Hg2+ used (mg) | Original conc of Hg AFS (ppb) | Final conc of Hg AFS (ppb) | Adsorption efficiency | Idea adsorption capacity (mg/g) | Experimental adsorption capacity (mg/g) Qe | Ce/Qe (g/L) | log (Ce) | log (Qe) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2.5 | 0.005 | 500.0 | 57 | 0.885 | 0.625 | 0.553 | 4.519 | 0.398 | -0.257 |
| 10.0 | 0.02 | 500.0 | 73 | 0.854 | 2.5 | 2.136 | 4.682 | 1.000 | 0.330 |
| 25.0 | 0.05 | 500.0 | 79 | 0.842 | 6.25 | 5.262 | 4.751 | 1.398 | 0.721 |
| 50.0 | 0.1 | 500.0 | 75 | 0.850 | 12.5 | 10.630 | 4.704 | 1.699 | 1.027 |
| 100.0 | 0.2 | 250.0 | 46 | 0.816 | 25 | 20.405 | 4.901 | 2.000 | 1.310 |
| 125.0 | 0.25 | 250.0 | 52 | 0.794 | 31.25 | 24.805 | 5.039 | 2.097 | 1.395 |
| 250.0 | 0.5 | 125.0 | 31 | 0.754 | 62.5 | 47.116 | 5.306 | 2.398 | 1.673 |
| 500.0 | 1 | 250.0 | 96 | 0.615 | 125 | 76.911 | 6.501 | 2.699 | 1.886 |
| 1000.0 | 2 | 500.0 | 264 | 0.474 | 250 | 117.992 | 8.475 | 3.000 | 2.072 |

Table S3. The pH effect on Hg remediation.

| Original Hg2+ concentration (ppm) | Hg2+ concentration after mixing and dilution (ppb) | pH | ICP-MS (ppb) | Efficiency |
| --- | --- | --- | --- | --- |
| 100 | 50 | 3 | 32.5 | 0.350 |
|  |  | 5 | 10.1 | 0.798 |
|  |  | 7 | 7.0 | 0.860 |
|  |  | 9 | 5.8 | 0.884 |
|  |  | 11 | 12.2 | 0.756 |

Table S4. The time effect on Hg remediation.

| Time (hr), pH=7 | Original Hg2+ concentration (ppm) | Hg2+ concentration after mixing (ppm) | Hg2+ concentration after dilution (*1000) (ppb) | ICP-MS (ppb) | Efficiency |
| --- | --- | --- | --- | --- | --- |
| 3 | 100 | 50 | 50 | 9.41 | 0.812 |
| 8 | 100 | 50 | 50 | 9.29 | 0.814 |
| 16 | 100 | 50 | 50 | 9.28 | 0.814 |
| 24 | 100 | 50 | 50 | 9.18 | 0.816 |