Supporting Information

A comprehensive investigation of the interactions of human serum albumin with polymeric and hybrid nanoparticles

Merve Seray Ural a,b, Joice Maria Joseph a,b, Frank Wien c, Xue Li a, My-An Tran a, Myriam Taverna, Claire Smadja b*, Ruxandra Gref a*

a Université Paris-Saclay, Institute of Molecular Sciences of Orsay, French National Center for Scientific Research, Orsay, France

b Université Paris-Saclay, Institute Galien, French National Center for Scientific Research, Châtenay-Malabry, France

c Université Paris-Saclay, Synchrotron Soleil, 91190 Saint-Aubin, France

Corresponding authors : Dr. Ruxandra Gref: ruxandra.gref@universite-paris-saclay.fr and Prof. Claire Smadja: claire.smadja@universite-paris-saclay.fr

Table SI1. Characteristics of the NPs: surfactant, hydrodynamic size, PDI and surface charge.

| NP | PLGA | PLGA-PEG | nanoMOF | nanoMOF-PEG |
| --- | --- | --- | --- | --- |
| Surfactant | PVA | PVA | - | - |
| Hydrodynamic size (nm) | 310 ± 15 | 418± 30 | 234 ± 16 | 286 ± 20 |
| PDI | 0.1 | 0.4 | 0.2 | 0.2 |
| Surface Charge (mV) | ̴0 | ̴0 | -18 | -16 |

Fig. SI1. HSA stability study carried on with 1 mg/mL HSA analysed by CE-UV without centrifugation and incubation (blue); after centrifugation without incubation (red); after centrifugation after 1 day incubation (black); after centrifugation after 3 days incubation (green).

Fig. SI2. CE-UV electropherograms of unbounded HSA recovered from supernatants after incubation with PLGA-PEG (orange) and PLGA (red, blue) and NPs during 1 day with a HSA: NP ratio of 1:3 and 1:10.  Black line is the reference HSA solutions of 1 mg/mL.

Fig. SI3. CE-UV electropherograms of unbounded HSA recovered from supernatants after incubation with PLGA (green) and PLGA-PEG (orange) and NPs during 1 day with a HSA: NP ratio of 1:3 and 1:10. Black line is the reference HSA solutions of 1 mg/mL.

A

Fig. SI4: The SR-CD spectra of the PLGA (red) and PLGA-PEG (green) NPs incubated with HSA with 1:3 (HSA:NPs) ratio during 3 days. Black line is the reference HSA solutions of 1 mg/mL incubated without NPs during 3 days.