Supplementary Information

Strong electron-phonon coupling and predicted high superconducting transition temperature of MXenes revealed in 2H-Mo2N under biaxial stress.

Komsilp Kotmool,1,∗ Prutthipong Tsuppayakorn-aek,2,3 Thiti Bovornratanaraks, 2,3 Thanayut Kaewmaraya,4,5 Rachsak Sakdanuphab,1,6 Aparporn Sakulkalavek,7,8 Rajeev Ahuja,8,9 and Wei Luo8

1College of Advanced Manufacturing Innovation, King Mongkut’s Institute of Technology Ladkrabang, Bangkok 10520, Thailand

2Extreme Conditions Physics Research Laboratory and Center of Excellence in Physics of Energy Materials (CE:PEM), Department of Physics, Faculty of Science, Chulalongkorn University, Bangkok 10330, Thailand

3Thailand Center of Excellence in Physics, Ministry of Higher Education, Science, Research and Innovation, 328 Si Ayutthaya Road, Bangkok, 10400, Thailand

4Integrated Nanotechnology Research Center, Department of Physics, Khon Kaen University, Khon Kaen, 40002, Thailand

5Institute of Nanomaterials Research and Innovation for Energy (IN-RIE), NANOTEC-KKU RNN on Nanomaterials Research and Innovation for Energy, Khon Kaen University, Khon Kaen, 40002, Thailand

6Research Center for Quantum Technology, Faculty of Science, Chiang Mai University, Chiang Mai 50200, Thailand

7Department of Physics, School of Science, King Mongkut’s Institute of Technology Ladkrabang, Bangkok 10520, Thailand

8Condensed Matter Theory Group, Materials Theory Division, Department of Physics and Astronomy, Uppsala University, Box 516, SE-75120, Uppsala, Sweden

9Department of Physics, Indian Institute of Technology (IIT), Ropar, Rupnagar 140001, Punjab, India

Stress-strain calculation

The atomic configurations of the 1T- and 2H-Mo2N are displayed in Fig. 1S. The vacuum-slab model of Mo2N is constructed with a vacuum thickness of 20 Å to prevent the interaction between the the nearest layers. The unstressed 1T- and 2H-Mo2N were performed by fully relaxing to get the free-strain crystal structures consisting of lattice parameter (a0) and layer thickness (d). To get the real thickness of two-dimensional materials, the covalent radius (1.45 Å) of Mo atoms is accounted. Therefore, the d value was measured between the topmost and bottommost of the electron distribution. The stress tensor (σxx) was calculated after optimizing atomic positions under a fixed biaxial strain (εb) as defined by Equation (1S). The biaxial stress (σb) is rescaled following Equation (2S).

εb=(a-a0)a0							(1S)

σb=σxx.cd 							(2S)

where a and c are the lattice constants of Mo2N at given biaxial strains.

Critical superconducting temperature (Tc)

Critical superconducting temperature (Tc) is calculated using the Allen-Dynes formula, as shown in equation (3S). The integration of electron-phonon coupling strength (l) and the logarithmic average of the spectral function (wlog) solved by the isotropic Eliashberg theory [1], are obeyed by equations (4S) and (5S), respectively.

TC=ωlog1.2exp-1.04(1+λ)λ-μ*(1+0.62λ)					(3S)

λ=20∞dωωα2F(ω)=qvλqv					(4S)

ωlog=exp2λ0∞dωωα2F(ω)lnω					(5S)

where λqv is electron-phonon coupling constant for mode v at wavevector q defined as

λqv=γqvπhNEfωqv2						(6S)

while γqv is phonon linewidth, and the spectral function (α2F(ω)) is defined as

α2Fω=12πhNEfqvγqvhωqvδ(ω-ωqv)			(7S)

Since l > 1.5, it is classified as strong electron-phonon coupling [2]. The Allen-Dynes formula is needed to be modified by adding the strong coupling correction as written as

Tcs=f1f2ωlog1.2exp-1.04(1+λ)λ-μ*(1+0.62λ)					(8S)

where f1=1+λ2.46(1+3.8μ*)3213, f2=1+(ωrmsωlog-1)λ2λ2+3.31(1+6.3μ*)ωrmsωlog, and ωrms=2λ0∞ωα2F(ω)dω12.

Figure 1S. Partial density of states (PDOS) of 1T and 2H phases of Mo2N at -5%, 0%, and 5% of strains.

Figure 2S. (a) Relative total energy respecting the energy of the 2H- Mo2N at e = 0%, and (b) relative enthalpy respecting those of the 1T- Mo2N via biaxial strain from -6% to 6%. The enthalpy (H) is calculated from the equation; H = E + PeqV, where E is total energy, V is volume of cell, and Peq is the equivalent pressure calculated from the stress tensors.

Figure 3S. Phonon dispersions derived by finite displacement method of 2H-Mo2N at (a) compressive strains of -5% and -7%, and (b) tensile strains of 5% and 6%.

Table 1S. Lattice parameter (a), numbers of electron density at the Fermi level (NEf), logarithmic average of the spectral function (ωlog), integration of the lambda (λ), and critical temperature (Tc) of Mo2N and Mo2C at certain biaxial strains (e).

|  | a (Å) | e (%) | NEf (Ry-1) | wlog (cm-1) | l | Tc (K) |
| --- | --- | --- | --- | --- | --- | --- |
| 2H-Mo2C | 2.835 | 0 | 17.3 | 213 | 0.58 | 4.3 |
| 1T-Mo2N | 2.786 | 0 | 17.8 | 248 | 0.98 | 16.8 |
| 2H-Mo2N | 2.818 | 0 | 17.6 | 227 | 1.32 | 22.7 |
|  | 2.677 | -5.0 | 19.7 | 215 | 1.51 | 24.7 |
|  | 2.705 | -4.0 | 23.2 | 240 | 2.00 | 34.5 |
|  | 2.747 | -2.5 | 22.9 | 195 | 2.22 | 30.1 |
|  | 2.790 | -1.0 | 20.9 | 213 | 1.54 | 25.0 |
|  | 2.846 | 1.0 | 19.4 | 220 | 1.19 | 19.4 |
|  | 2.888 | 2.5 | 20.0 | 212 | 1.25 | 20.0 |
|  | 2.931 | 4.0 | 21.6 | 183 | 1.56 | 21.6 |
|  | 2.959 | 5.0 | 25.3 | 158 | 2.24 | 24.4 |

Table 2S. Root mean square of frequency (wrms), strong-coupling correctness factors (f1 and f2), and superconducting temperatures (Tc and Tcs) of 2H-Mo2N at -4%, -2.5%, and 5% of strain obtained by using the modified Allen-Dynes formula.

| e (%) | wrms (cm-1) | f1 | f2 | f1×f2 | Tc (K) | Tcs (K) |
| --- | --- | --- | --- | --- | --- | --- |
| -4.0 | 222 | 1.13 | 0.97 | 1.09 | 34.5 | 37.8 |
| -2.5 | 203 | 1.15 | 1.02 | 1.18 | 30.1 | 35.4 |
| 5.0 | 166 | 1.15 | 1.03 | 1.18 | 24.4 | 28.9 |

References

[1] Philip B. Allen. Neutron spectroscopy of superconductors. Phys. Rev. B, 6:2577–2579, Oct 1972.

[2] P. B. Allen and R. C. Dynes. Transition temperature of strong-coupled superconductors reanalyzed. Phys. Rev. B, 12:905–922, Aug 1975.