Supplementary Information for

Giant Kerr nonlinearity of terahertz waves mediated by stimulated phonon polaritons in a microcavity chip

Yibo Huang1,2, Yao Lu1,2,*, Wei Li3, Xitan Xu1,2, Xinda Jiang1,2, Ruobin Ma1,2, Lu Chen1, Ningjuan Ruan3, Qiang Wu1,2,* and Jingjun Xun1,*

1The Key Laboratory of Weak-Light Nonlinear Photonics, Ministry of Education, TEDA Applied Physics Institute and School of Physics, Nankai University, Tianjin 300457, China

2Shenzhen Research Institute of Nankai University, Shenzhen, Guangdong 518083, China

3Beijing Institute of Space Mechanics & Electricity, China Academy of Space Technology, Beijing, 100094, China

Supplementary Note 1: Sample fabrication

The lithium niobite (LN) Fabry-Perot microcavity utilized in our experiment is fabricated using a chemically assisted femtosecond-laser direct writing technique1. Fig. S1 depicts the schematic diagram of the experimental laser-machining setup for the sample fabrication. The machining laser (800 nm central wavelength, 500 μJ per pulse, 1 kHz repetition rate, 120 fs pulse duration) first passes through a shutter, which is used to block the laser when moving from one machining region to the next, and then passes through a power control system composed of a half-wave plate (HWP) and a Glan-Taylor prism (GTP). After passing through a dichroic mirror (DM), the laser is focused on a x-cut LN slab coated with 1 μm thick silicon dioxide on both surfaces through an objective, wherein the sample is mounted on an xyz-translation stage with computer-controlled actuators. The air slots are cut out by focusing the laser at multiple depths spanning from the front to the back. To monitor the machining in real time, a beam of incoherent light illuminates the sample and is imaged on a CCD camera.

After the machining, the sample is immersed in hydrofluoric acid solution for 20-30 minutes to remove the coating along with accumulated debris. A microscope image of a microcavity we sued in the experiment is shown in Fig. S2, the width of an air slot is set to be 50 μm and the width of a LN pillar between two slots is also set to be 50 μm, the length of the cavity is set to be 245 μm. The machining error is approximately 2 microns, which has negligible effects on the experiment.

Fig. S1. Schematic diagram of the experimental laser-machining set-up for the sample fabrication. HWP: half-wave plate, GTP: Glan-Taylor prism, DM: dichroic mirror, CL: convex lens, CLS: cold light source.

Fig. S2. Microscope image of the microcavity used in the experiment. The air slot and LN pillar are designed to have a width of 50 microns, the cavity is intended to have a length of 245 microns, while the machining error is about 2 microns.

Supplementary Note2: Theoretical analysis of phonon-polariton enhanced optical Kerr nonlinearity with modified Huang equations.

Under an external driving of the THz wave, and along with the contribution of phonon-polaritons, the Vibration equation of ions is written as follows:

x+γx+ω02x=Nm-1/2bE-βx3+qmEexP=Nm1/2bx+ϵ0ε∞-1E#S1

where x represents the motion amplitude of ions, the electric charge, eigen angular frequency and effective mass of ions are indicated by q, ω0 and m. Eex stands for the corresponding driving THz field, and the strength of the damping force and the anharmonicity (i.e., the nonlinearity) are characterized by parameters γ and β, respectively. The contribution of phonon polariton is the term Nm-1/2b12E, and the values of the coupling coefficients are determined by b=ω0ϵ0ε0-ε∞, ϵ0 is the permittivity of vacuum, ε0 and ε∞ stand for the low- and high-frequency relative permittivity of the material. E represents the macroscopic electric field radiated by the ions. Cooperating with Maxwell’s equations, the polarization P can be eliminated from the above equations:

ϵ0μ0ε∞E+μ0Nm1/2bx-∇2E=0#S2

Adopting the slow time approximation, that is assuming x=x0ⅇ-jωt and E=E0ⅇ-jωt with ω being the angular frequency of the driving THz field, where x0 and E0 are independent of t, and assuming ∇2E=-k2E=ϵ0ω2/c2E, the following equation can be obtained:

Nm-1/2bE=ω02x#S3

Here, c=1ϵ0μ0 indicates the light speed in the vacuum and μ0 is the permeability of the vacuum. Finally, a Drude dispersion equation is obtained:

x+γx=-βx3+qmEex#S4

This equation indicates an impressive delocalization of phonon-polaritons, and that the mobility of phonon-polaritons is comparable to that of the free electrons in a metal. The ionic nonlinearity can be prodigiously enhanced because of phonon-polaritons.

Using the conventional method in nonlinear optics2, we seek a solution having the form of a power series in parameter ξ:

x=ξx1+ξ2x2+ξ3x3+⋯#S5

We insert this equation into the Drude dispersion equation, while retaining the terms up to ξ3, then get three equations:

x1+γx1=qEexm#S6

x2+γx2=0#S7

x3+γx3+βx13=0#S8

We can get the solutions as follows:

x1ωn,t=qE0ωnmDωn#S9

x2ωn,t=0#S10

x3ωq,t=mnpbq3E0ωmE0ωnE0ωpm3DωqDωmDωnDωpe-ⅈωqt#S11

Here, Dωn=-ωn2-iγωn, ωm, ωn, ωp and ωq are the angular frequency of the driving THz field, and ωq=ωm+ωn+ωp. The amplitude of the polarization component oscillation at frequency ωq is given in terms of this amplitude by

P3=-Nqx3ωq,t#S12

And the definition of the third-order nonlinear susceptibility is

P3=mnpϵ0χ3ωq;ωm,ωn,ωpEωmEωnEωp#S13

Based on the equations above, we finally get the third-order nonlinear susceptibility

χ3ωq;ωm,ωn,ωp=Nβq4m3ϵ0DωqDωmDωnDωp#S14

We assume that the harmonic and anharmonic term in the potential energy should be comparable in magnitude, we can get the parameter

β=ω02N2/3#S15

Take the values for an LN crystal, ω0=7.6 THz, N=6.29×1027m-3 and γ=0.84 THz, the reduced mass m=5 u, 1 u=1.66×10-27 kg, and the charge q= 5 e, where ⅇ=1.6×10-19 C is the elementary charge. The third-order nonlinear susceptibility at 0.63 THz is calculated to be Reχ3=7.25×10-15 m2∕V2.

For comparison, if neglecting the contribution of phonon-polaritons, the lattice vibration is described by the classical anharmonic oscillator model:

x+γx+ω02x+βx3=qmEex#S16

Using the same method as above, we finally get the third-order nonlinear susceptibility

χ3ωq;ωm,ωn,ωp=Nβq4m3ϵ0DωqDωmDωnDωp#S17

But here, Dωn=ω02-ωn2-iγωn, and the parameters are all the same as above, the third-order nonlinear susceptibility without the contribution of phonon polaritons at 0.63 THz is calculated to be Reχ3=4.58×10-22 m2∕V2. Our results align more with the enhanced susceptibility of phonon-polaritons rather than mere ionic nonlinearity, suggesting that the giant nonlinearity originates from the strong coupling between phonons and light.

References

1.	Sivarajah, P. et al. Chemically assisted femtosecond laser machining for applications in LiNbO3 and LiTaO3. Applied Physics A: Materials Science & Processing 112, 615-622 (2013).

2.  Boyd, R. W. Nonlinear Optics. 4th edition (Elsevier Science, 2020).