Supplementary data

Fig. S1. Zero-point charge of (A) Zn-impregnated water hyacinth, and (B) Quantitative Zn loading on water hyacinth.

Fig. S2. FESEM and Mapping images along with EDX of carbon hybrids obtained at 280 °C with (A) Fe/Zn-impregnation, (B) Cu/Zn-impregnation, and (C) Fe/Cu/Zn-impregnation.

Fig. S3. BET curves of carbon hybrids obtained at 280 °C with (A) Fe/Zn-impregnation, (B) Cu/Zn-impregnation, and (C) Fe/Cu/Zn-impregnation.

Fig. S4. 1H NMR of (A) Heavy oil, (B) Light oil, 13C NMR of (C) Heavy oil, and (D) Light oil by HTL of bi and tri-metallic impregnated water hyacinth at 280 °C.

Table S1. Proximate and ultimate analysis of Raw and metal-impregnated Water Hyacinth.

| Analysis | Raw-WH | Zn-WH | Fe/Zn-WH | Cu/Zn-WH | Fe/Cu/Zn-WH |
| --- | --- | --- | --- | --- | --- |
| Proximate analysisa |  |  |  |  |  |
| Volatile matter | 72.3 | 60.6 | 61.5 | 64.1 | 63.7 |
| Ash content | 7.10 | 10.9 | 12.7 | 21.6 | 27.8 |
| Fixed carbon | 20.6 | 28.5 | 25.8 | 14.3 | 8.50 |
| Ultimate analysisb |  |  |  |  |  |
| C | 35.9 | 34.7 | 29.4 | 28.6 | 29.6 |
| H | 5.39 | 5.46 | 4.70 | 5.93 | 4.78 |
| N | 2.11 | 1.61 | 3.03 | 6.10 | 2.37 |
| S | 0.01 | 0.02 | 2.00 | 6.90 | 1.11 |
| O* | 56.5 | 58.2 | 60.8 | 52.4 | 62.1 |
| Fe (MP-AES) | - | - | 8.13 | - | 1.83 |
| Cu (MP-AES) | - | - | - | 6.6 | 11.4 |
| Zn (MP-AES) | - | 8.04 | 8.38 | 4.07 | 7.19 |

a: dry basis, wt.%, b: dry and ash-free basis, wt.%, O*: 100 - (C+ H+ N+ S)