Figure S1: TLC analysis on effect of different pretreatment of CCB (Lanes 1-Commercial xylan; 2- Standard Xylose; 3- untreated CCB; 4-US+ZnO; 5- PC; 6- US 20 for 30 min ; 7- US 20 for 60 min; 8- SP 20 for 30 min; 9- SP 20 for 60 min)

Figure S2: TLC analysis of varying sonication amplitude on CCB xylan extraction

Lane1: commercial xylan; Lane2: Standard Xylose; Lane (3-5): SP 50, 70 and 90 respectively; Lane (6-8): US 50, 70 and 90 respectively.

Figure S3 : FTIR spectra of untreated and preated CCB with wavelength range of 400-4000cm-1

(b)

(a)

(c)

Figure S4: Particle size distribution of CCB (a) untreated, (b) PC (c) US and SP 90 pretreated

Table S1: Particle size of CCB before and after pretreatment

| Treatment | Size of CCB particle (μm) |
| --- | --- |
| Untreated | 417±1.5 |
| PC | 401±1.4 |
| US 90 & SP 90 | 170±1.2 |