Supplementary Information

Chemo-electro-mechanics of nanodefects in solid-state batteries: A phase-field simulation

Yuki Kamikawa,1,* Koji Amezawa,2 and Kenjiro Terada3

1Research Division, Nissan Motor Co., Ltd. Natsushima 1, Yokosuka, Kanagawa, 237-0061

2Institute of Multidisciplinary Research for Advanced Materials, Tohoku University, 2-1-1 Katahira, Aoba-ku, Sendai 980-8577, Japan

3International Research Institute of Disaster Science, Tohoku University, 468-1-S403, Aoba, Aramaki, Aoba-ku, Sendai 980-8572, Japan

Supplementary Note 1. First-principles simulations

Supplementary Note 2. Mathematical formulation of plastic flow

Supplementary Note 3. Boundary conditions for the phase-field simulation

Supplementary Note 1. First-principles simulations

The interfacial structures were constructed based on surface slabs with stable LLZO and Li metal terminations. A body-centered cubic (bcc)-type Li crystal structure was adopted in this study. A lattice matching strategy was performed to minimize the internal stress induced by the lattice-mismatch strain. The interface between the Li(100) and Zr-poor LLZO(100) faces was selected as it is the lowest energy surface. Rigid-body displacement was applied along directions parallel and perpendicular to the interfacial plane between the LLZO and Li metal. Based on previous density functional theory (DFT) results [35], the lengths of vectors of the created superlattice (u, v) and the angle between the two surface vectors (γ) of the lattice-matched superlattices were u = 13.205 Å, v = 12.675 Å, γ = 90 for LLZO(100), and u = v = 13.728 Å, γ = 90 for 4 × 4Li(100). The value of parallel (du,dv) and vertical displacement (dw) were set to du = 0.825 Å, dv= 0.792 Å and dw = 2 Å. First-principles calculations were performed within the framework of DFT, as implemented in the Quantum ESPRESSO package. For the exchange correlation energy, we used the Perdew–Burke–Ernzerhof (PBE) version of the generalized gradient approximation (GGA). Fermi smearing of the electron occupancy with 0.01 Ry and a plane-wave cut-off of 50 Ry were used. The underlying structures were optimized using the Broyden–Fletcher–Goldfarb–Shanno (BFGS) method, with the convergence criteria of 1 × 10-7 Ry for the energy and 3 × 10-4 Ry/Bohr for the force. The Monkhorst–Pack k-point mesh was selected following the rule that k × a ≥ 60 Å, where a is the length of the basis vector, and k is the number of k-points in any direction.

Supplementary Note 2. Mathematical formulation of plastic flow

The Levy–Mises associated flow rule was used to describe the plastic deformation of Li metal:

Φσ≡32devσ-σy=0

dεpl=dλ∂Φ∂σ

(s1)

where εpl is the yield stress of lithium, dεpl is the incremental of plastic strain tensor εpl, and dλ is the plastic multiplier that can be determined from the boundary conditions of the problem and from the constraint of perfect plasticity (or s:s=23σy2, where s is deviatoric stress).

Supplementary Note 3. Boundary conditions for the phase-field simulation

Dirichlet boundaries of φ= 0 and -0.1 V were used for the Li metal anode, and cLi+ = 1 and φ = 0.0 V were employed on the side opposite the anode to mimic the constant voltage plating condition. In this situation, note that no deviatoric component exists in the stress tensor; thus, the low yield stress of lithium metal is not relevant (i.e., the plastic flow of Li does not occur in the GBs). In both simulations, a roller boundary condition was applied at the left and bottom edges of the simulation domain. Symmetry was applied to the left and right sides of the model. All parameters used in the model are summarized in Table S1. The modeling framework elaborated above was implemented in the COMSOL Multiphysics platform using a finite element solver with implicit time integration.

Table S1. Parameters for phase-field simulation

| Domain | Physical properties |  | Ref |
| --- | --- | --- | --- |
| Bulk | Surface energy of LLZO | 0.85 J∙m−2 | [65] |
|  | Electron concentration of LLZO | 1.66 mol∙m-3 | [66] |
|  | Young's modulus of Li | 7.82 GPa | [67] |
|  | Young's modulus of LLZO | 149.8 GPa | [68] |
|  | Poisson's ratio of Li | 0.381 | [67] |
|  | Poisson's ratio of LLZO | 0.257 | [68] |
|  | Mobile Li ion concentration in LLZO | 5.26 × 103 mol∙m-3 | [41] |
|  | Site density of Li metal | 76.4 × 104 mol∙m-3 | [36] |
|  | Li+ diffusivity in Li | 5.0 × 10-15 m2∙s-1 | [69] |
|  | Li+ diffusivity in LLZO, DSE | 2.9 × 10-12 m2∙s-1 | [41] |
|  | Conductivity of Li | 1.03 × 107 S∙m-1 | [70] |
|  | Conductivity of LLZO, σSE | 6.34 × 10−1 S∙m-1 | [41] |
|  | Inelastic strain constant, K11 | 2.1 × 10-4 | [4] |
|  | Inelastic strain constant, K22 | 2.1 × 10-4 | [4] |
|  | Inelastic strain constant, K33 | 2.1 × 10-4 | [4] |
|  | Yield stress of Li | 1.26 MPa | [18] |
|  | Partial molar volume of Li, Vm | 1.3 × 10−5 m3/mol | [71] |
| Grain boundary | D for Σ1 | 0.06 | [25] |
|  | σ for Σ1 | 5.82 × 10−4 | [25] |
|  | C(=CGB/CSE) for Σ1 | 0.5 | [37] |
|  | D, for Σ3 | 1.78 | [25] |
|  | σ for Σ3 | 3.33 | [25] |
|  | C(=CGB/CSE) for Σ3 | 0.5 | [37] |
| Phase-field parameters | Interfacial mobility | 2.5 × 10-6 J(m∙s)-1 | [4] |
|  | Electrochemical pre-factor | 15.625 s-1 | [4] |
|  | Interface kinetics coefficient, 𝐿σ | 1.0 × 10-9 m2(N∙s)-1 | [72] |
|  | Height of the double-well potential | 3.5 × 106 J∙m-3 | [72] |
|  | Parameter for interpolation function, k | 0.01 |  |

Supplementary References

[65] Tian, H. -K., Xu, B., Qi, Y., Computational study of lithium nucleation tendency in Li7La3Zr2O12 (LLZO) and rational design of interlayer materials to prevent lithium dendrites. J. Power Sources 392, 79–86 (2018) (DOI 10.1016/j.jpowsour.2018.04.098)

[66] Squires, A. G. et al. Low electronic conductivity of Li7La3Zr2O12 solid electrolytes from first principles. Phys. Rev. Mater. 6, 085401 (2022) (DOI 10.1103/PhysRevMaterials.6.085401)

[67] Masias, A., Felten, N., Garcia-Mendez, R., Wolfenstine, J. & Sakamoto, J. Elastic, plastic, and creep mechanical properties of lithium metal. J. Mater. Sci. 54, 2585–2600 (2019) (DOI 10.1007/s10853-018-2971-3)

[68] Ni, J. E., Case, E. D., Sakamoto, J. S., Rangasamy, E. & Wolfenstine, J. B. Room temperature elastic moduli and Vickers hardness of hot-pressed LLZO cubic garnet. J. Mater. Sci. 47, 7978–7985 (2012) (DOI 10.1007/s10853-012-6687-5)

[69] Lodding, A., Mundy, J. N. & Ott, A. Isotope inter-diffusion and self-diffusion in solid lithium metal. Phys. Stat. Sol. b 38, 559–569 (1970) (DOI 10.1002/pssb.19700380206)

[70] Creffield, G.K., Down, M.G. & Pulham, R.J., Electrical resistivity of liquid and solid lithium. J. Chem. Soc. Dalton Trans. 21, 1974, 2325–2329 (1974) (DOI 10.1039/DT9740002325)

[71] Ahmad, Z. & Viswanathan, V. Stability of electrodeposition at solid-solid interfaces and implications for metal anodes. Phys. Rev. Lett. 119, 056003 (2017) (DOI 10.1103/PhysRevLett.119.056003)

[72] Zhao, Y., Wang, R. & Martínez-Pañeda, E. A phase field electro-chemo-mechanical formulation for predicting void evolution at the Li–electrolyte interface in all-solid-state batteries. J. Mech. Phys. Solids. 167, 104999 (2022) (DOI 10.1016/j.jmps.2022.104999)