Supporting Information for

Enhanced stability and optoelectronic properties of Potential Lead-free Double Perovskite Oxides Ba2TbBiO6 by Sb doping for solar cells

Md. Lokman Ali1*, Zahid Hasan1, Mithun Khan1

1Department of Physics, Pabna University of Science and Technology, Pabna-6600, Bangladesh

Dayal Chandra Roy2,

2Faculty of Science and Engineering, Iwate University, Morioka, 020-8551, Japan

Structural properties

Table S1. The calculated structural parameters of  Ba2TbBi1-xSbxO6 (x=0.0, 0.5) perovskite.

| Phase | Doping (%) | a (Å) | b (Å) | c (Å) | V (Å3) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Cubic | 0% | 8.7280 | 8.7280 | 8.7280 | 664.8814 | [This work] |
|  | 0% | 8.7397 | 8.7397 | 8.7397 | 667.5589 | Expt. [1] |
|  | 50% | 8.6390 | 8.6390 | 8.6390 | 644.7486 | [This work] |
| Monoclinic | 0% | 8.6897 | 6.1486 | 6.1887 | 330.4307 | [This work] |
|  | 0% | 8.7037 | 6.1652 | 6.1909 | 332.2040 | Expt. [1] |
|  | 50% | 10.5485 | 6.0946 | 5.0000 | 321.4444 | [This work] |

Lattice distortion

Table S2. The volumetric distortion (Δ) and linear distortion (δ) (i.e; the lattice mismatch strain) for cubic and monoclinic structure of Ba2TbBi1-xSbxO6(x=0,0.5) perovskite.

| Phase | Linear distortion along a, δa | Linear distortion along b, δb | Linear distortion along c, δc | Linear distortion, δ (≈∆3) | Volumetric distortion, Δ |
| --- | --- | --- | --- | --- | --- |
| Cubic | - | - | - | 0.03028 | 0.03028 |
| Monoclinic | 0.2139084 | 0.0087824 | 0.1920 | 0.138230 | 0.0271957 |

Elastic properties

The Born stability criteria for the cubic structure [2]:

| C11+ 2C12 > 0, C11-C12 > 0, and C44 > 0 |  |
| --- | --- |

and for the monoclinic structure [3]:

| C11 - P > 0, C22 - P > 0, C33 - P > 0, C44 - P > 0, C55 - P > 0, C66 - P>0 |  |
| --- | --- |
| C11 + C22 + C33 + 2C12 + 2C13 + 2C23 + 3P > 0 |  |
| (C11 – P) (C33 - P) > C235, (C44 - P) (C66 - P) > C246, (C22 + C33 – 2C23 – 4P) > 0 |  |
| (C22 – P) [(C33 – P) (C55 - P) – C235] + 2(C23 – P) C25C35 > (C23 + P)2 (C55 – P) + C225 (C33 – P) |  |
| 2C15C25[(C33 – P) (C12 + P) – (C13 + P) (C23 + P)]+2C15C35[(C22 – P) (C13 + P) – (C12 + P) (C23 + P)]+2C25C35[(C11 – P) (C12 + P) – (C12 + P) (C13 + P)] -C215 [(C22 – P) (C33 – P) – (C23 + P)2] – C225 [(C11 – P) (C33 – P) – (C13 + P)2] -C235 [(C11 – P) (C22 – P) – (C12 + P)2]+(C55 – P) [(C13 – P) (C22 – P) (C33 – P) – (C11 – P) – (C23 + P)2– (C22 – P) (C13 + P)2 – (C33 – P) (C12 + P)2 + 2(C12 + P) (C13 + P) (C23 + P)] > 0 |  |

These conditions are related to various crystal deformations. The calculated elastic constants of lead-free Ba2TbBi1-xSbxO6 (x=0.0, 0.5) perovskite meet the requirements, suggesting great mechanical stability.

Table S3. Computed elastic constants for the undoped and doped cubic phases of Ba2TbBi1-xSbxO6 (x=0.0, 0.5) perovskite.

| Doping (%) | C11 (GPa) | C12 (GPa) | C44 (GPa) |
| --- | --- | --- | --- |
| 0% | 250.77 | 61.68 | 59.92 |
| 50% | 261.56 | 66.73 | 67.79 |

Table S4. Computed elastic constants for the undoped and doped monoclinic phases of Ba2TbBi1-xSbxO6 (x=0.0, 0.5) perovskite.

| Doping (%) | C11 (GPa) | C22 (GPa) | C33 (GPa) | C12 (GPa) | C13 (GPa) | C23 (GPa) | C44 (GPa) | C55 (GPa) | C66 (GPa) | C15 (GPa) | C25 (GPa) | C35 (GPa) | C46 (GPa) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0% | 232.41 | 214.86 | 226.55 | 59.89 | 71.81 | 90.44 | 33.51 | 37.75 | 62.96 | 0.29 | 0.14 | 0.13 | -0.20 |
| 50% | 232.29 | 225.73 | 224.00 | 70.48 | 86.81 | 86.02 | 63.50 | 66.81 | 78.62 | 0.54 | 0.24 | 0.35 | -0.15 |

Mechanical properties

Table S5. The calculated bulk modulus, shear modulus, Young’s modulus, Pugh’s ratio, Poisson’s ratio of Ba2TbBiO6 perovskite.

| Phase | Doping (%) | Bulk modulus, B (GPa) | Shear modulus, G (GPa) | Young’s modulus, E (GPa) | Pugh’s ratio, B/G | Poisson’s ratio, ν |
| --- | --- | --- | --- | --- | --- | --- |
| Cubic | 0% | 124.70 | 71.98 | 181.08 | 1.73 | 0.258 |
|  | 50% | 131.23 | 78.023 | 195.35 | 1.68 | 0.252 |
| Monoclinic | 0% | 124.07 | 32.25 | 89.03 | 3.85 | 0.380 |
|  | 50% | 129.73 | 70.40 | 178.84 | 1.84 | 0.270 |

Table S6. The calculated bulk modulus B (GPa), shear modulus G (GPa), Young’s modulus E (GPa), Pugh’s ratio B/G , Poisson’s ratio ν, Universal Anisotropy AU, Kleinman parameter ζ,  and machinability index μM of Ba2TbBi1-xSbxO6 x=0.0, 0.5 perovskite.

| Phase | Doping (%) | BV | BR | B | GV | GR | G | E | B/G | ν | AU | ζ | μM |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cubic | 0% | 124.7 | 124.7 | 124.7 | 73.75 | 70.20 | 71.98 | 181.08 | 1.73 | 0.26 | 6.25 | 0.40 | 2.08 |
|  | 50% | 131.23 | 131.23 | 131.23 | 79.31 | 76.74 | 78.02 | 195.35 | 1.68 | 0.25 | 6.17 | 0.41 | 1.94 |
| Monoclinic | 0% | 124.23 | 123.9 | 124.07 | 50.92 | 13.57 | 32.25 | 89.03 | 3.85 | 0.38 | 25.76 | 0.41 | 3.70 |
|  | 50% | 129.85 | 129.61 | 129.73 | 71.03 | 69.76 | 70.40 | 178.84 | 1.84 | 0.27 | 12.09 | 0.45 | 2.04 |

Table S7. The minimum and maximum limits of E (GPa), β (TP-1), G (GPa), and 𝜈 of Ba2TbBi1-xSbxO6 x=0.0, 0.5 perovskite.

| Phase | Doping (%) | E |  |  | β |  |  | G |  |  | ν |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Emin | Emax | AE | βmin | βmax | Aβ | Gmin | Gmax | AG | νmin | νmax | Aν |
| Cubic | 0% | 154.9 | 226.39 | 1.46 | 2.67 | 2.68 | 1.00 | 59.91 | 94.51 | 1.58 | 0.15 | 0.40 | 2.67 |
|  | 50% | 172.2 | 234.6 | 1.36 | 2.53 | 2.56 | 1.01 | 66.98 | 97.45 | 1.45 | 0.16 | 0.37 | 2.31 |
| Monoclinic | 0% | 13.03 | 204.67 | 15.71 | 2.25 | 2.99 | 1.33 | 3.35 | 77.42 | 23.11 | -1.02 | 1.73 | -1.70 |
|  | 50% | 156.85 | 201.29 | 1.28 | 2.43 | 2.83 | 1.16 | 58.28 | 87.83 | 1.51 | 0.14 | 0.38 | 2.71 |

Table S8. Influence of doping on hardness of Ba2TbBi1-xSbxO6 x=0.0, 0.5 perovskite.

| Phase | Doping (%) | H1 | H2 | H3 | H4 | H5 | H6 | H7 | H8 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cubic | 0% | 12.01 | 10.99 | 10.62 | 11.50 | 9.83 | 7.92 | 11.50 | 43.35 |
|  | 50% | 12.64 | 11.86 | 11.51 | 12.40 | 10.90 | 8.75 | 13.02 | 43.94 |
| Monoclinic | 0% | 11.95 | 5.40 | 4.76 | 5.65 | 2.81 | 3.60 | 2.58 | 70.88 |
|  | 50% | 12.49 | 10.86 | 10.38 | 11.36 | 9.55 | 7.83 | 10.80 | 46.17 |

The formulae below can be used to calculate bulk anisotropy (AB) and shear anisotropy (AG) [4].

| For cubic phase, AG=Gv-GR2GH |  |
| --- | --- |
| For monoclinic phase,AG=Gv-GRGv+GR |  |
| AB=BV-BRBV+BR |  |

Also, the C44 values for Voigt and Reuss C44v and C44R , respectively, calculated by using the formulas below [5]:

| C44R=53 C44(C11-C12) 3 C11- C12+4C44 |  |
| --- | --- |
| C44V=35(C11-C12-2C44)² 3 C11- C12+4C44 |  |

Table S9. The Voigt and Reuss values of C44R &  C44V (in GPa), Aeq,AG, AB, and  AL of Ba2TbBi1-xSbxO6 x=0.0, 0.5 perovskite.

| Phase | Doping (%) | C44R | C44V | Aeq | AG | AB | AL |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Cubic | 0% | 23.40 | 3.57 | 6.01 | 0.02 | 0.00 | 9.40 |
|  | 50% | 25.73 | 2.46 | 5.94 | 0.02 | 0.00 | 11.74 |
| Monoclinic | 0% | 14.79 | 10.25 | 23.42 | 0.58 | 1.34 | 1.83 |
|  | 50% | 23.16 | 0.98 | 11.99 | 9.02 | 0.01 | 15.81 |

Thermodynamics properties

The mean speed of sound vm can be calculated by using the equation below [6]:

| vm=[122vt3+1vl3]- 13 |  |
| --- | --- |

where, vl denotes the longitudinal sound velocity and vt is the transverse sound velocity, which may be calculated using Nevier’s relation [6].

| vl=(3B+4G3ρ)12 |  |
| --- | --- |
| and,vt=(Gρ)12 |  |

Table 10. Influence of doping on density ρ, Transverse velocity vt, Longitudinal velocity vl, Debye Temperature ϴD, Grüneisen parameter γ, thermal expansion co-efficient, ∝, minimum thermal conductivity Kmin, and melting point Tm of Ba2TbBi1-xSbxO6(x=0,0.5) in cubic and monoclinic structure.

| Crystal Structure | Doping (%) | ρ (gmcm3) | vt (ms-1) | vl (ms-1) | vm (ms-1) | θD (K) | Kmin | γ | Tm | ∝ (10-5) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cubic | 0% | 7.38 | 3121.90 | 5466.44 | 2031.15 | 237.21 | 0.4304 | 1.55 | 1482.38 | 2.22 |
|  | 50% | 7.17 | 3299.90 | 5730.15 | 2105.99 | 248.48 | 0.4555 | 1.50 | 1529.21 | 2.05 |
| Monoclinic | 0% | 7.41 | 2085.50 | 4746.85 | 1582.96 | 185.24 | 0.3368 | 2.41 | 1391.06 | 4.96 |
|  | 50% | 7.18 | 3131.30 | 5580.46 | 2038.54 | 240.75 | 0.4417 | 1.60 | 1386.87 | 2.27 |

References

[1]  W.T.A. Harrison, K.P. Reis, A.J. Jacobson, L.F. Schneemeyer, J.V. Waszczak, Chem. Mater, 
       1995, 11, 2161-2167.

[2] M. Born, On the stability of crystal lattices. I., Mathematical Proceedings of the Cambridge  
       Philosophical Society, Cambridge University Press, 1940, vol. 36, iss. 2.

[3] Hosford, William F. "The mechanics of crystals and textured polycrystals." Oxford University 
       Press (USA), 1993, 248.

[4]  Naher MI, Naqib SH (2022) Possible applications of Mo2C in the orthorhombic and hexagonal phases 
        explored via ab-initio investigations of elastic, bonding, optoelectronic and thermophysical properties.  
        Results in Phys, 37:105505.

[5] Liu, S. Y., Zhang, S., Liu, S., Li, D. J., Li, Y., Wang, S., “Phase stability, mechanical properties 
      and melting points of high-entropy quaternary metal carbides from first-principles”, Journal 
      of the European Ceramic Society, 2021, 41(13), 6267-6274.

[6] Qi, L., Jin, Y., Zhao, Y., Yang, X., Zhao, H. and Han, P., 2015. The structural, elastic, electronic 
      properties and Debye temperature of Ni3Mo under pressure from first-principles. Journal of 
      Alloys and Compounds, 100(621), 383-388.