# ANNEX 1

Table 1. Means and standard deviation (SD) of removal torque analysis in N/cm2 of implants with different surface treatments at 15 and 45 days.

| Removal torque (N/cm2) | Groups |  |  |  |
| --- | --- | --- | --- | --- |
| Periods | C (Mean±SD) | MN (Mean±SD) | MNSr (Mean±SD) | MNSr+ (Mean±SD) |
| 15 days | 2,725±1,509 Aa | 3,214±1,533 Aa | 2,913±0,9553 Aa | 4,600±1,115 Aa |
| 45 days | 5,600±1,124 Aa | 9,144±3,100 Bb | 8,990±1,502 Bb | 11,10±4,098 Bb |

Distinct superscript letters (upper case compares periods in the column, lower case compares surface treatments in the row) indicate statistical difference to the Two-Way ANOVA test followed by Tukey (p<0.05).

Table 2. Means and standard deviation (SD) of bone-to-implant contact (BIC) analysis in percent in the cortical bone region of implants with different surface treatments at 15 and 45 days.

| Cortical BIC (%) | Groups |  |  |  |
| --- | --- | --- | --- | --- |
| Periods | C (Mean±SD) | MN (Mean±SD) | MNSr (Mean±SD) | MNSr+ (Mean±SD) |
| 15 days | 25,40±17,98 Aa | 54,77±22,45 Ab | 31,04±15,24 Aa | 32,16±14,57 Aab |
| 45 days | 32,12±20,95 Aa | 51,92±23,49 Aab | 56,85±20,26 Bb | 48,07±16,69 Aab |

Distinct superscript letters (upper case compares periods in the column, lower case compares surface treatments in the row) indicate statistical difference to the Two-Way ANOVA test followed by Tukey (p<0.05).

Table 3: Means and standard deviation (SD) of bone-to-implant contact analysis (BIC) in percent in the medullary bone region of implants with different surface treatments at 15 and 45 days.

| Medullary BIC (%) | Groups |  |  |  |
| --- | --- | --- | --- | --- |
| Periods | C (Mean±SD) | MN (Mean±SD) | MNSr (Mean±SD) | MNSr+ (Mean±SD) |
| 15 days | 18,35±8,852 Aa | 34,88±19,79 Aa | 32,39±17,89 Aa | 26,84±18,01 Aa |
| 45 days | 38,13±14,16 Ba | 52,06±22,33 Ba | 52,00±17,61 Ba | 43,80±20,29 Aa |

Distinct superscript letters (upper case compares periods in the column, lower case compares surface treatments in the row) indicate statistical difference to the Two-Way ANOVA test followed by Tukey (p<0.05).

Table 4. Means and standard deviation (SD) of Bone Area Fraction Occupancy (BAFO) analysis in percent in the cortical bone region on implants with different surface treatments at 15 and 45 days.

| Cortical BAFO (%) | Groups |  |  |  |
| --- | --- | --- | --- | --- |
| Periods | C (Mean±SD) | MN (Mean±SD) | MNSr (Mean±SD) | MNSr+ (Mean±SD) |
| 15 days | 31,42±9,424 Aa | 38,65±21,04 Aa | 41,74±15,01 Aa | 24,72±14,81 Aa |
| 45 days | 58,22±11,39 Ba | 53,71±22,86 Aa | 57,70±20,16 Ba | 47,94±19,34 Ba |

Distinct superscript letters (upper case compares periods in the column, lower case compares surface treatments in the row) indicate statistical difference to the Two-Way ANOVA test followed by Tukey (p<0.05).

Table 5. Means and standard deviation (SD) of Bone Area Fraction Occupancy (BAFO) analysis in percent in the medullary bone region on implants with different surface treatments at 15 and 45 days.

| Medullary BAFO (%) | Groups |  |  |  |
| --- | --- | --- | --- | --- |
| Periods | C (Mean±SD) | MN (Mean±SD) | MNSr (Mean±SD) | MNSr+ (Mean±SD) |
| 15 days | 33,83±11,10 Aa | 25,44±18,97 Aa | 31,21±9,871 Aa | 22,47±15,86 Aa |
| 45 days | 40,38±21,46 Aa | 37,19±18,10 Aa | 28,90±15,94 Aa | 23,99±13,68 Aa |

Distinct superscript letters (upper case compares periods in the column, lower case compares surface treatments in the row) indicate statistical difference to the Two-Way ANOVA test followed by Tukey (p<0.05).

Table 6. Means and standard deviation (SD) of bone volume fraction (BV/TV) in percent in the cortical bone region on implants with different surface treatments at 15 and 45 days.

| Cortical BV/TV (%) | Groups |  |  |  |
| --- | --- | --- | --- | --- |
| Periods | C (Mean±SD) | MN (Mean±SD) | MNSr (Mean±SD) | MNSr+ (Mean±SD) |
| 15 days | 23,28±2,134 Aa | 22,14±4,709 Aa | 21,98±1,123 Aa | 21,53±2,950 Aa |
| 45 days | 24,62±2,852 Aa | 21,24±3,926 Aa | 22,31±3,723 Aa | 21,36±2,067 Aa |

Distinct superscript letters (upper case compares periods in the column, lower case compares surface treatments in the row) indicate statistical difference to the Two-Way ANOVA test followed by Tukey (p<0.05).

Table 7: Means and standard deviation (SD) of bone volume fraction (BV/TV) in percent in the medullary bone region on implants with different surface treatments at 15 and 45 days.

| Medullary BV/TV (%) | Groups |  |  |  |
| --- | --- | --- | --- | --- |
| Periods | C (Mean±SD) | MN (Mean±SD) | MNSr (Mean±SD) | MNSr+ (Mean±SD) |
| 15 days | 21,60±3,463 Aa | 21,02±4,033 Aa | 22,53±2,162 Aa | 21,20±2,554 Aa |
| 45 days | 19,91±4,282Aa | 18,12±3,982 Aa | 22,33±2,545 Aa | 19,52±3,522 Aa |

Distinct superscript letters (upper case compares periods in the column, lower case compares surface treatments in the row) indicate statistical difference to the Two-Way ANOVA test followed by Tukey (p<0.05).

Table 8. Means and standard deviation (SD) of the analysis of trabecular bone thickness (Tb.Th), in millimeters in the cortical bone region on implants with different surface treatments at 15 and 45 days.

| Cortical Tb.Th (mm) | Groups |  |  |  |
| --- | --- | --- | --- | --- |
| Periods | C (Mean±SD) | MN (Mean±SD) | MNSr (Mean±SD) | MNSr+ (Mean±SD) |
| 15 days | 0,1188±0,01246 Aa | 0,1138±0,01923 Aa | 0,1038±0,01188 Aa | 0,1163±0,01685 Aa |
| 45 days | 0,1363±0,01188 Aa | 0,1211±0,02571 Aa | 0,1270±0,02406 Aa | 0,1289±0,01453 Aa |

Distinct superscript letters (upper case compares periods in the column, lower case compares surface treatments in the row) indicate statistical difference to the Two-Way ANOVA test followed by Tukey (p<0.05).

Table 9. Means and standard deviation (SD) of the analysis of trabecular bone thickness (Tb.Th), in millimeters in the medullary bone region on implants with different surface treatments at 15 and 45 days.

| Medullary Tb.Th (mm) | Groups |  |  |  |
| --- | --- | --- | --- | --- |
| Periods | C (Mean±SD) | MN (Mean±SD) | MNSr (Mean±SD) | MNSr+ (Mean±SD) |
| 15 days | 0,1138±0,01506 Aa | 0,1100±0,01927 Aa | 0,1050±0,01604 Aa | 0,1138±0,009161Aa |
| 45 days | 0,1163±0,03159 Aa | 0,1089±0,02804 Aa | 0,1280±0,02251Aa | 0,1078±0,01481 Aa |

Distinct superscript letters (upper case compares periods in the column, lower case compares surface treatments in the row) indicate statistical difference to the Two-Way ANOVA test followed by Tukey (p<0.05).

Table 10. Means and standard deviation (SD) of the analysis of Trabecular Number (Tb.N), in millimeters in the cortical bone region on implants with different surface treatments at 15 and 45 days.

| Cortical Tb.N (mm) | Groups |  |  |  |
| --- | --- | --- | --- | --- |
| Periods | C (Mean±SD) | MN (Mean±SD) | MNSr (Mean±SD) | MNSr+ (Mean±SD) |
| 15 days | 1,875±0,09008 Aa | 1,851±0,08790 Aa | 2,003±0,1545 Aa | 1,789±0,1256 Aa |
| 45 days | 1,731±0,09992 Aa | 1,683±0,1230 Aa | 1,715±0,09981 Ba | 1,586±0,1173 Ba |

Distinct superscript letters (upper case compares periods in the column, lower case compares surface treatments in the row) indicate statistical difference to the Two-Way ANOVA test followed by Tukey (p<0.05).

Table 11. Means and standard deviation (SD) of the analysis of Trabecular Number (Tb.N), in millimeters in the medullary bone region on implants with different surface treatments at 15 and 45 days.

| Medullary Tb.N (mm) | Groups |  |  |  |
| --- | --- | --- | --- | --- |
| Periods | C (Mean±SD) | MN (Mean±SD) | MNSr (Mean±SD) | MNSr+ (Mean±SD) |
| 15 days | 1,809±0,1755 Aa | 1,810±0,1345 Aa | 2,030±0,1973 Aa | 1,798±0,1586 Aa |
| 45 days | 1,704±0,1705 Aa | 1,611±0,1389 Aa | 1,696±0,1809 Ba | 1,697±0,1360 Aa |

Distinct superscript letters (upper case compares periods in the column, lower case compares surface treatments in the row) indicate statistical difference to the Two-Way ANOVA test followed by Tukey (p<0.05).

Table 12. Means and standard deviation (SD) of the analysis of Trabecular Separation (Tb.Sp), in millimeters in the cortical bone region on implants with different surface treatments at 15 and 45 days.

| Cortical Tb.Sp (mm) | Groups |  |  |  |
| --- | --- | --- | --- | --- |
| Periods | C (Mean±SD) | MN (Mean±SD) | MNSr (Mean±SD) | MNSr+ (Mean±SD) |
| 15 days | 0,7025±0,1347 Aa | 0,6363±0,02973 Aa | 0,6288±0,008345 Aa | 0,6300±0,02000 Aa |
| 45 days | 0,6538±0,01768 Aa | 0,6311±0,02571 Aa | 0,6370±0,02710 Aa | 0,6333±0,01414 Aa |

Distinct superscript letters (upper case compares periods in the column, lower case compares surface treatments in the row) indicate statistical difference to the Two-Way ANOVA test followed by Tukey (p<0.05).

Table 13. Means and standard deviation (SD) of the analysis of Trabecular Separation (Tb.Sp), in millimeters in the medullary bone region on implants with different surface treatments at 15 and 45 days.

| Medullary Tb.Sp (mm) | Groups |  |  |  |
| --- | --- | --- | --- | --- |
| Periods | C (Mean±SD) | MN (Mean±SD) | MNSr (Mean±SD) | MNSr+ (Mean±SD) |
| 15 days | 0,6875±0,1162 Aa | 0,6250±0,02449 Aa | 0,6313±0,01642 Aa | 0,6100±0,03024 Aa |
| 45 days | 0,6475±0,06944 Aa | 0,6356±0,06710 Aa | 0,6380±0,01989 Aa | 0,6200±0,01732 Aa |

Distinct superscript letters (upper case compares periods in the column, lower case compares surface treatments in the row) indicate statistical difference to the Two-Way ANOVA test followed by Tukey (p<0.05).

# ANNEX 2.

Gene table RT² Profiler PCR Array Analyzed

| Position | UniGene | GenBank | Symbol | Description |
| --- | --- | --- | --- | --- |
| A01 | Rn.87899 | NM_024486 | Acvr1 | Activin A receptor, type I |
| A02 | Rn.32083 | NM_012898 | Ahsg | Alpha-2-HS-glycoprotein |
| A03 | Rn.82764 | NM_013059 | Alpl | Alkaline phosphatase, liver/bone/kidney |
| A04 | Rn.3318 | NM_013132 | Anxa5 | Annexin A5 |
| A05 | Rn.9722 | NM_013414 | Bglap | Bone gamma-carboxyglutamate (gla) protein |
| A06 | Rn.783 | NM_017087 | Bgn | Biglycan |
| A07 | Rn.9305 | NM_031323 | Bmp1 | Bone morphogenetic protein 1 |
| A08 | Rn.90931 | NM_017178 | Bmp2 | Bone morphogenetic protein 2 |
| A09 | Rn.208979 | NM_017105 | Bmp3 | Bone morphogenetic protein 3 |
| A10 | Rn.10318 | NM_012827 | Bmp4 | Bone morphogenetic protein 4 |
| A11 | Rn.135799 | NM_001108168 | Bmp5 | Bone morphogenetic protein 5 |
| A12 | Rn.40476 | NM_013107 | Bmp6 | Bone morphogenetic protein 6 |
| B01 | Rn.18030 | XM_342591 | Bmp7 | Bone morphogenetic protein 7 |
| B02 | Rn.88925 | NM_030849 | Bmpr1a | Bone morphogenetic protein receptor, type IA |
| B03 | Rn.215592 | NM_001024259 | Bmpr1b | Bone morphogenetic protein receptor, type IB |
| B04 | Rn.59276 | NM_080407 | Bmpr2 | Bone morphogenetic protein receptor, type II (serine/threonine kinase) |
| B05 | Rn.102418 | NM_031561 | Cd36 | CD36 molecule (thrombospondin receptor) |
| B06 | Rn.8900 | NM_053392 | Cdh11 | Cadherin 11 |
| B07 | Rn.29459 | NM_057134 | Chrd | Chordin |
| B08 | Rn.217522 | XM_001053056 | Col10a1 | Collagen, type X, alpha 1 |
| B09 | Rn.99441 | NM_001130548 | Col14a1 | Collagen, type XIV, alpha 1 |
| B10 | Rn.2953 | NM_053304 | Col1a1 | Collagen, type I, alpha 1 |
| B11 | Rn.107239 | NM_053356 | Col1a2 | Collagen, type I, alpha 2 |
| B12 | Rn.10124 | NM_012929 | Col2a1 | Collagen, type II, alpha 1 |
| C01 | Rn.3247 | NM_032085 | Col3a1 | Collagen, type III, alpha 1 |
| C02 | Rn.53801 | NM_001135009 | Col4a1 | Collagen, type IV, alpha 1 |
| C03 | Rn.117 | NM_134452 | Col5a1 | Collagen, type V, alpha 1 |
| C04 | Rn.107165 | XM_215375 | Col6a1 | Collagen, type VI, alpha 1 |
| C05 | Rn.10343 | NM_012834 | Comp | Cartilage oligomeric matrix protein |
| C06 | Rn.83632 | NM_023981 | Csf1 | Colony stimulating factor 1 (macrophage) |
| C07 | Rn.44285 | XM_340799 | Csf2 | Colony stimulating factor 2 (granulocyte-macrophage) |
| C08 | Rn.53973 | NM_017104 | Csf3 | Colony stimulating factor 3 (granulocyte) |
| C09 | Rn.5598 | NM_031560 | Ctsk | Cathepsin K |
| C10 | Rn.11248 | NM_012943 | Dlx5 | Distal-less homeobox 5 |
| C11 | Rn.6075 | NM_012842 | Egf | Epidermal growth factor |
| C12 | Rn.88013 | NM_012846 | Fgf1 | Fibroblast growth factor 1 |
| D01 | Rn.31808 | NM_019305 | Fgf2 | Fibroblast growth factor 2 |
| D02 | Rn.9797 | NM_024146 | Fgfr1 | Fibroblast growth factor receptor 1 |
| D03 | Rn.12732 | NM_001109892 | Fgfr2 | Fibroblast growth factor receptor 2 |
| D04 | Rn.10239 | NM_019306 | Flt1 | Fms-related tyrosine kinase 1 |
| D05 | Rn.1604 | NM_019143 | Fn1 | Fibronectin 1 |
| D06 | Rn.8707 | NM_024375 | Gdf10 | Growth differentiation factor 10 |
| D07 | Rn.219157 | XM_345832 | Gli1 | GLI family zinc finger 1 |
| D08 | Rn.12 | NM_012967 | Icam1 | Intercellular adhesion molecule 1 |
| D09 | Rn.6282 | NM_178866 | Igf1 | Insulin-like growth factor 1 |
| D10 | Rn.10957 | NM_052807 | Igf1r | Insulin-like growth factor 1 receptor |
| D11 | Rn.8711 | NM_053384 | Ihh | Indian hedgehog |
| D12 | Rn.83597 | XM_345156 | Itga2 | Integrin, alpha 2 |
| E01 | Rn.154664 | NM_001108292 | Itga3 | Integrin, alpha 3 |
| E02 | Rn.54465 | NM_012711 | Itgam | Integrin, alpha M |
| E03 | Rn.23339 | NM_001106549 | Itgav | Integrin, alpha V |
| E04 | Rn.25733 | NM_017022 | Itgb1 | Integrin, beta 1 |
| E05 | Rn.9946 | NM_133514 | Mmp10 | Matrix metallopeptidase 10 |
| E06 | Rn.6422 | NM_031054 | Mmp2 | Matrix metallopeptidase 2 |
| E07 | Rn.44474 | NM_022221 | Mmp8 | Matrix metallopeptidase 8 |
| E08 | Rn.10209 | NM_031055 | Mmp9 | Matrix metallopeptidase 9 |
| E09 | Rn.2411 | XM_342346 | Nfkb1 | Nuclear factor of kappa light polypeptide gene enhancer in B-cells 1 |
| E10 | Rn.10154 | NM_012990 | Nog | Noggin |
| E11 | Rn.10999 | NM_012801 | Pdgfa | Platelet-derived growth factor alpha polypeptide |
| E12 | Rn.37861 | NM_013004 | Phex | Phosphate regulating endopeptidase homolog, X-linked |
| F01 | Rn.214214 | NM_053470 | Runx2 | Runt-related transcription factor 2 |
| F02 | Rn.98199 | NM_017173 | Serpinh1 | Serine (or cysteine) peptidase inhibitor, clade H, member 1 |
| F03 | Rn.10635 | NM_013130 | Smad1 | SMAD family member 1 |
| F04 | Rn.2755 | NM_019191 | Smad2 | SMAD family member 2 |
| F05 | Rn.10636 | NM_013095 | Smad3 | SMAD family member 3 |
| F06 | Rn.9774 | NM_019275 | Smad4 | SMAD family member 4 |
| F07 | Rn.146857 | NM_021692 | Smad5 | SMAD family member 5 |
| F08 | Rn.95369 | NM_030584 | Sost | Sclerosteosis |
| F09 | Rn.95086 | XM_343981 | Sox9 | SRY-box containing gene 9 |
| F10 | Rn.92200 | NM_181374 | Sp7 | Sp7 transcription factor |
| F11 | Rn.8871 | NM_012881 | Spp1 | Secreted phosphoprotein 1 |
| F12 | Rn.40136 | NM_021578 | Tgfb1 | Transforming growth factor, beta 1 |
| G01 | Rn.24539 | NM_031131 | Tgfb2 | Transforming growth factor, beta 2 |
| G02 | Rn.7018 | NM_013174 | Tgfb3 | Transforming growth factor, beta 3 |
| G03 | Rn.44402 | NM_012775 | Tgfbr1 | Transforming growth factor, beta receptor 1 |
| G04 | Rn.9954 | NM_031132 | Tgfbr2 | Transforming growth factor, beta receptor II |
| G05 | Rn.9953 | NM_017256 | Tgfbr3 | Transforming growth factor, beta receptor III |
| G06 | Rn.2275 | NM_012675 | Tnf | Tumor necrosis factor (TNF superfamily, member 2) |
| G07 | Rn.64517 | NM_057149 | Tnfsf11 | Tumor necrosis factor (ligand) superfamily, member 11 |
| G08 | Rn.161904 | NM_053530 | Twist1 | Twist homolog 1 (Drosophila) |
| G09 | Rn.11267 | NM_012889 | Vcam1 | Vascular cell adhesion molecule 1 |
| G10 | Rn.10911 | NM_017058 | Vdr | Vitamin D (1,25- dihydroxyvitamin D3) receptor |
| G11 | Rn.1923 | NM_031836 | Vegfa | Vascular endothelial growth factor A |
| G12 | Rn.198550 | NM_053549 | Vegfb | Vascular endothelial growth factor B |
| H01 | Rn.94978 | NM_031144 | Actb | Actin, beta |
| H02 | Rn.1868 | NM_012512 | B2m | Beta-2 microglobulin |
| H03 | Rn.47 | NM_012583 | Hprt1 | Hypoxanthine phosphoribosyltransferase 1 |
| H04 | Rn.107896 | NM_017025 | Ldha | Lactate dehydrogenase A |
| H05 | Rn.973 | NM_001007604 | Rplp1 | Ribosomal protein, large, P1 |
| H06 | N/A | U26919 | RGDC | Rat Genomic DNA Contamination |
| H07 | N/A | SA_00104 | RTC | Reverse Transcription Control |
| H08 | N/A | SA_00104 | RTC | Reverse Transcription Control |
| H09 | N/A | SA_00104 | RTC | Reverse Transcription Control |
| H10 | N/A | SA_00103 | PPC | Positive PCR Control |
| H11 | N/A | SA_00103 | PPC | Positive PCR Control |
| H12 | N/A | SA_00103 | PPC | Positive PCR Control |

Reference: RT2 Profiler PCR Array Data Sheet (Qiagen, EUA)