Supplementary materials

Sample L00 is a sample that has been welded according to the parameters determined by the Taguchi method to achieve a connection with the highest penetration depth and the lowest values of weld height and bead width. It is also named the predicted sample (In the welded sample, the current intensity was at level 1 with a value of 240 amps, the welding speed was at level 3 with a value of 36 cm.min-1, and the nanoparticle amount was in level 1 with 0.25 g).

Sample L0 is a sample in which welding has been done according to the parameters and without the presence of nanoparticles, and it is also named as a reference sample (In the welded sample, the current intensity was 261.5 amps, arc voltage was 24.2 volts, welding speed was 36.2  cm.min-1, and the deposition rate was 73.4 g/min).