Supporting Information

for

Zn(II) metal-organic framework nanoparticles: Synthesis, characterization and application as optical biosensor for prostate-specific antigen

Amal S. Basaleh1 and Said M. El-Sheikh2,*

1 Department of Chemistry, Faculty of Science, King Abdulaziz University, P.O. Box 80203, Jeddah 21589, Kingdom of Saudi Arabia.

2Nanomaterials and Nanotechnology Department, Central Metallurgical R & D Institute, Cairo, 11421, Egypt.

*Corresponding author

S. M. El-Sheikh, E-mail: selsheikh2001@gmail.com, Tel.: +20 1022316076

Fig.  S1: The proposed mechanism of the Zn-MOF-NPs synthesis.

Fig. S2: Mass spectrum of the Zn-MOF-NPs.

Fig. S3: The proposed fragmentation Scheme of the Zn-MOF-NPs.

Fig. S4: FT-IR spectra of Zn-MOF-NPs and nano organic linker.

Fig. S5: The electronic-reflection spectra of Zn-MOF-NPs and nano organic linker.

Fig. S6: The bandgap energy spectra of Zn-MOF-NPs and nano organic linker.

Fig. S7. The PL emission spectra at different excitation wavelength for the Zn(II)MOF-NPs .

Fig. S8. A full relationship (calibration graph) between the PL intensity of Zn(II)-MOF-NPs and the logarithm PSA concentration (log [PSA]).

| Peak | 2θ | Intensity | Intensity | d-value | θ(Radians) | Sin θ | Sin² θ | Ratio 1 | Ratio 2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| No. |  | Count | % | A° |  |  |  |  |  |
| 1 | 11.411 | 13.1 | 4.055728 | 7.748306848 | 0.09958 | 0.09942 | 0.00988 | 1 | 2 |
| 2 | 13.25 | 162 | 50.1548 | 6.676745483 | 0.115628 | 0.11537 | 0.01331 | 1.3467 | 2.693481 |
| 3 | 14.65 | 64 | 19.81424 | 6.041692205 | 0.127845 | 0.1275 | 0.01626 | 1.2213 | 2.442544 |
| 4 | 15.603 | 54.4 | 16.84211 | 5.674756376 | 0.136162 | 0.13574 | 0.01843 | 1.1335 | 2.267006 |
| 5 | 17.448 | 20.8 | 6.439628 | 5.07862653 | 0.152263 | 0.15167 | 0.02301 | 1.2485 | 2.497077 |
| 6 | 19.988 | 266 | 82.35294 | 4.438617001 | 0.174428 | 0.17355 | 0.03012 | 1.3092 | 2.618347 |
| 7 | 21.504 | 35.6 | 11.02167 | 4.129003516 | 0.187658 | 0.18656 | 0.0348 | 1.1556 | 2.311186 |
| 8 | 22.788 | 323 | 100 | 3.899173527 | 0.198863 | 0.19755 | 0.03903 | 1.1214 | 2.242722 |
| 9 | 23.679 | 13.7 | 4.241486 | 3.754432173 | 0.206638 | 0.20517 | 0.0421 | 1.0786 | 2.157181 |
| 10 | 24.406 | 38.2 | 11.82663 | 3.644217397 | 0.212983 | 0.21138 | 0.04468 | 1.0614 | 2.122804 |
| 11 | 25.638 | 59.8 | 18.51393 | 3.471823825 | 0.223734 | 0.22187 | 0.04923 | 1.1018 | 2.203551 |
| 12 | 27.698 | 267 | 82.66254 | 3.218112736 | 0.241711 | 0.23936 | 0.0573 | 1.1639 | 2.327785 |
| 13 | 29.326 | 59.2 | 18.32817 | 3.043061223 | 0.255918 | 0.25313 | 0.06408 | 1.1184 | 2.236717 |
| 14 | 29.736 | 39.4 | 12.19814 | 3.002030139 | 0.259496 | 0.25659 | 0.06584 | 1.0275 | 2.055045 |
| 15 | 32.177 | 45 | 13.93189 | 2.779644115 | 0.280797 | 0.27712 | 0.0768 | 1.1664 | 2.332823 |
| 16 | 33.166 | 27 | 8.359133 | 2.698980953 | 0.289428 | 0.2854 | 0.08146 | 1.0607 | 2.121333 |
| 17 | 33.979 | 16.1 | 4.98452 | 2.636240125 | 0.296523 | 0.2922 | 0.08538 | 1.0482 | 2.09633 |
| 18 | 34.669 | 67.3 | 20.83591 | 2.585335553 | 0.302544 | 0.29795 | 0.08877 | 1.0398 | 2.079534 |
| 19 | 35.448 | 28.6 | 8.854489 | 2.53028521 | 0.309342 | 0.30443 | 0.09268 | 1.044 | 2.087973 |
| 15 | 36.218 | 41.7 | 12.91022 | 2.478237545 | 0.316062 | 0.31083 | 0.09661 | 1.0424 | 2.08489 |
| 16 | 36.828 | 29.3 | 9.071207 | 2.438577466 | 0.321385 | 0.31588 | 0.09978 | 1.0328 | 2.065583 |
| 17 | 38.409 | 44.2 | 13.68421 | 2.34175864 | 0.335182 | 0.32894 | 0.1082 | 1.0844 | 2.168797 |
| 18 | 40.134 | 39.5 | 12.2291 | 2.244995302 | 0.350235 | 0.34312 | 0.11773 | 1.0881 | 2.176123 |
| 19 | 40.405 | 37.4 | 11.57895 | 2.230560897 | 0.3526 | 0.34534 | 0.11926 | 1.013 | 2.025969 |
| 20 | 41.046 | 42.1 | 13.03406 | 2.197195 | 0.358194 | 0.35058 | 0.12291 | 1.0306 | 2.061204 |
| 21 | 42.409 | 50.4 | 15.60372 | 2.12967846 | 0.370088 | 0.3617 | 0.13083 | 1.0644 | 2.128821 |
| 22 | 43.85 | 13.1 | 4.055728 | 2.062976118 | 0.382663 | 0.37339 | 0.13942 | 1.0657 | 2.131423 |
| 23 | 44.542 | 34.7 | 10.74303 | 2.032519144 | 0.388702 | 0.37899 | 0.14363 | 1.0302 | 2.060388 |
| 24 | 45.047 | 32.4 | 10.03096 | 2.010899889 | 0.393109 | 0.38306 | 0.14674 | 1.0216 | 2.043235 |
| 25 | 45.424 | 30.2 | 9.349845 | 1.995082872 | 0.396399 | 0.3861 | 0.14907 | 1.0159 | 2.031838 |
| 26 | 46.762 | 19.7 | 6.099071 | 1.941067303 | 0.408075 | 0.39684 | 0.15748 | 1.0564 | 2.11286 |
| 27 | 47.726 | 21.6 | 6.687307 | 1.904085774 | 0.416488 | 0.40455 | 0.16366 | 1.0392 | 2.078443 |
| 28 | 49.6 | 37.7 | 11.67183 | 1.83644338 | 0.432842 | 0.41945 | 0.17594 | 1.075 | 2.150047 |
| 29 | 52.148 | 32.8 | 10.1548 | 1.752547434 | 0.455077 | 0.43953 | 0.19319 | 1.098 | 2.196067 |
| 30 | 53.014 | 33.4 | 10.34056 | 1.725941441 | 0.462634 | 0.44631 | 0.19919 | 1.0311 | 2.062137 |
| 31 | 56.958 | 19.1 | 5.913313 | 1.615437992 | 0.497052 | 0.47684 | 0.22737 | 1.1415 | 2.282977 |
| 32 | 58.465 | 20.3 | 6.28483 | 1.577337031 | 0.510203 | 0.48835 | 0.23849 | 1.0489 | 2.097788 |
| 33 | 63.867 | 14 | 4.334365 | 1.456323641 | 0.557345 | 0.52893 | 0.27977 | 1.1731 | 2.34619 |

Table S1: Summary of XRD data, Miller indices and interplanar distances of Zn-MOF-NPs.

Table S2: Summary of calculated crystallite size of Zn-MOF-NPs at different position on XRD patterns

| Position | Area | Cry Size L(nm) | Microstrain | RMS Strain(%) |
| --- | --- | --- | --- | --- |
| 11.38552 | 4.855149 | 135.7 | 0.1 | 0.1 |
| 13.23369 | 43.44118 | 123.9 | 0.1 | 0.1 |
| 14.63309 | 16.7502 | 114.3 | 0.1 | 0.1 |
| 15.58916 | 18.16841 | 151.4 | 0.1 | 0.1 |
| 17.43039 | 7.355614 | 139.9 | 0.1 | 0.1 |
| 19.95442 | 83.19238 | 156 | 0.1 | 0.1 |
| 21.48416 | 9.773613 | 158.9 | 0.1 | 0.1 |
| 22.76481 | 121.5275 | 146.3 | 0.1 | 0.1 |
| 24.37391 | 12.47938 | 145.6 | 0.1 | 0.1 |
| 25.55095 | 31.52574 | 123.9 | 0.1 | 0.1 |
| 27.65815 | 91.70529 | 151.6 | 0.1 | 0.1 |
| 29.44304 | 44.44398 | 118.1 | 0.1 | 0.1 |
| 32.1089 | 16.86871 | 142.2 | 0.1 | 0.1 |
| 33.10664 | 10.92236 | 130.1 | 0.1 | 0.1 |
| 34.65973 | 42.66779 | 122.5 | 0.1 | 0.1 |
| 36.2363 | 37.32982 | 110.7 | 0.1 | 0.1 |
| 38.35792 | 16.15865 | 148 | 0.1 | 0.1 |
| 40.30312 | 27.3514 | 123.4 | 0.1 | 0.1 |
| 41.01343 | 16.14014 | 140.8 | 0.1 | 0.1 |
| 42.34565 | 16.44194 | 159.2 | 0.1 | 0.1 |
| 44.85477 | 46.3486 | 108.4 | 0.1 | 0.1 |
| 46.70172 | 9.631201 | 129.7 | 0.1 | 0.1 |
| 47.67431 | 7.208591 | 101.2 | 0.1 | 0.1 |
| 48.37956 | 10.19796 | 123.3 | 0.1 | 0.1 |
| 49.60343 | 21.3051 | 127.4 | 0.1 | 0.1 |
| 52.09599 | 20.96037 | 121 | 0.1 | 0.1 |
| 52.9366 | 24.26174 | 119.3 | 0.1 | 0.1 |
| 57.0886 | 77.75088 | 113 | 0.1 | 0.1 |
| 65.37826 | 43.0985 | 113 | 0.1 | 0.1 |

Table S3: Sensitivity and regression parameters for Zn(II)MOF-NPs chemosensor

| Parameter | Method |
| --- | --- |
| λex, nm | 305 |
| λem, nm | 372 |
| Linear range, fg/mL | 0.1 – 20000 |
| Limit of detection (LOD), fg/mL | 0.145 |
| Limit of quantification (LOQ), fg/mL | 0.438 |
| Regression equation | (Y=a+bX)* |
| Intercept (a) | 523.01 |
| Slope (b) | 105.21 |
| Standard deviation | 4.611 |
| Correlation coefficient (r2) | 0.983 |

*Y, is photoluminescence intensities; X, is the concentration of- PSA in fg/mL; a, is intercept; b, is slope.

Materials

Zinc acetate, 99.99% and 1, 2- phenylenediamine C6H8N2, 99.5% were purchased from Sigma-Aldrich. 5-aminoisophthalic acid C8H7NO4, 98%; was purchased from Acros-organics. Standard prostate-specific antigen (PSA) of different buffered concentrations were supplied by Monobind, USA.  All solvents and chemicals used in this study were of analytical reagent grade and were used as received.

Instruments

The characterization and applications were performed using different analytical techniques: The FE-SEM images and EDX spectroscopy spectra were recorded with a combination of field emission scanning electron microscopy (FE-SEM), and element mapping by spatially resolved energy-dispersive X-ray spectroscopy (EDX) (JEOL JSM-6510LV, Japan). The structures of the phases formed were examined by using a high-resolution transmission electron microscope (HR-TEM) with an acceleration voltage up to 200 kV (JEM-2100-JEOL, Japan). The mass spectra of solid Zn(II)MOF-NPs were recorded using a Thermo Scientific- ISQ single quadrupole mass spectrometer (Thermo Scientific, USA). The Fourier-transform infrared (FT-IR) spectra were recorded with a JASCO FT/IR-460 spectrophotometer with the use of KBr tablets in the range from 400 to 4000 cm−1 at room temperature (JASCO, USA). Elemental analysis (C-H-N) was performed using a Costech ECS-4010- analyzer (Costech, Italy). The UV-vis spectra were obtained using V-770 UV-Visible/NIR spectrophotometer (JASCO, USA), and the band gap was calculated with Optbandgap-204B soft wear. The oxidation states and species in the prepared materials were recorded by Thermo Scientific™ K-Alpha™ X-ray photoelectron spectrometer (XPS) (Thermo Scientific, USA), using Al-Kα micro-focused monochromator within an energy range up to 4 KeV. Differential Scanning Calorimetry/Thermogravimetric Analysis (DSC/TGA) of the samples was carried out with a Universal V4.5-TA Instruments (USA), with a rate of 10 °C min-1. The magnetic properties of the fabricated samples were measured using a vibrating sample magnetometer (7400-1 VSM, USA) in a maximum applied ﬁeld of 20 kOe. The photoluminescence (PL) spectra were investigated using a (Shimadzu RF-5301PC spectrofluorophotometer). The samples were used for subsequent PL measurements at different excitation wavelengths and then at an excitation wavelength 416 nm and emission wavelengths of 593 and 566 nm. The measurements were performed in a quartz cuvette of path length 1 cm, with a scan time of 30 s, at room temperature. The data were analysed with Origin-8. The structures, 3D geometrical structures and Schemes were drawn using "ChemBioDraw Ultra12" program.