Supporting Information

Lightweight insulating oil-well cement filled with hollow glass microspheres and numerical simulation of its unsteady heat transfer process

Hui Wanga,1, Chong Maa,1, Yihui Yuana*, Yanglei Chenb, Tao Liua, Ning Wanga*

aState Key Laboratory of Marine Resource Utilization in South China Sea, Hainan University, Hainan 570228, China

b Tarim Oilfield Company (TOC) of Petro China, Tarim 841001, China

* Corresponding author.

E-mail address: yuanyh@hainanu.edu.cn (Yihui Yuan)

Wangn02@foxmail.com (Ning Wang)

1These authors contributed equally to this work.

Table of Contents

Fig. S1. Particle size distribution of different HGM.	1

Fig. S2. Scanning electron microscopy (SEM) profiles of HGM/OWC LWTI composites with different HGM diameters and contents.	2

Fig. S3. Changes in left boundary temperature with time in the 2D mathematical model of HGM/OWC LWTI composite materials: (a) HGM-D36.5; (b) HGM-D39.9 and (c) HGM-D51.8.	3

Table S1. Chemical composition and physical properties of cement used for testing.	4

Table S2. Physical properties of different HGM.	5

Table S3. Fitting ratios of HGM/OWC LWTI composites with different contents and sizes of HGM.	6

Table S4 Comparison of analytical and numerical solution results for keff of composites. 	7

Table S5. Actual values and numerical simulation results of thermal conductivity of HGM/OWC LWTI composites.	8

Table S6. Compressive strength, specific strength, and flexural strength of HGM/OWC LWTI composites..	9

Fig. S1. Particle size distribution of different HGM.

Fig. S2. Scanning electron microscopy (SEM) profiles of HGM/OWC LWTI composites with different HGM diameters and contents.

| a |  | b |  | c |  |
| --- | --- | --- | --- | --- | --- |

Fig. S3. Changes in left boundary temperature with time in the 2D mathematical model of HGM/OWC LWTI composite materials: (a) HGM-D36.5; (b) HGM-D39.9 and (c) HGM-D51.8.

| Table S1. Chemical and mineral composition of G class oil well cement (wt.%). |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Chemical composition |  |  |  |  |  |
| CaO | SiO2 | Fe2O3 | Al2O3 | SO2 | Others |
| 44.1 | 50.1 | 3.4 | 2.2 | 0.1 | 0.1 |
| Mineralogical composition |  |  |  |  |  |
| C3S | C2S | C3A | C4AF | CaSO4 | Others |
| 40.6 | 14.0 | 11.2 | 10.4 | 0.4 | 34.5 |

Table S2. Physical properties of the different HGM.

| Model | Density (g/cm3) | Compressive strength (MPa) | Thermal Conductivity (W/(m·℃)) |
| --- | --- | --- | --- |
| D36.5 | 0.52 | 82.74 | 0.069 |
| D39.9 | 0.38 | 27.58 | 0.059 |
| D51.8 | 0.19 | 3.45 | 0.055 |

Table S3. Fitting ratios of HGM/OWC LWTI composites with different contents and sizes of HGM.

| HGM Content (vol.%) | Type | Cement Mass(g) | HGM Mass (g) | Water Mass (g) | Accelerator Mass (g) | SP Mass (g) | W/C |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | Blank | 200 | 0 | 48 | 20 | 3 | 0.24 |
|  | D36.5 | 150.00 | 5.10 | 39.60 | 15.00 | 2.25 | 0.26 |
| 10 | D39.9 | 150.00 | 3.75 | 39.00 | 15.00 | 2.25 | 0.26 |
|  | D51.8 | 150.00 | 1.76 | 37.76 | 15.00 | 2.25 | 0.25 |
|  | D36.5 | 150.00 | 11.50 | 44.10 | 15.00 | 2.25 | 0.29 |
| 20 | D39.9 | 150.00 | 8.43 | 42.70 | 15.00 | 2.25 | 0.28 |
|  | D51.8 | 150.00 | 3.93 | 40.00 | 15.00 | 2.25 | 0.27 |
|  | D36.5 | 125.00 | 17.50 | 42.25 | 18.75 | 1.88 | 0.34 |
| 30 | D39.9 | 125.00 | 12.05 | 39.60 | 12.50 | 1.88 | 0.32 |
|  | D51.8 | 125.00 | 5.60 | 35.60 | 12.50 | 1.88 | 0.28 |
|  | D36.5 | 100.00 | 21.7 | 39.2 | 15 | 1.5 | 0.39 |
| 40 | D39.9 | 100.00 | 15.00 | 36.00 | 10.00 | 1.50 | 0.36 |
|  | D51.8 | 100.00 | 7.00 | 31.00 | 10.00 | 1.50 | 0.31 |

Table S4. Comparison of analytical and numerical solution results for keff of composites.

| Content of HGM (vol.%) | Result of Liang [41] |  |  | This work |  |
| --- | --- | --- | --- | --- | --- |
|  | Actual value (W/(m·℃)) | Simulated value (W/(m·℃)) | Relative error(%) | Simulated value (W/(m·℃)) | Relative error(%) |
| 5 | 0.226 | 0.212 | 5.89 | 0.224 | 0.76 |
| 10 | 0.216 | 0.196 | 9.25 | 0.213 | 1.17 |
| 15 | 0.204 | 0.181 | 11.39 | 0.202 | 1.08 |
| 20 | 0.190 | 0.166 | 12.27 | 0.188 | 0.84 |

Table S5. Actual values and numerical simulation results of thermal conductivity of HGM/OWC LWTI composites.

| Content of HGM (vol.%) | Diameter (µm) | Thermal conductivity of actual value (W/(m·℃)) | Thermal conductivity simulated value (W/(m·℃)) | Error (%) |
| --- | --- | --- | --- | --- |
|  | D36.5 | 0.727 | 0.741 | 1.93 |
| 10 | D39.9 | 0.715 | 0.731 | 2.24 |
|  | D51.8 | 0.684 | 0.716 | 4.68 |
|  | D36.5 | 0.614 | 0.63 | 2.61 |
| 20 | D39.9 | 0.583 | 0.612 | 4.97 |
|  | D51.8 | 0.569 | 0.599 | 5.27 |
|  | D36.5 | 0.527 | 0.529 | 0.38 |
| 30 | D39.9 | 0.499 | 0.514 | 3.01 |
|  | D51.8 | 0.465 | 0.477 | 2.58 |
|  | D36.5 | 0.386 | 0.407 | 5.44 |
| 40 | D39.9 | 0.373 | 0.399 | 6.97 |
|  | D51.8 | 0.371 | 0.4 | 7.82 |

Table S6. Compressive strength, specific strength, and flexural strength of HGM/OWC LWTI composites.

| HGM content (vol.%) | Type | Compressive strength (MPa) | Specific strength (MPa/g/cm3) | Flexural strength (MPa) |
| --- | --- | --- | --- | --- |
| 0 | Blank | 44.31 | 21.30 | 14.88 |
|  | D36.5 | 42.50 | 21.91 | 14.18 |
| 10 | D39.9 | 41.25 | 21.37 | 13.48 |
|  | D51.8 | 40.63 | 21.38 | 13.07 |
|  | D36.5 | 39.56 | 22.61 | 12.42 |
| 20 | D39.9 | 38.25 | 21.68 | 11.95 |
|  | D51.8 | 37.75 | 21.95 | 11.7 |
|  | D36.5 | 38.91 | 24.94 | 11.02 |
| 30 | D39.9 | 36.39 | 23.70 | 10.66 |
|  | D51.8 | 34.02 | 22.37 | 10.08 |
|  | D36.5 | 32.91 | 24.98 | 9.38 |
| 40 | D39.9 | 30.43 | 23.97 | 8.79 |
|  | D51.8 | 29.44 | 22.07 | 8.44 |